ANNEX A - Specifications

UNHCR UKRAINE Invitation to Bid ITB 2021-01

Construction materials for Assistance

provided to Internally Displaced Persons (IDPs)

- QUANTITY OF PRODUCT

Bids should confirm ability to supply goods to the following quantities by category. The offer can be provided and evaluated for whole range within the category:

| # | Product category | Name | Unit of measure | Appr. annual q-ty |
| --- | --- | --- | --- | --- |
| 1 | Roofing sheets | Corrugated non-asbestos roofing sheet (length 1750 mm (+/-15mm deviations allowed), width 1130 mm, thickness 5.8 mm (+1,0/-0,3mm deviations allowed) | unit | 27282 |
| 2 | Timber, plank | 25 х 100 х 4500 mm | pcs | 36772 |
|  |  | 70 х 150 х 4500 mm | pcs | 4051 |
|  |  | 20 х 25 х 3000 mm | pcs | 2000 |
|  |  | 100 х 100 х 4500 mm | pcs | 90 |
|  |  | 100 х 200 х 4500 mm (for rafters) | pcs | 252 |
| 3 | Ruberoid | Roofing waterproof, 1х15 m, Basis: Fiberglass | pcs | 2711 |
| 4 | Roofing Ridge | zinced steel, 200x200x2000mm, 0,4-0,5mm thickness, edge rolled inside | pcs | 2702 |
| 5 | Nails roofing | 70 mm, Packed in bags/boxes 1 kilo each | kg | 1582 |
|  |  | 100 mm, Packed in bags/boxes 1 kilo each | kg | 762 |
|  |  | Nails (roofing sheet), 120 mm, Packed in boxes 1 kilo each | kg | 1496 |
| 6 | Nails | 5 X 200 mm, Packed in bags/boxes 1 kilo each | kg | 566 |
| 7 | Steel staple | D 8-L300 mm, length of the “claw”: min. 5.5 mm; packed in boxes | pcs | 1210 |
| 8 | Linoleum | Grade durability 23 | М2 | 320 |
| 9 | Mineral wool | Mineral wool, density ≥40 kg/m3, width 100 mm | М2 | 830 |
| 10 | Brick silicate | Facing Silicate Thickened Brick with the brand of strength of 150 | pcs | 5850 |
| 11 | Cement, bags | Portland cement PC II / B-SH-400, Packed in bags, 50 kg | bags | 390 |

Please note that quantities of goods stated in Specification are to enable bidders to have an indication of the projected requirements. It does not represent a commitment that UNHCR will purchase the above quantity. Quantities may vary and will depend on the actual requirements and funds available regulated by issuance of individual Purchase Orders against the Frame Agreement. In this regard, please indicate prices that will be effective regardless of the ordered volume of goods.

- SPECIFICATION OF PRODUCTS

The products should comply with specification described below.

Corrugated Non-Asbestos Roofing Sheet

According to standard: GOST 30340-95, European Standard

| Property | Quality |
| --- | --- |
| Dimensions | length 1750 mm (+/-15mm deviations allowed), width 1130 mm, thickness 5.8 mm (+1,0/-0,3mm deviations allowed) |
| Material | Asbestos free cement (meeting European quality standards) 40/150 (8 waves) |
| The corrugation high | 40 mm |
| The dimension between two corrugations measured at their center. | 150 mm |
| Certificates | Quality, Radiological research protocol, Conclusion of the state sanitary and epidemiological examination, Certificate of compliance of the plant's internal production control, Fire |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Timber

| Property | Quality |
| --- | --- |
| Material | Pine or fir tree, density P<0.5 (g/cm3) |
| Quality of drying / humidity % | CAT III / no more than 15% |
| Strength class / Standard | Class C27 according to MGB 52001 |
| Sort | Sort 2: 25 х 100 х 4500 mm Sort 1: 70 х 150 х 4500 mm 20 х 25 х 3000 mm 100 х 100 х 4500 mm 100 х 200 х 4500 (for rafters) |
| Antibacterial treatment | Yes |
| Deviation size, corresp. GOST 25346-89 | IT (13-17) |
| Compliance with radiological control/ certificate | yes |
| The nominative content of CS-137 Bq/kg – no more | 740 |
| The activity of CS-137 Bq/kg – no more | 5 |
| Certificate of origin of wood | yes |
| A phytosanitary certificate issued by the State Veterinary and Phytosanitary Service of Ukraine | yes |
| Conclusion of the State sanitary-epidemiological expertise for applied antiseptic | yes |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days. |

Ruberoid / Roofing waterproof

| Property | Quality |
| --- | --- |
| Dimensions | 1х15 m |
| Weight 1 m2 of material | not less than 1.5 kg |
| Basis | Fiberglass |
| Breaking tensile strength, not less than | 294 H |
| Water absorption for 24 hours, by weight, not more | 1.50 % |
| The temperature flexibility on a bar R = 25 mm | Not above -5 degrees. |
| Heat resistance, at least | 85 degrees |
| The potential lifetime | 10 years+ |
| Waterproof at a pressure of 0,001 MPa for 72 hours | absolutely |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Roofing Ridge

According to standard: GOST 14918-80

| Property | Quality |
| --- | --- |
| Type | edge rolled inside |
| Dimensions | 200*200*2000mm |
| Width | 0.4-0.5 |
| Materail | zinced steel |
| Certificates | Quality |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Nails (all types)

According to standard: DSTU GOST 4028:2008 or GOST 4028-63

| Property | Quality |
| --- | --- |
| Certificates | Quality |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Steel staple

| Property | Quality |
| --- | --- |
| Length | 300mm |
| Diameter | 8mm |
| Length of the “claw” | Minimum 5.5 mm |
| Certificates | Quality for material (or on the material of these staples, i.e. for the steel armature) |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Linoleum

According to standard: DSTU

| Property | Quality |
| --- | --- |
| Grade durability | 23 |
| Basis of linoleum | "numnah" |
| Linoleum structure | without pattern (neutral) |
| Thickness of the protective layer | 0.25-0.3 mm |
| Thickness of linoleum | 3 mm |
| Width | 4 m |
| Certificates | Quality, fire, sanitary |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Mineral wool

| Property | Quality |
| --- | --- |
| Density, kg / m³ | At least 40 |
| Thickness, mm | 100 |
| Thermal conductivity λ10, W / (m * K), not more, at (10 ± 0,5) 0C | 0, 034 |
| Thermal conductivity λA, W / (m * K), not more | 0, 04 |
| Thermal conductivity λb, W / (m * K), not more | 0, 044 |
| Compressive strength at 10% deformation, kPa, not less | 25 |
| Compressibility, %, not more | - |
| Border tensile strength in a direction perpendicular to the plane of the plate, kPa, not less | 10 |
| The content of organic substances, % by weight, not more | 4, 5 |
| Water absorption at full immersion, % by volume, not more | 1, 5 |
| Permeability, m 2 / (m * h * Pa), not less | 0, 3 |
| Humidity, % by weight, not more | 1, 00 |
| flammable group | NG |
| Efficient operation term, years, not less | 50 |
| Certificate of conformity | UkrSEPRO |
| Certificates | Radiological research protocol; Conclusion of the state sanitary and epidemiological examination; Certificate of compliance of the plant's internal production control |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

Brick silicate

| Facing Silicate Thickened Brick with the brand of strength of 150 Standards: СПЛ – 150/1,6/25 DSTU B.V. (ДСТУ Б.В) 2.7-80:2008 |  |
| --- | --- |
| Property | Quality |
| Size | 250*120*88 mm |
| Material | Silicate |
| Color | White |
| Standard | Compliance with DSTU B V. (ДСТУ Б.В.) 2.7-80:2008 |
| Brand of strength | 150 |
| Class average density | 1.6 |
| Mark of frost resistance | F25 |
| Usage | For external walls |
| Certificates | Conformity |
| Required delivery timeframe for 20% of the forecasted annual quantity | No more than 20 calendar days |

Portlandcement

According to standard: DSTU B V.2.7-46: 2010

| Property | Quality |
| --- | --- |
| Mark of Portland cement | PC II / B-SH-400 |
| Composition | Portland cement clinker - 65-79%; Granulated blast furnace slag - 21-35%; Pozzolanic materials-0%; Fly Ash - 0%; Limestone - 0%; Additional components - 0-5%. |
| Type | II |
| Shelf life | The goods supplied must be produced no earlier than 2 months before the date of delivery |
| Packaging | 50 kg bag |
| Certificates | Quality, DSTU compliance, radiological |
| Required delivery time for 20% of forecasted annual quantity which is indicated in this document | No more than 20 calendar days |

C - PACKAGING, LABELLING FOR TRANSPORTATION

The bidder shall describe the proposed packaging for transportation and defining a packing unit (PU). The quantity of items in each PU must be standardized and this information must be clearly specified along with its weight, volume and the equipment required to handle it in the technical offer. Each PU shall carry a label stating the content along with the Purchase Order number and UNHCR Logo.

D- PRODUCTION AND DELIVERY CAPACITY

The bidder shall state its annual production capacity and the quantities available after one week of production lead-time. The production capacity will be compared and measured against the offer with the highest production capacity.

The bidder shall state existing stock quantity available for immediate dispatch and the delivery time. Also the time of availability of the full initial requirements quantity shall be clearly stated.

The Supplier may be requested to deliver products to Kyiv and Sievierodonetsk. Time, conditions and limitations of such delivery shall also be stated. Additional points of delivery can be subject to agreement during the contract implementation.