ANNEX A

Specifications and required quantities of tents materials and second hand containers

To be purchased to the Sahrawi Refugees in the Tindouf camps - Algeria

Definition of products quality, and other requirements

- BLENDED CLOTH:

| Estimated Quantity | 2,010 |  |
| --- | --- | --- |
| Quality | Minimum of 40% Cotton and polyester (ISO1833). The canvas material must be in accordance with the specified characteristics and with ISO 10966 - Textiles – Fabric for tents – Specifications. |  |
| Colour | Light blue |  |
| Yarn count | 25x25 in warp and weft. “Free of defects and faults adversely affecting strength, waterproofness and durability” |  |
| Density | in warp | 60 threads per square inch |
|  | In weft | 60 threads per square inch |
| Weight | 132 g /m2 ±10% in finished state. |  |
| Width | 150 cm ±3% with no more than 3% dimensional variation when soaking in water, ISO 7771 |  |
| Length of the piece | 70 meters ±0.5% with no more than 3% dimensional variation when soaking in water, ISO 7771 |  |
| Packing | - |  |

- COTTON ROPE:

| Estimated Quantity | 2,010 |
| --- | --- |
| Quality | 100% cotton - UV treated |
| Diameter | 12-14 mm three standard braiding rope with a minimum tensile strength of 300 kg. |
| Length of the piece | 120 meters exactly |
| Packing | 120 in coil, wrapped in Hessian cloth and tied in plastic straps |

- BAMBOO POLES:

| Estimated Quantity | 4,020 |
| --- | --- |
| Quality | Bamboo: Maturity 3-5 years old, hard surface and clean with no evidence of insect or fungi attack. Maximum extent of longitudinal cracking and splitting is 100 mm and No circumferential cracks are allowed. Tolerance to overall diameter is 15%. |
| Length | 14 feet with a pin in the end on a rivet of 5 inches in length at the top of the bamboo cane |
| Diameter | 40mm on the top and 70mm at the bottom |
| Packing | 10 tied poles with their ends protected with Hessian cloth |

- IRON PEGS:

| Estimated Quantity | 24,120 |
| --- | --- |
| Quality | Iron |
| Length | 50cm |
| Diameter | 15mm |

- CONTAINERS:

| Estimated Quantity | 06 |
| --- | --- |
| Quality | seaworthy quality, clean, dry, and free from structural damage. must be provided with CSC (safety approval) plate. |
| Size | 40 Fts |