UNOPS

##### UNITED NATIONS OFFICE FOR PROJECT SERVICES

TECHNICAL SPECIFICATIONS FOR K-SPAN BUILDING

&

DRAWINGS

- Demolition / Removal

  - Demolition and removal of waste materials from the immediate vicinity of the site located on the west of the Jabal-Al-Serage MOPW  compound.

See the attached Pictures.

The rate includes full compensation for the demolition and removal of all materials within or in the immediate vicinity of the area of the works, and removal from the site, to outside the Jabal-Al-Serage town limits.

- General Building Works

  - Excavation:

Excavation shall be measured from the boundary wall of MoPW Compound (+0.00). The dept shall be 300mm and the wide minimum 350mm for R-beams properly leveled.

Excavation for shear keys to be done 5500mm deep and minimum 300mm wide at each 1500 mm on both longitudinal sides of the warehouse.

Excavation of the rump to be done with 6% slope for the truck.

  - Compaction:

The area for the ground slab to be properly compacted with role machine.

  - RCC Shear key:

Shear key  M:200 (1:1.5:2) reinforced concrete to be done @  each 1.50 m OC reinforced w/ 6-12 mm vertical bars and 8 mm stirrup @ 150 OC. including 10 days curing, for 300x300x350, connected with the R-Beam.

Drawings and instruction by UNOPS staff to be considered.

  - R-Beam:

Construction of R-Beam: Includes  reinforcement 4x14mm longitudinal and 8mm rebar @ 200mm cc, mold, M:200 (1:1.5:2)  concrete, 150x150x6mm plate @ each 1500mm.

The R-Beam is to be constructed in two steps i.e 400 mm before and 150mm after erection of arch panel. 10 days curing is required for R-Beam.

Drawings and instruction by UNOPS staff to be considered.

  - RCC slabs for warehouses:

Includes all activities, material and labor cost, including 10 days curing, for 20cm thick, M:200 (1:1.5:2) reinforced concrete  slabs of the warehouse on the ground level with 12mm bars @300mm cc both ways, top & bottom for large slabs and 12mm bars @300mm cc both ways for small slabs.

Expansion joints @ each 4000mm with removable plywood 25x750mm are required. Expansion joints to be filled with bitumen. Typical drawing for the slabs reinforcement is available.

2.06	RCC walls:

Reinforced concrete walls to be belt for two ramps. The height of two walls on both sides of the ramp are 20000mm long, with slop 800mm on one end, and 1400mm on the other end. The wall along the warehouses would be 20000mm long and 1400mm hiegh. All walls are 200mm thick , and reinforced with 10mm bars @150mm cc both ways and both sides.

2.07     RCC slabs for ramps:

Includes all activities, material and labor cost, including 10 days curing, for 20cm thick, M:200 (1:1.5:2) reinforced concrete  slabs of the ramp on the ground level with 12mm bars @150mm cc both ways, top & bottom.

Expansion joints @ each 4000mm with removable plywood 25x750mm are required. Expansion joints to be filled with bitumen. Typical drawing for the slabs reinforcement is available.

- General Works:

3.01	Thorough cleaning the work site of unused materials, spoil, etc. after completion of the work.