# Annex A Specifications

SPECIFICATIONS

CONTENTS

- SPECIFICATIONS

Section 1: General

101	Introduction

102	Definitions

103	Scope of Work

104	Materials

105	Construction Equipment

106	Drawings

107	Site Information

108	Setting Out

109	Public Utilities

110	Safety and Precautions for Safeguarding the Environment

111	Arrangement for Traffic during Construction

112	General Rules for the Measurement of Works for Payment

113	Scope of Rates for Different Items of Work

114	Methodology and Sequence of Work

115	Use of Surfaces by Construction Traffic

116	Mobilization

117	Demobilization

118	Site Preparation

119	Security measures

120	Topographic Survey

121	Insurance

Section 2: Earthworks

201	Site Clearance (Clearing and Grubbing)

202	Removal of Structures and Obstructions

202.1	Scope

202.2	Dismantling Culverts and Bridges

202.3	Dismantling Pavements and Other Structures

202.4	Back-filling

202.5	Disposal of Materials

202.6	Method of Measurement

202.7	Rates

203	Road Excavation

203.1	Scope

203.2	Classification of Excavated Material

203.3	Construction Operations

203.4	Plying of Construction Traffic

203.5	Preservation of Property

203.6	Preparation of Cut Formation

203.7	Method of Measurement

203.8	Rates

204	Structure Excavation

204.1	Scope

204.2	Classification of Excavation

204.3	Construction Operations

204.4	Method of Measurements

204.5	Rates

205	Embankment and Fill

205.1	Scope

205.2	Material Requirements

205.3	Construction Operations

205.4	Construction of Embankment and Sub grade under special Conditions

205.5	Plying of Traffic

205.6	Surface Finish and Quality Control of Work

205.7	Sub grade Strength

205.8	Measurements for Payment

205.9	Rates

206	Subgrade Preparation

206.1	Scope

206.2	Construction Operation

206.3	Method of Measurement

206.4	Rates

Section 3: Road Works

301	Granular Sub-base Course

301.1	Scope

301.2	Materials

301.3	Strength of Sub· Base

301.4	Construction Operation

301.5	Surface Finish and Quality Control of Work

301.6	Method of Measurement

301.7	Rates

302	Prime Coat

302.1	Scope

302.2	Materials

302.3	Construction Operation

302.4	Method of Measurement

302.5	Rates

303	Tack Coat

303.1	Scope

303.2	Materials

303.3	Construction Operation

303.4	Method of Measurement

303.5	Rates

304	Bituminous Concrete

304.1	Scope

304.2	Materials

304.3	Mixture Design

304.4	Construction Operations

304.5	Opening to traffic

304.6   Tests and Standards of Acceptance

304.7	Method of measurement

304.8	Rates

305	Control of Alignment, Level, and Surface Regularity

305.1	General

305.2	Horizontal Alignment

305.3	Surface Levels

305.4	Surface Regularity of Pavement Courses

305.5	Rectification

306	Concrete Curbs

306.1	Scope

306.2	Materials

306.3	Type of Construction

306.4	Construction Requirements

306.5	Method of Measurement

3069.6	Rates

307	Road Marking

307.1	Scope

307.2	Materials

307.3	Construction Requirements

307.4	Method of Measurement

307.5	Rates

308	Traffic Signs

308.1	General

308.2	Materials

308.3	Installation

308.4	Method of Measurement

308.6	Rates

Section 4: Concrete Works

401	Structural Concrete

401.1	Scope

401.2	Materials

401.3	Grade of Concrete and their use

401.4	Proportioning of Concrete

401.5	Admixtures

401.6	Equipment

401.7	Mixing Concrete

401.8	Transporting, Placing and Compaction of Concrete

401.9	Construction Joints

401.10	Concreting Under Water

401.11	Adverse Weather Conditions

401.12	Protection and Curing

401.13	Finishing

401.14	Tolerances

401.15	Tests and Standards of Acceptance

401.16	Method of Measurement

401.17	Rates

402	Reinforcing Steel

402.1	Scope

402.2	Material

402.3	Bending of Reinforcement

402.4	Placing of Reinforcement

402.5	Bar Splices

402.6	Testing and Acceptance

402.7	Method of Measurement

402.8	Rates

403	Formwork

403.1	Scope

403.2	Materials

403.3	Design of Formwork

403.4	Workmanship

403.5	Formed Surface and Finish

403.6	Precautions

403.7	Preparation of Formwork Before Concrete

403.8	Removal of Formwork

403.9	Re-Use of Formwork

403.10	Specialized Formwork

403.11	Tests and Standards of Acceptance

403.12	Method of Measurement

403.13	Rates

Section 5: Masonry Works

501	Stone Masonry

501.1	Scope

501.2	Materials

501.3	Type of Masonry

501.4	Construction Operations

501.5	Scaffolding

501.6	Weep Holes

501.7	Tests and Standard of Acceptance

501.8	Method of Measurement

501.9	Rates

501	Brickworks

502.1	Scope

502.2	Materials

502.3	Cement Mortar

502.4	Soaking of Bricks

502.5	Joints

502.6	Laying

502.7	Jointing Old and New Work

502.8	Curing

502.9	Scaffolding

502.10	Equipment

502.11	Acceptance of Work

502.12	Method of Measurement

502.13	Rates

Section 6: Structural Steel Works

601	I-Beam Steel Girder for Pedestrian Bridge

602     GI Pipe for Guard Pipe

Section 7: Drainage

701	Pipe Culverts

701.1	Scope

701.2	Materials

701.3	Excavation for Pipe

701.4	Bedding for Pipe

701.5	Laying of Pipe

701.6	Backfilling

701.7	Connecting box and ancillary works

701.8	Opening to Traffic

701.9	Method of Measurement

701.10	Rates

702	Side drain, infiltration inlet and culvert pit

702.1	Scope

702.2	Materials

702.3	Construction Requirements

702.4	Method of Measurement

702.5	Rates

703	Stone Pitching Ditches

703.1	Scope

703.2	Materials

703.3	Construction Requirements

703.4	Method of Measurement

703.5	Rates

Section 8: Gabion works

801	Gabion

801.1   General

801.2   Material

801.3   Filling and Placing

801.4   Gabion wire protection

801.5   Measurement and payment of Gabion

SECTION 1: GENERAL

101	Introduction

Specifications shall commonly apply to all the road works as executed under The Project for Rehabilitation of Small Irrigation Facilities and Village Accessibility in Dehsabz area, Kabul Province through Grant Aid Project for Community Development of the Government of Japan in the Islamic Republic of Afghanistan.

The works shall be carried out to the satisfaction of the Engineer to the location, lines, dimensions, grades and cross sections shown on the drawings or as indicated by the Engineer. The quality of materials, processing of materials as may be needed at the site, salient features of the construction work and quality of finished work shall comply with the requirements set forth in succeeding sections. Where the drawings and Specifications describe a portion of the work in only general terms, and not in complete detail, it shall be understood that only the best general practice is to prevail, materials and workmanship of the best quality are to be employed and instructions of the Engineer are to be fully complied with.

102	Definitions

The words like Contract, Contractor, Engineer (synonymous with Employer's Representative's Consultant or Engineer-in-charge), Drawings, Employer, Government, Works and Work Site used in these Specifications shall be deemed to have the meaning as understood from the definitions of these terms given in the General Conditions of Contract.

The following abbreviations shall have the meaning as set forth below:

AASHTO	: American Association of State Highway and Transportation Officials

ASTM	: American Society for Testing and Materials

ACI	: American Concrete Institute

BS	: British Standard published by the British Standards Institution

CBR	: California Bearing Ratio

cum or m3	: Cubic meter(s)

Dia. or Փ	: Diameter

Drg. or Dwg	: Drawing

JIS	: Japan Industrial Standard

Kg	: Kilogram(s)

kN	: Kilo Newton

Lin. m or m	: Linear meter(s)

Ltr	: Liter(s)

Max.	: Maximum

Min.	: Minimum

mm	: Millimeter(s)

mm2	: Square millimeter(s)

MPa	: Mega Pascal

N	: Newton

N/mm2	: Newton per square millimeter

no. or nos.	: Number

P.C.	: Pre-stressed Concrete

R.C.	: Reinforced Concrete

sqm or m2 	: Square meter(s)

T or ton	: Metric tonne

103	Scope of Work

- The work to be carried out under the Contract shall consist of the various items as generally described in the Tender Documents as well as in the Bill of Quantities furnished in the Tender Documents.

- The works to be performed shall also include all general works preparatory to the construction of roads, drainage, retaining wall and all other related works. The works shall include work of any kind necessary for the due and satisfactory construction, completion and maintenance of the works to the intent and meaning of the drawings and these Specifications and further drawings and orders that may be issued by the Engineer from time to time. The scope of work shall include compliance by the Contractor with all General Conditions of Contract, whether specially mentioned or not in the various clauses of these Specifications, all materials, apparatus, plant, equipment, tools, fuel, water, strutting, timbering, transport, offices, stores, workshop, staff, labor and the provision of proper and sufficient protective works, diversions, temporary fencing and lighting. It shall also include safety of workers, first-aid equipment, suitable accommodation for the staff and workmen with adequate sanitary arrangements, the effecting and maintenance of all insurances, the payment of all wages, salaries, fees, royalties, duties or other charges arising out of the erection of works and the regular clearance of rubbish, reinstatement and clearing-up of the site as may be required on completion of works, safety of the public and protection of the works and adjoining land.

- The Contractor shall ensure that all actions are taken to build in quality assurance in the planning and execution of works. The quality assurance shall cover all stages of work such as setting out, selection of materials, selection of construction methods, selection of equipment and plant, deployment of personnel and supervisory staff, quality control testing, etc. The work of building in quality assurance shall be deemed to be covered in the scope of the work.

- The Contractor shall furnish, at least 15 days in advance of commencement of work, his programme, the method of working he intends to adopt for various items of work such as site clearance, earthworks, pavement construction, drainage works, curbstones, road markings, installation of traffic signs, and such other items for which the Engineer demands the submission of the method of working. He shall provide information regarding the details of the method of working and equipment he proposes to employ and satisfy the Engineer about the adequacy and safety of the methods adopted by the Contractor which will, however, rest on the Contractor, irrespective of any approval given by the Engineer.

104	Materials

- General

Unless otherwise specifically provided in this Contract, all items incorporated in the completed work, such as plant, materials and other articles are to be new and the most suitable grade for the purpose intended. Unless otherwise specifically provided in this Contract, reference to any plant, material, article, or patented process, by trade name, maker, or catalogue number, shall be regarded as establishing a standard or quality and shall not be construed as limiting competition, and the Contractor may, at his option, use any plant, material, article, or process which, in the judgment of the Engineer, is equal to that named. Unless otherwise specified or instructed, all proprietary materials shall be used in accordance with the Manufacturer's instructions.

When required by the Engineer, the Contractor, before placing any order for materials or manufactured articles to be incorporated in the Permanent Works, shall submit for approval a complete description of such items, the names of the firms from whom he proposes to obtain them, and a list of such of the items that he proposes the firms should supply. When so directed, the Contractor shall submit samples and certificates for approval.

- Storage of Materials

- Materials shall be stored so as to ensure preservation of their specified quality and fitness for the work. They shall be placed on a hard, clean surface and, when required, they shall be placed under cover. Stored materials shall be located so as to facilitate prompt inspection. Private property shall not be used for storage purposes without written permission of the owner and lessee and payment to them, if necessary.

- The stockpile site shall be prepared by clearing and leveling as directed by the Engineer.

- The centre of all aggregate stockpile areas shall be raised and sloped to the sides as required so as to provide proper drainage of excess moisture. The material shall be stored in such manner as to prevent segregation and coning and to ensure proper gradation and moisture content. Coarse aggregate storage piles shall be built up and removed in layers not exceeding one meter. The height of such stockpiles shall be limited to five meters.

- Royalties

The Contractor shall be responsible for all compensation and royalties due in respect of quarried materials. No separate payment will be made for the compensation of royalties, but all such costs shall be included in the applicable unit price and total of the Bill of Quantities.

105	Construction Equipment

In addition to the general conditions indicated in the Contract Documents, the following conditions regarding use of equipment in works shall be satisfied:

- The Contractor shall be required to give a trial run of the equipment for establishing their capability to achieve the laid down Specifications and tolerances to the satisfaction of the Engineer before commencement of the work;

- All equipment provided shall be of proven efficiency and shall be operated and maintained at all times in a manner acceptable to the Engineer;

- All the plant/equipment to be deployed on the works shall be got approved from the Engineer for ensuring their fitness and efficiency before commencement of work;

- Any material or equipment not meeting the approval of the Engineer shall be removed from the site forthwith;

- No equipment will be removed from site without permission of the Engineer; and

- The Contractor shall also make available the equipment for site quality control work as directed by the Engineer.

106	Drawings

- The Contract Drawings provided for tendering purposes shall be as contained in the Tender Documents and shall be used as a reference only. The Contractor should visualize the nature and type of work contemplated and to ensure that the rates and prices quoted by him in the Bill of Quantities have due consideration of the qualitative and quantitative variations, as may be found at the site and complexities of work involved during actual execution/construction.

- The tendered rates/prices for the work shall be deemed to include the cost of preparation, supply and delivery of all necessary drawings, prints, tracings and electronic data which the Contractor is required to provide in accordance with the Contract.

- The Contractor shall prepare the necessary working drawings including road plans and profiles taking into consideration of the topographical survey of the existing site conducted by the Contractor. Three (3) copies of drawings, on the basis of which actual execution of the work is to proceed, with electronic copy shall be submitted to the Engineer for approval, 28 days prior to the commencement of any work.

- Examination and/or approval by the Engineer of any drawings or other documents submitted by the Contractor shall not relieve the Contractor of his responsibilities or liabilities under the Contract.

- The Contractor shall prepare and submit three (3) sets of "As Built" Drawings with electronic copy, including plans, profile, cross sections and details of the roads, structures and facilities, prior to the commencement of the Tests on Completion as indicated in the General Conditions of Contract.

107	Site Information

- The information about the site of work and site conditions in the Tender Documents is given in good faith for guidance only but the Contractor shall satisfy himself regarding all aspects of site conditions.

- The location of the works and the general site particulars are as generally shown on the Site plan/Index plan enclosed with the Tender Documents.

- Whereas the right-of-way to the road sites shall be provided to the Contractor by the Engineer, the Contractor shall have to make his own arrangement for the land required by him for site offices, labor camps, stores, etc.

- The Contractor shall make all arrangements, inclusive of payment, if necessary, for the use of any land required for working areas outside the site or right-of-way, and the Employer will not accept any liability in connection with the use of such land. Any exceptions to this will be given in the Particular Specifications or at the time of Bidding.

108	Setting Out

- The Contractor shall check working Bench Marks tied with the reference Bench Mark in the area soon after taking possession of the site. The reference and working Bench Marks for the area are as indicated in the Contract Documents and the values of the same shall be obtained by the Contractor from the Engineer. The working Bench Marks are more than the rate of four per km along the proposed road. The working Bench Marks/levels shall be approved by the Engineer. Checks must be made on these Bench Marks once every month and adjustments, if any, as agreed by the Engineer and recorded. An up·to·date record of all Bench Marks including approved adjustments, if any, shall be maintained by the Contractor and also a copy shall be supplied to the Engineer for his record.

- The lines and levels of formation, side slopes, drainage works, carriageways and shoulders shall be carefully set out and frequently checked, care being taken to ensure that correct gradients and cross sections are obtained everywhere.

- In order to facilitate the setting out of the works, the centerline of the carriageway or roadway must be accurately established by the Contractor and approved by the Engineer. It must then be accurately referenced in a manner satisfactory to the engineer, every 50m intervals in plain and rolling terrains and in all curve points as directed by the Engineer, with marker pegs and chainage boards set in or road side, and a schedule of, reference dimensions shall be prepared and supplied by the Contractor to the Engineer. These markers shall be maintained until the works reach finished formation level and are accepted by the Engineer.

- On construction reaching the formation level stage, the centerline shall again be set out by the Contractor and when approved by the Engineer, shall be accurately referenced in a manner satisfactory to the Engineer by marker pegs set at the outer limits of the formation.

- No reference peg or marker shall be moved or withdrawn without the approval of the Engineer and no earthwork or structural work shall be commenced until the centerline has been referenced.

- The Contractor will be the sole responsible party for safeguarding all survey monuments, bench marks, beacons, etc. The Engineer will provide the Contractor with the available data necessary for setting out of the centerline. All dimensions and levels shown on the drawings or mentioned in documents forming part of or issued under the contract shall be verified by the Contractor on the site and he shall immediately inform the Engineer of any apparent errors or discrepancies in such dimensions or levels. The Contractor shall, in connection with the staking out of the centerline, survey the terrain along the road and shall submit to the Engineer for his approval, a profile along the road centerline and cross-sections at intervals as required by the Engineer.

- After obtaining approval of the Engineer, work on earthwork can commence and the profile and cross-sections shall form the basis for measurements and payment. The Contractor shall be responsible for ensuring that all the basic traverse points are in place at the commencement of the contract and if any are missing, or appear to have been disturbed, the Contractor shall make arrangements to re·establish these points. A "Survey File" containing the necessary data will be made available for this purpose. If in the opinion of the Engineer, design modifications of the centerline or grade are advisable, the engineer will issue detailed instructions to the Contractor and the Contractor shall perform the modifications in the field, as required, and modify the ground levels on the cross-sections accordingly as many times as required. There will be no separate payment for any survey work performed by the Contractor. The cost of these services shall be considered as being included in the cost of the items of work in the Bill of Quantities.

- The work of setting out shall be deemed to be a part of general works preparatory to the execution of work and no separate payment shall be made for the same.

109	Public Utilities

- Drawings scheduling the affected services like water pipes, sewers, pipelines, cables, gas ducts etc. owned by various authorities including Public Undertakings and Local Authorities included in the Contract Documents shall be verified by the Contractor for the accuracy of the information prior to the commencement of any work.

- Notwithstanding the fact that the information on affected services may not be exhaustive, the final position of these services within the works shall be supposed to have been indicated based on the information furnished by different bodies and to the extent the bodies are familiar with the final proposals. The intermediate stages of the works are, however, unknown at the design stage, these being dictated by the Contractor's methods of working. Accordingly, the Contractor's programme must take into account the period of notice and duration of diversionary works of each body as given on the Drawings and the Contractor must also allow for any effect of these services and alterations upon the Works and for arranging regular meetings with the various bodies at the commencement of the Contract and throughout the period of the works in order to maintain the required coordination. The Engineer and the DCDA will assist such coordination with the local authorities. During the period of the Works, the Contractor shall have no objection if the public utility bodies vary their decisions in the execution of their proposals in terms of programme and construction, provided that, in the opinion of the Engineer, the Contractor has received reasonable notice thereof before the relevant alterations are put in hand.

- No clearance or alterations to the utility shall be carried out unless specially ordered by the Engineer.

- Any services affected by the Works must be temporarily supported by the Contractor who must also take all measures reasonably required by the various bodies to protect their services and property during the progress of the Works.

- The Contractor may be required to carry out certain works for and on behalf of the various bodies and he shall also provide, with the prior approval of the Engineer, such assistance to the various bodies as may be authorized by the Engineer.

- The work of temporarily supporting and protecting the public utility services during execution of the Works shall be deemed to be part of the contract and no extra payment shall be made for the same.

- The Contractor may be required to carry out the removal or shifting of certain services/utilities on specific orders from the Engineer for which payment shall be made to him. Such works shall be taken up by the Contractor only after obtaining clearance from the Engineer and the relevant authorities and ensuring adequate safety measures.

110	Safety and Precautions for Safeguarding the Environment

- The Contractor will be responsible for the safety of the public legitimately passing through the site. All excavations, equipment or items of potential danger to the public must be barricaded and signposted to the satisfaction of the Engineer and the Contractor must provide sufficient watchmen to ensure the safety of the public at all times. All existing pedestrian routes shall be maintained in a safe condition unless an alternative route is provided to the satisfaction of the Engineer.

- All works must be carried out in such a way as to minimize danger to the public and the workmen on the site.

- The Contractor shall take all precautions for safeguarding the environment during the course of the construction of the works. He shall abide by all laws, rules and regulations in force governing pollution and environmental protection that are applicable in the area where the works are situated.

- The Contractor shall carry out the works in such a manner that soil erosion is fully controlled, and sedimentation and pollution of natural water courses, ponds, tanks and reservoirs is avoided.

- Bituminous hot mix plants and concrete batching plants shall be located sufficiently away from habitation, agricultural operations or industrial establishments. The Contractor shall take every precaution to reduce the levels of noise, vibration, dust and emissions from his plant and shall be fully responsible for any claims for damages caused to the owners of property, fields and residences in the vicinity.

- The Contractor shall not use or generate any materials in the works which are hazardous to the health of persons, animals or vegetation. Where it is necessary to use some substances which can cause injury to the health of workers, the Contractor shall provide protective clothing or appliances to his workers.

- The Contractor must take all reasonable steps to minimize dust nuisance during the construction of the works.

- All existing roads used by vehicle of the Contractor or any of his sub- contractors or suppliers of materials or plant, and similarly any new roads which are part of the works and which are being used by traffic, shall be kept clean and clear of all dust/mud or other extraneous materials dropped by the said vehicles or their tires. Similarly, all dust/mud or other extraneous materials from the works spreading on these highways shall be immediately cleared by the Contractor.

- Clearance shall be effected immediately by manual sweeping and removal of debris, if so directed by the Engineer, by mechanical sweeping and clearing equipment, and all dust, mud and other debris shall be removed entirely from the road surface shall be hosed or watered using suitable equipment.

- Any structural damage caused to the existing roads by the Contractor's construction equipment shall be made good without any extra cost.

- The cost of complying with this Clause will not be paid for directly, but will be considered to be included in the general items of Contract prices for any pay items under this Contract.

111	Arrangement for Traffic during Construction

- General
The Contractor shall at all-time carry out works on the roadway in a manner creating least interference to the flow of traffic while consistent with the satisfactory execution of the same. For all works involving improvements to the existing roadway, the Contractor shall, in accordance with the directives of the Engineer, provide and maintain, during execution of the work, a passage for traffic either along a part of the existing carriageway under improvement. The Contractor shall take prior approval of the Engineer regarding traffic arrangements during construction.

112	General Rules for the Measurement of Works for Payment

All measurements shall be made in the metric system. Different items of work listed in the Bill of Quantity shall be measured in accordance with the procedures set forth in the relevant sections read in conjunction with the General Conditions of Contract.

113	Scope of Rates for Different Items of Work

- For item rate Contracts, the Contract unit rates for different items of work shall be payment in full for completing the work to the requirements of the Specifications including full compensation for all the operations detailed in the relevant sections of these Specifications under "Rates.” In the absence of any directions to the contrary, the rates are to be considered as the full inclusive rate for finished work covering all labor, materials, wastage, temporary work, plant, equipment, overhead charges, taxes and profit as well as the general liabilities, obligations, insurance and risks arising out of General Conditions of Contract.

- The general items (Preliminary) quoted by the Contractor shall, unless otherwise specified, also include compliance with/supply of the following:

- General works such as setting out, clearance of site before setting out and clearance of works after completion, etc.;

- A detailed programme for the construction and completion of the work (using CPM/PERT technique) giving, in addition to construction activities, detailed network activities for the submission and approval of materials, procurement of critical materials and equipment. fabrication of special products/equipment and their installation and testing, and for all activities of the Employer that are likely to affect the progress of work, etc., including updating of all such activities on the basis of the decisions taken at the periodic site review meetings or as directed by the Engineer.

- Samples of various materials proposed to be used on the Work for conducting tests thereon as required as per the provisions of the Contract.

- Design of mixes as per the relevant Clauses of the Specifications giving proportions of ingredients, sources of aggregates and binder along with accompanying trial mixes as per the relevant clauses of these Specifications to be submitted to the Engineer for his approval before use on the Works;

- Detailed design calculations and drawings for all Temporary Works (such as form-work, staging, centering; specialized constructional handling and launching equipment and the like);

- Detailed drawings for templates, support and end anchorage, details for pre-stressing cable profiles, bar bending and cutting schedules for reinforcement, material lists for fabrication of the Specifications;

- Mill test reports for all mild and high tensile steel and cast steel as per the relevant provisions of the Specifications;

- Testing of various finished items and materials including bitumen, cement, concrete, bearings as required under these Specifications and furnishing test reports/certificates;

- Inspection Reports in respect of form work, staging, reinforcement and other items of work as per the relevant Specifications;

- Any other data which may be required as per these Specifications or the Conditions of contract or any other annexure/schedules forming part of the Contract;

- Any other item of work which is not specifically provided in the Bill of Quantities but which is necessary for complying with the provisions of the Contract;

- All temporary works, formwork and false work;

- Establishing and running a laboratory with facilities for testing for various items of works as specified in these Specifications, where there is no separate item in the Bill of Quantities for establishing and running a laboratory;

- Cost of in-built provisions for Quality Assurance;

- Cost of safeguarding the environment; and

- Cost of providing "as-built drawings.”

- The Contractor is recommended to visit the site and satisfy himself with the existing conditions of construction there in, the risk of injury or damage to existing property or to the occupiers of this property. The nature of materials existing and conditions under which the works will be carried out, the supply of and conditions affecting labor and facilities for obtaining the articles or materials referred in the Bills of Quantities. No claim by the Contractor for additional payment will be allowed on the grounds of any misunderstanding. Any damage to existing components must be made good.

- Defects, shrinkages or other faults which are attributed by the Project Supervisor to work executed under this contract shall be made good by the Contractor at his own cost

- The Contractor must allow for providing, erecting and maintaining 2 No. site sign boards, the size, type of construction and lettering of which shall be to the Engineer's design. One sign board is to be erected in a suitable location on the main road, which indicates the direction of the site and one erected at the work site. On completion of the works, the sign boards shall be removed and making good shall be carried out as necessary

- The Contractor shall furnish all reports such as daily, weekly, and monthly reports and photos at every construction stages at the completion of the works.

114	Methodology and Sequence of Work

Prior to start of the construction activities at site, the contractor shall, within 14 days after the date of the commencement, submit to the Engineer for approval, the detailed construction methodology including mechanical equipment proposed to be used, sequence of various activities and schedule from start to end of the project. Programme relating to pavement and shoulder construction shall be an integrated activity to be done simultaneously in a co-ordinated manner. The methodology and the sequence shall be so planned as to provide proper safety, drainage and free flow of traffic.

115	Use of Surfaces by Construction Traffic

Ordinarily, no construction traffic shall be allowed on pavement under construction unless authorized by the Engineer. Even in that case the load and intensity of construction traffic should be so regulated that no damage is caused to the sub grade or pavement layers already constructed. Where necessary, service roads shall be constructed for this purpose and the same shall be considered as incidental to the work.

The wheels or tracks of plant moving over the various pavement courses shall be kept free of deleterious materials.

Bituminous base course shall be kept clean and uncontaminated as long as the same remains uncovered by a wearing course or surface treatment. The only traffic permitted access to the base course shall be that engaged in laying and compacting the wearing course or that engaged on such surface treatment where the base-course is to be blinded and/or surface dressed. Should the base course or tack coat on the base course become contaminated, the Contractor shall make good by clearing it to the satisfaction of the Engineer, and if this is impracticable, by removing the layer and replacing it to Specification without any extra cost.

116 Mobilizations

Mobilization of plant, equipment, temporary works including site office as mentioned below, personnel, etc required to carry out the works shall be prepared by the Contractor.

Living Quarters, Sheds, and Stores

The Contractor shall supply, equip and maintain for the Contract period all his own living accommodation, sheds and stores necessary for the execution of the Work, and shall make his own arrangements, subject to the approval of the Engineers, with the owner of any land required and, if necessary, pay for its use.

The furnishing and maintenance of living quarters, sheds, and stores shall be paid separately and deemed to be included in the cost of mobilizations and demobilization items in the Bill of Quantities.

117 Demobilizations

Demobilization of plant, equipment, temporary works, personnel, etc required to carry out the works. On completion of the contract, the site and the works shall be cleared of all plant, scaffolding, rubbish and unused materials and shall be delivered up clean and in perfect condition in every respect to the satisfaction of the Engineer. These costs deemed to be included in the cost of mobilization and demobilizations item in the Bill of Quantities.

118 Site preparations

The Contractor shall keep close relationship with local communities and authorities.

Meetings with Representative of CDC or Malik shall be held prior to commencement of the works for smooth implementation of the works. These costs deemed to be included in the cost of preliminary item in the Bill of Quantities.

119 Security measures

Security measures shall be taken for safety of workmen and smooth implementation of the works. The Contractor shall allow for providing for the safety, health and welfare of workers and for complying with any relevant ordinances, regulations or Union Agreement. These costs deemed to be included in the cost of These costs deemed to be included in the cost of preliminary item in the Bill of Quantities.

120 Topographic survey

Center line survey, longitudinal survey and cross section survey for the road alignment and installation of pegs shall be carried out prior to the commencement of construction works. These costs deemed to be included in the cost of Topographic survey item in the Bill of Quantities.

121 Insurance

Insurance shall cover for workmen, equipment and third party. The minimum insurance amounts and deductibles shall be:

(a) for the Works, Plant and Materials: 110% of the contract amount.

(b) for loss or damage to Equipment: Afghani 250,000

(c) for loss or damage to property in connection with Contract but excepting the Works, Plant, Materials, and Equipment: 150% of the contract amount

(d) for personal injury or death:

(i) of the Contractor’s employees:Afghani1,250,000 per event.

(ii) of other people: Afghani1,250,000 per event

These costs deemed to be included in the cost of Insurance item in the Bill of Quantities.

SECTION 2: EARTHWORKS

201	Site Clearance (not applied)

202	Removal of Structures and Obstructions

202.1	Scope

This work shall consist of removing, as hereinafter set forth, existing culverts, bridges, pavements, curbs and other structures like guard-rails, fences, utility services, manholes, catch basins, inlets, etc., which are in place but interfere with the new construction or are not suitable to remain in place, and of salvaging and disposing of the resulting materials and back filling the resulting trenches and pits.
Existing culverts, bridges, pavements and other structures which are within the right-of-way and which are designated for removal, shall be removed up to the limits and extent specified in the drawings or as indicated by the Engineer.

Dismantling and removal operations shall be carried out with such equipment and in such a manner as to leave undisturbed, adjacent pavement, structures and any other work to be left in place.

All operations necessary for the removal of any existing structure which might endanger new construction shall be completed prior to the start of new work.

202.2	Dismantling Culverts and Bridges

The structures shall be dismantled carefully and the resulting materials so removed as not to cause any damage to the serviceable materials to be salvaged, the part of the structure to be retained and any other properties or structures nearby.

Unless otherwise specified, the superstructure portion of culverts/bridges shall be entirely removed and other parts removed below the ground level or as necessary depending upon the interference they cause to the new construction. Removal of overlying or adjacent material, if required in connection with the dismantling of the structures, shall be incidental to this item. Where existing culverts/bridges are to be extended or otherwise incorporated in the new work, only such part or parts of the existing structure shall be removed as are necessary and directed by the Engineer to provide a proper connection to the new work. The connecting edges shall be cut, chipped and trimmed to the required lines and grades without weakening or damaging any part of the structure to be retained. Due care should be taken to ensure that reinforcing bars which are to be left in place so as to project into the new work as dowels or ties are not injured during removal of concrete.

Pipe culverts shall be carefully removed in such a manner as to avoid damage to the pipes. Steel structures shall, unless otherwise provided, be carefully dismantled in such a manner as to avoid damage to members thereof if specified in the drawings or directed by the Engineer that the structure is to be removed in a conditions suitable for re-erection, all members shall be match-marked by the Contractor with white lead paint before dismantling; end pins, nuts, loose plates, etc., shall be similarly marked to indicate their proper location; all pins, pin holes and machined surfaces shall be painted with a mixture of white lead and tallow and all loose parts shall be securely wired to adjacent members or packed in boxes.

Timber structures shall be removed in such a manner as to avoid damage to such timber or lumber as is designated by the Engineer to be salvaged.

202.3	Dismantling Pavements and Other Structures

In removing pavements, curbs, gutters, and other structures like guard-rails, fences, manholes, catch basins, inlets, etc., where portions of the existing construction are to be left in the finished work, the same shall be removed to an existing joint or cut and chipped to a true line with a face perpendicular to the surface of the existing structure. Sufficient removal shall be made to provide for proper grades and connections with the new work as directed by the Engineer.

All concrete pavements, base course in carriageway and shoulders etc. designated for removal shall be broken to pieces whose volume shall not exceed 0.02cu.m, and stockpiled at designated locations if the material is to be used later or otherwise arranged for disposal as directed (see Clause 202.5).

202.4	Back-filling

Holes and depressions caused by dismantling operations shall be back-filled with excavated or other approved materials and compacted to required density as directed by the Engineer.

202.5	Disposal of Materials

All materials obtained by dismantling shall be the property of the Government. Unless otherwise specified, materials having any salvage value shall be placed in neat stacks of like materials within the right-of-way, as directed by the Engineer with all lifts and up to a lead of 1000 m.

Pipe culverts that are removed shall be cleaned and neatly piled on the right-of-way at points designated by the Engineer with all lifts and lead up to 1000 m. Structural steel removed from old structures shall, unless otherwise specified or directed, be stored in a neat and presentable manner on blocks in locations suitable for loading. Structures or portions thereof which are specified in the contract for re-erection shall be stored in separate piles.

Timber or lumber from old structures which is designated by the Engineer as materials to be salvaged shall have all nails and bolts removed there from and shall be stored in neat piles in locations suitable for loading.

All materials obtained from dismantling operations which, in the opinion of the Engineer, cannot be used or auctioned shall be disposed of as directed by the Engineer with all lifts and up to a lead of 10 km.

202.6	Method of Measurement

The work of dismantling structures shall be paid for in units indicated below by taking measurements before and after, as applicable:

202 (1) Dismantling brick/stone masonry structures	cu. m.

202 (2) Dismantling plain concrete structure   	cu. m.

202 (3) Chipping of reinforced concrete structures	cu. m

202.7	Rates

The Contract unit rates for the various items of dismantling shall be paid in full for carrying out the required operations including full compensation for all labor, materials, tools, equipment, safeguards and incidentals necessary to complete the work. These will also include excavation and back-filling where necessary to the required compaction and for handling, salvaging, piling and disposing of the dismantled materials within all lifts and up to a lead of 10 km.

203	Road Excavation

203.1	Scope

The work shall consist of excavation, removal and satisfactory disposal of all materials necessary for the construction of roadway, side drains and waterways in accordance with requirements of these Specifications and the lines, grades and cross' sections shown in the drawings or as indicated by the Engineer. It shall include the hauling and stacking of or hauling to sites of embankment and sub grade construction, suitable cut materials as required, as also the disposal of unsuitable cut materials in specified manner, trimming and finishing of the road to specified dimensions or as directed by the Engineer.

203.2	Classification of Excavated Material

203.2.1	Classification

All materials involved in excavation shall be classified by the Engineer in the following manner:

(1) Soil

This shall comprise topsoil, turf, sand, silt, loam, clay, mud, peat, black cotton soil, soft shale or loose moorum, a mixture of these and similar material which yields to the ordinary digging implement. Removal of gravel or any other nodular material having dimension in any one direction not exceeding 75ml11 occurring in such strata shall be deemed to be covered under this category.

(2) Ordinary Rock (not requiring blasting)
This shall include:

- rock types such as laterites, shale and conglomerates, varieties of limestone and sandstone etc., which may be quarried or split with crow bars, also including any rock which in dry state may be hard, requiring blasting but which, when wet, becomes soft and manageable by means other than blasting.

- Macadam surfaces such as water bound and bitumen/tar bound; soling of roads, paths etc. and hard core; compact moorum or stabilized soil requiring grafting tool or pick or both and shovel, closely applied; gravel and cobble stone having maximum dimension in any one direction between 75 and 300mm;

- Lime concrete, stone masonry in lime mortar and brick work in lime/cement mortar below ground level, reinforced cement concrete which may be broken up with crow bars or picks and stone masonry in cement mortar below ground level; and

- Boulders which do not require blasting having maximum dimension in any direction of more than 300mm, found lying loose on the surface or embedded in river bed, soil, talus, slope wash and terrace material of dissimilar origin.

203.2.2 Authority for classification

The classification of excavation shall be decided by the Engineer and his decision shall be final and binding on the Contractor. Merely the use of explosives in excavation will not be considered as a reason for higher classification unless blasting is clearly necessary in the opinion of the Engineer.

203.3 Construction Operations

203.3.1 Setting Out

After the site has been cleared as per Clause 201, the limits of excavation shall be set out true to lines, curves, slopes, grades and sections as shown on the drawings or as directed by the Engineer. The Contractor shall provided all labor, survey instruments and materials such as strings, pegs, nails, bamboos, stones, lime, mortar, concrete, etc., required in connection with the setting out of works and the establishment of bench marks. The Contractor shall be responsible for the maintenance of bench marks and other marks and stakes as long as in the opinion of the Engineer, they are required for the work.

203.3.2 Stripping and storing topsoil

When so directed by the Engineer, the topsoil existing over the sites of excavation shall be stripped to the specified depths and stockpiled at designated locations for re-use in covering embankment slopes, cut slopes, berms and other disturbed areas where re-vegetation is desired. Prior to stripping the topsoil, all trees, shrubs etc. shall be removed along with their roots, with approval of the Engineer.

203.3.3 Excavation General

All excavation shall be carried out in conformity with the directions laid here-in-under and in a manner approved by the Engineer. The work shall be so done that the suitable materials available from excavation are satisfactorily utilized as decided upon beforehand.

While planning or executing excavations, the Contractor shall take all adequate precautions against soil erosion, water pollution etc., and take appropriate drainage measures to keep the site free of water.

The excavations shall conform to the lines, grades, side slopes and levels shown on the drawings or as directed by the Engineer. The Contractor shall not excavate outside the limits of excavation. Subject to the permitted tolerances, any excess depth/width excavated beyond the specified levels/dimensions on the drawings shall be made good at the cost of the Contractor with suitable material of characteristics similar to that removed and compacted to the requirements in the relevant clause in the Specification.

All debris and loose material on the slopes of cuttings shall be removed. No backfilling shall be allowed to obtain required slopes excepting that when boulders or soft materials are encountered in cut slopes, these shall be excavated to approved depth on instructions of the Engineer and the resulting cavities filled with suitable material and thoroughly compacted in an approved manner.

After excavation, the sides of excavated area shall be trimmed and the area contoured to minimize erosion and ponding, allowing for natural drainage to take place. If trees were removed, new trees shall be planted, as directed by the Engineer. The cost of planting new trees shall be deemed to be incidental to the work.

203.3.4	Methods, tools and Equipments

Only such methods, tools and equipment as approved by the Engineer shall be adopted/used in the work. If so desired by the Engineer, the Contractor shall demonstrate the efficacy of equipment to be used before the commencement of work.

203.3.5 Dewatering

The Contractor shall arrange for the rapid dispersal of water collected/accumulated on the earthwork or completed formation during construction or on the existing roadway or which enters the earthwork or any other item of work from any source, and where practicable, the water shall be discharged in to the permanent outfall of the drainage system. The arrangements shall be made in respect of all earthworks including excavation for pipe trenches, foundations or cuttings.

The Contractor shall provide, where necessary, temporary water courses, ditches, drains, pumping or other means for maintaining the earthwork free from water. Such provisions shall include carrying out the work of forming the cut sections and embankments in such manner that their surfaces have at all times a sufficient minimum cross fall and where practicable, a sufficient longitudinal gradient to enable them to shed water and prevent ponding.

If water is met with in the excavations due to springs, seepage, rain or other causes, it shall be removed by suitable diversions, pumping or bailing out and the excavation kept dry whenever so required or directed by the Engineer. Care shall be taken to discharge the drained water into suitable outlets as not to cause damage to the works, crops or any other property. Due to any negligence on the part of the Contractor, if any such damage is caused, it shall be the sole responsibility of the Contractor to repair/restore to the original condition at his own cost o r compensate for the damage.

203.3.6 Disposal of excavated materials

All the excavated materials shall be the property of the employer. The material obtained from the excavation of roadway, shoulders, verges, drains, cross-drainage works etc., shall be used for filling up of (i) roadway embankment, (ii) the existing pits in the right-of-way and (iii) for landscaping of the road as directed by the Engineer, including leveling and spreading with all lifts and lead up to 500m and no extra payment shall be made for the same.

All hard materials, such as rubble not intended for use as above shall be stacked neatly on specified land as directed by the Engineer with all lifts and lead up to 500 m.

Unsuitable and surplus material not intended for use within the lead specified above shall also, if necessary, be transported with all lifts and lead beyond initial 500m, disposed of or used as approved by the Engineer.

203.3.7 Backfilling

Backfilling of masonry/concrete/hume pipe drain excavation shall be done with approved material after concrete/masonry/hume pipe is fully set and carried out in such a way as not to cause undue thrust on any part of the structure and/or not to cause differential settlement. All space between the drain walls and the side of the excavation shall be refilled to the original surface making due allowance for settlement, in layer generally not exceeding 150 mm compacted thickness to the required density, using suitable compaction equipment such as mechanical tamper, rammer or plate compactor as approved by the Engineer.

203.4 Plying of Construction Traffic

Construction traffic shall not use the cut formation and finished subgrade without the prior permission of the Engineer. Any damage arising out of such use shall be made good by the Contractor at his own expense.

203.5 Preservation of Property

The Contractor shall undertake all reasonable precautions for the protection and preservation of any or all existing roadside trees, drains, sewers or other sub "surface drains, pipes, conduits and any other structures under or above ground, which may be affected by construction operations and which, in the opinion of the Engineer, shall be continued in use without any change. Safety measures taken by the Contractor in this respect, shall obtain approval from the Engineer. However, if any of these objects is damaged by reason of the Contractor's negligence, it shall be replaced or restored to the original condition at his expense. If the Contractor fails to do so, within the required time as directed by the Engineer or if, in the opinion of the Engineer, the actions initiated by the Contractor to replace/restore the damaged objects are not satisfactory, the Engineer shall arrange the replacement/restoration directly through any other agency at the risk and cost of the Contractor after issuing a prior notice to the effect.

203.6 Preparation of Cut Formation

The cut formation, which serves as a sub grade, shall be prepared to receive the sub-base/base course as directed by the Engineer.

Where the material in the sub grade (that is within 500 mm from the lowest level of the pavement) has a density less than 95% of the maximum dry density determined according to AASHTO T 99, the same shall be loosened to a depth of 500 mm and compacted in layers in accordance with the requirements of Clause 205 "Embankment.” Any unsuitable material encountered in the sub grade level shall be removed as directed by the Engineer and replaced with suitable material compacted in accordance with Clause 205 "Embankment.”

In rocky formations, the surface irregularities shall be corrected and the levels brought up to the specified elevation with granular base material as directed by the Engineer, laid and compacted in accordance with the respective Specifications for these materials. The unsuitable material shall be disposed of in accordance with Clause 203.3.9 "Disposal of Excavated Materials.” After satisfying the density requirements, the cut formation shall be prepared to receive the sub-base/base course in accordance with Clause 206 "Subgrade Preparation" to receive the sub-base/base course.

203.7 	Method of Measurement

Excavation for roadway shall be measured by taking cross sections at suitable intervals in the original position before the work starts and after its completion and computing the volumes in cubic meters. By the method of average end areas for each class of material encountered. Where it is not feasible to compute volumes by this method because of erratic location of isolated deposits, the volumes shall be computed by other accepted methods.

At the option of the Engineer, the Contractor shall leave depth indicators during excavations of such shape and size and in such position as directed so as to indicate the original ground level as accurately as possible. The Contractor shall see that these remain intact till the final measurements are taken.

203 (1) Road Excavation:		    cum

203(2) Transport of soil 500m-1000m  cum

203(3) Transport of soil up to 2000m     cum

203.8 Rates

The Contract unit rate for the item of road excavation shall be payment in full for carrying out the operations required regardless of any classification of soil including full compensation for

- Setting out;

- Transporting the excavated materials and depositing the same on sites of embankments, spoil banks or stacking as directed within all lifts and lead specified in these Specifications;

- trimming bottoms and slopes of excavation;

- dewatering;

- keeping the work free of water; and

- all labors, materials, tools, equipment, safety measures, testing and incidentals necessary to complete the work to Specifications.

204 Structure Excavation

204.1 Scope

Excavation for structures shall consist of the removal of material for the construction of foundation for culverts, retaining walls, headwalls, cutoff walls, pipe culverts, and other similar structures, in accordance with the requirements of these Specifications and the lines and dimensions shown on the drawings or as indicated by the Engineer. The work shall include construction of the necessary cofferdams and cribs and their subsequent removal; all necessary sheeting, shoring, bracing, draining and pumping; the removal of all logs, stumps, grubs and other deleterious matter and obstructions, necessary for placing the foundations; trimming bottoms of excavations; backfilling and clearing up the site and the disposal of all surplus material.

It shall also include the furnishing and placing of approved foundation fill material to replace unsuitable material encountered below the foundation elevation of structures.

204.2	Classification of Excavation

All materials involved in excavation shall be classified in accordance with Clause 201.2.

204.3	Construction Operations

204.3.1	Setting out

After the site has been cleared, the limits of excavation shall be set out true to lines, curves and slopes.

204.3.2	Excavation

Excavation shall be taken to the width of the lowest step of the footing and the sides shall be left plump where the nature of soil allows it. Where the nature of soil or the depth of the trench and season of the year do not permit vertical sides, the Contractor at his own expense shall put up necessary shoring, strutting and planking or cut slopes to a safer angle or both with due regard to the safety of personal and works and to the satisfaction of the Engineer.

The depth to which the excavation is to be carried out shall be as shown on the drawings, unless the type of material encountered is such as to require changes, in which case the depth shall be as ordered by the Engineer. Propping shall be undertaken when any foundation or stressed zone from an adjoining structure is within a line of 1 vertical to 2 horizontal from the bottom of the excavation.

204.3.3	Dewatering and protection

Normally, open foundations shall be laid dry. Where water is met with in excavation due to stream flow, seepage, springs, rain or other reasons, the Contractor shall take adequate measures such as bailing, pumping, constructing diversion channels, drainage channels, bunds, depression of water level by well "point system, cofferdams and other necessary works to keep the foundation trenches dry when so required and to protect the green concrete/masonry against damage by erosion or sudden rising of water level. The methods to be adopted in this regard and other details thereof shall be left to the choice of the Contractor but subject to approval of the Engineer. Approval of the Engineer shall, however, not relieve the Contractor of the responsibility for the adequacy of dewatering and protection arrangements and for the quality and safety of the works.

Where cofferdams are required, these shall be carried to adequate depths and heights, be safely designed and constructed and be made as watertight as is necessary for facilitating construction to be carried out inside them. The interior dimensions of the cofferdams shall be such as to give sufficient clearance for the construction and inspection and to permit installation of pumping equipments, etc., inside the enclosed area.

If it is determined beforehand that the foundations cannot be laid dry or the situation is found that the percolation is too heavy for keeping the foundation dry, the foundation concrete shall be laid under water by tremie pipe only. In case of flowing water or artesian springs, the flow shall be stopped or reduced as far as possible at the time of placing the concrete.

Pumping from the interior of any foundation enclosure shall be done in such a manner as to preclude the possibility of the movement of water through any fresh concrete. No pumping shall be permitted during the placing of concrete or for any period of at least 24 hours thereafter, unless it is done from a suitable sump separated from the concrete work by a watertight wall or other similar means.

At the discretion of the Contractor, cement grouting or other approved methods may be used to prevent or reduce seepage and to product the excavation area.

The Contractor shall take all precautions in diverting channels and in discharging the drained water as not to cause damage to the works, crops or any other property.

204.3.4 Preparation of foundation

The bottom of the foundation shall be leveled both longitudinally and transversely or stepped as directed by the Engineer. Before foundation is laid, the surface shall be slightly watered and rammed in the event of excavation having been made deeper than that shown on the drawings or as otherwise ordered by the Engineer, the extra depth shall be made up with concrete or masonry of the foundation at the cost of the Contractor. Ordinary filling shall not be used for the purpose to bring the foundation to level.

When rock or other hard strata is encountered it shall be freed of all soft and loose material, cleaned and cut to a firm surface either level and stepped as directed by the Engineer. All seams shall be cleaned out and filled with cement mortar or grout to the satisfaction of the Engineer. In the case of excavation in rock, annular space around footing shall be filled with lean concrete (1:3:6 nominal mix) up to the top level of rock.

The foundation shall be as shown on the Drawings.

When gravel or crushed stone foundation fill is shown in the Drawings, it shall be laid and compacted to the thickness shown in the Drawings in layers not greater than 150 mm. In case such foundation fill is not shown in the Drawings but the excavation bottom is soft or mucky or otherwise unsuitable, as determined by the Engineer, the Contractor shall remove the unsuitable material and replaced by gravel or crushed stone foundation fill and compacted in layers not greater than 150mm. Lean concrete of strength not less than 15 MPa shall be placed over the excavation bottom or top of the gravel or crushed stone foundation fill to the bottom level of the structure foundation. The thickness of the lean concrete shall be as shown on the drawings and shall not be less than 50mm.

204.3.5	Slips and slip·outs

If there are any slips or slip-outs in the excavation, these shall be removed by the Contractor at his own cost.

204.3.6	Public safety

Near towns, villages and all frequented places, trenches and foundation pits shall be securely fenced, provided with proper caution signs and marked with red lights at night to avoid accidents. The contractor shall take adequate protective measures to see that the excavation operations do not affect or damage adjoining structures.

204.3.7	Backfilling

Backfilling shall be done with approved material after concrete or masonry is fully set and carried out in such a way as not to cause undue thrust on any part of the structure. All space between foundation masonry or concrete and the sides of excavation shall be refilled to the original surface or designed ground level in layers not exceeding 150 mm of compacted thickness. The compaction shall be done with the help of suitable equipment such as mechanical tamper, ramper, plate vibrator etc., after necessary watering, so as to achieve a density not less than the field density before excavation.

204.4 Method of Measurements

Excavation for structures shall be measured in cubic meters regardless of any class of material encountered, limited to the dimensions shown on the drawings or as directed by the Engineer. Excavation over increased width, cutting of slopes, shoring, shuttering and planking shall be deemed as convenience for the Contractor in executing the work and shall not be measured and paid for separately.

Foundation preparation shall be measured in square meters in final position of structures.

Stone foundation, when shown in drawings, shall be measured in cubic meters in the final position with the special granular material placed below the foundation of structures as specified, completed in place and accepted.

Structure backfilling shall be measured in cubic meters.

204 (1) Structure Excavation	cum

204 (2) Foundation preparation	sqm

204(3) Stone foundation           cum

204 (4) Structure backfilling 	cum

204.5 Rates

The Contract unit rate for the structure excavation shall be payment in full for carrying out the required operations including full compensation for:

- setting out;

- construction of necessary cofferdams, cribs, sheeting, shoring and bracing and their subsequent removal;

- removal of all logs, stumps, grubs and other deleterious matter and obstructions for placing the foundations including pumping when no separate provision for it is made in the Contract;

- clearing up the site and disposal of all surplus material within all lifts and leads up to 500m or as otherwise specified; and

- all labors, materials, tools, equipment, safety measures, diversion of traffic and incidentals necessary to complete the work to Specification.

205	Embankment and Fill

205.1	Scope

These Specifications shall apply to the construction of embankments including subgrades, earthen shoulders and miscellaneous backfills with approved material obtained from roadway and structure excavation, borrow pits or other sources. All embankments, sub grades, earthen shoulders and miscellaneous backfills shall be constructed in accordance with the requirements of these Specifications and in conformity with the lines, grades, and cross' sections shown on the drawings or as directed by the Engineer.

205.2	Material Requirements

205.2.1	Physical requirements

The materials used in embankments, sub grades, earthen shoulders and miscellaneous backfills shall be soil, gravel, a mixture of these or any other material approved by the Engineer. Such materials shall be free of logs, stumps, roots, rubbish or any other ingredient likely to deteriorate or affect the stability of the embankment/subgrade.

The following types of material shall be considered unsuitable for embankment and fill:

(a) Materials from swamps, marshes and bogs;

(b) Peat, log, stump and perishable material;

(c) Materials in a frozen condition;

(d) Clay having liquid limit exceeding 70 and plasticity index exceeding 45; and

(e) Material with salts resulting in leaching in the embankment.

205.2.2	Source of Materials

The materials for embankment shall be obtained from approved sources with preferences given to materials becoming available from nearby roadway excavation or any other excavation under the same Contract.

The work shall be so planned and executed that the best available materials are saved for the sub grade and the embankment portion just below the sub grade.

Where the materials are to be obtained from designated borrow areas, the location, size and shape of these areas shall be as indicated by the Engineer and the same shall not be opened without his written permission. Where specific borrow areas are not designated by the Employer/the Engineer, arrangement for locating the source of supply of material for embankment and sub grade as well as compliance to environmental requirements in respect of excavation and borrow areas as stipulated, from time to time by the relevant authority of the Government of Afghanistan and the local bodies, as applicable, shall be the sole responsibility of the Contractor.

Borrow pits along the road shall be discouraged. If permitted by the Engineer, these shall not be dug continuously. Ridges of not less than 8 m width should be left at intervals not exceeding 300 m. Small drains shall be cut through the ridges to facilitate drainage. The depth of the pits shall be so regulated that their bottom does not cut an imaginary line having a slope of 1 vertical to 4 horizontal projected from the edge of the final section of the bank, the maximum depth in any case being limited to l.5 m. Also, no pit shall be dug within the offset width from the toe of the embankment required as per the consideration of stability with a minimum width of 10 m.

Haulage of material to embankments or other areas of fill shall proceed only when sufficient spreading and compaction plant is operating at the place of deposition.

No excavated acceptable material other than surplus to requirements of the Contract shall be removed from the site. Should the Contractor be permitted to remove acceptable material from the site to suit his operational procedure, then he shall make good any consequent deficit of material arising therefrom.

Where the excavation reveals a combination of acceptable and unacceptable material, the Contractor shall, unless otherwise agreed by the Engineer, carry out the excavation in such a manner that the acceptable materials are excavated separately for use in the permanent works without contamination by the unacceptable materials. The acceptable materials shall be stockpiled separately.

The Contractor shall ensure that he does not adversely affect the stability of excavation or fills by the representative samples from each of the identified borrow areas and have these tested at the size laboratory following a testing programme approved by the Engineer. It shall be ensured that the subgrade material when compacted to the density requirements shall yield the design CBR value of the subgrade.

205.3	Construction Operations

205.3.1	Setting out

After the site has been cleared to Clause 201, the work shall be set out to Clause 203.3. l. The limits of embankment/subgrade shall be marked by fixing batter pegs on both sides at regular intervals as guides before commencing the earthwork. The embankment/ subgrade shall be built sufficiently wider than the design dimension so that surplus material may be trimmed, ensuring that the remaining material is to the desired density and in position specified and conforms to the specified side slopes.

205.3.2 Dewatering

If the foundation of the embankment is in an area with stagnant water, and in the opinion of the Engineer it is feasible to remove it, the same shall be removed by bailing out or pumping, as directed by the Engineer and the area of the embankment foundation shall be kept dry. Care shall be taken to discharge the drained water so as not to cause damage to the works, crops or any other property. Due to any negligence on the part of the Contractor, if any such damage is caused, it shall be the sole responsibility of the Contractor to repair/restore it to original condition or compensate the damage at his own cost.

205.3.3	Stripping and storing topsoil

In localities where most of the available embankment materials are not conductive to plant growth, or when so directed by the Engineer, the topsoil from all areas of cutting and from all areas to be covered by embankment foundation shall be stripped to specified depths not exceeding 150 mm and stored in stockpiles of height not exceeding 2 m for covering embankment slopes. Cut slopes and other disturbed areas where re-vegetation is desired. Topsoil shall not be unnecessarily trafficked either before stripping or when in a stockpile. Stockpiles shall not be surcharged or stripping or otherwise loaded and multiple handle shall be kept to a minimum.

205.3.4	Compacting ground supporting embankment1subgrade

Where necessary, the original ground shall be leveled to facilitate placement of first layer of embankment, scarified, mixed with water and then compacted by rolling so as to achieve 95 percent of the maximum dry density determined according to AASHTO T 99.

In case where the difference between the subgrade level (top of the sub grade on which pavement rests) and ground level is less than 0.5 m and the ground does not have 95 percent of the maximum dry density, the ground shall be loosened up to a level 0.5 m below the sub grade level, watered and compacted in layers in accordance with Clauses 205.3.5 and 205.3.6 to not less than 95 percent of the maximum dry density determined according to AASHTO T 99. Where so directed by the Engineer, any unsuitable material occurring in the embankment foundation shall be removed and replaced by approved materials laid in layers to the required degree of compaction.

Embankment or sub grade work shall not proceed until the foundations for embankment/subgrade have been inspected by the Engineer for satisfactory condition and approved.

Any foundation treatment specified for embankments especially high embankments, resting on suspect foundations as revealed by borehole logs shall be carried out in a manner and to the depth as desired by the Engineer. Where the ground on which an embankment is to b e built has any of the material types (a) to (f) n Clause 205.2. 1, a t least 500 mm o f such material must b e removed and replaced by acceptable fill material before embankment construction commences.

205.3.5 Spreading material in layers and bringing to appropriate moisture content

The embankment and subgrade material shall be spread in layers of uniform thickness not exceeding 200 mm compacted thickness over the entire width of embankment by mechanical means, finished by a motor grader and compacted as per Clause 205.3.6. The motor grader blade shall have hydraulic control suitable for initial adjustment and maintain the same so as to achieve the specific slope and grade. Successive layers shall not be placed until the layer under construction has been thoroughly compacted to 95 percent of the maximum dry density determined according to AASHTO T 99 and approved by the Engineer. Each compacted layer shall be finished parallel to the final cross' section of the embankment.

Moisture content of the material shall be checked at the site of placement prior to commencement of compaction; if found to be out of agreed limits, the same shall be made good. Where water is required to be added in such constructions, water shall be sprinkled from a water tanker fitted with sprinkler capable of applying water uniformly with a controllable rate of flow to variable widths of surface but without any flooding. The water shall be added uniformly and thoroughly mixed in soil until uniform moisture content is obtained throughout the depth of the layer.

After adding the required amount of water, the soil shall be processed by means of graders, harrows, rotary mixers or as otherwise approved by the Engineer until the layer is uniformly wet.

Clods or hard lumps of earth shall be broken to have a maximum size of 75 mm when being placed in the embankment and a maximum size of 50 mm when being placed in the sub grade. Embankment and other areas of fill shall, unless otherwise required in the Contract or permitted by the Engineer, be constructed evenly over their full width and their fullest possible extent and the Contractor shall control and direct construction plant and other vehicular traffic uniformly over them. Damage by construction plant and other vehicular traffic shall be made good by the Contractor with material having the same characteristics and strength as the material had before it was damaged.

Embankment and other areas of unsupported fills shall not be constructed with steeper side slopes, or to greater widths than those shown in the Contract, except to permit adequate compaction at the edges before trimming back, or to obtain the final profile following any settlement of the fill and the underlying material.

Whenever fill is to be deposited against the face of a natural slope, or sloping earthworks face including embankments, cuttings, other fills and excavations steeper than 1 vertical on 4 horizontal, such faces shall be benched as per Clause 205.4.1 immediately before placing the subsequent fill.

All permanent faces of side slopes of embankments and other areas of fill formed shall, subsequent to any trimming operations, be reworked and sealed to the satisfaction of the Engineer and tracking a tracked vehicle, considered suitable by the Engineer, on the slope or any other method approved by the Engineer.

205.3.6	Compaction

Only the compaction equipment approved by the Engineer shall be employed to compact the different material types encountered during construction. Smooth wheeled, vibratory, pneumatic tired, pad foot rollers, etc. of suitable size and capacity as approved by the Engineer shall be used for the different types and grades of materials required to be compacted either individually or in suitable combinations.

The compaction shall be done with the help of vibratory roller of 80 to 100 kN static weight with plain or pad foot drum or heavy pneumatic tired roller of adequate capacity capable of achieving required compaction. The Contractor shall demonstrate the efficacy of the equipment he intends to use by carrying out compaction trials. The procedure to be adopted for these site trials shall first be submitted to the Engineer for approval.

Earthmoving plant shall not be accepted as compaction equipment nor shall the use of a lighter category of plant to provide any preliminary compaction to assist the use of heavier plant be taken into account.

Each layer of the material shall be thoroughly compacted to 95 percent of the maximum dry density determined according to AASHTO T 99. Subsequent layers shall be placed only after the finished layer has been tested and accepted by the Engineer.

When density measurements reveal any soft areas in the embankment/subgrade/earthen shoulders, further compaction shall be carried out as directed by the Engineer. If in spite of that the specified compaction is not achieved, the material in the soft areas shall be removed and replaced by approved material, compacted to the density requirements and satisfaction of the Engineer.

205.3.7	Drainage

The surface of the embankment/subgrade at all times during construction shall be maintained at such a cross fall (not flatter than that required for effective drainage of an earthen surface) as will shed water and prevent ponding.

205.3.8	Repairing of damages caused by rain/spillage of water

The soil in the affected portion shall be removed in such areas as directed by the Engineer before next layer is laid and refilled in layers and compacted using appropriate mechanical means such as small vibratory roller, plate compactor or power rammer to achieve the required density in accordance with Clause 205.3.6. If the cut is not sufficiently wide for use of required mechanical means for compaction, the same shall be widened suitably to permit their use for proper compaction. Tests shall be carried out as directed by the Engineer to ascertain the density requirements of the repaired area. The work of repairing the damages including widening of the cut, if any, shall be carried out by the Contractor at his own cost, including the arranging of machinery/equipment for the purpose.

205.3.9	Finishing operations

Finishing operations shall include the work of shaping and dressing the shoulders/verge/roadbed and side slopes to conform to the alignment, levels, cross/sections and dimensions shown on the drawings or as directed by the Engineer subject to the acceptable surface tolerance. Both the upper and lower ends of the side slopes shall be rounded off t o improve appearance and to merge the embankment with the adjacent terrain. The topsoil, removed and conserved earlier shall be spread over the fill slopes as per directions of the Engineer to facilitate the growth of vegetation. Slopes shall be roughened and moistened slightly prior to the application of the topsoil in order to provide satisfactory bond. The depth of the topsoil shall be sufficient to sustain plant growth, the usual thickness being from 75 mm to 150 mm.

Where directed, the slopes shall be turfed with sods in accordance with Clause 207. If seeding and mulching of slopes is prescribed, this shall be done to the requirement of Clause 208. When earthwork operations have been substantially completed, the road area shall be cleared of all debris, and ugly scars in the construction area responsible for objectionable appearance shall be eliminated.

205.4	Construction of Embankment and Subgrade under special Conditions

205.4.1	Earthwork for widening existing road embankment

When an existing embankment and/or sub grade is to be widened and its slopes are steeper than 1 vertical on, 1 horizontal, continuous horizontal benches, each at least 300 mm wide, shall be cut into the old slope for ensuring adequate bond with the fresh embankment/sub grade material to be added. The material obtained from cutting of benches could be utilized in the widening of the embankment/subgrade. However, when the existing slope against which the fresh material is to be placed is flatter than 1 vertical on 4 horizontal, the slope surface may only be ploughed or scarified instead of resorting to benching.

Where the width of the widened portions is insufficient to permit the use of conventional rollers, compaction shall be carried out with the help of small vibratory rollers/plate compactors/power rammers or any other appropriate equipment approved by the Engineer. End dumping of material from trucks for widening operations shall be avoided except in difficult circumstances when the extra width is too narrow to permit the movement of any other types of hauling equipment.

205.4.2	Earthwork for embankment and subgrade to be placed against sloping ground

Where an embankment/subgrade is to be placed against sloping ground, the latter shall be appropriately benched or ploughed/scarified as required in Clause 205.4.1 before placing the embankment/subgrade material. Extra earthwork involved in benching or due to plowing/scarifying etc. shall be considered incidental to the work. For wet conditions, benches with slightly inward fall and subsoil at the lowest point shall be provided as per the drawings, before the fill is placed against sloping ground.

205.4.3	Earthwork over existing road surface

Where the embankment is to be placed over an existing road surface, the work shall be carried out as indicated below:

- If the existing road surface is of granular or bituminous type and lies within 1 m of the new sub grade level, the same shall be scarified to a depth of 50 mm or more if specified, so as to provide ample bond between the old and new material ensuring that at least 500 mm portion below the top of new sub grade level is compacted to the desired density.

- If the existing road surface is of cement concrete type and lies within 1 m of the new sub grade level the same shall be removed completely.

- If the level difference between the existing road surface and the new formation level is more than 1 m, the existing surface shall be permitted to stay in place without any modification.

205.4.4	Embankment and subgrade around structures

To avoid interference with the construction of abutments, wing walls or return walls of culvert/bridge structures, the Contractor shall, at points to be determined to such structures, until such time as the construction of the latter is sufficiently advanced to permit the completion of approaches without the risk of damage to the structure. Unless directed otherwise, the filling around culverts, bridges and other structures up to a distance of twice the height of the road from the back of the abutment shall be carried out independent of the work on the main embankment. The fill material shall not be placed against any abutment or wing wall, unless permission has been given by the Engineer but in any case not until the concrete or masonry has been in position for 14 days. The embankment and sub grade shall be brought up simultaneously in equal layers on each side of the structure to avoid displacement and unequal pressure. The sequence of work in this regard shall be got approved from the Engineer.

The material used for backfill shall not be an organic soil or highly plastic clay having plasticity index and liquid limit more than 20 and 40 respectively when tested according to AASHTO T89 and T90 or other relevant international codes accepted by the Engineer. The fill material shall be deposited in horizontal layers in loose thickness and compacted thoroughly to 95 percent of the maximum dry density determined according to AASHTO T 99.

Where it may be impracticable to use conventional rollers, the compaction shall be carried out by appropriate mechanical means such as small vibratory roller, plate compactor or power rammer. Care shall be taken to see that the compaction equipment does not hit or come too close to any structural member so as to cause any damage to them or excessive pressure against the structure.

205.4.5	Construction of embankment over ground incapable of supporting construction equipment

Where embankment is to be constructed across ground which will not support the weight of repeated heavy loads of construction equipment, the first layer of the fill may be constructed by placing successive loads of material in a uniformly distributed layer of a minimum thickness required to support the construction equipment as agreed by the Engineer. The Contractor, if so desired by him, may also use suitable geosynthetic material to increase the bearing capacity of the foundation. This exception to normal procedure will not be permitted where, in the opinion of the Engineer, the embankments could be constructed in the approved manner over such ground by the use of lighter or modified equipment after proper ditching and drainage have been provided where this exception is permitted, the selection of the material and the construction procedure to obtain an acceptable layer shall be the responsibility of the Contractor. The cost of providing suitable traffic conditions for construction equipment over any area of the Contract will be the responsibility of the Contractor and no extra payment will be made to him. The remainder of the embankment shall be constructed as specified in Clause 205.4.

205.4.6	Embankment construction under water

Where filling or backfilling is to be placed under water, only acceptable granular material or rock shall be used unless otherwise approved by the Engineer. Acceptable granular material shall consist of graded, hard durable particles with maximum particle size not exceeding 75 mm. The material should be non-plastic having uniformity co·efficient of not less than 10. The material placed in open water shall be deposited by end tipping without compaction.

206.4.7	Earthwork for high embankment

In the case of high embankments, the Contractor shall normally use the material from the specified borrow area. In case he desires to use different material for his own convenience, he shall have to carry out necessary soil investigations and redesign the high embankment at his own cost. The Contractor shall then furnish the soil test data and design of high embankment for approval of the Engineer, who reserves the right to accept or reject it.

If necessary, stage construction of fills and any controlled rates of filling shall be carried out in accordance with the Contract including installation of instruments and it's monitoring. Where required, the Contractor shall surcharge embankments or other areas of fill with approved material for the periods specified in the Contract. If settlement of surcharged fill results in any surcharging material, which is unacceptable for use in the fill being surcharged, lying below formation level, the Contractor shall remove the unacceptable material and dispose it as per direction of the Engineer. He shall then bring the resultant level up to formation level with acceptable material.

205.4.8 Settlement period

Where settlement period is specified in the Contract, the embankment shall remain in place for the required settlement period before excavating for abutment, wing wall, retaining wall, footings, etc., or driving foundation piles. The duration of the required settlement period at each location shall be as provided for in the Contract or as directed by the Engineer.

205.5 Plying of Traffic

Construction and other vehicular traffic shall not use the prepared surface of the embankment and/or sub grade without the prior permission of the Engineer. Any damage arising out of such use shall, however, be made good by the Contractor at his own expense as directed by the Engineer.

205.6 Surface Finish and Quality Control of Work

The surface finish of construction of sub grade shall conform to the requirements of Clause 206.

Control on the quality of materials and works shall conform to as specified in the relevant clauses of these Specifications.

205.7 Subgrade Strength

It shall be ensured prior to actual execution that the borrow area material to be used in the sub grade satisfies the requirements of design CBR.

Sub grade shall be compacted and finished to the design strength consistent with other physical requirements. The actual laboratory CBR values of constructed sub grade shall be determined on undisturbed samples cut out from the compacted subgrade in CBR mould fitted with cutting shoe or on remolded samples, compacted to the field density at the field moisture con tent.

205.8 Measurements for Payment

Earth embankment/subgrade construction shall be measured separately by taking cross sections at intervals in the original position before the work starts and after its completion and computing the volumes of earthwork in cubic meters by the method of average end areas. The measurement of fill material from borrow areas shall be the difference between the net quantities of compacted fill and the net quantities of suitable material brought from roadway and drainage excavation. For this purpose, it shall be assumed that one cum_ of suitable material brought to site from road and drainage excavation forms one cum. of compacted fill and all bulking or shrinkage shall be ignored.

205 (1) Embankment Fill               cum

205.9 Rates

The Contract unit rates for the items of embankment construction shall be payment in full for carrying out the required operations including full compensation for :

- Cost of arrangement of land as a source of supply of material of required quantity for construction unless provided otherwise in the Contract;

- Setting out;

- Compacting ground supporting embankment except where removal and replacement of unsuitable material or loosening and recompacting is involved;

- Scarifying or cutting continuous horizontal benches 300 mm wide on side slopes of existing embankment and subgrade as applicable;

- Cost of watering or dying of material in borrow areas and/or embankment and subgrade during construction as required;

- Spreading in layers, bringing to appropriate moisture content and compacting to Specification requirements;

- Shaping and dressing top and slopes of the embankment including rounding of corners;

- Restricted working at sites of structures;

- Working on narrow width of embankment;

- Excavation in all soils f.rom borrow pits/designated borrow areas including clearing and grubbing and transporting the material to embankment site with all lifts and leads unless otherwise provided for in the Contract;

- All labor, materials, tools , equipment and incidentals necessary to complete the work to the Specifications;

- Dewatering; and

- Keeping the embankment/completed formation free of water.

206	Subgrade Preparation

206.1	Scope

The sub grade preparation shall be that part of the work which is prepared for the sub' base or, if there is no sub-base, the base of the pavement. It shall extend to the full width of the roadbed including the shoulders and lay-byes such limited areas as shown on the Drawings or as instructed by the Engineer.

206.2	Construction Operation

Preparation and surface treatment of the formation, that is top of the sub grade, shall be carried out only after completion o f any specified sub grade drainage and unless otherwise agreed by the Engineer, immediately prior to laying the sub, base or the road base where no sub-base is required. The sequence of operations shall be as follows:

- All surfaces below carriageway, lay-byes, footways and hard shoulders shall, after reinstatement of any soft areas to the required Specifications be well cleaned and freed of mud and slurry.

- The surface shall be compacted by 4 passes of a smooth wheeled roller of 80 to 100 kN weight after spraying requisite amount of water, if required, before the commencement of rolling.

- The formation shall, wherever necessary, be regulated and trimmed to the requirements of Clause 205.3.9 with motor grader.

- The trimmed formation shall be rolled by one pass of smooth wheeled roller of 80 to 100 kN weight after spraying requisite amount of water, if required, before the commencement of rolling.

Where the completed formation is not immediately covered with sub-base or road base material, its moisture content shall be maintained to prevent cracking in the formation by suitable measures as approved by the Engineer. The entire work of surface treatment of formation shall be deemed as incidental to the work of sub-base/base course to be provided on the subgrade and as such no extra payment shall be made for the same.

206.3 Method of Measurement

The quantities to be paid for shall be the number of square meters of sub grade in cut or in fill, prepared as hereinbefore prescribed, tested and accepted. For the purpose of payment no differentiation is made between sub-grade in cut or fills areas. The area to be measured for payment will be limited to the sub-grade below sub-base, in areas of new pavement construction. Areas to be sodded or footpath pavement will not be measured for payment under this Clause. In case no item for sub grade preparation is given in the Bill of Quantities, it shall be deemed to be inclusive in the unit rate of sub-base or base course as the case may be.

206.4	Rates

The quantities, determined as provided in the Clause above shall be paid for at the pay item listed below. This payment shall be full compensation for furnishing all labors, equipment and material necessary to complete the work including scarifying, reworking, wetting or drying, compacting, proof rolling, shaping and finishing, maintenance and other incidental items of work prescribed in this Clause.

206 (1) Sub grade Preparation	sqm

SECTION 3: ROAD WORKS

301 Granular Sub-base Course

301.1 Scope

This work shall consist of laying and compacting well-graded material on prepared sub-grade in accordance with the requirements of these Specifications. The material shall be laid in one or more layers as sub-base as necessary according to lines, grades and cross-sections shown on the drawing or as directed by the Engineer.

301.2 Materials

The Material to be used for the work shall be natural sand, gravel, crushed stone, or combination thereof depending upon the grading required. Materials like crushed slag, crushed concrete, and brick may be allowed only with the specific approval of the Engineer. The material shall be free from organic or other deleterious constituents and conform to one of the 6 gradings given in AASHTO M147 or other international codes and standards approved by the Engineer.

The grading to be adopted for a project shall be as specified in the Contract.

Table 301-1 Grading Requirements for Soil-Aggregate Materials (AASHTO M147 Grading A)

| Sieve Designation (mm) | Mass Percentage Passing (%) |
| --- | --- |
| 40 | 100 |
| 25 | - |
| 9.5 | 30-65 |
| 4.75 | 25-55 |
| 2.00 | 15-40 |
| 0.425 | 8-20 |
| 0.075 | 2-8 |

Unless otherwise specified in the Drawings, the lower sub-base course shall be of Grading A and upper sub-base course (or base course) shall be of Grading D of AASHTO M147.

301.3 Strength of Sub-Base

It shall be ensured prior to actual execution that the material to be used in the sub-base satisfies the requirements of CBR and other physical requirements when compacted and finished.

When directed by the Engineer, this shall be verified by performing CBR tests in the laboratory as required on specimens remolded at field dry density and moisture content and any other tests for the "quality" of materials, as may be necessary.

301.4 Construction Operation

301.4.1 Preparation of Sub grade

Immediately prior to the laying of sub-base, the sub-grade already finished to Clause 206 shall be prepared by removing all vegetation and other extraneous matter, lightly sprinkled with water if necessary and rolled with two passes of 80 - 100 kN smooth wheeled roller.

301.4.2 Spreading and Compacting

The sub-base material of grading specified in the Contract shall be spread on the prepared sub- grade with the help of a motor grader of adequate capacity, its blade having hydraulic controls suitable for initial adjustment and for maintaining the required slope and grade during the operation or other means as approved by the Engineer.

When the sub-base material consists of combination of materials mentioned in Clause 301.2 mixing shall be done mechanically by the mix' in-place method.

Manual mixing shall be permitted only where the width of laying is not adequate for mechanical operations, as in small-sized jobs. The equipment used for mix-in-place construction shall be rotavator or similar approved equipment capable of mixing the material to the desired degree. If so desired by the Engineer, trial runs with the equipment shall be carried out to establish its suitability for the work.

Moisture content of the loose material shall be checked in accordance with relevant international codes and standards approved by the Engineer and suitably adjusted by sprinkling additional water from a truck mounted or trailer mounted water tank and suitable for applying water uniformly and at controlled quantities to variable widths of surface or other means approved by the Engineer so that, at the time of compaction, it is from 1 percent above or 2 percent below the optimum moisture content. While adding water, due allowance shall be made for evaporation losses. After water has been added, the material shall be processed by mechanical or other approved means like disc harrows, rotavators until the layer is uniformly wet.

Immediately thereafter, rolling shall start. If the thickness of the compacted layer does not exceed 100 mm, a smooth wheeled roller of 80 to 100 kN weight may be used. For a compacted single layer up to 225 mm the compaction shall be done with the help of a vibratory roller of minimum 80 to 100 kN static weight with plain drum or pad foot-drum or heavy pneumatic typed roller of minimum 200 to 300 kN weight having a minimum tire pressure of 0.7 MN/m2 or equivalent capacity roller capable of achieving the required compaction. Rolling shall commence at the lower edge and proceed towards the upper edge longitudinally for portions having unidirectional cross-fall and super-elevation and shall commence at the edges and progress towards the centre for portions having cross-fall on both sides.

Each pass of the roller shall uniformly overlap not less than one third of the track made in the proceeding pass. During rolling, the grade and cross' fall shall be checked and any high spots or depressions, which become apparent, corrected by removing or adding fresh material. The speed of the roller shall not exceed 5 km per hour.

Rolling shall be continued till the density achieved is at least 95 percent of the maximum dry density for the material determined as AASHTO T99 or other relevant international codes and standards approved by the Engineer. The surface of any layer of material on completion of compaction shall be well closed, free from movement under compaction equipment and fro m compaction planes, ridges cracks or loose material. All loose, segregated or otherwise defective areas shall be made good to the full thickness of layer and recompacted.

301.5 Surface Finish and Quality Control of Work

The surface finish of construction shall conform to the requirements of Clause 307 of these Specifications.

Control on quality of materials and works shall be accepted by the Engineer.

301.6 Method of Measurement

Granular sub-base shall be measured as finished work in position in square meters.

The protection of edges of granular sub-base extended over the full formation as shown in the drawing shall be considered incidental to the work of providing granular sub-base and as such no extra payment shall be made for the same.

301 (1) Granular sub-base          	sq.m

301 (2) Granular pavement          	sq.m

301.7 Rates

The Contract unit rate for granular sub-base shall be payment in full compensation for carrying out the required operation including full compensation for:

- Making arrangements for traffic

- furnishing all materials to be incorporated in the work including all royalties, fees, rents where necessary and all leads and lifts;

- all labors, tools, equipment and incidentals to complete the work to the Specifications;

- carrying out the work in part widths of road where directed; and

- carrying out the required tests for quality control.

302 Prime Coat

302.1 Scope

The work shall consist of the application of a single coat of low viscosity liquid bituminous material to a porous granular surface preparatory to the superimposition of bituminous treatment or mix.

302.2 Materials

302.2.1 Bituminous Material

Bituminous material shall be of type and grade called for in the Drawings and shall conform to the requirements of the specifications listed below.

Cationic Emulsified Asphalt		:	AASHTO M 208 (ASTM D 2397)

Medium-curing cut back asphalt	:	AASHTO M 82

Rapid-curing cut back asphalt	:	AASHTO M 81

The grade (with temperatures of application in degrees C) shall be MC-70 (43 - 85 degrees) or RC-250 (60 - 100 degrees).

302.3 Construction Operation

302.3.1 Weather and Seasonal Limitations

Bituminous primer shall not be applied to a wet surface or during a dust storm or when the weather is foggy, rainy or windy or when the temperature in the shade is less than l0°C. Surfaces which are to receive primer should be damp, but no free or standing water shall be present.

302.3.2 Equipment

The primer distributor shall be a self-propelled or towed bitumen pressure sprayer equipped for spraying the material uniformly at specified rates and temperatures. Hand spraying of small areas, inaccessible to the distributor, or in narrow strips shall be sprayed with a pressure hand sprayer, or as directed by the Engineer.

302.3.3 Preparation of road surface

Immediately before applying the bituminous material, all loose dirt and other objectionable material shall be removed from the surface with a power broom and/or blower as required. If the Engineer so orders, the surface shall be lightly bladed and rolled immediately prior to the application of bituminous material, in which case brooming or blowing will not be required. When so ordered by the Engineer a light application of water shall be made just before the application of bituminous material. The area to be treated shall be approved by the Engineer prior to application.

302.3.4 Application of bituminous primer

Bituminous material shall be applied to the width of the section to be primed by means of a bitumen distributor in a uniform, continuous spread. The rate of application shall be as specified in the Drawings or as directed by the Engineer which shall usually be in the range of 1.0 to 2.0 litter/sqm. Care shall be taken that the application of bituminous material at the junction of spreads is not in excess of the specified amount. Excess bituminous material shall be sponged from the surface. Skipped areas or deficiencies shall be corrected. Building paper shall be placed over the end of the previous applications and the joining application shall start on the building paper. Building paper used shall be removed and satisfactorily disposed of.

302.3.5 Curing of primer and opening to traffic

A primed surface shall be allowed to cure for a t least 24 hours or such other period as is found to be necessary to allow all the volatiles to evaporate before any subsequent surface treatment or mix is laid. Any unabsorbed primer shall first be blotted with an application of sand, using the minimum quantity possible. A primed surface shall not be opened to traffic other than that necessary to lay the next course. A very thin layer of clean sand may be applied to the surface of the primer, to prevent the primer picking up under the wheels of the paver and the trucks delivering bituminous material on the paver.

302.4 Method of Measurement

Prime coat shall be measured in terms of surface area of application in square meters.

302 (1) Prime Coat	     sqm

302.5 Rates

The Contract unit rate for prime coat shall be payment in full for carrying out the required operation including full compensation for:

- Making arrangement for traffic except for initial treatment to verges, shoulders and construction of diversions;

- furnishing all materials to be incorporated in the work including all royalties, fees, rents where necessary and all leads and lifts;

- all labor, tools, equipment and incidentals to complete the work to the Specifications;

- carrying out the work in part widths of road where directed; and carrying out the required tests for quality control.

303 Tack Coat

303.1 Scope

This work shall consist of the application of a single coat of low viscosity liquid bituminous material to an existing bituminous road surface preparatory to the superimposition of a bituminous mix, when specified in the Contract or instructed by the Engineer

303.2 Materials

303.2.1 Binder

Bituminous material shall be of type and grade called for in the Drawings and shall conform to the requirements of the specifications listed below.

Cationic Emulsified Asphalt		:	AASHTO M 208 (ASTM D 2397)

Rapid-curing cut back asphalt	:	AASHTO M 81

Medium-curing cut back asphalt	:	AASHTO M 82

The grade (with temperatures of application in degrees C) shall be MC-70 (43-85 degrees) or RC-250 (60-80 degrees)

303.3	Construction Operation

303.3.1	Weather and Seasonal Limitations

Bituminous material shall not be applied to a wet surface or during a dust storm or when the weather is foggy, rainy or windy or when the temperature in the shade is less than 10°C. Where the tack coat to be applied, the surface shall be dry or slightly damp.

303.3.2	Equipment

The tack coat distributor shall be of a self-propelled or towed bitumen pressure sprayer, equipped for spraying the material uniformly at a specified rate. Hand spraying of small areas, inaccessible to the distributor, or in narrow strips, shall be sprayed with a pressure hand sprayer, or as directed by the Engineer.

303.3.3 Preparation of base

The surface on which the tack coat is to be applied shall be clean and free from dust, dirt and any extraneous material. Immediately before the applications of the tack coat, the surface shall be swept clean with a mechanical broom, and high pressure air jet, or by other means as directed by the Engineer.

303.3.4 Application of tack coat

The application of tack coat shall be at the rate specified in the Contract, and shall be applied uniformly. If the rate of application of Tack Coat is not specified in the Contract then it shall be at the rate within the range of 0.4 to 0.8 litter/sqm. The normal range of spraying temperature for a bituminous emulsion shall be 20°C to 70°C and for a cutback, 50°C to 80°C if RC-70/MC-70 is used. The method of application of the tack coat will depend on the type of equipment to be used, size of nozzles, pressure at the spray bar, and speed of forward movement. The Contractor shall demonstrate at a spraying trial, that the equipment and method to be used is capable of producing a uniform spray, within the tolerances specified.

303.3.5 Curing of tack coat

The tack coat shall be left to cure until all the volatiles have been evaporated before any subsequent construction is started. No plant or vehicles shall be allowed on the tack coat other than those essential for the construction.

303.4 Method of Measurement

Tack coat shall be measured in terms of surface area of application in square meters.

303 (1) Tack Coat		sqm

303.5 Rates

The contract unit rate for tack coat shall be payment in full for carrying out the required operations including full compensation for:

- making arrangement for traffic to Clause 112 except for initial treatment to verges, shoulders and construction of diversions;

- furnishing all materials to be incorporated in the work including all royalties, fees, rents where necessary and all leads and lifts;

- all labors, tools, equipment and incidentals to complete the work to the Specifications;

- carrying out the work in part widths of road where directed; and

- carrying out the required tests for quality control.

304 Asphalt Concrete

304.1 Scope

This clause specifies the construction of Asphalt Concrete, for use in surface and profile corrective courses. This work shall consist of construction in single or multiple layers of asphalt concrete on a previously prepared bituminous surface or sub-base. A single layer shall be 50 mm in thickness.

304.2 Materials

304.2.1 Bitumen

The bitumen shall be asphalt cement for pavement construction grade AC-10 (penetration 70-80) complying with AASHTO M226 or equivalent complying with other international codes and standards approved by the Engineer.

304.2.2 Coarse aggregates

The coarse aggregates shall consist of crushed rock. Crushed gravel or other hard material retained on the 2.36 mm sieve. They shall be clean, hard and durable, of cubical shape, free from dust and soft or friable matter, organic or other deleterious substances. Where the Contractor's selected sources of aggregates have poor affinity for bitumen, as a condition for the approval of that source, the bitumen shall be treated with an approved anti-stripping agent, as per the manufacture's recommendations, without additional payment. Before approval of the source, the aggregates shall be tested for stripping. The aggregates shall satisfy the physical requirements specified in the following Table.

Table 304-1 Physical Requirements for Coarse Aggregate for Asphalt Concrete Pavement

| Property | Test | Specification |
| --- | --- | --- |
| Cleanliness | Grain size analysis | Max. 5% passing 0.0075 mm sieve |
| Particle shape | Flakiness and elongation index (combined) | Max. 30% |
| Strength | Los Angels abrasion value, Aggregate impact value | Max. 30% Max. 24% |
| Polishing | Polished stone value | Min. 55% |
| Durability | Soundness Sodium sulphate Magnesium sulphate | Max. 12% Max. 18% |
| Water absorption | Water absorption | Max. 2% |
| Stripping | Coating and stripping of bitumen aggregate mixtures | Minimum retained coating 95% |
| Water sensitivity | Retained tensile strength | Min. 80% |

304.2.3 Fine aggregates

Fine aggregates shall consist of crushed or naturally occurring mineral material, or a combination of the two, passing the 2.36mm sieve and retained on the 75 micron sieve. They shall be clean, hard, durable, dry and free from dust and soft or friable matter, organic or other deleterious matter.

The fine aggregate shall have a sand equivalent value of not less than 50 when tested in accordance with AASHTO T176 or other equivalent international codes and standards approved by the Engineer.

The plasticity index of the fraction passing the 0.425 mm sieve shall not exceed 4 when tested in accordance with AASHTO T89 and T90 or other equivalent international codes and standards approved by the Engineer.

304.2.4 Filler

Filler shall consist of finely divided mineral matter such as rock dust, slug dust, hydrated lime, hydraulic cement, fly ash or other suitable materials approved by the Engineer.

The filler shall be graded within the limits indicated in the following Table in accordance with AASHTO M 1 7 or ASTM D242.

Table 304-2 Grading Requirements for Mineral Filler (AASHto M17)

| Sieve Designation (mm) | Percent passing by mass (%) |
| --- | --- |
| 1.18 | 100 |
| 0.6 | 97-100 |
| 0.3 | 95-100 |
| 0.075 | 70-100 |

The filler shall be free from organic impurities and have plasticity index not greater than 4. The plasticity index requirement shall not apply if filler is cement or lime. When the coarse aggregate is gravel, 2 percent by weight of total aggregate, shall be Portland cement or hydrated lime and the percentage of fine aggregate reduced accordingly. Cement or hydrated lime is not required when the limestone aggregate is used. Where the aggregates fail to meet the requirements of the water sensitivity test in Table 305-1, then 2 percent by total weight of aggregate of hydrated lime shall be added without additional cost.

304.2.5 Aggregate grading and binder content

The combined grading of the coarse and fine aggregates and added filler shall fall within the limits shown in the following Table unless otherwise directed by the Engineer.

Table 304-3 Aggregate Gradation for Hot Asphalt Mixes (Asphalt Institute Manual No.22)

| Sieve Size (mm) | Percent Passing by Weight (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Asphalt Concrete Surface Course (AI MS 22-12.5mm) |  | Asphalt Concrete Base Course (AI MS 22-25mm) |  |
|  | Min. | Max. | Min. | Max. |
| 37.5 | - | - | 100 | 100 |
| 25.4 | - | - | 90 | 100 |
| 19 | 100 | 100 | - | - |
| 12.5 | 90 | 100 | 56 | 80 |
| 9.5 | - |  | - | - |
| 4.75 | 44 | 74 | 29 | 59 |
| 2.36 | 28 | 58 | 19 | 45 |
| 1.18 | - | - | - | - |
| 0.60 | - | - | - | - |
| 0.30 | 5 | 21 | 5 | 17 |
| 0.075 | 3 | 8 | 3 | 8 |

304.3 Mixture Design

304.3.1 Requirements for the mixture

Apart from conformity with the grading and quality requirements for individual ingredients, the mixture shall meet the requirement set out in the following Table.

Table 304-4 Mix Property Requirement

| Mix Properties |  | Asphalt Concrete Surface Course | Asphalt Concrete Base Course |
| --- | --- | --- | --- |
| Total Bitumen Content: (% by weight of total mix) (AI MS-22 2nd Ed. Table 2.05) (These percentages shall be considered “effective” content calculated as max. per AI MS-2) | Min. | 4.0% | 3.0% |
|  | Max. | 5.5% | 5.0% |
| Marshall Specimens: (AI MS-22 2nd Ed. Table 3.07) Number of blows each end specimen |  | 75 | 75 |
| Stability | Min. | 6,000 N | 6,000 N |
| Flow | Min. | 2 mm | 2 mm |
|  | Max. | 5 mm | 5 mm |
| Air Voids | Min. | 3 % | 3 % |
|  | Max. | 5 % | 5 % |
| Air Void at Refusal Density (Refusal Marshall Compaction) | Min. | 2 % | 2 % |
| Voids in the Mineral Aggregate (VMA) | Min. | 14 % | 12 % |
| Voids filled with Asphalt (VFA) | Min. | 65 % | 65 % |
|  | Max. | 78 % | 78 % |
| Retained Marshall Stability (AASHTO T-165) | Min. | 70 % | 70 % |

All volumetric Marshall properties are to be calculated as shown in the Asphalt Institute’s MS-26th, edition Chapter 4.

304.3.2 Binder content

The binder content shall be optimized to achieve the requirements of the mixture set out in Table 305-4. The Marshall method for determining the optimum binder contents shall be adopted as described in the Asphalt Institute Manual MS-2, replacing the aggregates retained on 26.5 mm sieve and retained on the 22.4 mm sieve, where approved by the Engineer.

304.3.3 Job mix formula

The Contractor shall inform the Engineer in writing, at least 20 days before the start of the work, of the job mix formula proposed for use in the works, and shall give the following details;

- Source and location of all materials

- Proportion of all materials expressed as follows where each is applicable;

- Binder type and percentage by weight of total mixture;

- Coarse aggregate/fine aggregate/mineral filler as percentage by weight of total aggregate including mineral filler;

- A single definite percentage passing each sieve for the mixed aggregate;

- The individual grading of the individual aggregate fractions, and the proportion of each in the combined grading;

- The results of tests enumerated in Table 305-5 as obtained by the Contractor;

- Where the mixer is a batch mixer, the individual weights of each type of aggregate and binder per batch;

- Test results of physical characteristics of aggregates to be used; and

- Mixing temperature and compacting temperature.

- While establishing the job mix formula, the Contractor shall ensure that it is based on a correct and truly representative sample of the materials that will actually be used in the work and that the mixture and its different ingredients satisfy the physical and strength requirements of these Specifications.

Approval of the job mix formula shall be based on independent testing carried out by authorized laboratory and witnessed by the Engineer for which samples of all ingredients of the mix shall be furnished by the Contractor as required by the Engineer.

The approved job mix formula shall remain effective unless and until a revised job mix formula is approved. Should a change in the source of materials be proposed, a new job mix formula shall be forwarded to the Engineer for approval before placing of the material.

304.3.4 Plant trials

Once the laboratory job mix formula is approved, the Contractor shall carry out plant trials at the mixer to establish that the plant can be set up to produce a uniform mix conforming to the approved job mix formula. The permissible variations of the individual percentages of the various ingredients in the actual mix from the job mix formula to be used shall be within the limits as specified in the Table below. These variations are intended to apply to individual specimens taken for quality control tests.

Table 304-5 Permissible Variations from the Job Mix Formula

| Description | Approximate Permissible Variations |  |
| --- | --- | --- |
|  | Base Course | Wearing Course |
| Aggregate passing 19mm sieve or larger | 8% | 7% |
| Aggregate passing 13.2mm, 9.5mm | 7% | 6% |
| Aggregate passing 4.75mm | 6% | 5% |
| Aggregate passing 2.36mm, 1.18mm, 0.6mm | 5% | 4% |
| Aggregate passing 0.3mm, 0.15mm | 4% | 3% |
| Aggregate passing 0.075mm | 2% | 1.5% |
| Binder content | 0.3% | 0.3% |
| Mixing temperature | 10 degree C | 10 degree C |

Once the plant trials have been demonstrated the capability of the plant, and the trials are approved, the laying operation may commence. Over the period of the first month of production for laying on the works, the Engineer shall require additional testing of the product to establish the reliability and consistency of the plant.

304.3.5 Laying trials

Once the plant trials have been successfully completed and approved, the Contractor shall carry out laying trials, to demonstrate that the proposed mix can be successfully laid, and compacted. The laying trial shall be carried out on a suitable area which is not form part o f the works, unless specifically approved in writing b y the Engineer. The area o f the laying trials shall be a minimum of 100 sqm of construction similar to that of the Project road, and it shall be in all respects, particularly compaction, the same as the Project construction, on which the bituminous material is to be laid.

The Contractor shall previously inform the Engineer of the proposed method for laying and compacting the material. The plant trials shall then establish if the proposed laying plant, compaction plant, and methodology is capable of producing satisfactory results. The density of finished paving layer shall be determined by taking cores, no sooner than 24 hours after laying, or by other approved method.

Once the laying trials have been approved, the same plant and methodology shall be applied to the laying of the material on the Project, and no variation of either shall be acceptable, unless approved in writing by the Engineer, who may at his discretion require further laying trials.

304.4 Construction Operations

304.4.1 Weather and seasona1 1imitations

Laying shall be suspended while free-standing water is present on the surface to be covered, or during rain, fog and dust storms. After rain, the bituminous surface, prime or tack coat, shall be blown off with a high pressure air jet to remove excess moisture, or the surface left to dry before laying shall start. Laying of bituminous mixtures shall not be carried out when the air temperature at the surface on which it is to be laid is below 10°C or when the wind speed at any temperature exceeds 40km/hr at 2m height unless specifically approved by the Engineer.

304.4.2 Preparation of base

The surface on which the asphalt concrete is to be laid shall be prepared in accordance with the followings or as directed by the Engineer.

(1) Preparing existing granular surface

Where the bituminous material is to be laid on the existing granular surface, the surface shall be primed in accordance with Clause 302.

The surface finish of all granular layers on which bituminous works are to be placed shall unless otherwise specifically instructed by the Engineer be free from dust. All such layers must be capable of being swept after removal of any non-integral loose material, by means of a mechanical broom, without shedding significant quantities of material and dust removed by air jet, washing, or other means approved by the Engineer. In locations where mechanical broom cannot access, other approved methods shall be used as directed by the Engineer.

After cleaning the surface shall be correct of line and level within the tolerances specified for base course.

(2) Laying the profile corrective course

- Laying on granular base
After preparing the granular surface, the profile corrective course shall be laid using materials as shown on the drawings or as directed by the Engineer, and compacted to the requirement.

- Laying on existing bituminous surface
The existing bituminous surface shall be prepared by patching of pot holes and sealing of cracks and after allying tack coat conforming to Clause 303, the bituminous profile corrective course shall be laid and compacted to the requirement.

- Correction of local depressions
Where local sags or depression occur in the existing pavement, a specific filing operation shall be instructed by the Engineer, which should be laid in flat layers. Normally, the maximum layer thickness at any point should not exceed 100 mm.

(3) Covering the profile corrective course

Profile corrective course shall be so planned that the layer shall be covered by the designed base/wearing course at the earliest opportunity, before opening to regular traffic.

304.4.3 Mixing of the mixture

Premixed bituminous materials shall be prepared in a hot mix plant of adequate capacity and capable of yielding a mix of proper and uniform quality with thoroughly coated aggregates. Appropriate mixing temperature can be found in the Table below.

Table 304.6  Appropriate Mixing Temperature

| Bitumen Penetration | Bitumen Mixing (℃) | Aggregate Mixing (℃) | Mixed Material (℃) | Laying (℃) | Rolling (℃) |
| --- | --- | --- | --- | --- | --- |
| 35 | 160-170 | 160-175 | 170 max. | 130 min. | 100 min. |
| 65 | 150-165 | 150-170 | 165 max. | 125 min. | 90 min. |
| 90 | 140-160 | 140-165 | 155 max. | 115 min. | 80 min. |

The difference in temperature between the binder and aggregate should at no time exceed 14°C. In order to ensure uniform quality of the mix and better coating of aggregates, the hot mix plant shall be calibrated from time to time.

304.4.4 Transportation of the Mixture

Bituminous materials shall be transported in clean insulated vehicles, and unless otherwise agreed by the Engineer, shall be covered while in transit or awaiting tipping. Subject to the approval of the Engineer, a thin coating of diesel or lubricating oil may be applied to the interior of the vehicle to prevent sticking and to facilitate discharge of the material.

304.4.5 Spreading

Except in areas where a mechanical paver cannot access, bituminous materials shall be spread, leveled and tamped by an approved self-propelled machine, As soon as possible after arrival at site; the materials shall be supplied continuously to the paver and laid without delay.

The rate of delivery of material to the paver shall be regulated to enable the paver to operate continuously. The travel rate of the paver, and its method of operations, shall be adjusted to ensure an even and uniform flow of bituminous material across the screed, free from dragging, tearing and segregation of the material. In areas with restricted space where mechanical paver cannot be used, the material shall be spread, raked and leveled with suitable hand tools by experienced staff, and compacted to the satisfaction of the Engineer.

The minimum thickness of material laid in each paver pass shall be in accordance with the minimum values given in the relevant part of these Specifications. When laying binder course or wearing course approaching an expansion joint of a structure, machine laying shall stop 300mm short of the joint. The remainder of the pavement up to the joint, and the corresponding area beyond it, shall be laid by hand, and the joint or joint cavity shall be kept clear of surfacing material.

Bituminous material, with a temperature greater than 145°C, shall not be laid or deposited on bridge deck waterproofing systems, unless precautions against heat damage have been approved by the Engineer.

Hand placing of premixed bituminous materials shall only be permitted in the following circumstances.

- For laying regulating courses of irregular shape and varying thickness

- In confined space where it is impracticable for a paver to operate

- For footways

- At the approaches to expansion joints at bridges, viaducts or other structures

- For filling of potholes

- Where directed by the Engineer.

Manual spreading of premixed wearing course material or the addition of such material by hand-spreading to the paved area, for adjustment of level, shall only be permitted in the following circumstances.

(i)	At the edges of the layers of material and at gullies and manholes

(ii)	At the approaches to expansion joints at bridges, viaducts or other structures

(iii)	As directed by the Engineer.

304.4.6 Cleanliness and overlaying

Bituminous material shall be kept clean and uncontaminated. The only traffic permitted to run on bituminous material to be overlaid shall be that engaged in laying and compacting the next course or, where a binder course is to be sealed or surface dressed, that engaged on such surface treatment. Should any bituminous material become contaminated, the Contractor shall make it good to the satisfaction of the Engineer, in compliance with Clause 304.4.2

Binder course material shall not remain uncovered by either the wearing course or surface treatment, whichever is specified in the Contract, for more than three consecutive days after being laid. The engineer may extend this period, by the minimum amount of time necessary, because of weather conditions or of for any other reason_ If the surface of the base course is subjected to traffic, or not covered within three days, a tack coat shall be applied, as directed by the Engineer.

304.4.7 Rolling

Bituminous materials shall be laid and compacted in layers which enable the specified thickness, surface level, regularity requirements and compaction to be achieved.

Compaction of bituminous materials shall commence as soon as possible after laying. Compaction shall be substantially compacted before temperature falls below the minimum rolling temperatures stated in the relevant part of these Specifications. Rolling of longitudinal joints shall be done immediately behind the paving operations. After this, rolling shall commence at the edges and progress towards the center longitudinally except that on super elevated and unidirectional cambered portions, it shall progress from the lower to the upper edge parallel to the centerline of the pavement. Rolling shall continue until all roller marks have been removed from the surface. All deficiencies in the surface after laying shall be made good by the attendants behind the paver, before initial rolling is commenced. The initial or breakdown rolling shall be done with 80-100 kN dead weight smooth-wheeled rollers. The intermediate rolling shall be done with 80-100 kN dead weight or vibratory roller with a pneumatic tire roller of 120 to 150 kN weight having nine wheels, with a tire pressure of at least 0.6 MN/m2. The finish rolling shall be done with 60 to 80 kN smooth wheeled tandem rollers.

Where compaction is to be determined by density of cores, the requirements to prove the performance of rollers shall apply in order to demonstrate that the specified density can be achieved. In such cases the Contractor shall nominate the plant, and the method by which he intends to achieve the specified level of compaction and finish at temperatures above the minimum specified rolling temperature. Laying trials shall then demonstrate the acceptability of the plan and method used.

Bituminous materials shall be rolled in a longitudinal direction, with the driven rolls nearest the paver. The roller shall first compact material adjacent to joints and then work from the lower to the upper side of the layer, overlapping on successive passes by at least one-third of the width of the rear roll or, in the case of pneumatic-tire roller, at least the nominal width of 300mm.

In portions with super-elevated and unidirectional camber, after the edge has been rolled, the roller shall progress from the lower to the upper edge.

Roller should move at a speed of not more than 5 km per hour. The roller shall not be permitted to stand on pavement which has not been fully compacted, and necessary precautions shall be taken to prevent dropping of oil, grease, petrol or other foreign matter on the pavement either when the rollers are operating or standing. The wheels of rollers shall be kept moist with water, and spray system provided with the machine shall be in good working order, to prevent the mixture from adhering to the wheels. Only sufficient moisture to prevent adhesion between the wheels rollers and the mixture should be used. Surplus water shall not be allowed to stand on the partially compacted pavement.

304.5 Opening to Traffic

The newly laid surface shall not be open to traffic for at least 24 hours after laying and the completion of compaction, without the express approval of the Engineer in writing.

304.6 Teats and Standards of Acceptance

The thickness and density of the compacted asphalt concrete shall be checked at every 500m2 . Tolerances of thickness shall be – 10mm and +15 mm to the stipulated thickness in total. Tolerance of density shall be 94 % of the stipulated density.

Temperatures of the hot mix of asphalt concrete shall be checked prior to spreading. Tolerance of range of temperatures is within 110℃ and 140℃.

304.7 Method of measurement

Asphalt concrete shall be measured as finished work by the square meter at a specified thickness as detailed on the Contract drawings, or documents, or as directed by the Engineer.

304 (1) Asphalt Concrete, base course	sqm

304 (2) Asphalt Concrete, surface course	sqm

304.8 Rates

The contract unit rate for asphalt concrete shall be payment in full for carrying out the all required operations as specified including full compensation for, but not necessarily limited to;

- Making arrangements for traffic;

- Preparation of the surface to receive the material;

- Providing all materials to be incorporated in the work including arrangement for stock yards, all royalties, fees, rents where necessary and all leads and lifts;

- Mixing, transporting, laying and compacting the mix, as specified;

- All labors, tools, equipment, plant including installation of hot mix plant, power supply units and all machinery, incidental to complete the work;

- Carrying out the work in part widths of the road where directed;

- Carrying out all tests for control of quality; and

- The rate shall cover the provision of bitumen at the rate specified in the contract, width the provision that the variation in actual percentage of bitumen used will be assessed and the payment adjusted accordingly;

- The rates for premixed material are to include for all wastage in cutting of joints, etc.

- The rates are to include for all necessary testing mix design, transporting and testing of samples, and cores. If there is not a project specific laboratory, the Contractor must arrange to carry out all necessary testing at an outside laboratory, approved by the Engineer, and all costs incurred are deemed to be included in the rate quoted for the material;

- The cost of all plant and laying trials as specified to prove the mixing and laying methods is deemed to be included in the Contractor's rate for the material.

305 Control of Alignment, Level and Surface Regularity

305.1 General

All works performed shall conform to the lines, grades, cross-sections, and dimensions shown on the drawings or as directed by the Engineer, subject to the permitted tolerances described herein -after.

305.2 Horizontal Alignment

Horizontal alignments shall be reckoned with respect to the centre line of the carriageway as shown on the drawings. The edges of the carriageway as constructed shall be correct within a tolerance of ± 10 mm there from. The corresponding tolerance for edges of the roadway and lower layers of pavement shall be ± 25 mm.

305.3 Surface Levels

The levels of the sub grade and different pavement courses as constructed, shall not vary from those calculated with reference to the longitudinal and cross-profile of the road shown on the drawings or as directed by the Engineer beyond the tolerances mentioned below.

1. Sub grade 				+20mm, -25 mm

2. Sub-base				+10mm

(a) Flexible pavement			-20mm

3. Base-course for flexible pavement

(a) Bituminous course			+6 mm, -6mm

(b) Other than bituminous

i) Machine laid				+10 mm, -10mm

ii) Manually laid				+15mm, -15mm

4. Wearing course for flexible pavement

(a) Machine laid				+6 mm, - 6mm

(b) Manually laid				+10mm, -10mm

Provided, however, that the negative tolerance for wearing course shall not be permitted in conjunction with the positive tolerance for base course, if the thickness of the former is thereby reduced by more than 6 mm for flexible pavements and 5 mm for concrete pavements. For checking compliance with the above requirement for subgrade, sub-base and base courses, measurements of the surface levels shall be taken on a grid of points placed at 6.25m longitudinally and 3.5 m transversely. For any 10 consecutive measurements taken longitudinally or transversely, not more than one measurement shall be permitted to exceed the tolerance as above, this one measurement being not in excess of 5 mm above the permitted tolerance. For checking the compliance with the above requirement for bituminous wearing courses and concrete pavements, measurements of the surface levels shall be taken on a grid of points spaced at 6.25 m along the length and at 0.5 m from the edges and at the centre of the pavement. In any length of pavement, compliance shall be deemed to be met for the final road surface, only if the tolerance given above is satisfied for any point on the surface.

305.4 Surface Regularity of Pavement Courses

The longitudinal profile shall be checked with a 3 meter long straight edge/moving straight-edge as desired by the Engineer at the middle of each traffic lane along a line parallel to the centre line of the road. The maximum permitted number of surface irregularities shall be as per Table 307-1.

Table 305-1 Surface Irregularities

| Items | Surface of carriageways and paved shoulder |  |  |  | Surface of laybys, service areas and all bituminous base courses |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Irregularity | 4mm |  | 7mm |  | 4mm |  | 7mm |  |
| Length (m) | 300 | 75 | 300 | 75 | 300 | 75 | 300 | 75 |
| Roads of lower category | 40 | 18 | 4 | 2 | 60 | 27 | 6 | 3 |

* Category of each lection of road as described in the Contract.

The maximum allowable difference between the road surface and underside of a 3 m straight-edge when placed parallel with, or at right angles to the centre line of the road at points decided by the Engineer shall be:

- for pavement surface (asphalt and cement concrete)		3mm

- for bituminous base courses				6mm

- for granular sub-base/base courses			8mm

- for sub-bases under concrete pavements			10mm

305.5 Rectification

Where the surface regularity of sub grade and the various pavement courses fall outside the specified tolerances, the Contractor shall be liable to rectify these in the manner described below and to the satisfaction of the Engineer.

- Subgrade: Where the surface is high, it shall be trimmed and suitably compacted. Where the same is low, the deficiency shall he corrected by scarifying the lower layer and adding fresh material and recompacting to the required density. The degree of compaction and the type of material to be used shall conform to the requirements of Clause 205 of these Specifications.

- Granular Sub-base: Same as at (i) above, except that the degree of compaction and the type of material to be used shall conform to the requirements of Clause 301 of these Specifications.

- Lime/Cement Stabilized Soil Sub-base: For lime/cement treated materials where the surface is high, the same shall be suitably trimmed while taking care (hat the material below is not disturbed due to this operation. However, where the surface is low, the same shall be corrected as described herein below. For cement treated material, when the time elapsed between detection of irregularity and the lime of mixing of the material is less than 2 hours, the surface shall be scarified to a depth of 50 mm supplemented with freshly mixed materials as necessary and recompacted to the relevant specification. When this time is more than 2 hours, the full depth of the layer shall be removed from the pavement and replaced with fresh material to Specification. This shall also apply to lime treated material except that the time criterion shall be 3 hours instead of 2 hours.

- Bituminous Constructions: For bituminous construction other than wearing course, where the surface is low, the deficiency shall be corrected by adding fresh material over a suitable tack coat if needed and recompacting to specifications. Where the surface is high, the full depth of the layer shall be removed and replaced with fresh material and compacted to specifications.
For wearing course, where the surface is high or low, the full depth of the layer shall be removed and replaced with fresh material and compacted to specifications, in all cases where the removal and replacement of a bituminous layer is involved, the area treated shall not be less than 5 m in length and not less than 3.5 m in width.

- Cement concrete pavement: The defective areas having surface irregularly exceeding 3 mm but not greater than 6 mm may be rectified by bump cutting or scrabbling or grinding using approved equipment. When required by the Engineer, areas which have been reduced in level by the above operation(s) shall be retextured in an approved manner either by cutting grooves (5 mm deep) or roughening the surface by hacking the surface. IS high areas in excess 6 mm or low areas in excess of 3mm occur, exceeding the permitted numbers and if the Contractor cannot rectify, the slab shall be demolished and reconstructed at the Contractor's expense and in no case the area removed shall be less than the full width of the lane in which the irregularity occurs and full length of the slab.
If deemed necessary by the Engineer, any section of the slab which deviates from the specified levels and tolerances shall be demolished and reconstructed at the Contractor's expense.

306 Concrete Curbs

306. 1 Scope

This work shall consist of constructing cement concrete curbs in the central median and/or along the footpaths or separators in conformity with the lines, levels and dimensions as specified in the drawings.

306.2 Materials

Curbs shall be provided in cement concrete of compressive strength specified in the Drawings but shall not be less than 18 N/mm2 in accordance with Section 4 of these Specifications.

306.3 Type of Construction

Curbs can be of either cast-in-situ construction or pre-cast concrete blocks when accepted by the Engineer.

306.4 Construction Requirements

306.4.1 Foundation

Excavation shall be made to the required depth and the base upon which the curb is to be set shall be leveled and compacted to a firm and even surface and slightly watered to make it damp. All soft and unsuitable material shall be removed and replaced with suitable material. Curbs shall be laid on firm cast-in-situ cement concrete foundation of C15 grade or on extended width of pavement as shown on the Drawings. The foundation shall have at least a projection of 50 mm beyond the curb stone. Bed course material shall be placed and compacted to form a bed of the required thickness when shown in the Drawings.

Forms shall conform to the requirements set forth in Section 4 "Concrete Works.”

306.4.2 In case of cast-in-situ concrete curves

Forms to hold the concrete shall be built and set· in-place as described in Section 4 "Concrete Works.” Forms for at least 50 m of curb and/or gutter shall be in place and checked for alignment and grade before concrete is placed. Curbs and/or gutters constructed on curves shall have forms of either wood or metal and they shall be accurately shaped to the curvature shown in the Drawings.

Mixing, placing, curing and finishing of concrete shall conform to the requirements in Section

4 "Concrete Works" as modified by the requirements below.

The top of the concrete shall be finished to a smooth and even surface and the edges rounded to the radii shown in the Drawings. Before the concrete is given the final finishing, the surface of the gutter shall be tested with a 3-m straight-edge and any irregularity of more than 10 mm in 3m shall be rectified.

The curb and/or gutter shall be constructed in uniform sections of not more than 50 m in length except where shorter sections are required to coincide with the location of weakened planes or contraction joints of the concrete pavement, or for closures, but no section shall be less than 2m long. After laying the curbs and just prior t o hardening of the concrete, saw cut grooves shall he provided at 5 m intervals or as specified by the Engineer.

Expansion joints shall be formed at intervals shown in the Drawings or as approved by the Engineer. Where a curb is placed next to a concrete pavement, expansion joints in the curb shall be located opposite expansion joints in the pavement. Preformed sponge rubber and cork expansion joint fillers conforming to the requirements of AASHTO M 153 or other equivalent international standard approved by the Engineer may be used.

The form shall be removed within 24 hours after the concrete has been placed. Minor defects shall be repaired with mortal' containing one part of cement and two parts of fine aggregate. Plastering shall not be permitted and all rejected portions shall be removed and replaced at the Contractor's expense. The exposed surface shall be finished while the concrete is still fresh by rubbing the surfaces with wetted soft brick or wood until they are smooth. The surfaces shall be wetted thoroughly, either by dipping the brick or wood in water, or by throwing water on the surfaces with a brush. After the concrete has been rubbed smooth using water, it shall then be rubbed with a thin grout containing one part of cement and one part of fine aggregate. Rubbing with grout shall continue until uniform color is produced.

306.4.3 In case of pre-cast concrete curves

Pre-cast concrete curbs shall be produced using moulds assuring the dimensions shown in the Drawings in a workshop having sufficient capacity for production, curing, testing and storage and transported to site. Care shall be taken not to damage the curbs during handling and transporting. Damaged curbs shall be rejected when found at site and shall be disposed by the Contractor at his own cost.

Pre-cast concrete curbs shall be laid firmly on the foundation with mortar containing one part of cement and two parts of fine aggregate, and accurately along the horizontal and vertical alignment shown in the Drawings.

Vertical and horizontal tolerances with respect to true line and level shall be ± 3 mm.

306.5 Method of Measurement

The length of curb shall be the number of lineal meters of curb of the required dimensions shown in the Drawings measured along its front face in-place, completed and accepted. No deductions shall be made for flattering of curbs at entrances and no additional allowances shall be made for curbs constructed on curves.

306 (1) Concrete Curb		lin.m

306.6 Rates

The Contract unit rate for the curbs and/or surface gutter shall constitute full compensation for furnishing and placing all materials, labors, equipment, tools and any incidentals necessary to complete the work including excavation, bedding, finishing, etc.

307 Road Marking

307.1 Scope

This work shall consist of furnishing and applying Type A and Type B painted road markings on the finished paved area in accordance with these Specifications, at the locations and of the dimensions shown on the Drawings, or as directed by the Engineer.

The markings Type A shall be used mainly for permanent works and Type B shall be used mainly for semi-permanent works at the boundaries between contract sections.

307.2 Materials

- Class A material shall be white thermoplastic material incorporating glass beads and conforming to AASHTO M 249 or equivalent.

- Class B material shall be white ready-mixed traffic paint conforming to AASHTO M 248 or equivalent.

- Glass beads applied to the surface of both Class A and Class B material shall conform to AASHTO M 247 (Type 2) or equivalent.

307.3 Construction Requirements

- Existing lines and markings to be removed will be designated by the Engineer and shall be removed by grit-blasting or other approved method causing minimum damage to the road surface.

- The surface area to be marked shall be clean, dry and free from loose particles. Setting out and location of all markings shall be approved by the Engineer before work begins. Except where approved by the Engineer, all marks shall be laid by self propelled machines equipped with cut-off valves and nozzles capable of forming clean and sharp edged lines and markings, of the specified thickness.

- Type A material shall be laid by spray or screed to the dimensions shown on the Drawings and agreed by the Engineer. The finished thickness of the material shall be a minimum 1.5 mm for spray application and 3 mm for screed application, both exclusive of the glass beads described in (e) below. Preparation and application of the material shall be in accordance with the manufacturer's instructions or as agreed by the Engineer. On concrete surfaces the Contractor shall first apply a tack coat of a type compatible with the thermoplastic material.

- Type B material shall be laid by spray type machine equipped with a mechanical agitator. Each nozzle shall be equipped with suitable guide lines consisting of metallic shrouds or air blasts, and with a satisfactory cut-off valve capable of applying broken or skip lines automatically. Spread rate shall be not less than 40 liters/100m2. In areas where machine laying is impossible, the Engineer may give approval to brush application.

- Glass beads shall be applied to the surface of Type A and Type B markings immediately after they have been laid. Unless otherwise approved by the Engineer, all glass beads shall be applied by pressure or spray application at a rate not less than 450 gm/m2.

- All road markings shall be protected from traffic as instructed by the Engineer. All markings shall present a clean cut, uniform and workmanlike appearance and the surface shall be free from streaks and cracks. All markings which do not have a uniform satisfactory appearance by day and night shall be corrected by the Contractor at his own expense.

307.4 Method of Measurement

The quantity to be paid for removal of existing markings will be the number of square meters of marking designated by the Engineer for removal and removed to his satisfaction.

The quantities of road marking to be paid for will be the number of lenear meters of the relevant material applied to the surface, completed and accepted in accordance with the Drawings, these Specifications, or as directed by the Engineer. For the purposes of measurement each type of material may be divided into two categories as follows;

General Application: Center lines, edge lines, lane markings and other work which is basically parallel to the centerline of a carriageway or ramp.

Special Application: Arrows, pedestrian markings, striping and other work which is transverse or sharply angled to the direction of traffic flow.

3 07 (1) Road Marking Type B (ready-mixed traffic paint)	l.m

307.5 Rate.

The Contract unit rate shall constitute full compensation for furnishing and placing all materials, including all labors, equipment. tools and incidentals necessary to complete the work in accordance with the Specification.

308 Traffic Sign

308.1 General

All signs shall be manufactured in accordance with the Specification issued by the relevant authority of Afghanistan or as shown on the drawings. In the absence of any details or for any missing details, the signs shall be provided as directed by the relevant authority and accepted by the Engineer.

The signs shall be non-reflectorized as shown on the drawings or as directed by the Engineer.

308.2 Materials

The various materials and fabrication of the traffic signs shall conform to the following requirements:

- Concrete: Concrete shall be of the grade shown on the Contract drawings or otherwise as directed by the Engineer.

- Reinforcing steel: Reinforcing steel shall conform to the requirement of Item 402 of this specification unless otherwise shown on the drawings or directed by the Engineer.

- Bolts, nuts, washers: Bolts, nuts and washers shall conform to relevant international codes and standards approved by the Engineer.

- Plates and supports: Plates and support sections for the sign posts shall conform to relevant international codes and standards approved by the Engineer.

- Aluminum: Aluminum sheets used for sign boards shall be of smooth, hard and corrosion resistant aluminum alloy conforming to ASTM B 209 "Standard Specification for Aluminum and Aluminum Alloy Sheet and Plate" or other relevant international codes and standards approved by the Engineer.

Signs with a maximum side dimension not exceeding 600 mm shall not be less than 1.5 mm thick. All others shall be at least 2 mm thick. The thickness of the sheet shall be related to the size of the sign and its support and shall that it does not bend or deform under the prevailing wind and other loads.

308.4 Installation

Sign posts, their foundations and sign mountings shall be so constructed as to hold these in a proper and permanent position against the normal storm wind loads or displacement by vandalism. Normally, signs with an area up to 0.9 sqm shall be mounted on a single post, and for greater area two or more supports shall be provided. Sign supports may be of mild steel, reinforced concrete or galvanized iron (G.L). Post-end(s) shall be firmly fixed to the ground by means o f properly designed foundation. The work o f foundation shall conform to relevant Specifications as specified.

All components of signs and supports, other than the reflective portion and G.I posts shall be thoroughly descaled, cleaned, primed and painted with two coats of epoxy paint. Any part of mild steel (M.S.) post below ground shall be painted with three coats of red lead paint. The signs shall be fixed to the posts by bolts and nuts, fastener, or welding in the case of steel posts and by bolts and washers of suitable size in the case of reinforced concrete or G.I posts. After the nuts have been tightened, the tails of the bolts shall be furred over with a hammer to prevent removal.

308.5 Method of Measurement

The measurement of standard cautionary, mandatory and information signs shall be in number of signs supplied and fixed, while for direction and place identification signs, these shall be measured by area in square meters.

308 (l) Traffic signs 		nos.

308.6 Rates

The Contract unit rate shall be payment in full for the cost of making the road sign, including all materials, paintings, foundations, installation at site, and all other incidentals to complete the work in accordance with the Specifications.

SECTION 4: CONCRETE WORKS

401 Structural Concrete

401.1 Scope

The work shall consist of furnishing and placing structural concrete and incidental construction in accordance with these Specifications and in conformity with the lines, grades and dimensions, as shown on the drawings or as directed by the Engineer.

401.2 Materials

401.2.1 General

Materials to be used in the work shall conform to the specifications mentioned on the drawings, the requirements laid down in this section and specifications for relevant items of work covered under these specifications.

401.2.2 Sources of materials

The Contractor shall notify the Engineer of his proposed sources of materials prior to delivery. If it is found after trial that sources of supply previously approved do not produce uniform and satisfactory products, or if the product from any other source proves unacceptable at any time, the Contractor shall furnish acceptable material from other sources at his own expense.

401.2.3 Cement

Cement to be used in the works shall comply with the requirement specified in AASHTO M85, ASTM C 150 or equivalent subject to the prior approval of the Engineer.

401.2.4 Coarse aggregates

For plain and reinforced cement concrete (PCC and RCC) or pre-stressed concrete (PSC) works, coarse aggregate shall consist of clean, hard, strong, dense, non-porous and durable pieces of crushed stone, crushed gravel, natural gravel or a suitable combination thereof or other approved inert material. They shall not contain pieces of disintegrated stones, soft, flaky, elongated particles, salt, alkali, vegetable matter or other deleterious materials in such quantities as to reduce the strength and durability of the concrete, or to attack the steel reinforcement. Coarse aggregate having positive alkali-silica reaction shall not be used. All coarse aggregates shall conform to AASHTO M80, ASTM C33 or other equivalent international standard approved by the Engineer.

401.2.5 Fine aggregates

For plain and reinforced cement concrete (PCC and RCC) or pre-stressed concrete (PSC) works, fine aggregate shall consist of clean, hard, strong and durable pieces of crushed stone, crushed gravel, or a suitable combination of natural sand, crushed stone or gravel. They shall not contain dust, lumps, soft or flaky, materials, mica or other deleterious materials in such quantities as to reduce the strength and durability of the concrete, or to attack the embedded steel. Motorized sand washing machines should be used to remove impurities from sand. Fine aggregate having positive alkali-silica reaction shall not be used. All fine aggregates shall conform to AASHTO M06, ASTM C33 or other equivalent international standard approved by the Engineer.

401.2.6 Water

Water used for mixing and curing shall be clean and free from injurious amounts of oils, acids, alkalis, salts, sugar, organic materials or other substances that may be deleterious to concrete or steel. Potable water is generally considered satisfactory for mixing concrete. Mixing and curing with sea water shall not be permitted. As a guide, the following concentrations represent the maximum permissible values:

- To neutralize 200 ml sample of water using phenolphthalein as an indicator, it should not require more than 2 ml of 0.1 normal NaOH.

- To neutralize 200 ml sample of water using methyl orange as an indicator, it should not require more than 10 ml of 0.1 normal HCI.

401.2.7 Admixtures

Admixtures are materials added to the concrete before or during mixing with a view to modify one or more of the properties of concrete in the plastic or hardened state.

Concrete admixtures are proprietary items of manufacture and shall be obtained only from established manufacturers with proven track record, quality assurance and full fledged laboratory facilities for the manufacture and testing of concrete. The contractor shall provide the following information concerning each admixture after obtaining the same from the manufacturer:

- Normal dosage and detrimental effects, if any, of under dosage and over dosage.

- The chemical names of the main ingredients in the admixtures.

- The chloride content, if any, expressed as a percentage by the weight of the admixture.

- Values of dry material content, ash content and relative density of the admixture which can be used for Uniformity Tests.

- Whether or not the admixture leads to the entertainment of air when used as per the manufacturer’s recommended dosage, and if so to what extent

- Where two or more admixtures are proposed to he used in any one mix, confirmation as to their compatibility.

- There would be no increase in risk of corrosion of the reinforcement or other embedment as a result of using the admixture.

Admixtures to be used in concrete shall be subject to prior approval by the Engineer.

Calcium chloride or admixtures containing chloride from other than impurities from admixture ingredients shall not be used in pre-stressed concrete, in concrete containing embedded aluminum, or in concrete cast against stay-in-place galvanized metal forms.

Air-entraining admixtures shall conform to the requirements of AASHTO M154 or other equivalent international standard approved by the Engineer.

Chemical admixtures, if specified or permitted, shall conform to the requirements of AASHTO M194 (ASTM C260) "Standard Specification for Air-Entraining Admixtures for Concrete" or other equivalent international standard approved by the Engineer.

401.2.8 Storage of Materials

401.2.8.1 General

All materials may be stored at proper places so as to prevent their deterioration or intrusion by foreign matter and to ensure their satisfactory quality and fitness for the work. The storage space must also permit easy inspection, removal and re-storage of the materials. All such materials even though stored in approved godowns/places, must be subjected to acceptance test prior to their immediate use.

401.2.8.2 Aggregates

Aggregate stockpiles may be made on ground that is denuded of vegetation, is hard and well drained. If necessary, the ground shall be covered with 50 mm plank. Coarse aggregates, unless otherwise agreed by the Engineer in writing, shall be delivered to the site in separate sizes (2 sizes when nominal size is 25 mm or less and 3 sizes when the nominal size is 32 mm or more). Aggregates placed directly on the ground shall not be removed from the stockpile within 300 mm of the ground until the final cleaning up of the work, and then only the clean aggregate will be permitted to be used. In the case of fine aggregates, these shall be deposited at the mixing site not less than 8 hours before use and shall have been tested and approved by the Engineer.

401.2.8.3 Cement

Cement shall be transported, handled and stored on the site in such a manner as to avoid deterioration or contamination. Cement shall be stored above ground level in perfectly dry and water' tight sheds and shall be stacked not more than eight bags high. Wherever bulk storage containers are used their capacity should be sufficient to cater to the requirement at site and should be cleaned at least once every 3 to 4 months. Each consignment shall be stored separately so that it may be readily identified and inspected and cement shall be used in the sequence in which it is delivered at site. Any consignment or pan of a consignment of cement which had deteriorated in any way, during storage, shall not be used in the works and shall be removed from the site by the Contractor without charge to the Employer. The Contractor shall prepare and maintain proper records on site in respect of delivery, handling, storage and use of cement and these records shall be available for inspection by the Engineer at all times. The Contractor shall make a monthly return to the Engineer on the date corresponding to the interim certificate date, showing the quantities of cement received and issued during the month and in stock at the end of the month.

401.2.8.4 Water

Water shall be stored in containers/tanks covered at top and cleaned at regular intervals in order to prevent intrusion by foreign matter or growth of organic l11atter. Water from shallow, muddy or marshy surface shall not be permitted. The intake pipe shall be enclosed to exclude silt, mud, grass and other solid materials and there shall be a minimum depth of 0.60 m of water below the intake at all times.

401.2.9 Tests and standard of acceptance

All materials, even though stored in an approved manner shall be subjected to an acceptance test prior to their immediate use. Independent testing of cement for every consignment shall be done by the Contractor at site in the laboratory approved by the Engineer before use. Any cement with lower quality than those shown in manufacturer's certificate shall be debarred from use. In case of imported cement, the same series of tests shall be carried out before acceptance.

401.2.9.1 Testing and Approval of Material

The Contractor shall furnish test certificates from the manufacturer/supplier of materials along with each batch of material(s) delivered to site. The Contractor shall set up a field laboratory with necessary equipment for testing of all materials, finished products used in the construction as per requirements of conditions of contract and the relevant specifications. The testing of all the materials shall be witnessed by the Engineer or his representative for whom the Contractor shall make all the necessary arrangements and bear the entire cost. Tests which cannot be carried out in the field laboratory have to be got done at the Contractor's cost at any recognized laboratory / testing establishments approved by the Engineer.

401.2.9.2 Sampling of Materia1s

Samples provided to the Engineer or his representative for their retention, are to be in labeled boxes suitable for storage. Samples required for approval and testing must be supplied well in advance by at least 48 hours or minimum period required for carrying out relevant tests to allow for testing and approval. Delay to works arising from the late submission of samples will not be acceptable as a reason for delay in the completion of the works. If materials are brought from abroad, the cost of sampling/testing whether in Afghanistan or abroad shall be borne by the Contractor.

401.2.9.3 Rejection of Materials not Conforming to the Specifications

Any stack or batch of material(s) of which sample(s) does not conform to the prescribed tests and quality shall be rejected by the Engineer or his representative and such materials shall be removed from site by the Contractor at his own cost. Such rejected materials shall not be made acceptable by any modifications.

401.2.9.4 Testing and Approval of Plant and Equipment

All plants and equipment used for preparing, testing and production of materials for incorporation into the permanent works shall be in accordance with manufacturer's specifications and shall be got approved by the Engineer before use.

401.3 Grade of Concrete and their use

The following grades of concrete shall be used unless otherwise shown on the Drawings or directed by the Engineer.

Table 401-1 Classification of Concrete

| Concrete Mix by Volume | One 50kg Bag of cement by volume (Liter) | Total Aggregate by volume (Liter) | Fine Aggregates by volume (Liter) | Coarse Aggregates by volume (Liter) | Quantity of water (Liter) |
| --- | --- | --- | --- | --- | --- |
| 1:2:4 (15Mpa) | 35 | 210 | 70 | 140 | 31 |
| 1:1.5:3 (20Mpa) | 35 | 158 | 53 | 105 | 28 |
| 1:1:2 (25Mpa) | 35 | 105 | 35 | 70 | 25 |

Compressive Strength shall be based on the compressive strength test on Cylindrical Concrete Specimens in accordance with AASHTO T22 or other equivalent international standard approved by the Engineer.

The concrete shall meet the requirement given in the following table.

Table 401-2 Requirements for Each Grade of Concrete

| CONCRETE GRADE | RATIO BETWEEN CEMENT, SAND AND GRAVEL | BATCH WITH ONE BAG CEMENT |  |  | MATERIAL REQUIRED FOR |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | NUMBER OF BOXES |  | APPROX YIELD PER BATCH | 1 CUBIC METER FINISHED |  |  |
|  |  | OF AGGREGATE |  |  | CONCRETE (APPROX) |  |  |
|  |  | FINE | COARSE |  | CEMENT IN | FINE | COARSE |
|  |  | (SAND) | (GRAVEL) |  | BAGS (KG) | (M3) | (M3) |
| 15 | 1:2:4 (20 mm) | 2 | 4 | 0.16 m3 | 6 (300kg) | 0.42 | 0.84 |
| 20 | 1:1.5:3 (20 mm) | 1.5 | 3 | 0.14m3 | 7.3 (380kg) | 0.38 | 0.76 |
| 25 | 1:1:2 (20 mm) | 1 | 2 |  |  |  |  |

401.4 Proportioning of Concrete

Prior to the start of construction the Contractor shall design the mix in case of "Design Mix Concrete" and submit to the Engineer for approval, the proportions of materials, including admixtures to be used. Water-reducing admixtures (including plasticizers or super-plasticizers) may be used at the Contractor's option, subject to the approval of the Engineer. Other types of admixtures shall be prohibited, unless specifically permitted by the Engineer.

401.4.1 Requirements of Consistency

The mix shall have the consistency which will allow proper placement and consolidation in Standard Specifications the required position. Every attempt shall be made to obtain uniform consistency.

401.4.2 Requirements for Designed Mixes

The Contractor shall give notice to enable the Engineer to be present at the making of trial mixes and preliminary testing of the specimens. The Contractor shall prepare trial mixes, using samples of approved materials typical of those he proposes to use in the works, for all classes to the Engineer's satisfaction prior to commencement of concreting. The initial trial mixes shall generally be carried out in an established laboratory approved by the Engineer. In exceptional cases, the Engineer may permit the initial trial mixes to b e prepared a t the site laboratory of the Contractor, if a full fledged concrete laboratory has been established well before testing of materials forming the constituents of proposed design mix shall have been carried out prior to making trial mixes.

Sampling and testing procedures shall be in accordance with AASHTO T23 (ASTM C3l), AASHTO R39 (ASTM C192) and AASHTO T22 (ASTM C39), or other equivalent international standard approved by the Engineer.

Test specimens shall be taken from trial mixes as follows. For each mix, at least set of six cylindrical specimens shall be made from each of three consecutive batches. At least three specimens from each set of six shall be tested at an age of 28 days and three at an earlier age approved by the Engineer. The specimens shall be made, cured, stored, transported and tested in accordance with these Specifications. The average strength of all the specimens at 28 days shall exceed the specified compressive strength.

401.4.3 Additional Requirements

Concrete shall meet with any other requirements as specified on the drawing or as directed by the Engineer. Additional requirements shall also consist of the following overall limits of deleterious substances in concrete:

- The total chloride content of all constituents of concrete as a percentage of mass of cement in mix shall be limited to values given below:

- Pre-stressed Concrete					:	0.06 percent

- Reinforced concrete exposed to chlorides in service	
(e.g. structures located near sea coast)			:	0.15percent

- Reinforced concrete that will be dry or protected from
moisture in service 1.00 percent				:	1.00percent

- Other reinforced concrete construction			:	0.30 percent

- The total sulphur anhydride (SO3) content of all the constituents of concrete as a percentage of mass of cement in the mix shall be limited to 4 per cent.

401.4.4 Suitability of proposed mix portions

The Contractor shall submit the following information for the Engineer's approval:

- Nature and source of each material

- Quantities of each material per cubic meter of fully compacted concrete.

- Either of the following:

- appropriate existing data as evidence of satisfactory previous performance for the target mean strength, current margin, consistency and water / cement ratio and any other additional requirement(s) as specified.

- full details of tests on trial mixes.

- Statement giving the proposed mix proportions for nominal mix concrete.

Any change in the source of material or in the mix proportions shall be subject to the Engineer's prior approval.

401.5 Admixtures

Use of admixtures such as super-plasticizers for concrete may be made with the approval of the Engineer.

401.6 Equipment

Unless specified otherwise, equipment for production, transportation and compaction of concrete shall be as under:

- For Production of Concrete:

- For side drain and concrete boxes:batch type concrete mixer diesel or electric operated, with a minimum size of 200 liters.

- All measuring devices of the equipment shall be maintained in a clean and serviceable condition. Its accuracy shall be checked over the range in use, when set up at each site and thereafter periodically as directed by the Engineer.

- For Concrete Transportation	:	depending upon actual requirement

- Concrete dumpers			minimum 2 tonnes capacity

- Powered hoists			minimum 0.5 tonne capacity

- Chutes

- Buckets handled by cranes

- Transit truck mixer

- Concrete pump

- Concrete distributor booms

- Belt conveyor

- Cranes with skips

- Tremies

- For Compaction of concrete:

- Internal vibrators			size 25 mm to 70 mm

- Form vibrators			minimum 500 watts

- Screed vibrators			full width of carriageway (up to two lanes)

401.7 Mixing Concrete

Concrete shall be mixed either in a concrete mixer or in a batching and mixing plant, as per these Specifications. Hand mixing shall not be permitted. The mixer o r the plant shall be at an approved location considering the properties of the mixes and the transportation arrangements available with the Contractor. The mixer or the plant shall be approved by the Engineer.

Mixing shall be continued till materials are uniformly distributed and a uniform color of the entire mass is obtained and each individual particle of the coarse aggregate shows complete coating of mortar containing its proportionate amount of cement. In no case shall mixing be done for less than 2 minutes.

Mixers which have been out of use for more than 30 minutes shall be thoroughly cleaned before putting in a new batch. Unless otherwise agreed to by the Engineer, the first batch of concrete from the mixer shall contain only two thirds of the normal quantity of coarse aggregate. Mixing plant shall be thoroughly cleaned before changing from one type of cement to another.

401.8 Transporting, Placing and Compaction of Concrete

The method of transporting and placing concrete shall be approved by the Engineer. Concrete shall be transported and placed as near as practicable to its final position, so that no contamination, segregation or loss of its constituent materials takes place. Concrete shall not be freely dropped into place from a height exceeding 1.5 meters.

When concrete is conveyed by chute, the plant shall be of such size and design as to ensure practically continuous flow, slope of the chute shall be so adjusted that the concrete flows without the use of excessive quantity of water and without any segregation of its ingredients. The delivery end of the chute shall be as close as possible to the point of deposit. The chute shall be thoroughly flushed with water before and after each working period and the water used for this purpose shall be discharged outside the form work

All form work and reinforcement contained in it shall be cleaned and made free f.rom standing water, dust, snow or ice immediately before placing of concrete.

No concrete shall be placed in any part of the structure until the approval of the Engineer has been obtained.

If concreting is not started within 24 hours of the approval being given, it shall have to be obtained again from the Engineer. Concreting then shall proceed continuously over the area between the construction joints. Fresh concrete shall not be placed against concrete which has been in position for more than 30 minutes unless a proper construction joint is formed. Except where otherwise agreed to by the Engineer, concrete shall be deposited in horizontal layers to a compacted depth of not more than 450 mm when internal vibrators are used and not exceeding 300 mm in all other cases.

Concrete when deposited shall have a temperature of not less than 5 degrees Celsius, and not more than 40 degrees Celsius. It shall be compacted in its final position within 30 minutes of its discharge from the mixer, unless carried in properly designed agitators. Operating continuously, when this time shall be within 1 hour of the addition of cement to the mix and within 30 minutes of its discharge from the agitator. It may be necessary to add retarding admixtures to concrete if trials show that the periods indicated above are unacceptable. In all such matters the Engineer's decision shall be final.

Concrete shall be thoroughly compacted by vibration or other means during placing and worked around the reinforcement, tendons or duct formers, embedded fixtures and into corners of the formwork to produce a dense homogeneous void-free mass having the required surface finish. When vibrators are used, vibration shall be done continuously during the placing of each batch of concrete until the expulsion of air has practically ceased and in a manner that does not promote segregation. Over vibration shall be avoided to minimize the risk of forming a weak surface layer. When external vibrators are used, the design of form work and disposition of vibrator shall be such as to ensure efficient compaction and to avoid surface blemishes, vibrations shall not be applied through reinforcement and where vibrators of immersion type are used, contact with reinforcement and all inserts like ducts etc., shall be avoided. The internal vibrators shall be inserted in an orderly manner and the distance between insertions should be about one and a half times the radius of the area visibly affected by vibration. Additional vibrators in serviceable condition shall be kept at site so that they can be used in the event of breakdowns.

401.9 Construction Joints

401.9.1 Location

The location of construction joints shall be as shown on the drawings or as approved by the Engineer. The joints shall be provided in a direction perpendicular to the member axis.

401.9.2 Preparation of Joint Surface

Laitance shall be removed before fresh concrete is cast. The surface shall be roughened. Care shall be taken that they should not dislodge the coarse aggregates. Concrete may be brushed with a stiff brush soon after casting while the concrete is fresh.

If the concrete has partially hardened, it shall be treated by wire brushing or with a stiff water jet followed by drying with air jet immediately.

Fully hardened concrete shall be treated with mechanical hand tools or grit blasting, taking care not to split or crack aggregate particles.

Before further concrete is cast, the surface should be thoroughly cleaned to remove debris and accumulated rubbish, one effective method being by ail' jet.

Where there is likely to be a delay before placing the next concrete lift, protruding reinforcement shall be protected. Before the next lift is placed, rust, loose, mortal or other contamination shall be removed from the reinforcements. In aggressive environment, the concrete shall be cut back to expose the reinforcements for a length of about 50 mm to ensure that contaminated concrete is removed.

The joint surface shall not be contaminated with release agents, dust or curing membrane.

401.9.3 Concreting of Joints

The old surface shall be thoroughly cleaned and soaked with water. Standing water shall be removed shortly before the new concrete is placed and the new concrete shall be thoroughly compacted. Concreting shall be carried out continuously up to the construction joints. Surface retarders may be used to improve the quality of construction joints.

For a vertical construction joint, a stopping board shall be fixed previously at the predetermined position and shall be properly stayed to prevent its displacement or bulging when concrete is compacted against it. Concreting shall be continued right up to the board.

401.10 Concreting Under Water

When it is necessary to deposit concrete under water, the methods, equipment, materials and proportions of mix to be used shall be got approved from the Engineer before any work is started. Concrete shall contain 10 per cent more cement than that required for the same mix placed in the dry.

Concrete shall not be placed in water having a temperature below 5 degrees Celsius. The temperature of the concrete, when deposited, shall not be less than 16 degrees Celsius, nor more than 40 degrees Celsius.

Coffer dams or forms shall be sufficiently tight to ensure still water conditions, if practicable, and in any case to reduce the flow of water to less than 3 meters per minute through the space into which concrete is to be deposited. Coffer dams or forms in still water shall be sufficiently tight to prevent loss of mortar through the joints in the walls. Pumping shall not be done while concrete is being placed, or until 24 hOU1'S thereafter. To minimize the formation of laitance, great care shall be exercised not to disturb the concrete as far as possible while it is being deposited.

All under water concreting shall be carried out by tremie method only, using tremie of appropriate diameter. The number and spacing of the tremies should be worked out to ensure proper concreting. The tremie concreting when started should continue without interruption for the full height of the member being concreted. The concrete production and placement equipment should be sufficient to enable the underwater concrete to be completed uninterrupted within the stipulated time. Necessary stand' by equipment should be available for emergency situation.

The top section of the tremie shall have a hopper large enough to hold one full batch of the mix or the entire contents of the transporting bucket as the case may be. The tremie pipe shall not be less than 200 mm in diameter and shall be large enough to allow a free flow of concrete and strong enough to withstand the external pressure of the water in which it is suspended, even if a partial vacuum develops inside the pipe. Preferably, flanged steel pipe of adequate strength for the job shall be used. A separate lifting device shall be provided for each tremie pipe with its hopper at the upper end. Unless the lower end of the pipe is equipped with a n approved automatic check valve, the upper end of the pipe shall be plugged with a wadding of gunny sacking or other approved material before delivering the concrete to the tremie pipe through the hopper; so that when the concrete is forced down from the hopper to the pipe, it will force the plug (and along with it any water in the pipe) down the pipe and out of the bottom end, thus establishing a continuous stream of concrete. It will be necessary to raise slowly the tremie in order to allow a uniform flow of concrete, but it shall not be emptied so that water is not allowed to enter above the concrete in the pipe. At all times after placing of concrete is started and until all the required quantity has been placed, the lower end of the tremie pipe shall be kept below the surface of the plastic concrete. This will cause the concrete to build up from below instead of flowing out over the surface and thus avoid formation of layers of laitance. If the charge in the tremie is lost while depositing, the tremie shall be raised above the concrete surface and unless sealed by the check valve, it shall be replugged at the top end, as at the beginning, before refilling for depositing further concrete.

401. 11 Adverse Weather Conditions

401.11.1 Cold Weather Concreting

Where concrete is to be deposited at or near freezing temperature, precautions shall be taken to ensure that at the time of placing, it has a temperature of not less than 5 degrees Celsius and that the temperature of not less than 5 degrees Celsius and that the temperature of the concrete shall be maintained above 4 degrees Celsius until it has thoroughly hardened. When necessary, concrete ingredients shall be heated before mixing but cement shall not be heated artificially other than by the heat transmitted to it from other ingredients of the concrete. Stock-piled aggregate may be heated by the use of dry heat or steam. Aggregates shall not be heated directly b y gas o r o n sheet metal over fire. In general, the temperature of aggregates or water shall not exceed 65 degrees Celsius. Salt or other chemicals shall not be used for the prevention of freezing. No frozen material or materials containing ice shall be used. All concrete exposed to freezing weather shall have entrained air and the water content of the mix shall not exceed 30 liters per 50 kg of cement.

401.11.2Hot Weather Conditions

When depositing concrete in very hot weather, precautions shall be taken so that the temperature of wet concrete does not exceed 40 degrees Celsius while placing. This shall be achieved by stacking aggregate under the shade and keeping them moist, using cold water, reducing the time between mixing and placing to the minimum, cooling form work by sprinkling water, starting curing before concrete dries out and restricting concreting as far as possible to early mornings and late evenings. When ice is used to cool mixing water, it will be considered a part of the water in design mix. Under no circumstances shall be mixing operation be considered complete until all ice in the mixing drum has melted.

The Contractor will be required to state his methodology for the Engineer's approval when temperatures of concrete are likely to exceed 40 degrees Celsius during the work.

401.12 Protection and Curing

Concreting operations shall not commence until adequate arrangements for concrete curing have been made by the contractor.

Curing and protection of concrete shall start immediately after compaction of the concrete to protect it form:

- Premature drying out particularly by solar radiation and wind

- High internal thermal gradients

- Leaching out by rain and flowing water.

- Rapid cooling during the first few days after placing.

- Low temperature or frost

- Vibration and impact which may disrupt the concrete and interfere with its bond to the reinforcement.

Where members are of considerable size and length, with high cement content, accelerated curing methods may be applied, as approved by the Engineer.

401.12.1 Water Curing

Water for curing shall be as specified in clause 401.2.6 of this Specification.

Entire surface of concrete shall be kept continuously in a damp or wet condition by application of water for a minimum period of 7 days after the concrete has been placed. Cotton mats, rugs, sacks, blankets, carpets, canvas or similar materials may be used to retain the moisture. At the expiration of the curing period the concrete surface shall be cleared of the curing medium.

40l.12.3 Curing Compounds

Curing compounds shall only be permitted in special circumstances and will require specific approval of the Engineer. Curing compounds shall not be used on any surface which requires further finishing to be applied. All construction joints shall be moist, cured and no curing compound will be permitted in locations where concrete surfaces are required to be bonded together.

Curing compounds shall be continuously agitated during use. All concrete cured by this method shall receive two applications of the curing compound. The first coat shall be applied immediately after acceptance of concrete finish. If the surface is dry, the concrete shall be saturated with water and curing compound applied as soon as the surface film of water disappears. The second application shall be made after the first application has set. Placement in more than two coats may be required to prevent streaking.

401.13 Finishing

Immediately after the removal of forms, exposed bars or bolts, if any, shall be cut inside the concrete member to a depth of at least 50 mm below the surface of the concrete and the resulting holes filled with cement mortar. All fins caused by form joints, all cavities produced by the removal of form ties and all other holes and depressions, honey comb spots, broken edges or corners, and other defects, shall be thoroughly cleaned, saturated with water, and carefully pointed and rendered true with mortal' of cement and fine aggregate mixed in the proportions used in the grade of concrete that is being finished and of as dry a consistency as is possible to use. Considerable pressure shall be applied in filling and pointing to ensure thorough filling in all voids. Surfaces which have been pointed shall be kept moist for a period of twenty thousand four hours. Special pre-packaged proprietary mortars shall be used where appropriate or where specified in the drawing.

All construction and expansion joints in the completed work shall be left carefully tooled and free from any mortar and concrete. Expansion joint filler shall be left exposed for its full length with clean and true edges.

Immediately after removal of forms, the concrete work shall be examined by the engineer before any defects are made good.

- The work that has sagged or contains honeycombing to an extent detrimental to structural safety or architectural appearance shall be rejected.

- Surface defect of a minor nature may be accepted. On acceptance of such work by the Engineer, the same shall be rectified as directed by the Engineer.

401.14 Tolerances

Tolerance for dimensions/shape of various components shall be as shown in the table below or indicated elsewhere in these specifications or shown on the drawings or as directed by the Engineer.

Table 401-1 Tolerances in Concrete Elements

|  | Description | Tolerances |
| --- | --- | --- |
| Substructure | (a) Variation in cross sectional dimensions | +10mm, -5mm |
|  | (b) Misplacement from specified position in plan | 10mm |
|  | (c) Variation of levels at the top | ± 10mm |
|  | (d) variation of reduced levels of bearing areas | ± 5mm |
|  | (e) Variation from plumb over full height | ± 10mm |
|  | (f) Surface irregularities measured with 3m straight edge All surfaces except bearing areas | 5mm |

401.15 Tests and Standards of Acceptance

Concrete shall conform to the surface finish and tolerance as prescribed in these specifications for respective components.

Random sampling and lot by lot of acceptance inspection shall be made for the 28 days compressive strength of concrete.

Concrete under acceptance shall be notionally divided into lots for the purpose of sampling, before commencement of work. The delimitation of lots shall be determined by the following:

- No individual lot shall be more than 30 cum. in volume

- At least one specimen forming an item of the sample representing the lot shall be taken from concrete of the same grade and mix proportions cast on any day.

- Different grades of mixes of concrete shall be divided into separate lots.

- Concrete of a lot shall be used in the same identifiable component of the bridge.

- Sampling and testing

- Concrete for making 3 test specimens shall be taken from a batch of concrete at point of delivery into construction.

- A random sampling procedure to ensure that each of the concrete batches forming the lot under acceptance inspection has equal chance of being chosen for taking specimens shall be adopted.

- Cylindrical specimens shall be made, cured and tested at the age of 28 days for compressive strength in accordance with AASHTO T22, ASTM C39 or equivalent. The 28·day test strength result for each specimen shall form an item o f the sample.

- Test specimen and sample strength

Three test specimens shall be made from each sample for testing at 28 days. Additional specimens may be required for various purposes such as to determine the strength of concrete at 7 days or for any other purpose.

The test strength of the sample shall be the average of the strength of 3 specimens. The individual variation should not be more than ± 15 percent of the average.

- Frequency

The minimum frequency of sampling of concrete of each grade shall be in accordance with the following Table.

Table 401-1 Minimum Frequency of Sampling of Concrete

| Quantity of Concrete in Work, m3 | No. of Samples |
| --- | --- |
| 150m3 and above | 1 + one additional sample for each additional 150 m3 or part thereof |

At least one sample shall be taken from each shift of work.

- Acceptance criteria

- Compressive Strength
When both the following conditions are met, the concrete complies with the specified compressive strength:

- The mean strength determined from any group of four consecutive samples should exceed the specified characteristic compressive strength.

- Strength of any sample is not less than the specified characteristic compressive strength minus 3 MPa.

The quantity of concrete represented by the test results include the batches from which the first and last samples were taken, together with all intervening batches.

- Chloride and Sulphate Content
The total chloride and sulphuric anhydride (SOs) content of all the constituents of concrete as a percentage of mass of cement in the mix shall not exceed the values given in this section of the specifications.

If the concrete is not able to meet any of the standards of acceptance as prescribed, the effect of such deficiency on the structure shall be investigated by the contractor as directed by the Engineer. The Engineer may accept the concrete as sub· standard work. Any additional work required by the engineer for such acceptance shall be carried out by the contractor at his cost. In case the concrete is not found to be acceptable after investigation, the Contractor shall remove the rejected concrete forthwith.

401.16 Method of Measurement

Structural concrete unless covered as structural component in other items shall be measured in cubic meters for each grade of concrete. In reinforced concrete, the volume occupied by reinforcement shall not be deducted. The slab shall be measured as running continuously through and the beam as the portion below the slab.

401 (1) Structural Concrete, M15		cum

401 (2) Structural Concrete, M20		cum

401.17 Rates

The Contract unit rate for structural concrete shall cover cost of all materials, labors, tools, plant and equipment required for mixing, transporting and placing in position, vibrating and compacting, finishing and curing as per this Section or as directed by the Engineer, including all incidental expenses, sampling and testing, quality assurance and supervision. Unless mentioned separately as an item in the Contract, the Contract unit rate for concrete shall also include the cost of providing, fixing and removing formwork and joint (wood or rubber) required for concrete work.

402 Reinforcing Steel

402.1 Scope

This work shall consist of furnishing and placing coated or uncoated mild steel or high strength deformed reinforcement bars (untensioned) of the shape and dimensions shown on the drawings and conforming to these Specifications or as approved by the Engineer.

402.2 Material

402.2.1 Reinforcement

Reinforcement steel shall be of the grade indicated in the Drawings or instructed by the Engineer conforming to AASHTO M31 (or ASTM A615) "Deformed and Plain Carbon Steel Bars for Concrete Reinforcement" or other equivalent international standards approved by the Engineer.

Table 402-1 Tensile Requirements of AASHTO M31 (ASTEM A615)

| Grade | Grade 280 |
| --- | --- |
| Tensile strength, min (Moa) | 420 |
| Yield strength, min (MPA) | 280 |
| Elongation in 200mm, min (%) Bar Designation No. 10 13, 16 19 | 11 12 12 |

Bar mats for concrete reinforcement shall conform to ASTM A 184 "Specification for Fabricated Deformed Steel Bar Mats for Concrete Reinforcement" or other equivalent international standard approved by the Engineer.

Deformed wire for concrete reinforcement shall com form to ASTM A496 "Specification for Steel Wire, Deformed, for Concrete Reinforcement" or other equivalent international standard approved by the Engineer.

Welded plain wire fabric for concrete reinforcement shall conform to ASTM A185 "Specification for Steel Welded Wire Fabric, Plain, for Concrete Reinforcement" or other equivalent international standard approved by the Engineer.

Welded deformed wire fabric for concrete reinforcement shall conform to ASTM A497 "Specification for Steel Welded Wire fabric, Deformed, for Concrete Reinforcement" or other equivalent international standard approved by the Engineer.

All steel shall be procured from original producers and no re-rolled steel shall be incorporated in the work.

Only new steel shall be delivered to the site. Every bar shall be inspected before assembling on the work and defective, brittle or burnt bar shall be discarded. Cracked ends of bars shall be discarded.

Mill sheet or technical data sheet with certification of purchased reinforcing steel shall be submitted for approval of the Engineer.

402.2.2 Protection of Reinforcement

Uncoated reinforcing steel shall be protected from rusting or chloride contamination. Reinforcements shall be free from rust, mortar, loose mill scale, grease, oil or paints. This 1uay be ensured either by using reinforcement fresh from the factory or thoroughly cleaning all reinforcement to remove rust using any suitable method such as san blasting, mechanical wire brushing, etc., as directed by the Engineer. Reinforcements shall be stored on blocks, racks or platforms and above the ground in a clean and dry condition and shall be suitably marked to facilitate inspection and identification.

Portions of uncoated reinforcing steel and dowels projecting from concrete shall be protected within one week after initial placing of concrete with a brush coat of neat cement mixed with water to a consistency of thick paint. This coating shall be removed by lightly tapping with a hammer or other tool not more than one week before placing of the adjacent pour of concrete. Coated reinforcing steel shall be protected against damage to the coating. If the coating on the bars is damaged during transportation or handling and cannot be repaired, the same shall be rejected.

402.3 Bending of Reinforcement

Bar bending schedule shall be furnished by the Contractor and approved by the Engineer before start of work. Reinforcing steel shall conform to the dimensions and shapes given in the approved Bar Bending Schedules. The approval of bar bending schedule by the Engineer shall in no way relieve the responsibility of the Contractor. Any expense incident to the incorrectness of the bar bending schedule to make them comply with the Drawings shall be borne by the Contractor.

Bars shall be bent cold to the specified shape and dimensions or as directed by the Engineer using a proper bar bender, operated by hand or power to obtain the correct radii of bends and shape. Bars shall not be bent or straightened in a manner that will damage the parent material or the coating.

Bars bent during transport or handling shall be straightened before being used on work and shall not be heated to facilitate straightening.

402.4 Placing of Reinforcement

402.4. 1	The reinforcement cage should generally be fabricated in the yard at ground level and then shifted and placed in position. The reinforcement shall be placed strictly in accordance with the drawings and shall be assembled in position only when the structure is otherwise ready for placing of concrete. Prolonged time gap between assembling of reinforcements and casting of concrete, which may result in rust formation on the on the surface, shall not be permitted.

402.4.2	Reinforcement bars shall be placed accurately in position as shown on the drawings. The bars, crossing one another shall be tied together at every intersection with binding wire (annealed) to make the skeleton of the reinforcement rigid such that the reinforcement does not get displaced during placing of concrete, or any other operation. The diameter of binding wire shall not be less than 1 mm.

402.4.3 Bars shall be kept in position usually by the following methods:

- In case of beam and slab construction, cover blocks made of concrete of thickness equal to the specified cover shall be placed between the bars and formwork. The concrete cover blocks shall have the same strength and specification as those of the member. Industrially produced polymer cover blocks subject to satisfactory evidence that the polymer composition is not harmful to concrete and reinforcement may be permitted by the Engineer.

- In case of dowels for columns and walls, the vertical reinforcement shall be kept in position by means of timber templates with slots cut in them accurately, or with cover blocks tied to the reinforcement. Timber templates shall be removed after the concreting has progressed up to a level just below their location.

- Layers of reinforcements shall be separated by spacer bars at approximately one meters intervals. The minimum diameter of spacer bars shall be 12 mm or equal to maximum size of main reinforcement or maximum size of coarse aggregate, whichever is greater. Horizontal reinforcement shall not be allowed to sag between supports.

- Necessary stays, blocks, metal chairs, spacers, metal hangers, supporting wires etc., or other subsidiary reinforcement shall be provided to fix the reinforcements firmly in its correct position.

- Use of pebbles, broken stone, metal pipe, brick, mortar or wooden blocks etc., as devices for positioning reinforcement shall not be permitted.

402.4.4	Bars coated with epoxy or any other approved protective coating shall be placed on supports that do not damage the coating. Supports shall be installed in a manner such that planes of weakness are not created in hardened concrete. The coated reinforcing steel shall be held in place by use of plastic or plastic coated binding wires especially manufactured for the purpose. Reference shall be made to Section 1000 for other requirements.

402.4.5	Placing and fixing of reinforcement shall be inspected and approved by the Engineer before placing concrete.

402.5 Bar Splices

402.5.1 Lapping

All reinforcement shall be furnished in full lengths as indicated on the drawing. No splicing of bars, except where shown on the drawing, will be permitted without approval of the Engineer. The lengths of the splice shall be as indicated on drawing or as approved by the Engineer. Where practicable, overlapping bars shall be bound with annealed steel binding wire, not less than 1 mm diameter and twisted tight such a manner as to maintain minimum clear cover to the reinforcement from the concrete surface. Lapped splices shall be staggered or located at points, along the span where stresses are low.

402.5.2 Welding

Splicing by welding of reinforcement shall not be permitted unless if detailed on the drawing or approved by the Engineer. Weld shall develop an ultimate strength equal to or greater than that of the bars connected.

402.5.3 Mechanical Coupling of Bars

Bars may b e joined with approved patented mechanical devices as indicated on the drawing or as approved by the Engineer e.g. by special grade steel sleeves swagged on to bars in end to end contact or by screwed couplers. In case such devices are permitted by the Engineer, they shall develop at least 125 per cent of the characteristic strength of the reinforcement bar.

402.6 Testing and Acceptance

The material shall be tested in accordance with relevant Specifications and necessary test certificates shall be furnished. Additional tests, if required, shall be carried out by the Contractor at his own cost.

The fabrication, furnishing and placing of reinforcement shall be in accordance with these Specifications and shall be checked and accepted by the Engineer.

402.7 Method of Measurement

Reinforcement shall be measured in length including hooks, if any, separately for different diameters as actually used in work, excluding overlaps. From the length so measured, the weight of reinforcement shall be calculated in tonnes on the basis of the unit weight of steel is equal to 7.85 tonne/m3. Wastage, overlaps, couplings, welded joints, spacer bars, chairs, stays, hangers and annealed steel wire or other methods for binding and placing shall not be measured and cost of these items shall be deemed to be included in the rates for reinforcement.

402 (1) Reinforcement, deformed bars (D10mm dia.)		ton

402 (2) Reinforcement, deformed bars (D16mm dia.)		ton

402 (3) Reinforcement, deformed bars (D18mm dia.)		ton

402.8 Rates

The contract unit rate for uncoated reinforcement shall cover the cost of material, fabricating, transporting, storing, bending, placing, binding and fixing in position as shown on the drawings as per these Specifications and as directed by the Engineer, including all labors, tools, equipment, supplies, royalty, transportation, incidentals, sampling, testing and supervision.

403 Form work

403. 1 Scope

Form work shall include all temporary or permanent forms required for forming the concrete of the shape, dimensions and surface finish as shown on the drawing or as directed by the Engineer, together with all props, staging, centering, scaffolding and temporary construction required for their support.

403.2 Materials

Timber materials shall conform to AASHTO M168 or equivalent. Metal materials shall conform to the relevant international standards or equivalent.

Materials and components used for form work shall be examined for damage or excessive deterioration before use/re·use and shall be used only if found suitable after necessary repairs. In case of timber form work, the inspection shall not only cover physical damages but also signs of attacks by decay, rot or insect attack or the development of splits.

Forms shall be constructed with metal or timber. The metal used for forms shall be of such thickness that the forms remain true to shape. All bolts should be countersunk. The use of approved internal steel ties or steel or plastic spacers shall be permitted. Structural steel tubes used as support for forms shall have a minimum wall thickness of 4 mm. Other materials may also be used if approved by the Engineer.

403.3 Design of Formwork

403.3. 1	The Contractor shall furnish the design and drawings of complete formwork (i.e. the forms as well as their supports) for approval of the Engineer before any erection is taken up. If proprietary system of formwork is used, the Contractor shall furnish detailed information to the Engineer for approval.
Notwithstanding any approval or review of dl·awing and design by the Engineer, the Contractor shall be entirely responsible for the adequacy and safety of formwork.

403.3.2	The design of the formwork shall ensure that the forms can be conveniently removed without disturbing the concrete. The design shall facilitate proper and safe access to all parts of form work for inspection.

403.4 Workmanship

403.4.1	The form work shall be robust and strong and the joints shall be leak·proof. Staging must have cross bracings and diagonal bracings in both directions. Staging shall be provided with an appropriately designed base plate resting on firm strata.

403.4.2	The number of joints in the formwork shall be kept to a minimum by using large size panels. The design shall provide for proper "soldiers" to facilitate alignment. All joints shall be leak proof and must be properly sealed. Use of PVC T-section is essential to prevent leakage of grout.

403.4.3	As far as practicable, clamps shall be used to hold the forms together. Where use of nails is unavoidable minimum number of nails shall be used and these shall be left projecting so that they can be withdrawn easily. Use of double headed nails shall be preferred.

403.4.4	Use of ties shall be restricted, as far as practicable. Wherever ties are used they shall be used with HDPE sheathing so that the ties can easily be removed. No parts prone to corrosion shall be left projecting or near the surface. The sheathing shall be grouted with cement mortar of the same strength as that of the structure.

403.4.5	Unless otherwise specified, or directed, chamfers or fillets of sizes 25 mm x 25 mm shall b e provided at all angles o f the form work to avoid sharp corners. The chamfers, beveled edges and moldings shall be made in the formwork itself. Opening for fixtures and other fittings shall be provided in the shuttering as directed by the Engineer.

403.4.6	Shuttering for walls, sloping members and thin sections of considerable height shall be provided with temporary openings to permit inspection and cleaning out before placing of concrete.

403.4.7	The formwork shall be constructed with pre-camber to the soffit to allow for deflection of the formwork. Pre-camber to allow for deflection of form work shall be in addition to that indicated for the permanent structure in the drawings.

403.4.8	Where centering trusses or launching trusses are adopted for casting of superstructure, the joints of the centering trusses, whether welded, riveted or bolted should be thoroughly checked periodically. Also, various members of the centering trusses should be periodically examined for proper alignment and unintended deformation before proceeding with the concreting. They shall also be periodically checked for any deterioration in quality due to steel corrosion.

403.4.9	The formwork shall be so made as to produce a finished concrete true to shape, line and levels and dimensions as shown on the drawings, subject to the tolerances specified in respective sections of these Specifications, or as directed by the Engineer.

403.4.10 Where metal forms are used, all bolts and rivets shall be countersunk and well ground to provide a smooth, plane surface. Where timber is used it shall be well seasoned, free from loose knots, projecting nails, splits or other defects that may mar the surface of concrete.

403.4.11	Forms shall be made sufficiently rigid by the use of ties and bracings to prevent any displacement or sagging between supports. They shall be strong enough to withstand all pressure, ramming and vibration during and after placing the concrete. Screw jacks or hard wood wedges where required shall be provided to make up any settlement in the formwork either before or during the placing of concrete.

403.4.12	The form work shall take due account of the calculated amount of positive or negative camber so as to ensure the correct final shape of the structures, having regard to the deformation of false work, scaffolding or propping and the instantaneous or deferred deformation due to various causes affecting pre-stressed structures.

403.4.13	Suitable camber shall be provided to horizontal members of structure, especially in long spans to counteract the effects of deflection. The form work shall be so fixed as to provide for such camber.

403.4.14	The formwork shall be coated with an approved release agent that will effectively prevent sticking and will not stain the concrete surface. Lubricating (machine oils) shall be prohibited for use as coating.

403.5 Formed Surface and Finish

The form work shall be lined with material approved by the Engineer so as to provide a smooth finish of uniform texture and appearance. This material shall leave no stain on the concrete and so fixed to its backing as not to impart any blemishes. It shall be so fixed to its backing as not to impart any blemishes. It shall be of the same type and obtained from only one source throughout for the construction of any one structure. The Contractor shall make good any imperfections in the resulting finish as required by the Engineer. Internal ties and embedded metal parts shall be carefully detailed and their use shall be subject to the approval of the Engineer.

403.6	Precautions

- Special measures in the design of form work shall be taken to ensure that it does not hinder the shrinkage of concrete. The soffit of the form work shall be so designed as to ensure that the formwork does not restrain the shortening and/or hogging of beams during pre·stressing. The forms may be removed at the earliest opportunity subject to the minimum time for removal of forms with props retained in position.

- Where necessary, formwork shall be so arranged that the soffit form, property supported on props only can be closed with the same grade of concrete as the adjoining structure immediately after removal of form work ensuring watertight joints.

- Any cut· outs or openings provided in any structural member to facilitate erection of formwork shall be closed with the same grade of concrete as the adjoining structure immediately after removal of formwork ensuring watertight joints.

- Provision shall be made for safe access on, to and about the formwork at the levels as required.

- Close watch shall be maintained to check for settlement of formwork during concreting. Any settlement of formwork during concreting shall be promptly rectified.

- Water used for curing should not be allowed to stagnate near the base plates supporting the staging and should be properly drained.

403.7 Preparation of Formwork Before Concrete

The inside surfaces of forms shall, except in the case of permanent form work or where otherwise agreed to by the Engineer be coated with a release agent supplied by approved manufacturer or of an approved material to prevent adhesion of concrete to the form work. Release agents shall be applied strictly in accordance with the manufacturer's instructions and shall not be allowed to come into contact with any reinforcement or pre-stressing tendons and anchorages, Different release agents shall not be used in formwork for exposed concrete. Before re-use of forms, the following actions shall be taken:

- The contact surfaces of the forms shall be cleaned carefully and dried before applying a release agent.

- It should be ensured that the release agent is appropriate to the surface to be coated. The same type and make of release agent shall be used throughout on similar form work materials and different types should not be mixed.

- The form surfaces shall be evenly and thinly coated with release agent. The vertical surface shall be treated before horizontal surface and any excess wiped out.

- The release agent shall not come in contact with reinforcement or the hardened concrete.

All forms shall be thoroughly cleaned immediately before concreting.

The Contractor shall give the Engineer due notice before placing any concrete in the forms to permit him to inspect and approve the formwork, but such inspection shall not relieve the Contractor of his responsibility for safety of form work, men, machinery, materials and finish or tolerances of concrete,

403.8 Removal of Formwork

The scheme for removal of formwork (i.e. de-shuttering and de-centering) shall be planned in advance and furnished to the Engineer for scrutiny and approval. No form work or any part thereof shall be removed without prior approval of the Engineer.

The formwork shall be removed so as not to cause any damage to concrete. Centering shall be gradually and uniformly lowered in such a manner as to permit the concrete to take stresses due to its own weight uniformly and gradually to avoid any shock or vibration.

Where not specifically approved, the time of removal of form work (when ordinary Portland cement is used without any admixtures at an ambient temperature exceeding 10 degrees Celsius) shall be as under:

- Walls, piers, abutments, columns and	:	12 to 48 hours as may be decided by
vertical faces of structural members		the Engineer

- Soffits of Slabs	:	3 days
(with props left under)

- Props (left under slabs)	:	14 days

- Soffit of Girders	:	7 days
(with props left under)

- Props(left under girders)	:	21 days

Where there are re-entrant angles in the concrete sections, the form work should be removed at thee sections as soon as possible after the concrete has set, in order to avid cracking due to shrinkage of concrete.

403.9 Re-Use of Formwork

When form work is dismantled, its individual components shall be examined for damage and damaged pieces shall be removed for rectification. Such examination shall always be carried out before being used again. Before re-use all components shall be cleaned of deposits of soil, concrete or other unwanted materials. Threaded parts shall be oiled after cleaning.

All bent steel props shall be straightened before re·use. The maximum deviation from straightness is 11600 of the length. The maximum permissible axial loads in used props shall be suitably reduced depending upon their condition. The condition of the timber components, plywood and steel shuttering plates shall be examined closely for distortion and defects before re·use

403.10 Specialized Formwork

Specialized form work may be required in the case of slip-form work, underwater concreting, segmental construction etc. Such specialized formwork shall be designed and detailed by competent agencies and a set of complete working drawings and installation instructions shall be supplied to the Engineer. The site personnel shall be trained in the erection and dismantling as well as operation of such specialized form work. In case proprietary equipment is used, the supplier shall supply drawings, details, installation instructions, etc., in the form of manuals along with the formwork. Where specialized form work is used, close coordination with the design of permanent structure is necessary.

For slip form the rate of slipping the form work shall be designed for each individual case taking into account various parameters including the grade of concrete, concrete strength, concrete temperature, ambient temperature, concrete admixtures, etc. in the case of segmental construction, the concrete mix shall be normally designed for developing high early strength so that the formwork is released as early as possible.

In order to verify the time and sequence of striking/removal of specialized form work, routine field tests for the consistency of concrete and strength development are mandatory and shall be carried out before adoption.

For specialized form work, the form lining material may be either plywood or steel of appropriate thickness. Plywood is preferred where superior quality of surface is desired, whereas steel sheeting is normally used where large number of repetitions is involved.

403.11 Tests and Standards of Acceptance

The material shall be tested in accordance with these Specifications and shall meet the prescribed criteria.

The work shall conform to these Specifications and shall meet the prescribed standards of acceptance.

403.12 Method of Measurement

Unless stated otherwise the rate for concrete in plain concrete and reinforced concrete shall be deemed to include all form work required in accordance with this section and shall not be measured separately.

403.13 Rates

The Contract unit rate of the plain concrete and reinforced concrete as defined in respective sections shall be deemed to cover the costs of all formwork, including cost of all materials, labors, tools and plant required for design, construction and removal of formwork and supervision as described in this section including properly supporting the members until the concrete is cured, set and hardened as required.

SECTION 5: MASONRY WORKS

501 Stone Masonry

501.1 Scope

This work shall consist of the construction of structures with stones jointed together by cement mortar in accordance with the details shown on the drawings and these specifications or as approved by the Engineer.

501.2 Materials

Stones shall be of the type specified. It shall be hard, sound, free from cracks, decay and weathering and shall be freshly quarried from an approved quarry. Stone with round surface shall not be used. The stones, when immersed in water for 24 hours, shall not absorb water by more than 5 per cent of their dry weight when tested in accordance with AASHTO T85 or other equivalent international standard. The length of stones shall not exceed 3 times its height nor shall they be less than twice its height plus one joint. No stone shall be less in width than the height and width on the base shall not be greater than three' fourth of the thickness of the wall nor less than 150 mm.

Cement mortar shall conform to Clause 501.4 of this Specification.

501.3 Type of Masonry

The type of masonry used for structures shall be random masonry (coursed or uncoursed) or coursed rubble masonry (First sort). However, for bridge work generally, course rubble stone masonry shall be used. The actual type of masonry used for different parts of structures shall be specified on the drawings.

501.4 Construction Operations

501.4. 1 Laying

The masonry work shall be laid to lines, levels, curves and shapes as shown in the Drawings. The height in each course shall be kept same and every stone shall be fine tooled on all beds joints and face full and true. The exposed faces shall be gauged out, grooved, regulated and sunk or plain molded as the case may be. The faces of each stone between the drafts shall be left rough as the stone comes from quarry except where sacrificial layer is to be provided or plastering is resorted to due to aggressive environment.

Stone shall be sufficiently wetted before laying to prevent absorption of water from mortar. Stratified stones must be laid on their natural beds. All bed joints shall be normal to the pressure upon them.

Stones in the heading shall be laid on their broadest face that given a better opportunity to fill the spaces between stones.

The courses of the masonry shall ordinarily be pre·determined. They shall generally be of the same height. When there is to be variation in the height of courses, the larger courses are to be placed at lower levels, heights of courses decreasing gradually towards the top of the wall. The practice of placing loose mortar on the course and pouring water on it to fill the gaps in stones is not acceptable. Mortar may be fluid mixed thoroughly and then poured in the joints. No dry or hollow space shall be left anywhere in the masonry and each stone shall have all the embedded faces completely covered with mortar.

In tapered walls, the beds of the stones and the planes of course should be at right angles to the batter. In case of bridge piers with batter on both sides, the course shall be horizontal

The bed which is to receive the stone shall be cleaned, wetted and covered with a layer of fresh mortar. All stones shall be laid full in mortar both in bed and vertical joints and settled carefully in place with a wooden mallet immediately on placement and solidly embedded in mortar before it has set. Clean chips and spalls shall be wedged into the mortar joints and bed wherever necessary to avoid thick beds or joints of mortar. When the foundation masonry is laid directly on rock, the face stones of the first course shall be dressed to fit into rock snugly when pressed down in the mortar bedding over the rock. No dry or hollow space shall be left anywhere in the masonry and each stone shall have all the embedded faces completely covered with mortar. For masonry works over rock, a leveling course of 100 mm thickness and in concrete of C15 shall be laid over rock and then stone masonry work shall be laid without foundation concrete block.

Face works and hearting shall be brought up evenly but the top of each course shall not be leveled up by the use of flat chips. For sharp corners especially in skew bridges, through stones shall be used in order to avoid spalling of corners.

In case any stone already set in mortar is disturbed or the joints broken, it shall be taken out without disturbing the adjoining stones and joints. Dry mortar and stones thoroughly cleaned from the joints and stones and the stones reset in fresh mortar. Attempt must never be made to slide one stone on top of another, freshly laid.

Shaping and dressing shall be done before the stone is laid in the work. No dressing and hammering, which will loosen the masonry, will be allowed after it is once placed. All necessary chases for joggles, dowels and clamps should be formed before hand

Sufficient transverse bonds shall be provided by the use of bond stone extending from the front to the back of the wall and in case of thick wall from outside to the interior and vice versa. In the latter case, bond stones shall overlap each other in their arrangement.

In case headers are not available, pre cast headers of M 15 concrete shall be used. Cast· in-situ headers are not permitted.

Stones shall break joint on the face for at least half the height of the course and the bond shall be carefully maintained throughout.

In bank work at all angle junctions of walls, the stones at each alternate course shall be carried into each of the respective walls so as to unite the work thoroughly.

The practice of building up thin faces tied with occasional through stones and filling up the middle with small stuff or even dry packing is not acceptable.

All quoins and the angles of the opening shall be made from selected stones, carefully squared and bedded and arranged to bond alternately long and short in both directions.

All vertical joints shall be truly vertical. Vertical joints shall be staggered as far as possible. Distance between the nearer vertical joints of upper layer and lower shall not be less than half the height of the course.

Only rectangular shaped bond stones or headers shall be used. Bond stones shall overlap each other by 150 mm or more.

All connected masonry in a structure shall be carried up nearly at one uniform level throughout but when breaks are unavoidable the masonry shall be raked in sufficiently long steps to facilitate jointing of old and new work. The stepping of raking shall not be more than 45 degrees with horizontal.

501.4.2 Random Masonry (Uncoursed and coursed)

(1) Dressing

Stone shall be hammer dressed on the face, the sides and beds to enable it to come in proximity with the neighboring stone. The bushing on the exposed face shall not be more than 40 mm.

(2) Insertion of chips

Chips and spalls of stone may be used wherever necessary to avoid thick mortar beds or joints and it shall be ensured that no hollow spaces are left anywhere in the masonry. The chips shall not be used below hearting stones to bring these up to the level of face stones. Use of chips shall be restricted to filling of interstices between the adjacent stones in hearting and they shall not exceed 20 per cent of the quantity of stone masonry.

(3) Hearting stones

The hearting or interior filling of the wall face shall consist of rubble stones not less than 150 mm in any direction. Carefully laid, hammered down with a wooden mallet into position and solidly bedded in mortar. The hearting should be laid nearly level with facing and backing.

(4) Bond stones

Through bond stones shall be provided in masonry up to 600 mm thickness and in case of masonry above 600 mm thickness, a set of two or more bond stones overlapping each other at least by 150 mm shall be provided in a line from face to back. In case of highly absorbent types of stones (porous limestone and sandstones, etc.,) the bond stone shall extend only abut two-third into the wall, as through stones in such cases may give rise to penetration of dampness and therefore, for all thickness of such masonry, a set of two or more bond stones overlapping each other by at least 150 mm shall be provided. One bond stones shall be provided for every 0.50 sq. m. of the masonry surface.

(5) Quoin stone

Quoin stone i.e. stone specially selected and neatly dressed for forming an external angle in masonry work, shall not be less than 0.3 cubic meters in volume.

(6) Plum stone

The plum stones are selected long stones embedded vertically in the interior of the masonry to form a bond between successive courses and shall be provided at about 900 mm intervals.

(7) Laying

The masonry shall be laid with or without courses as specified. The quoins shall be laid header and stretcher alternately. Every stone shall be fitted to the adjacent stone so as to form neat and close joint. Face stone shall extend and bond well in the back. These shall be arranged to break joints, as much as possible, and to avoid long vertical lines of joints.

(8) Joints

The face joints shall not be more than 20 mm thick, but shall be sufficiently thick to prevent stone-to-stone contact and shall be completely filled with mortar.

501.4.3 Pointing

Pointing shall be carried out using mortal not learner than 1:3 by volume of cement and sand or as shown on the drawing. The mortar shall be filled and pressed into the raked out joints before giving the required finish. The pointing shall be ruled type for which it shall, while still green, be ruled along the centre with half round tools of such width as may be specified by the Engineer. The super flush mortal shall then be taken off from the edges of the lines and the surface often masonry shall be cleaned of all mortal.

The maximum thickness of joints in different work shall be as follows:

• Random Rubble		: 	20 mm

501.4.5 Curing

Green work shall be protected from rain by suitable covering and shall be kept constantly moist on all faces for a minimum period of seven days, Stone masonry work carried out during the day shall be suitably marked indicating the date on which the work is done so as to keep a watch on the curing period. The top of the masonry work shall be left flooded with water at the close of the day. Watering may be done carefully so as not to disturb or wash on the green mortar. During hot weather, all finished or partly completed work shall be covered or wetted on in such a manner as will prevent rapid drying o f the brickwork.

During the period of curing of brickwork, it shall be suitably protected from all damages. At the close of day's work or for period of cessation, watering and curing shall have to be maintained. Should the mortar perish i.e. become dry, white or powdery through neglect of curing, work shall be pulled down and rebuilt as directed by the Engineer. If any stains appear during watering, the same shall be removed from the face.

501.5 Scaffolding

The scaffolding shall be sound, strong and safe to withstand all loads likely to come upon it. The holes which provide resting space for horizontal members shall not be left in masonry under one meter in width or immediately near the skew backs of arches. The holes left in the masonry work for supporting the scaffolding shall be filled and made good. Scaffolding shall be got approved by the Engineer. However, the Contractor shall be responsible for its safety.

501.6 Weep Holes

Weep holes shall be provided in solid plain concrete/reinforced concrete, brick/stone masonry, abutment, wing wall and return walls as shown on the drawing or directed by the Engineer to drive moisture from the back filling. Weep holes shall be provided with 100 mm diameter PVC pipe for structures in plain/ reinforced concrete or brick masonry unless otherwise indicated in the Drawings. In case of stone masonry, weep holes shall be 80 mm wide, 150 mm high or circular with 150 mm diameter unless otherwise indicated in the Drawings. Weep holes shall extend through the full width of concrete/masonry with slope of about 1 vertical: 20 horizontal towards the draining face. The spacing of weep holes shall generally be I m in either direction or as shown in the drawing with the lowest at about 150 mm above the low water level or ground level whichever is higher or as directed by the Engineer.

501.7Tests and Standard of Acceptance

All work shall be done to the lines and levels as indicated on the drawing or as directed by the Engineer subject to tolerances as specified in these specifications.

Mortar cubes shall be tested for compressive strength in accordance with AASHTO T106 or other equivalent international standards approved by the Engineer. The frequency of testing shall be one sample for every two cubic meters of mortar subject to a minimum 3 samples for a day's work.

501.8 Method of Measurement

Stone masonry shall be measured in cubic meters.

In arches, the length of arch shall be measured as the mean length between the extrados and intrados.

501 (1) Stone masonry		cum

501.9	Rates

The contract unit rate for stone masonry shall include the cost of all labors, materials, tools and plant, scaffolding, sampling and testing, supervision, other expenses incidental to the satisfactory completion of the work as described herein above and cost for pointing as well.

502 Brickworks

502.1 Scope

Brickwork shall consist of construction of structures with bricks jointed together by cement mortal' in accordance with the details shown on the drawings or as approved by the Engineer.

502.2 Materials

502.2.1 Bricks

Clay or shale bricks shall conform to the requirements of the followings or other equivalent international standards approved by the Engineer.

Sewer and Manhole Brick (Made from Clay or Shale): 	AASHTO M91 (or ASTM C32)

- Brick for sewer or drainage structures shall conform
to the physical properties for the specified Grades SS or 
SM.

- Brick for manholes, catch basins, and other related
structures shall conform to the physical properties for
the specified Grades MS or MM.

- Unless otherwise specified by the purchaser, brick of
Grade SS shall be accepted instead of Grade SM; also
Grade MS shall be accepted instead of Grade MM.

Building Brick (Solid Masonry Units Made from Clay or AASHTO M11Z (or ASTM C6Z)

Shale):

- Unless otherwise specified on the Drawings or directedby the Engineer, grade MW (Moderate Weathering) shallbe used.

502.2.2 Cement

Cement shall conform to the requirements laid down in Section 4.

502.3 Cement Mortar

Cement and sand shall be mixed in specified proportions given in the Drawings. Cement shall be proportioned by volume, taking the unit volume of cement as 1 to sand of 6. All mortar shall be mixed with a minimum quantity of water to produce desired workability consistent with maximum density of mortar. The mix shall be clean and free from injurious type of soil/acid/alkali/organic matter or deleterious substances.

The mixing shall preferably be done in a mechanical mixer operated manually or by power. Hand mixing can be resorted to as long as uniform density of the mix and its strength are assured subject to prior approval of the Engineer. Where permitted, hand mixing operation shall be carried out on a clean watertight platform, where cement and sand shall be first mixed dry in the required proportion by being turned over and over, backwards and forwards several times till the mixture is of uniform color. Thereafter, minimum quantity of water shall be added to bring the mortar to the consistency of a stiff paste. The mortar shall be mixed for at least two minutes after addition of water.

Mortar shall be mixed only in such quantity as required for immediate use. The mix, which has developed initial set, shall not be used. Initial set of mortar with ordinary Portland cement shall normally be considered to have taken place in 30 minutes after mixing. In case the mortar has stiffened during initial setting time because of evaporation of water, the same can be re-tempered by adding water as frequently as needed to restore the requisite consistency, but this re·tempering shall not be permitted after 30 minutes. Mortar unused for more than 30 minutes shall be rejected and removed from site of work.

502.4 Soaking of Bricks

All bricks shall be thoroughly soaked in a tank filled with water for a minimum period of one hour prior to being laid. Soaked bricks shall be removed from the tank sufficiently in advance so that they are skin dry at the time of actual laying. Such soaked bricks shall be stacked on a clean place where they are not contaminated with dirt, earth, etc.

502.5 Joints

The thickness of joints shall not exceed 1 0 mm. All joints on exposed faces shall be tooled to give concave finish.

502.6 Laying

All brickwork shall be laid in an English bond, even and true to line, in accordance with the drawing or as directed by the Engineer, plumb and level and all joints accurately kept. Half and cut bricks shall not be used except when necessary to complete the bond. Closer in such cases shall be cut to the required size and used near the ends of the walls. The bricks used at the face and also at all angles forming the junction of any two walls shall b e selected whole bricks of uniform size, with true and rectangular faces.

All bricks shall be laid with frogs up on a full bed of mortar except in the case of tile bricks. Each brick shall be properly bedded and set in position by slightly pressing while laying, so that the mortar gets into all their surface pores to ensure proper adhesion. All head and side joints shall be completely filled by applying sufficient mortar to brick already placed and on brick to b e placed. All joints shall b e properly flushed and packed with mortar so that no hollow spaces are left. No bats or cut bricks shall be used except to obtain dimensions of the different courses for specified bonds or wherever a desired shape so requires.

The brickwork shall be built in uniform layers, and for this purpose wooden straight edge with graduations indicating thickness of each course including joint shall be used. Corners and other advanced work shall be raked back. Brickwork shall be done true to plumb or in specified batter. All courses shall be laid truly horizontal and vertical joints shall be truly vertical. Vertical joints in alternate courses shall come directly one over the other. During construction, no part of work shall rise more than one meter above the general construction level, to avoid unequal settlement and improper jointing. Where this is not possible in the opinion of the Engineer, the works shall be raked back according to the bond (and not toothed) at an angle not steeper than 45 degrees with prior approval of the Engineer. Toothing may also be permitted where future extension is contemplated,

Before laying bricks in foundation, the foundation slab shall be thoroughly hacked, swept clean and wetted. A layer of mortar not less than 1 2 mm thick shall be spread on the surface of the foundation slab and the first course of bricks shall be laid.

502. 7 Jointing Old and New Work

Where fresh masonry is to join with masonry that is partially I entirely set, the exposed jointing surface of the set masonry shall be cleaned, roughened and wetted, so as to effect the best possible bond with the new work. All loose bricks and mortar or other material shall be removed,

In the case of vertical or inclined joints, it shall be further ensured that proper bond between the old and new masonry is obtained by interlocking the bricks. Any portion of the brickwork that has been completed shall remain undisturbed until thoroughly set. In case of sharp corners especially in skew bridges, a flat cutback of 100 mm shall be provided so as to have proper and bonded laying of bricks.

502.8 Curing

Green work shall be protected from rain by suitable covering and shall be kept constantly moist on all faces for a minimum period of seven days, Brickwork carried out during the day shall be suitably marked indicating the date on which the work is done so as to keep a watch on the curing period. The top of the masonry work shall be left flooded with water at the close of the day. Watering may be done carefully so as not to disturb or wash on the green mortar. During hot weather, all finished or partly completed work shall be covered or wetted on in such a manner a s will prevent rapid drying o f the brickwork.

During the period of curing of brickwork, it shall be suitably protected from all damages. At the close of day's work or for period of cessation, watering and curing shall have to be maintained. Should the mortar perish i.e. become dry, white or powdery through neglect of curing, work shall be pulled down and rebuilt as directed by the Engineer. If any stains appear during watering, the same shall be removed from the face.

502.9 Scaffolding

The scaffolding shall be sound, strong and safe to withstand all loads likely to come upon it. The holes which provide resting space for horizontal members shall not be left in masonry under one meter in width or immediately near the skew backs of arches. The holes left in the masonry work for supporting the scaffolding shall be filled and made good. Scaffolding shall be got approved by the Engineer. However, the Contractor shall be responsible for its safety. 502.10 Equipment

All tools and equipment used for mixing, transporting and laying of mortar and bricks shall be clean and free from set mortar, dirt or other injurious foreign substances.

502.11 Acceptance of Work

All the work shall be true to the lines and levels as indicated on the drawing or as directed by the Engineer, subject to tolerances as indicated in these Specifications.

Mortar cubes shall be tested for compressive strength in accordance with AASHTO T106 or other equivalent international standards approved by the Engineer. The frequency of testing shall be one sample for every 2 cubic meters of mortar, subject to a minimum 3 samples for a day's work.

In case of plaster finish, the minimum surface thickness shall not be less than the specified thickness by more than 3 mm.

502.12 Method of Measurement

All brickwork shall be measured in cubic meters. Any extra work done by the Contractor over the specified dimensions shall be ignored.

In arches, the length of arch shall be measured as the mean length between the extrados and intrados.

The work of plastering and pointing when separately shown in the Bill of Quantity shall be measured in square meters of the surface treated. In case no item for plastering and pointing is provided in the Bill of Quantity, the cost shall be deemed to be included in the Brickworks.

502 (1) Brickwork			cum

502.13 Rates

The Contract unit rate for brick work shall include the cost of all labors, materials, tools and plant, scaffolding and other expenses incidental to the satisfactory completion of the work, sampling, testing and supervision as described in these specifications and as shown on the drawings.

SECTION 6: STRUCTURAL STEEL

601 I-Beam Steel Girder for Pedestrian Bridge

601.1 Scope

The Contractor shall furnish and install I-Beam Steel Girder for Pedestrian Bridge as shown on the Drawings and conforming to these Specifications or as approved by the Engineer.

601.2 Materials

Except as otherwise specified, all material and methods of fabrication shall conform to the standards listed below:

Table 601-1 Standard and Metal Work

| Item | Standard |
| --- | --- |
| Structural Steel | ASTM A 36 or JIS G 3101 SS 41 |
| Bolt and Nut | ASTM A 307 Grade A or JIS B 1180 |

601.3 Construction Requirement

a)	Standard details of metalwork are shown on the relevant Drawings for the proposed structures.

b)	No further detailed drawings for metal works other than those included in the Tender Documents will be provided by the Engineer.  The Contractor shall perform all necessary design and provide the complete shop drawings required for the fabrication and installation of all metalwork.  Any fabrication or procurement of items prior to approval of the design and shop drawings and supporting data shall be at the Contractor's risk.

c)	All shop drawings and designs prepared by the Contractor shall be submitted 28 days before commencement of the work to the Engineer for approval.

601.3.1 Fabrication

a)	Metalwork shall be shop-fitted and shop assembled where possible and shall conform to the details on the approved shop drawings.

b)	All fastening, anchors and accessories required for fabrication and erection shall be provided by the Contractor.  Exposed fastenings shall be kept to an absolute minimum, evenly spaced and neatly set out.  Wood or plastic plugs will not be permitted.

c)	All welding shall be performed by operators who have been tested and meet the requirements of the American Welding Society (AWS), JIS Z 3801, JIS Z 3821, JIS Z 3841, or approved equivalent.  Welding shall be carried out in accordance with the requirements of the American Institute of Steel Construction (AISC) or approved equivalent and shall conform to the standard code of AWS or approved equivalent.

d)	Workmanship in fabrication shall conform to the best modern shop and field practice.  All joints and intersecting members shall be accurately fitted and all works shall be fabricated on true planes with adequate fastenings.

601.3.2 Embedment of Metalwork

a)	Metalwork to be embedded in concrete shall be secured in position and embedded when the concrete is being placed or, if shown on the Drawings or directed, recesses or block outs shall be made in the concrete and the metalwork shall be grouted in place using a non-shrink cement grout or mortar or embedded in second-stage concrete.

b)	The surfaces of all metalwork to be in contact with concrete shall be thoroughly cleaned immediately before the grout, mortar or concrete is placed and shall be prepared in accordance with Sub-clause 601.3.2 of this Clause.

c)	Metalwork shall be accurately positioned and aligned to the tolerances specified in Clause TS8.24 or as shown on the Drawings or approved shop drawings, and shall be held securely in the correct position during placing and setting of the concrete.

d)	Where it is impracticable to place anchors or anchor bolts required for the installation of comparatively light metalwork when the concrete is placed, holes shall be drilled into the concrete after it has set for 28 days and expansion bolts, adhesive anchor bolts, or other approved anchors shall be installed.  For galvanized metalwork, galvanized expansion bolts or adhesive anchor bolts shall be used.  For painted metalwork, corrosion-resistant steel expansion bolts or adhesive anchor bolts shall be used.

601.3.3 Non-shrink Grout or Mortar and Dry-pack for Metalwork

a)	Non-shrink grout or mortar, or dry-pack for metalwork shall be mixed in the proportions and to the consistency directed.  The Contractor shall furnish cement and fine aggregate complying with Section 4 for all grout or mortar.  The cost of materials for and the mixing and placing of non-shrink grout and mortar shall be included in the rates tendered in the priced Bill of Quantities for furnishing and installing the various items of metalwork for which the grout, mortar or dry-pack is required.

b)	Before placing grout, mortar or dry-pack, the surfaces of existing concrete on which the grout, mortar or dry-pack will be placed shall be roughened and shall be cleaned of all laitance, loose or defective concrete coatings and other foreign material by approved means followed by thorough washing.  Such surfaces shall be kept moist for at least 24 hours immediately before placing grout, mortar or dry-pack.

601.3.4 Protective Coatings

a)	Except where otherwise specified, all metalwork shall, on completion of fabrication and inspection by the Engineer, be hot dipped galvanized at a rate of 0.6 kilograms per square meter and galvanizing shall be performed in accordance with ASTM A 123 or JIS H 8641.

b)	The protective coating shall be carried out in accordance with Section 902 Surface Treatment of steel.

601.4 Method of Measurement

a)	The cost of preparing designs, shop drawings and data for metalwork and submitting designs, shop drawings and data to the Engineer and accessories such as channel, anchor bolts, rubber bearings, elastic filler and etc. shall be included in the rate tendered in the priced Bill of Quantities for the item to which it is appurtenant.

I-Beam Girder shall be measured in linear meters.

601(1)  Furnishing and installation of I-Beam Girder (I-300x150) 		lin. m

601.5 Rate

The contract unit rate for I-Beam Girder shall include the cost of all labors, materials, tools and plant, hauling, scaffolding, shop design and drawing, shop assembly test, supervision, accessories such as channel, anchor bolts, rubber bearings, elastic filler and etc. and other expenses incidental to the satisfactory completion of the work as described herein above.

The cost of reinforced cement concrete and reinforcement bars shall be excluded in this cost item.

602	GI Pipe for Guard Pipe

602.1 Scope

The Contractor shall furnish and install Guard Pipe as shown on the Drawings and conforming to these Specifications or as approved by the Engineer.

602.2 Materials

Except as otherwise specified, all material and methods of fabrication shall conform to the standards listed below:

Table 601-1 Standard and Metal Work

| Item | Standard |
| --- | --- |
| Galvanized mild steel pipe | ASTM 120 Schedule 40 or JIS G 3444 |

602.3 Construction Requirement

Guard pipe shall be fabricated from the galvanized mild steel pipe with diameters of 60mm and 35mm with reinforced concrete foundation.

a)	Standard details of metalwork are shown on the relevant Drawings for the proposed structures.

b)	No further detailed drawings for metal works other than those included in the Tender Documents will be provided by the Engineer.  The Contractor shall perform all necessary design and provide the complete shop drawings required for the fabrication and installation of all metalwork.  Any fabrication or procurement of items prior to approval of the design and shop drawings and supporting data shall be at the Contractor's risk.

c)	All shop drawings and designs prepared by the Contractor shall be submitted 28 days before commencement of the work to the Engineer for approval.

602.4 Method of Measurement

a)	The cost of preparing designs, shop drawings and data for metalwork and submitting designs, shop drawings and data to the Engineer shall be included in the rate tendered in the priced Bill of Quantities for the item to which it is appurtenant.

Measurement, for payment, of the Guard Pipe shall be made of the projected horizontal length along the top of the Guard Pipe installed as shown on the Drawings or directed. The Guard Pipe shall be measured in linear meters.

602(1)  Furnishing and installation of Guard Pipe		lin. m

602.5 Rate

The contract unit rate for Guard Pipe shall include the cost of all labors, materials, tools and plant, hauling, scaffolding, shop design and drawing, shop assembly test, supervision and other expenses incidental to the satisfactory completion of the work as described herein above.

S

ECTION 7: DRAINAGE

701 Pipe Culverts

701.1 Scope

This work shall consist of furnishing and installing reinforced cement concrete pipes. Diameter and length required at the locations are shown on the drawings or as ordered by the Engineer and in accordance with the requirements of these specifications.

701.2 Materials

All materials used in the construction of reinforced concrete pipe culverts shall conform to the requirements of Section 4 "Concrete Works" of these Specifications.

Each consignment of cement concrete pipes shall be inspected, tested, if necessary, and approved by the Engineer either at the place of manufacture or at the site before their incorporation in the works.

701.3 Excavation for Pipe

The foundation bed for pipe culverts shall be excavated true to the lines and grades shown on the drawings or as directed by the Engineer. The pipes shall be placed in shallow excavation of the natural ground or in open trenches cut in existing embankments, taken down to levels as shown on the drawings. In case of high embankments where the height of fill is more than three times the external diameter of the pipe, the embankment shall first be built to an elevation above the top of the pipe equal to the external diameter of the pipe, and to width on each side of the pipe of not less than five times the diameter of pipe, after which a trench shall be excavated and the pipe shall be laid.

Where trenching is involved, its width on either side of the pipe shall be a minimum of 150 mm or one fourth of the diameter of the pipe whichever is more and shall not be more than one' third the diameter of the pipe. The sides of the trench shall be as nearly vertical as possible.

The pipe shall be placed where the ground for the foundation is reasonably firm. Installation of pipes under existing bridges or culverts shall be avoided as far as possible. When during excavation the material encountered is soft, spongy or other unstable soil, and unless other special construction methods are called for on the drawings or in special provisions, such unsuitable material shall be removed to such depth, width and length as directed by the Engineer. The excavation shall then be backfilled with approved granular material which shall be properly shaped and thoroughly compacted up to the specified level.

Where bed-rock or boulder strata are encountered, excavation shall be taken down to at least 200 mm below the bottom level of the pipe with prior permission of the Engineer and all rock/boulders in this area be removed and the space filled with approved earth, free from stone or fragmented material, shaped to the requirements and thoroughly compacted to provide adequate support for the pipe.

Trenches shall be kept free from water until the pipes are installed and the joints have hardened.

701.4 Bedding for Pipe

The bedding surface shall provide a firm foundation of uniform density throughout the length of the culvert shall conform to the specified levels and grade and shall be of one of the following two types as specified on the drawings:

- Granular bedding: The pipe shall be evenly bedded on a continuous layer of well compacted approved granular material, shaped concentrically to fit the lower part of the pipe exterior for at least ten per cent of its overall height or as otherwise shown on the drawings. The bedding material shall be well graded sand or another granular material passing 5.6 mm sieve suitably compacted/rammed. The compacted thickness of the bedding layer shall be as shown on the drawings and in no case shall it be less than 75 mm.

- Concrete cradle bedding: When indicated on the drawings or directed by the Engineer, the pipe shall be bedded in a cradle constructed of concrete having a mix not leaner than Grade C15 conforming to Section 4 of the Specification. The shape and dimensions of the cradle shall be as indicated on the drawings. The pipes shall be laid on the concrete bedding before the concrete has set.

701.5 Laying of Pipe

No pipe shall be laid in position until the foundation has been approved by the Engineer. Where two or more pipes are to be laid adjacent to each other, they shall be separated by a distance equal to at least one third of the diameter of the pipe subject to a minimum of 50 mm. The arrangement for lifting, loading and unloading pipes from factory/yard and at site shall be such that the pipes do not suffer any undue structural strain, any damage due to fall or impact.

Lowering the pipe in the bed may be carried out with tripod pulley arrangement or simply by manual labor in a manner that the pipe is placed in the proper position without damage.

The laying of pipes on the prepared foundation shall start from the outlet and proceed towards the inlet and be completed to the specified lines and grades. In case of use of pipes with bell-mouth, the belled end shall face upstream. The pipes shall be fitted and matched so that when laid in work they form a culvert with a smooth uniform invert.

Any pipe found defective or damaged during laying shall be removed at the cost of the Contractor.

701.6 Backfilling

Trenches shall be backfilled immediately after the pipes have been laid and the jointing material has hardened. The backfill soil shall be clean, free form boulders, large roots, excessive amounts of sods or other vegetable matter, and lumps and shall be approved by the Engineer. Backfilling up to 300 mm above the top of the pipe shall be carefully done and the soil thoroughly rammed, tamped or vibrated in layers not exceeding 150 mm, particular care being taken to thoroughly consolidate the materials under the haunches of the pipe. Approved pneumatic or light mechanical tamping equipment can be used.

Filling of the trench shall be carried out simultaneously on both sides of the pipe in such a manner that unequal pressures do not occur.

In case of high embankment, after filling the trench up to the top of the pipe in the above said manner, a loose fill of a depth equal to external diameter of the pipe shall be placed over the pipe before further layers are added and compacted.

701.7 Connecting box and other Ancillary Works

Connecting boxes and other ancillary works shall be constructed in accordance with the details shown on the Drawings or as directed by the Engineer. Concrete works and masonry shall conform to Section 4 and Section 5 respectively.

701.8 Opening to Traffic

No traffic shall be permitted to cross the pipe line unless height of filling above the top of t he pipe line is at least 600 mm.

701.9 Method of Measurement

Pipe culverts shall be measured along their centre between the inlet and outlet ends by numbers of pipes with length of 2.44m each.

Selected granular material and cement concrete for pipe bedding, when items are separately given in the Bill of Quantities (BOQ), shall be measured as laid in cubic meters.

Ancillary works shall be measured as provided for under the respective sections.

701 (1) RCC pipe Փ 450mm        	no.

701.10 Rate.

The Contract unit rate for the pipe culvert shall include the cost of pipes, loading, unloading, hauling, handling, storing, laying in position and jointing complete and all incidental costs to complete the work as per these specifications. Ancillary works such as connecting boxes etc. shall be paid for separately, as provided under the respective Clauses.

702 Side drain, infiltration inlet and culvert pit

702.1 Scope

The work shall consist of the construction of side drain, infiltration inlet and culvert pit in accordance with this specification and in reasonably close conformity with the lines and grades shown in the drawings or as established by the Engineer.

702.2 Materials

All the materials for concrete works shall comply with requirements specified in Section 4 "Concrete Works.”

Unless otherwise indicated in the drawings, joint mortar shall be composed of one part Portland cement and two parts fine aggregate by volume to which hydrated lime has been added in an amount equal to 10 percent of the cement by weight. All materials for mortar shall meet the require meets of Section 4.

702.3 Construction Requirements

Excavation and backfill shall be carried out in accordance with Section 1 "Earthworks.”

Concrete construction shall conform to the requirements specified in Section 4 "Concrete Works.”

Expansion joints shall be provided for long concrete side drain at spacing not greater than 10m unless otherwise shown in the drawings. Expansion joints shall be filled with wood or rubber approved by the Engineer of not less than 20mm thick or otherwise specified in the drawings or as directed by the Engineer.

Pipe sections shall be flushed on the inside of the structure wall and projected outside sufficiently for proper connection with next pipe section.

Upon completion, each structure shall be cleaned of any accumulations of silt, debris, or foreign matter of any kind and shall be kept clear of such accumulation until final acceptance of the work.

702.4 Method of Measurement

The quantities of side drain, infiltration inlets etc completed and accepted in accordance with the Drawings, these Specifications and as directed by the Engineer, shall be measured as follows:

702.5 Rate.

The Contract unit rate for the work shall constitute full compensation for furnishing and placing all materials, labor, equipment, tools and incidentals necessary to complete the work including fabrication, excavation, installation, etc.

Section 8 Gabion Works

801 Gabion Works

801.1 General

The quality of stone for gabion shall as specified in Clause 501.2. The stone size ranges from 200 mm to 350mm. Small stones should be avoided. The stones used should have a minimum size of not less than “D” (mesh width) and not greater than 3.5 times “D”, where D is the specified mesh width as given below. Larger stones can be used provided that their total volume does not exceed 5% of the cell volume.

801.2 Material

Gabions shall be of the types and sizes shown on the Drawings. The cages shall be constructed from mild steel wire complying with BS 1052, “Specification for testing zinc coatings on steel wire and for quality requirements” wire used for the formation of the mesh panel will have a diameter of 3.0 mm.

801.3 Filling and placing

The foundation for each gabion and mattress shall be prepared by the Contractor to the satisfaction of the Engineer. Irregularities in the foundation shall be excavated or tightly filled with gravel to produce a surface which has no protrusions or cavities in excess of 100mm.

The gabions and mattresses shall be flexible galvanized gabions of the size shown on the Drawings and shall be fabricated from wire mesh. Each gabion and mattress shall be divided by diaphragms into cells, whose length shall not be greater than the width of the gabions or mattress plus 100mm. the gabion and mattress boxes shall be fabricated ‘Maccaferri’ type or equivalent supplied by an approved manufacturer.

The prefabricated gabions and mattresses shall be obtained complete with sufficient suitable galvanized wire for completing the wiring of the gabions and mattresses on Site.

The wire in the gabions and mattresses shall be galvanized similar to or stronger than that used in ‘Macerferri’ galvanized gabions. The wires in the gabions and mattresses shall be arranged so that the spacing between the wire is similar to or smaller than in ‘Marcerferri’ gabions and mattresses.

The empty gabions shall be placed to line and level as shown on the Drawings or as directed by the Engineer and then stretched so that the gabions regain their shape on being filled. Diaphragms shall be provided at not more than one meter (1m) intervals for baskets and not more than 1.2 meter intervals for mattress. A gabion shall not be completely filled until the adjacent basket or mattress has been half filled, unless otherwise directed, in order not to cause displacements from bulging during filling.

Because of small horizontal movements associated with the settlement or considation, gabion walls must not be constructed with a vertical front face as it subsequently tilts forward slightly, all gabion walls must not be constructed with the front face at the slight angle to the vertical ( 10:1-vertical: Horizontal). This should be achieved by sloping the foundation accordingly as shown in the diagram below:

Before tilling, adjacent baskets should be secured together using steel lacing wire provided for the purpose and conforming to the specification. The sides must be secured in straight lines with no gaps left between the sides of adjacent baskets. Where more than one layer of baskets is laid, they must be placed as shown on the Drawings or as directed by the Engineer with a minimum step of 0.15 m between the faces of the lower and upper gabion boxes.

All gabions must be connected to each other along corners with same lacing operation. For correct lacing operation, the wire should be passed through each mesh, making a double twist every other mesh. Careful attention must be given to the filling operation to ensure that the stones are placed evenly in the baskets with minimum voids in between. Smaller stones can be used to fill the central voids of the boxes, but all external stones must be at least 1.5 D where D is the diameter of the mesh.

The stones selected for the top layer of gabion baskets must have a flat surface to ensure that the wire that does not rest on sharp corners. They must have a minimum dimension of 1.5 D in all directions and be placed to ensure a minimum number of voids.

Bracing wires must be fixed at depths of 1/3 H where. “H” is the height of gabion box. The horizontal distance between the bracing wires should be 1/3 H thus for a gabion basket of 2mx1mx0.5m dimension, eight bracing wires are provided. For the gabion boxes used on the project the bracing wires should be placed at the following depths and spacing.

Table 801-1 Gabion Dimensions

| Gabion Dimensions |  |  |  |  | Horizontal Distance between Bracing (meters) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Length | Width | Depth | 1st Brace | 2nd Brace |  |  |  |  |
| 2.00 | 1.00 | 0.50 | 0.25 | - | 0.40 | 0.80 | 1.2 | 1.6 |

Stones should be filled to the depth of the first brace and then the bracing wires placed directly above the level of the stone making sure the wire passes around at least two mesh widths. The procedure should then be followed for the next layer.

In aprons downstream of weirs and similar places where falls directly on the gabions, vertical bracing wires between the top an bottom mesh must be provided. Additional horizontal bracing must be used at the comers of structure.

801.4 Gabion Wire Protection

A concrete layer will be provided on the crest of wires as shown in the Drawings or directed by the Engineer to protect the gabion mesh against damage. This should be of minimum thickness of 0.10 meter and should be provided once the structure has been completed and any initial settlement has taken place. Construction joints should be provided at regular intervals which should not exceed 3 meters.

A rigid capping of concrete to gabions walls is not to be provided as this restricts the flexibility of the gabion structure. When the Engineer recommends protection of such walls, as in the case of protection of theft of wire, a thickness of 0.05 m should be provided. Where greater thickness is recommended, a flexible protection material must be used.

801.5 Measurement and payment of Gabions

Gabions and Mattresses: Measurement for payment, of furnishing and placing gabions and mattresses will be made of the numbers of completed gabions and mattresses in place to the lines, grades and dimensions shown on the Drawings or as directed. Payment for furnishing and placing gabions and mattresses will be made at the applicable rate tendered thereof in the period Bill of Quantities. These rates shall include the cost of all freight, labor, fabrication, erection, filling and placing of gabions and mattresses required to complete the work.

801(1) Gabion mattress                                          No.

801.5.1 Gabion Baskets and Mattresses

The unit of measurement shall be number of mattress

801.5.2 Inclusion and exclusion

The rate shall include quarrying of suitable stone, supply of gabion baskets and mattresses, supply of wire, transport of stone and wire to the sit, transport of stone and wire to the site, assembling the wire crates, filling with selected stone, bracing and the like.