SECTION: 8

CARPENTRY AND JOINERY

1	Timber

All softwood for carpentry and joinery work shall be well seasoned sound , bright , free form shakes , large loose or dead knots , waney edges , warp , incipient decay , stained sapwood or other defects and shall be to the approval of the Engineer .

Timber for carpentry work shall be carefully sawn square and shall hold the full dimensions shown on the Drawings.

The hardwood for joinery work shall be to the approval of the Engineer, well seasoned, close grained and free form all defects. Hardwood for polishing or clear treatment shall be selected and kept clean.

Any preservative treatment shall be approved by the Engineer.

The Contractor shall allow for all necessary cutting of timber to size and shape, for preparation of surfaces, for all fixings, for properly jointing and putting together including farming , gluing , doweling screwing and mortising , for all cutting and waste , notching , sinking , scribing , mitres , ends , short lengths and any other sundry items of like nature and for priming all concealed surfaces of joinery. Aluminium primer shall be applied to concealed surfaces of all joinery timber.

All sizes and dimensions shown on the Drawings are finished sizes unless otherwise stated.

Timber for joinery work shall be finished work to the exact sizes shown on the Drawings with pencil rounded exposed arrises and no joinery shall be built in until inspected and approved by the Engineer.

The whole of hardwood joinery shall be rubbed down to a smooth surface and left clean and ready to receive any oiled or other finish

Where screw fixings would show on the surface of hardwood, the heads shall be countersunk 6mm below timber surface and grain matched fillets not less than 6mm thick and traped and cut from matching timber shall be glued in and finished off flush with the face. This will apply equally to hardwood which is to be painted.

2	Moisture Content of Timber

The softwood generally shall have a maximum moisture content of 12%.

The hardwood shall have a maximum moisture content of 10% and shall have been kiln dried.

The whole of the timber for joinery work shall be properly stacked and protected from rain and ground moisture.

3	Plywood

The minimum thickness shall be 5mm.

Plywood face veneers shall be approved by the Engineer.

Plywood adhesives shall be approved by the Engineer.

The Contractor shall not be permitted to make up the required thickness by gluing together sheets of thinner plywood.

4	Veneers

Timber   for face   veneer   shall generally be first grade   hardwood    as indicated on the

Drawings and obtained from an approved supplier.

The minimum thickness of timber face veneers shall be 0.6 mm thick.

The face veneers shall be hard, durable, and capable of being finished easily to a smooth surface.   They  shall  be  free  from  knots,  worm  and  beetle  holes,  splits,  dots,  glue  stains, filling  and inlay of any kind  or other  defects.

The  face  veneers  shall  be  applied  to  one or both sides  of wood  panels  as shown  on the Drawings,

Where  veneers   are  shown   to  be  applied   to  one  face  only,   the  other  side  shall  have  a balancing  veneer  applied  to prevent  warping.

Adhesives   shall  comply  with the requirements   of BS  1203:1991   Synthetic  resin adhesives for plywood  (Phenolic  and  aminoplastic)   and shall  ensure  proper  adhesion  between  plies.

5      Plastic Laminate

Unless  otherwise   indicated  on drawings  or specified  plastic  laminate  facings  shall conform to  BS  2572:1990:     PHENOLIC    LAMINATED    SHEET   and  shall  be  a  minimum   0.9  mm thick,   containing    Decorative    surface    papers   impregnated    with   melamine    resins   and Pressed  over  kraft  paper  core  sheets  impregnated   with  Phenolic   resin,  pressure  bonded at  1000  Ibs./sq.in.  pressure  to  300  of  temperature    and  with  sanded   Back  for  glue- application.

Colour and pattern shall conform to the sample approved by the Engineer.

Plastic  laminate  sheets  shall  be  applied  with  a water  proof,  heat-  resistant  adhesive  of a type  recommended    by the  plastic  laminate   manufacturer   and  applied   in accordance   with the manufacturer's   instructions.

6	Fixing and Jointing

Softwood in carpentry work shall be put together with steel nails except where described as framed when it shall be properly jointed and held together with glue and steel screws. Fixings shall be stout steel nails and screws.

Joinery work shall be carefully put together and properly jointed in accordance with best practice; all joints shall be glued and screwed or doweled. Any screws appearing on facework shall have the heads let in and pellated unless otherwise described. Softwood fixings shall be stout steel screws.

Where joinery is required to be put together and fixed with brass cups and screws, the cups for fixing hardwood joinery shall be cast brass cups with milled edges and shall be neatly let in to finish flush with the face of the work.

Nail lengths shall not be more than total thickness of sections to be joined less 5mm, but otherwise not less than twice the thickness of the section through which nails are driven.

Screw lengths shall be not more than total thickness of sections to be joined less 5mm, but otherwise not less than 1 times the thickness of the section through which screws are driven.

Proprietary plugs shall be approved by the Engineer.

Steel nails shall comply with BS 1202: Part 1.

Wood screws shall be brass complying with Bs 1210 with slotted countersunk heads.

Screw cups shall be brass complying with BS 1494: Part 2.

Synthetic resin gap-filling adhesives shall comply with BS 1204: Part 1, type WBP.

Synthetic resin close-contact adhesives shall comply with BS 1204: Part 2, type WBP.

7	Spacings and Additional Supports

Where no dimensions are specified or shown on Drawings, space battens, fillets, grounds studs etc., shall be used in accordance with the recommendations of the manufacture of the sheets and/or sections being fixed.

Where not shown on Drawings, additional supports shall be positioned and fixed for appliances, fixtures, edges of sheets etc., in accordance with the manufacturer's recommendations.

8	Doors

Doors shall be as specified below or in the Particular Conditions obtained from one of the approved manufacturers and shall be capable of withstanding the particular weather conditions of the Middle East.

Door leaves with a polished finish are to be veneered as described in the Particular Conditions with the approved hardwood veneered plywood factory finished and supplied with protective wrappings, and with all necessary preparation for ironmongery carried out.

All edges are to be lipped with hardwood and all beads and lippings are to match face veneers.

All doors whether light cored, solid cored and/or fire resisting shall conform to BS 459 and 476 and 4787 as appropriate with adequate blocking out for ironmongery etc.

Door frames shall be as shown on the Drawings and made of galvanized steel in accordance with door manufacturer's recommendations and should be manufactured and finished by the door manufacturer where possible.

9	Windows

Windows and fanlight sashes shall be framed to the size shown on the Drawings. Sashes hung folding shall have meeting beads screwed on. Glazing bars if required shall be of twice rebated section.

Aluminium windows (Best quality) will be used. Colour and type of section must be approved by the Engineer.

10	Flyscreens

Flyscreens to doors shall be framed and braced with rails styles and braces and filled in with aluminium mesh, 18x16 meshes per inch.

11	Frames

Frames to doors, windows and flyscreens shall be provided and built in to the sizes shown on the Drawings or as directed by the Engineer.

Frames shall be securely tied to walls by means of steel or similar metal cramps, galvanised or dipped in bitumen and provided as follows:

(a)   Door frames: three cramps to each side.

(b)   Window frames: two or more cramps to each side according to size.

(c)    Any other way approved by the Engineer (e .g. foam bond)

Doors, windows, etc. shall be carefully and accurately fitted to the frames to give a uniform clearance of not more than 3mm all round.

12	Architraves, Door Stops etc.

Architraves, door stops etc. shall be as shown on the Drawings and all properly mitered at intersections as approved by the Engineer.

Glazing beads where required shall be wrought splayed and rounded and shall be neatly mitered and fixed with small brads or lost-head nails.

13	Fittings

In connection with fittings such as wardrobes, cupboards, counters etc., the doors, frames, drawers, rails and framing etc. shall be properly and accurately framed together.

Before starting repetitive fabrication of any component, prototypes shall be prepared and approved.

Unless components are specified to be built in, these shall not be made until all site dimensions have been checked.

Matching clearance holes shall be provided for all sizes of screw and matching pilot holes for screws of 6 gauges or more for screwing softwood.

Clearance and pilot holes to match screw sizes shall be provided for screwing hardwood.

Pilot holes shall be provided slightly less than half the diameter of the screw for screwing particle board.

All nail heads which will be visible in completed work shall be punched below timber surface.

14	Finish

All joinery which is to be polished, varnished or painted shall be finished smooth and clean by rubbing down with fine sandpaper.

15	Protection

All joinery shall be protected from damage during the course of the Works and on completion shall be to the Engineer's entire satisfaction. Before handing over the Contractor shall ensure that all doors, drawers, etc., work easily and shall make all necessary adjustments including those needed during the maintenance period.