SECTION: 10

METAL WORKS

To be read in conjunction with General Conditions and General Specification Section.

1101.     Scope

This specification covers ferrous and non-ferrous metal intended to  be used in  the  Works all  in accordance with the Drawings and as directed by the Engineer.

MATERIALS

1102.     Steel

Steel plates and structural steel shaped sections shall conform to the requirements of BS 4: Part 1:

1993 for Hot-rolled sections, BS 4848: Part 2: 1991 for Hot Finished Hollow Sections and BS 4848: Part

4: 1986 for Equal and Unequal Angles.

1103.     Bolts and Nuts

Bolts and nuts shall conform to the requirements of BS 4190:19611 for “ISO metric black hexagon bolts, screws, and nuts.”

1104.     Washers

Plain washers shall be made of galvanized steel. Taper or other specially shaped washers shall be made of steel or malleable cast iron and shall conform to the requirements of BS 4320:1968 Metal washers for general engineering purposes.

1105.     Galvanized Steel Pipes

Galvanized steel pipes shall conform to the requirements of BS 13811:1985 (1990) ISO "Medium Series".

1106.     Paint

Paint for Metal Worker shall comply with the applicable requirements as specified under "PAINTING AND DECORATING".

1107.     Aluminum

All aluminum elements shall be manufactured of extruded sections of aluminium alloy, to BS 1474:1987

Type HE9 or ISO AI, Mg.Si 6063 or AA 6063 T5 mechanically jointed.

All parts and members shall be of aluminium commercial quality like (A1-Mg-Si) heat-treated, free from defects impairing their strength and durability and containing not more than 0.1% copper.

All exposed surfaces shall be polished to a mirror-like surface, free from defects, and shall be light etched and anodized or polyester powder coated or super durable powder coated to colours and/or finishes as shown on Drawings and/or as directed in writing by the Engineer.

Aluminum shall be treated to comply with BS 1615:1993 and BS 3987:1991 to provide an anodization not less than 20 microns thickness or polyester powder coated by electrostatic spraying and hard stoved to not less than 60 micron thickness to comply with BS 6496:1984 (1991) or super durable powder coated to not less than 60 micron thickness.

All aluminium sections shall present clear straight and sharply defined lines and shall be free from defects and imperfections that may impair their strength.

All screws, bolts and other necessary accessories shall be of aluminium or stainless steel or other non- corrodible material and shall match in colour and consistency of the finish of the anodization or the polyester powder coating or duranar coating as applicable.

Aluminum elastic glazing beads shall be provided to all windows and doors, which are assembled by pressure to fit with the relevant groove in the profile.

The glazing bars shall be threaded or interlaced at points of intersections and machine tenoned to frame.

1108.     Stainless Steel

Stainless steel sections, sheets and strips shall be of austenitic non-magnetic steels to BS 3100: 1991 and BS 1449:Part 2:1983: 18/10/3 chromium-nickel-molybdenum group, Grade 316 (marine grade) as detailed on drawings as applicable and as approved by the Engineer.

MANUFACTURE

1109.     General

The Contractor shall be responsible for the correctness and accuracy of the dimensions of the finished articles.

He shall carefully check the dimensions indicated on the Drawing, verify any changes, and ascertain the sizes at Site, which will enable him to prepare Final Working Drawings for fabrication and erection purposes. Such Drawings shall be submitted to the Engineer for his verification and approval.

Fabrication Orders can only be placed after the contractor has obtained in writing the approval of the

Engineer on the above Drawings.

The steel sections where specified to be factory rust-proofed shall be rust-proofed by hot dip galvanizing, metalizing or sheradizing process. The rust-proofing shall be sufficient to withstand the 72 hours salt-spray test as provided for in BS 7479:1991 If the rustproof coating suffers   any damage during the progress of work, the damaged part shall be recoated to a min. of the original thickness to the satisfaction of the Engineer.

1110.     Louvers, Sand-trap Louvers, Rails, Screens, etc.

Louvers, Sand-trap Louvers, Rails, Screens, etc.. with all necessary accessories and fitting shall be of the  pattern,  design,  dimensions  and  thicknesses shown  on  the  Drawings  and  obtained from  an approved manufacturer and shall comply with the following standards:

-      American Aluminum Associations (AA)

-      American Architectural Aluminum Manufacturer's Association

-      American Institute of Steel Construction (AISC)

-      American Iron and Steel Institute (AISI)

-      American National Standards Institute (ANSI)

-      American Society of Testing Materials (ASTM)

-      American Federal Specifications (FS)

-      American Insulating Glass Certification Council

-      American Flat Glass Marketing Association (FGMA)

1111.     Metal Louvers

Galvanized steel/Aluminum louvers shall be from a proprietary manufacturer and shall be to the Engineer's approval. The surface coating shall be as detailed on the drawings and or as specified herein to colours approved by the Engineer.

1112.     Powder Coating

Extrusions, cast Aluminum, sheet or plates, etc. where indicated on drawings shall be treated and provided with a pigmented organic durable powder coating and shall be applied in the factory to meet the performance requirements of AAMA 2604-98.

The coatings shall be as manufactured and applied by an applicator approved in writing by the coating manufacturer and under the coating manufacture’s direction. Colours and sheen shall be as indicated on drawings or as approved by the Engineer and shall be uniform with no variations detectable by the naked eye at a distance of 1.5 m or more.

Pre treatment of metal surfaces shall be done as per the written instruction and  recommendations of the manufacturer so as to provide the proper surface for applying the specified coating.

The coating shall be applied to a minimum thickness of 40 microns but not exceeding 120 microns and shall be stoved at 200o C for 10 minutes.

Material with damaged finish shall not be incorporated into the work. Damaged items shall be reprocessed by the applicator i.e. stripped, pre-treated and coated, or replaced unless specifically authorized by Engineer for localized repairs.

Warranty : The coating shall be warranted for a period of 10 years.   The contractor shall pass on executed copies of warranty for the above period signed and counter signed by the Contractor and the applicator against any defects in meta coating and workmanship and shall undertake to remove and replace the damaged work without any extra cost to the Client.

1113.    Aluminum

The Contractor shall furnish and install all aluminium units as indicated on the Drawings. Workmanship and installation shall be in accordance with recommended standards of first class Aluminum Manufacturers.

All aluminium work shall be performed in a shop where the grade of metalwork is of recognized quality acceptable to the Engineer. All items shall be installed plumb, straight, square, level and in proper elevation, plane location and alignment with other work. All work shall be designed for adjustment to field variations, fitted with proper joints and intersections, adequately anchored in place, strictly in accordance with best practice.

Where aluminium surfaces come in contact with metals other than stainless steel, zinc, white bronze or small areas of other metals compatible with aluminium surfaces, they shall be kept from direct contact with such parts by painting the dissimilar metal with a prime coat of zinc chromate primer or other suitable primer, followed by one or two coats of aluminium metal and masonry paint or other suitable protective coating, excluding those containing lead pigments, or a non-absorptive tape or gasket shall be placed between aluminium and dissimilar metals. Steel anchors and connecting members shall be hot dip galvanized or zinc plated after fabrication.

Aluminum surfaces in contact with lime mortar, concrete, plaster or other masonry materials,

shall be painted with alkaline- resistant coatings such as heavy-bodied bituminous paint or water- white methacrylate lacquer.

Aluminum in contact with wood or absorptive materials, which may become repeatedly wet shall be painted with two coats of aluminium metal and masonry paint or a coat of heavy-bodied bituminous

paint. Alternatively paint the wood or other absorptive material with two coats of aluminium house paint and seal joints with a good quality of caulking compound.

Where aluminium is in contact with treated wood, wood shall be treated with pentachlorophenol, 5% minimum concentration or approved equal, followed with the protective measures described for aluminium in contact with wood or other absorptive materials.

The aluminium work shall be designed and anchored so that the work will not be distorted nor the fasteners overstressed from the expansion and contraction of the metal.

Before shipment from factory, aluminium surfaces requiring protection shall be given a coating which will protect the metal during construction. In areas where appearance of the finish on aluminium items is important, a coating of methacrylate type lacquer shall be applied as specified hereinafter.

Apply two sprayed coats of water-white methacrylate lacquer having a total minimum thickness of 0.015 mm, which when applied to the aluminium surface shall be capable of withstanding the action of lime mortar for a period of at least one week in an atmosphere of 100% relative humidity at 40 degree centigrade, the action of 10% (by weight) muriatic acid for a period of six hours at 20 degree centigrade, and the action of atmospheric weathering for a period of 12 months. The coating shall be applied in the manufacturer's plant to the exposed surfaces of all aluminium components subject to staining from alkaline mortar and plaster, abrasion and other construction abuses. Before application of lacquer, the manufacturer shall remove all fabrication compounds, moisture, dirt, accumulations and other foreign materials to ensure proper lacquer adhesion.

Upon completion, the Contractor shall clean all aluminium work as required by removing protective tape or other coating, using mild soap or detergents and clear petroleum spirits.

Acids, caustics and abrasives shall not be used. Where cleaners are used to remove excess sealing compounds care shall be exercised to prevent damage to seals or staining or damage to adjacent work.

The Contractor shall be responsible for the protection of all aluminium work until the completion of the works, and only units in perfect working order and in perfect condition shall be accepted.

Structural Performance:

Design, engineer, fabricate and install the Aluminum works to withstand effects of the following:

-        Design Wind Velocity (wind resistance) as defined in British Standard CP3, Chapter V (1972)

of 120 kph.

-	Design wind pressure shall be calculated based on the above wind speed, height of the buildings, etc., acting inward and outward, normal to the plane of the wall.  When tested in accordance with ASTM E330, no material failures or permanent deformation of structural members shall occur.

Thermal Movements:

Shall be capable of withstanding thermal movements resulting from an ambient temperature differential of 50 degree C, without causing buckling, stresses on glass, failure of sealants, damaging loads on fasteners, or other detrimental effects.

Prints of shop Drawings for aluminium windows, doors, frames,  etc., showing the dimensions, sizes, thickness, materials, finishes, joining, attachments, fasteners and the relation to adjoining work, shall be submitted to the Engineer for approval before ordering any material. All work shall be fabricated and erected in accordance with the approved Drawings.

All aluminium windows, doors, frames, etc., shall be factory assembled and reinforced according to the Drawings, complete with hinges, glazing gaskets and anchors. The only Site work allowed on aluminium units is fixing in position and glazing. The finished surfaces shall present a clear surface free from alloy defects, scratches, or other surface blemishes.

All aluminium windows, doors, etc. shall be provided with all necessary Ironmongery required for its efficient functioning.

Handrails & Balusters

Handrails and guardrails shall be designed to withstand a simultaneous horizontally and vertical force of  not less than 75 kg/m, and a  single concentrated load of 100 kg, these loads not imposed simultaneously.

External handrails exposed to wind load shall be designed to permanently resist Design Wind Velocity (wind resistance) as defined in British Standard CP3, Chapter V (1972) of 160 kph and shall be calculated based on the wind speed, height of the buildings, etc., acting inward and outward, normal to the plane of the wall.

Intermediate rails (all those except the handrail), balusters, and panel filters shall be designed to withstand a horizontally applied normal load of 122 kg/m2  over their entire tributary area, including openings and space between rails.   Reactions due to this loading need not be superimposed with those of either preceding paragraphs.

Handrails and balustrades shall be fixed as indicated on drawings.

All fittings except bases shall be one piece extrusion machined to final shape. Castings and cast bases shall not be used.

All pipe cuts shall be square and accurate for minimum joint-gap.  Cut shall be clean and straight, free of “chamfer” from deburring, burs and nicks. All holes shall be drilled and countersunk the proper size, as required for a tight, flush fit of rivets. Where protection is applied for prevention of dissimilar materials electrolysis care shall be taken that non of the protective materials is visible when assembly is completed. All posts grouted in concrete must have one weep hole 6 mm diameter drill 13 mm to 19 mm above post collar, in place of rail.

The Contractor shall use all precautions necessary to protect the finish from scratches, nicks, gouges, dents etc., during storage, assembly and installation.

All surfaces components in contact with other materials and permanently exposed to moisture shall be painted with a coating of Zinc Chromate Primer to prevent contact between the two surfaces.  All shall be installed so that no drainage over them has previously been contaminated from copper, caustics or alkalis.

1114.     Steel Door Frames

Steel door frames shall be obtained from a specialist manufacturer in accordance with the ASTM E152 or BS 1245: 1986 and to the approval of the Engineer. Frames for fire rated doors shall be to fire ratings indicated on the drawings and in accordance with NFPA 80 or BS 476: Part 20: 1987, Part 22: 1987, Part 23: 1987 and Part 31.

Frames shall be 11 gauge (3mm) zinc-coated primed and finish cold rolled steel units with single, double or no rabbet as detailed on the drawings. The rabbet shall be designed to suit the size of the shutter thickness as detailed on drawings.

Frames shall be finished in self etch stoved primer compatible to the paint system specified for the doors and frames, ready to receive further coats and shall be reinforced and prepared for hinges, lock strike plates, etc. Frames shall be supplied with steel wall anchors for building into jambs.

It shall be the contactors responsibility to ensure that the appropriate primer compatible to the final paint system is applied as the place of manufacture of the door frames.

The Contractor shall submit shop drawings along with detailed catalogues for the approval of the Engineer before placing orders or commencing any work.

1115.     Steel Doors

Steel doors shutters shall be obtained from a specialist manufacturer with a proven record of at least 6 years and to the approval of the Engineer. Door shall comply with ASTM E152 or BS 6510.

Shutters shall be a reinforced double skin hollow shell construction of 14 gauge (2mm) zinc coated primed and finished cold rolled steel sheets, with internal reinforcing members fitted to incorporate and protect hardware items. Doors should not have visible seam on edges, and must have continuous reinforcing channel to full perimeter of doors inside. Doors shall be specially constructed with internal reinforcing members fitted to incorporate and protect hardware items. The doors shall be supplied self etch primed compatible to the paint system specified for the doors and frames, ready for installation and receiving further costs of paint.

It shall be the Contractors responsibility to ensure that the appropriate primer compatible to the final paint system is applied at the place of manufacture of the doors.

All steel doors shall be provided with a complete set of ironmongery commensurate with the intended use and efficient performance of the doors they are designed for and shall follow the type, design and material selected for the timber doors.

The Contractor shall submit shop drawings along with detailed catalogues for the approval of the Engineer before placing orders or commencing any work.

1116.     Cat Ladders

Cat ladders shall be fabricated either of stainless steel grade 316 or aluminum or galvanized steel as per Drawings & Bills of Quantities, anchored/fixed to walls as shown on drawings and to dimensions indicated therein.  Where indicated cat ladders shall be provided with protection cage to dimensions shown on drawings.  The Contractor shall be responsible to ensure that the sections and anchoring/ fixing are sufficient for the carrying a minimum load of 100 kg. With a factor of safety of three (3) Shop drawings indicating details of materials, fabrication including any surface treatment required, anchoring/fixing, etc., shall be submitted to the Engineer for approval before fabrication and placing orders.  Approval  accorded by  the  Engineer  shall  not  absolve  the  Contractor from  nay  of  his contractual obligations and responsibilities.

1117.     Recessed Access Panels

Recessed access panels shall be proprietary make from an approved manufacturer.  Access panels shall be to sizes shown on drawings. Exposed surfaces rear, sides and edges shall be epoxy painted as specified under painting to ferrous surfaces. Access panels shall be of the recessed type to receive the finishes of the walls in which they are placed.  The recess shall be appropriate to receive the finish.  Ironmongery shall include concealed hinges and budget lock.  The method of fixing shall be as recommended by the manufacturer and as approved by the Engineer.

1118.     Chequered Plate floors

Floors and trench to be provided with Chequered Plates shall match sizes indicated on drawings and to suit the site measurements.  Chequered Plate floors shall be galvanized steel plates (5 + 1 ½) cut ends  unless  otherwise indicated, and  shall  be  ground  to  a  smooth  finish  without  any  burs  or undulations. Key holes for lifting shall be provided at suitable intervals approved by the Engineer.  2 sets of keys shall be provided to the Engineer.

50 x 50 x 5mm mild steel angles with 8mm thick square bars welded to it to support the chequered plate to be flush with the surrounding finished surfaces shall be provided along the perimeter and cast into concrete with fish tail anchors welded to the angles. These shall also be galvanized.

Galvanization shall be carried out after all cutting, grinding, welding, etc., are completed. The Contractor shall submit shop drawings for the approval of the Engineer.

1119	Aluminium Windows and Doors

Extruded aluminum section 7000 shall be used to color approved by Engineer.

Aluminum sections shall be as per Engineer approval anodized to a minimum thickness of 25 microns or powder coated to a minimum thickness of 60 microns. The supplier must submit necessary evidence to the satisfaction of the Engineer that the thickness of coating meets the requirements.. In case of doubt the Engineer reserves the right to send sample pieces to independent testing laboratories, at the supplier's expense.

Glazing for doors and windows shall be as follows:

- For external windows (Sliding & Tilt & Turn)

Use Double Glazing

4 mm Float Glass for outer pane

6 mm Air Space

4 mm Float Glass for inner pane

- For Bath rooms Tilting Window

Use Single Glazing

4 mm wired glass

- For Detention Room fixed glass window

Use Single Glazing

6mm thick wired glass

- For Special windows (reception & pharmacy)

Use Single Glazing

6mm thick clear float glass

- All frames shall be made to fit the actual openings with a 5mm clearance all round. Discrepancies in overall width or height exceeding 5mm will not be allowed and the frames will be rejected in such cases. All small discrepancies shall have the gaps suitably backed and then filled with gun- applied mastic / sealant as approved by the Engineer.

- At all opening windows and doors and where there are louvred screens and doors a flyscreen shall be provided to the approval of the Engineer, constructed following the principles and specifications as described elsewhere in this Specification.

- Insect screens shall be in aluminium mesh, 18x16 meshes per inch.  The gap between the insect screen and the shutter shall be covered with an adaptor PVC section.

- For reference to window types see general arrangement drawings and elevations.

- Tolerances are to be approved by the Engineer before manufacture.

- All ironmongery which is to have the same finish as the frames it is to be installed on shall be approved by the Engineer.

- The Contractor shall provide shop drawings for aluminium windows and doors which shall be submitted in quadruplicate to the Engineer for approval.

- Approval by the Engineer of the shop drawings shall not relieve the Contractor of his responsibilities under the Contract.

- All assembly screws shall be in 18-8 stainless steel.

- Glazing sections shall be in special heat-resisting PVC and of channel type. Separate glazing sections on each side of the glass will not be permitted.

Sliding Windows and Doors

Weatherstripping - high density acrilan or wool weather - pile shall be used. There shall be double brushes at every contact between shutter and frame sections for complete insulation .These shall be present consistently throughout the unit between the inside and the outside and no portions without it are permitted .

The rollers for sliding shutters for windows and doors shall be of an adjustable type. The adjusting screws shall be accessible in the assembled state of the shutters and a vertical adjustment of 7mm shall be possible.

All sections for sliding windows and doors shall be of tubular shape and the cross sectional dimensions of same shall be not less than 60x 40 mm.

The outer frame must be suitable for accommodating sliding flyscreens as required or as directed by the Engineer.

The handle-latch set shall have all visible surfaces of anodized or powder coated aluminium or similar non-rusting material to Engineer approval. The handle shall have a proper grip. A small projecting flange or a recess in the shutter sections shall not be accepted to serve as a handle. The latching mechanism shall not be surface mounted but shall be concealed within the sections.

Side Hung Windows, Doors And Ventilators

All windows and doors shall be weatherstripped with heat resistant PVC sections. The weather fighting action shall be achieved by a positive compressive action against the PVC section and shall not depend on an external contact with the PVC section. At every contact between two profiles two weatherstipping sections shall be provided for complete weather protection.

The bottom sections of hinged doors shall be capable of being adjusted vertically if necessary. The gap between the bottom section and the floor shall be covered with a pair of special flay-type PVC sections.

The shutter sections for windows and doors shall be of tubular type and shall be of overall size 57x45mm for windows and overall size 81x45mm for doors (including flanges).

The shutters of the windows and doors shall be assembled with concealed corners of high rigidity. Hinges shall be concealed within the sections.

Hinges shall be in anodized or powder coated aluminium with stainless steel pins and nylon washers. Handles shall be in anodized or powder coated aluminium and mounted with self - lubricating nylon washers.

A mortice cylinder rim automatic deadlock of high quality with double pin tumbler shall be used.

Windows shall have anodized or powder coated aluminium handles and a latching mechanism securing the shutter to the frame both at the top and bottom.

Flyscreens

Flyscreens shall be fitted to all opening leaves of windows, consisting of a separate metal sub-frame filled in with flywire as previously described. The flyscreens shall be adequately secured with suitable clips, set screws or turn buckles and shall be removable for maintenace purposes. Flyscreen doors shall consist of similar sections to the metal casement doors and shall be fitted with removable panels of flywire, in a manner similar to that described for window flyscreens.

1120	Expansion Joint

The below sealant & trims shall be provided if indicated on drawings.

Joint Sealing

The Contractor shall ensure that joints are dry and shall remove all loose material, dust and grease.

Joints shall be prepared in accordance with sealant manufacturer's recommendations using recommended solvents and primers where necessary as approved by the Engineer.

Backing strips shall be inserted in all joints to be pointed with sealant.When using backing strips, the   contractor shall not leave gaps and shall not reduce depth of joint for sealant to less than the minimum recommended by the manufacturer.

The top 25mm portion of the joint shall be filled with a sealant (approved by Engineer) after priming concrete surface in contact with sealant.

Sealant shall be tooled to form a smooth flat bed.

Excess sealant shall be removed from adjoinig surfaces using cleaning materials recommended by the sealant manufacturer, and shall be left clean.

Joint Trims

The Contractor is to provide at all expansion joints in floors , roofs, ceilings , walls and columns with extruded aluminium expansion joint cover systems as appropriate and as shown on the Drawings and fixed in accordance with their printed instructions including all necessary components and fixings .

Floor joint covers shall be 2" deep. Butt joints within continuing runs shall be a maximum of 20 feet apart and will be sealed during installation.

Wall and ceiling joint covers shall be standard grey.

Transition pieced at changes of direction and at joints between horizontal and vertical joint covers shall be factory fabricated.

END OF SECTION