SECTION: 4

BLOCKWORK

1 		 Manufacture

Generally the blocks used shall be of local manufacture made with concrete in approved vibrated pressure machines. The fine aggregate to be used for blocks shall be clean and sharp approved sand. It shall be chemically and structurally stable and shall comply with the Table of Gradings given hereunder. The cement, coarse aggregate and water to be used for blocks shall comply with the requirements given for Concrete Works, and the methods of measuring and mixing the material shall be the same. The following Mixing Table shall be strictly adhered to in all cases.  Water/cement ratio shall be strictly governed to produce a mix of nil - slump.

Mixing Table

Nominal Mix (all by volume)

1 part Cement, 2 parts Fine Aggregate and 5 parts Coarse Aggregate

Table Of Grading

(a) Fine aggregate

BS 410 Sieve No. 	Approximate size: mm	Percentage (by weight) Passing BS sieve

-				10.00			100

-				5.00			90-100

7				2.36			75-100

14				1.18			55-90

25				0.60			35-59

52				0.30			8-30

100				0.15			0-10

b) Coarse aggregate 10mm single size aggregate.

The blocks shall be hard, sound, square and clean with sharp well defined arrises and shall, unless previously approved by the Engineer, be a work size of (400 x 200 x 200mm) with properly formed half blocks for bonding.

Hollow blocks, where required, shall be similar quality and overall size to solid blocks, and shall be of local manufacture made with concrete as described above in approved vibrated pressure machines. The design of the cavities and webs shall be submitted to the Engineer for approval before manufacture.  The thickness of the membranes or solid portions of hollow blocks shall be not less than (30 mm) each and the combined thickness of the solid portion shall exceed one third of the total thickness in either horizontal direction

(Light weight lime - blocks can be used according to drawings, bills of quantities and Engineer's approval)

Arrises shall be sharp and true; blocks which have damaged arrises are not to be used in the works and shall be discarded at the expense of the Contractor.

Immediately after moulding the blocks shall be placed on clean, level, non-absorbent pallets. Blocks shall not be removed from the pallets until inspected and approved by the Engineer. Blocks shall be cured by being kept thoroughly wet by means of water sprinklers or other approved means for a period determined by the Engineer but in all cases for not less than three days. Blocks must not be left on earth or sand during the curing process. Blocks shall be stacked in honeycomb fashion. Solid stacking will not be permitted.

The average crushing strength of solid or hollow blocks shall be not less than 35 kg/cm of gross area (average of 12 blocks).

2	Mortars

The sand to be used for mortar shall be clean and sharp. It shall be chemically and structurally stable and shall comply with the Table of Gradings below. The lime if used for mortar shall be hydrated lime complying with BS 890.

Where coloured mortars are required these shall be obtained either by the use of coloured cement or by addition of pigments complying with BS 1014.

The cement and water to be used for mortar shall comply with the requirements given under Concrete Works Section, and the methods of measuring and mixing shall be the same. The following Mixing Table shall be strictly adhered to in all cases.

Mixing Table

Nominal Mix	Cement Kilos	Sand m	Lime (Dry Hydrate) Kilos

1:4	360	1.00	as approved by the Engineer

Table Of Grading

BS 410 Sieve No.	Approximate Size: mm	Sand Passing Through Sieve: percentage

-				3				95-100

7				2.4				80-100

14				.2				60-100

25				0.6				30-100

52				0.3				5-65

100				0.15				0-15

200				0.08				0-5

Note: the above figures represent the limits of percentages (by weight) passing sieves of the sizes mentioned.

The mortar generally shall be cement and sand (1:4) mix.

Where plasticiser is added to the mortar the following mixes shall be used:

(a) Building mortar - cement and sand (1:6) and

(b) Mortar for pointing - cement and sand (according to plasticizer manufacturer

recommendation)

The plasticiser shall be used strictly in accordance with the manufacturer's instructions, and subject to the Engineer's approval.

All mortars shall be used before the initial set has begun. Mortar shall not be remixed after the initial set has taken place. The full description given under Plaster Work Section, shall apply also to the measuring, mixing etc. of mortar for blockwork.

3		Construction

All blockwork shall be set out and built to the dimensions shown on the Drawings.

Walls shall be carried up regularly without leaving any part more than one meter lower than another unless the permission of the Engineer is first obtained. Work which is left at different levels shall be racked back. In the case of cavity walls, both thicknesses shall not be carried up more than about 400 mm.

The courses of blockwork shall be properly leveled. The perpen-dicular joints shall be properly lined and quoins, jambs and other angles plumbed as the work proceeds.

All walls shall be thoroughly bonded in accordance with the best constructional practice and as directed by the Engineer. Broken blocks shall not be used except where required for bond (if approved by the Engineer).

All concrete blocks shall be soaked with water before being used and the tops of walls left off shall be wetted before work is resumed. The faces of walls shall be kept clean and free from mortar droppings and splashes

All blocks shall be properly spread with mortar before being laid and all joints shall be thoroughly flushed up solid through the full thickness of the wall at each course as the work proceeds.

For block walls the gauge shall be ten courses to 2100 mm.

Walls to be left unplastered shall have a fair face consisting of selected blocks pointed with a neat weathered or flush joint as the work proceeds using the same mortar mix as for jointing.

Walls to be plastered shall have the horizontal joints raked out to depth of 8 mm to form a key.

Blockwork shall be bonded to concrete columns and the like with 200 x 60 x 6 mm non ferrous metal ties cast in concrete and subsequently bent down, ragged and built into every 2 courses of blockwork. Gunning ties to concrete will not be permitted (other ways of bond must be approved by the Engineer).