SECTION: 5

ROOFING & INSULATION

1	Screeds

The provisions of Concrete Work section shall apply to the construction of solid reinforced concrete slab roofs and to hollow slab roofs. The actual finish will be specifically shown on the Drawings or in the Particular Specification.

Concrete screeds for obtaining falls shall be (1:3:6) mix.

All screeds shall be laid in bays not exceeding 10 square metres and formed between stop boards of the correct height and cut on each side to indicate the slope required in the roofing. The screed shall then be trowelled with a wooden float to true and accurate falls or cross falls up to the stop boards. A 10mm side gap shall be left between each screed bay for the full depth of the screed. The screeds shall be allowed to cure thoroughly to attain maximum shrinkage. Any cracks which appear due to shrinkage shall be made good. The gaps between bays shall then be filled in with cold bitumen.

Where the roof screeds are to be reinforced with one layer of galvanised wire mesh, this shall be supported on top of the base on spacers to ensure that it is maintained at between 10mm and 15mm below the top of the finished screeds. It shall be at least 100mm wide, securely wired together. It shall be stopped 20mm from the edge of each bay.

2	APP Water Proofing Membrane

The waterproofing membrane for protection of concrete roofs shall be 4 mm thick, reinforced with 180 gm/m2 of non woven polyester inlay and modified bituminous compound presenting high thermal stability, plasticity and flexibility characteristics as detailed on drawings and as specified in this Section. The thickness of the membrane shall be 4 mm as specified and indicated on drawings.

The typical characteristics of a 4 mm thick membrane when tested according to ASTM D 5147 shall be as follows:

| Tests | Unit | Required Val. | Tolerance |
| --- | --- | --- | --- |
| Thickness | mm | 4 | ± 5% |
| Aeric Mass | Kg/m | 4.6 | ±10% |
| Tensile strength; Long Tranv | N/5 cm N/5 cm | 800 650 | ±20% ±20% |
| Lap joint strength; Long Tranv | N/5 cm N/5 cm | 900 700 | ±20% ±20% |
| Elongation at break; Long Tranv | % % | 35 40 | ±15% ±15% |
| Cold Bending | 0C | -50 | < -5 |
| Form Stability | 0C | 100 | >100 |
| Water pressure resistance (DIN 16935) | KPa | No leakage at 1000 mm water head/24 hrs. | < 1000 |
| Softening point (ASTM D36) | 0C | 150 | <150 |
| Down penetration 250C (ASTM D5) | dmm | 25 | ±5 |

Top surface should have a layer of medium size white aggregates (2-3mm)

Applying asphalt sheets should be made according to the manufacturer instructions.

Top surface of screeds should be cleaned and a suitable prime should be sprayed before  using asphalt sheets.

An overlap of 15-20cm should be made on sheets.

Sheets should have at least 15cm vertical edges, all around the roof (a special groove should be made in the roof parapet to erect the vertical side of the sheets)

During erecting asphalt sheets, contractor should prevent air pockets entrained under  the sheets, which will be full flame applied.

4	Expansion Joints

The expansion joints, if any, shall generally be of 10mm thick fibreboard impregnated with bitumen accurately cut, with butt joints and fixed vertical and straight .The top 10mm of the joint shall be filled with a grey polyurethane gun grade sealant which confirms with BS 4254.

Expansion joints shall continue into the tilted tile, skirtings and fillets.

5	Completion

On completion of roofing works, the roof shall be tested for water leakage by immersing the surface with water and leaving it for 48 hours. If leakage is detected, the Contractor shall do the necessary repairs to the satisfaction of the Engineer and the test repeated.

5	Warrantee

The Contractor shall submit to the Engineer a guarantee stating that all Works of waterproofing system have been carried out in accordance with the drawings and specifications and shall be guaranteed free from defects in material and workmanship and shall be leak-proof for a period of ten (10) years from the date of issuance of the completion certificate.  The Contractor shall agree to repair (including any replacement of materials) any leaks resulting from defective materials or workmanship during the guarantee period at no additional cost to the Client.