SECTION: 7

TILING WORKS

1	General

The British Standards (BS) governs the work covered in this section.

2	Materials

Portland cement, fine aggregate and water shall be as previously specified in Concrete Work section.

The marble chipping shall be of an approved quality in irregular pieces varying from 2 mm to 10 mm in size depending on the effect required. The pieces should preferably be roughly cubical in shape where flaky shaped pieces shall not be used.

The granite chipping shall be of an approved quality graded from 12 mm down with not more than 5 percent fine material passing a No.100 sieve.

Marble and granite aggregates shall comply generally with the Table of Grading. In connection with marble aggregates the percentages are approximate only. The actual grading should be selected to produce the surface effects required.

Table of Grading

BS 410 Sieve No.         Approximate Size mm	% of Aggregate Passing Through

GRANITE             MARBLE

-			13		100			-

-			10		95-100			95-100

-			5		30-60			25-60

7			2.4		20-50			5-30

14			1.2		15-40			0-10

25			0.6		10-30			-

59			0.3		5-15			-

100			0.15		0-5			-

NOTE: the above figures represent the limits of percentages (by weight) passing sieves of the sizes mentioned.

3	Cement and Sand Tiles

Cement and sand tiles shall be formed with a (1:2) mix of white or coloured cement, or in white cement with a colour pigment added , and sand applied as a facing not less than 7.5mm thick to a Portland cement and sand (1:5) mix backing .

The tiles shall be cast in heavy moulds under pressure to the proportions and sizes shown in the following table.

Cement and Sand Tile Dimensions

Size  mm	Size tolerances  mm	Minimum total thickness mm

200x200	 	0.5			20

250x250	 	0.5			25

300x300	  	1.0			25

400x400	 	1.0			30

Coloured cement and sand skirting to match tiles; 100mm or 200mm with chamfered top edges shall be produced in the same way as the tiles using the same mixes.

All cement and sand tiles shall be cured by totally immersing them, after the initial set has taken place, in a tank of clean water for at least 24 hours.

Cement and sand tiles shall be laid and bedded direct onto a concrete sub-floor on a cement and sand (1:4) mix screed. This screed shall be 25mm thick in the case of 25mm tiles and 30mm thick in the case of 20mm tiles. The total thickness of cement and sand screed and tiles shall not exceed 50mm.  All tiles shall be laid with square joints.

All tiling shall be grouted up on completion, care being taken to fill all joints completely. The grout shall consist of neat cement of a colour to match the tiling.  Any surplus grout shall be cleaned off the face of the tiling and surrounding surfaces immediately and all tiling shall be carefully cleaned off.

4	Terrazzo Tiles

Terrazzo tiles shall be formed with a (1:2 1/2) mix of white or coloured cement or white cement with a colour pigment added and granular marble chippings applied as a facing not less than 5 mm thick to a Portland cement and sand (1:5)) mix backing .

The tiles shall be cast in heavy metal moulds under pressure to the proportions and sizes shown in the following table.

Terrazzo Tile Dimensions

Size  mm	Size tolerances  mm	Minimum total thickness mm

200x200	  	0.5			20

250x250	 	0.5			25

300x300	  	1.0			25

400x400	  	1.0			30

Tiles shall be cured as for cement and sand tiles and then ground, filled and polished before distribution to site.

Grinding shall be done wet by means of a No. 80 carborundum stone. Filling shall be carried out with a neat cement grout of the same colour as the facing mix and this shall be worked into the surface with a wooden shaper to fill all voids and air holes.

Surplus grout shall be removed with a dry cloth. After a minimum period of 24 hours polishing shall be carried out wet by means of a No. 140 carborundum stone.

Terrazzo skirtings 100mm or 200mm high with chamfered top edges shall be produced in the same way as for tiles using the same mixes.

Terrazzo tiles shall be laid and bedded direct onto a sand layer with a cement and sand (1:4) mix mortar. This mortar shall be 25mm thick in the case of 25mm tiles and 30mm thick in the case of 20mm tiles. The total thickness of the cement and sand screed and tiles shall not exceed 50 mm.

All tiling shall be grouted up on completion; care being taken to fill all joints completely.  The grout shall consist of neat cement of a colour to match the tiling.  Any surplus grout shall be cleaned off the face of the tiling and surrounding surfaces immediately and all tiling shall be carefully cleaned off.

All terrazzo surfaces shall be polished on completion. Large areas such as floors shall be wet polished by means of approved machines using No. 140 carborundum wheel.  Any surface too small for convenient machine polishing may be polished by hand using a No.140 carborundum stone and water  Care must be taken during any polishing operation not to damage any of angles or arrises .

Terrazzo covering to items such as sills , treads and risers to steps , skirtings etc. , shall generally be applied in accordance with theforegoing specification except that the  thickness of the facing shall be at least 10 mm ( marble can be used if approved by the Engineer ) .

5	Marble or Granite Floorings

Marble flooring shall generally be 30 mm thick and the size, type and pattern shall be as stated in the Particular Specification and/or shown on the Drawings.  The marble slabs shall be fixed solid on a bed of cement and sand (1:4) mix 30 mm thick with tight joints grouted in lime putty . A protective slurry of lime putty at least 3 mm thick shall be applied to the marble pavings and subsequently cleaned off.

Treads shall be 30mm thick fixed solid on a bed of cement and sand (1:4) mix 30mm thick. Risers to stairs shall be 20mm thick fixed solid on a backing of cement and sand (1:4) mix 30 mm thick.  Window sills shall be 40mm thick bedded hollow on 	plaster slabs. Skirtings shall be 10mm thick , in lengths of about 1.5 meters , fixed solid on a backing of cement and to coincide with joints in adjacent pavings .  Rounded arrises, nosing and moldings shall be adequately protected by means of timber casings.  Treads, risers, skirtings and window sills shall be grouted and protected in a manner similar to pavings.

The exposed faces and edges of all marble shall be polished smooth and be free from scratches or other defects.  Concealed faces of marble shall be treated with shellac or bituminous paint.

6 	Marble Lining

Marble lining to walls, columns and the like shall generally be 20 mm thick and the size, type and pattern shall be as stated in the Particular Specifications and/or as shown on the drawings.

The marble slabs shall be cut square and true and shall be uniform in shape and thickness. Patterns and mouldings shall be accurately formed in accordance with the Drawings.

Exposed edges and mouldings shall be protected by means of timber casing or lime putty coating. The exposed edges and faces of all marble shall be polished smooth and shall be free from scratches or other defects.

7 	Ceramic Floor Tiling

Ceramic floor tiles shall be matt finish, vitrified plain clay tiles manufactured in accordance with BS 6431. Skirtings shall be coved edge type 80-100 mm high. Acid resistant tiles shall be used where specified. Tile pattern and colour shall be to the Engineer's approval. The tile sizes and make shall be as detailed on drawings.

Water absorption according to ASTM C373 shall be less than 3% and coefficient of friction according to ASTM C-1028 greater than 0.6.

The tiles shall be true to shape, flat and free from flaws, cracks and crazing and keyed on the reverse side and shall be of amanufacture approved by the Engineer.

Bedding mortar shall be cement and sand all in accordance with the materials stated in Concrete Work and Blockwork sections.

Any admixtures to the mortar must be approved before use.

Grout pointing shall be white or coloured cement.

Cement and sand mortar bed of not more than 20 mm or thickness of the tile shall be laid.

Tiles shall be firmly tamped into mortar to form a level surface.

The Contractor shall ensure that when fixing tiles with thin bed adhesive, the base to receive tiles is clean, level and dry, with no loose and friable areas and surface dusting.

Cement-based adhesive shall be prepared and used in accordance with the manufacturer's recommendations to form a bed not more than 3 mm thick.

Tiles shall be laid dry and tamped well down into the adhesive to ensure a proper bond with base and a level surface.

When bedding tiles on thick bed, semi-dry cement and sand (1:4) mortar bed shall be spread not less than 25 mm thick.

Before the compacted bed has set a cement and sand slurry (1:1) about 3mm thick shall be spread over the surface.

The tiles shall be laid dry and tamped into the slurry to form a level surface.

Joints shall be even and not more than 3mm wide, in both directions.

Joints shall be continuous both horizontally and vertically.

The tiles shall be grouted up with white or coloured cement mortar (1:1) worked well into joints when bed is sufficiently firm to prevent disturbances of the tiles; surplus grout shall be cleaned off from faces of tiles.

Movement joints shall be provided not less than 6 mm wide where shown on the Drawings or as directed by the Engineer.

Movement joints shall be carried through the depth of tile and bedding and partially filled with filling strip and finished flush with sealant to manufacturer's recommendations.

Where tiling abuts against wood or metal frames or other tiling at angles and around pipes etc. , it shall be carefully cut and fitted to form a close neat joint .  Open irregular joints filled with cement and sand or plaster will not be permitted.

Tiles shall be cleaned off and polished at completion.

Water shall not be allowed on new tiling until bedding and grouting have completely set.

No traffic shall be allowed on the floor until 4 days after completion and then only light traffic for a further 10 days.

8 	Porcelain Floor Tiling

Porcelain tiles shall be colored non- slip, square edges, of approved thickness; smooth surface; unglazed, manufactured in accordance with BS 6431. Skirting shall be coved edge type where requested, 100 mm high. Acid resistant tiles shall be used where specified. Tile pattern and color shall be to the Engineer's approval. The tile sizes and make shall be as detailed on drawings.

Tiles shall be made of Sandwich obtained by overlapping two Laminam 3mm slabs with intermediate fiberglass blanket. Nominal overall thickness 7 mm and Weight: 15 kg/sqm

Water absorption according to ASTM C373 shall be average value 0.1% (< 0.3%) and coefficient of friction according to ASTM C-1028 greater than 0.6.

9	Glazed Ceramic Wall Tiling

Glazed ceramic wall tiles shall conform to the requirements of BS 6431 and the size shall be as shown in the Drawings and of an approved pattern and colour. Single edge and double edge rounded tiles, coves and corner pieces shall be of the same quality, colour, and finish. The tile sizes and make shall be as detailed on drawings.

The tiles shall be true to shape, flat and free form flaws, cracks and crazing and keyed on the reverse side and shall be of a manufacture approved by the Engineer.

Bedding mortar shall be cement and sand (1:3) all in accordance with the materials stated in Concrete Work and Blockwork sections

Any admixtures to the mortar must be approved before use.

Mastic adhesives shall be of an approved manufacture and shall comply with the performance requirements of CP 212: Part 1, if approved by the Engineer.

Grout pointing shall be neat white or coloured cement.

The Contractor shall ensure that the cement render backing is at least 14 days old, firmly bonded to its background, free from dust, with surfaces plumb and true to 3mm in any 1800 mm.

Fixing Tiles with Cement and Sand Mortar

The tiles shall be immersed in water for 6 hours or until saturated then stacked tightly together to drain with end tiles turned glaze outwards. Tiles shall be fixed as soon as surface water has drained.

The render coat shall be wetted sufficiently to prevent it absorbing water from the bedding coat.

Mortar bedding shall be applied to render background to an even thickness of approximately 10mm.

Each tile shall be buttered evenly with mortar and tapped firmly into position so that the bed is solid throughout.

Thickness of finished bed shall be not less than 6mm or more than 12 mm.

Any necessary adjustment to tiles shall be made within ten minutes of fixing and tiles cleaned off after not less than two hours.

Fixing Tiles with Adhesive

The tiles shall be fixed in accordance with the recommendations of the adhesive manufacturer.

Adhesive shall be applied as a continuous screed to a thickness of approximately 3mm on the surface to be tiled.

Dry tiles shall be pressed on to the adhesive and tapped firmly into position to ensure solid bedding without voids.

Any necessary adjustment to tiles shall be made immediately after bedding.

Tiles shall be cleaned off as soon as bedding is complete.

Joints shall be even and not more than 2mm wide using spacer lug tiles or spacer pegs.

Joints shall be continuous both horizontally and vertically.

Tiles shall be fixed to a finished surface that is plumb and true to 2mm in any 2m.

Joints shall be grouted up not less than 24 hours after fixing tiles to porous surfaces and not less than 3 days after fixing to impervious surfaces.

Tiles shall be grouted by pressing mix firmly into joints, working in areas of not more than 1sq.m.

Surplus grout shall be cleaned off as the work proceeds.

Where tiling abuts against wood or metal frames or other tiling at angles and around pipes etc..., it shall be carefully cut and fitted to form a close neat joint .   Open irregular joints filled with cement and sand or plaster will not be permitted.

Tiles shall be cleaned off and polished on completion.

External tiling shall be protected from inclement weather until grouting is completely set.

No water is to be allowed on new tiling until bedding and grouting have completely set.

10	Precast Concrete Tiles

Tiles shall be laid in accordance with BS 5385: Part 5: 1990, BS 8204: Part 4: 1993 and/or BS 8000: Section 11.1: 1989 as applicable and as directed by the Engineer. Tiles shall be laid on a (1:3) mix of cement and sand mortar and any admixtures approved by the Engineer. The finished floor level shall be maintained as indicated on drawings by providing an approved sand layer of required thickness.

All tiles shall be laid with square joints and shall be grouted up on completion, care being taken to fill all joints completely.

The grout shall consist of neat cement of a color to match the tiling. Any surplus grout shall be cleaned off the face of the tiling and surrounding surfaces immediately and all tiling shall be carefully cleaned off.

Tiles shall be cut with a suitable cutting tool and rough edges shall be rubbed smooth. Cut-tile misfits shall be replaced with properly cut tiles. Straight edges shall be accurately set to the lines established and reset at suitable intervals to keep the joints parallel over the entire area.

Broken tiles or tiles showing the least signs of defects will not be accepted and if laid by the Contractor shall be removed and replaced with sound tiles, at his own expense.

Tiles shall be laid out from the centre line of each space outward and adjustment made along walls, partitions, and borders, so as to symmetrize the pattern with a minimum of cut tiles. Tiles of less than half of their full size along one side after cutting should be avoided.

11	Interlock Paving Tiles

Interlock paving tiles shall consist of precast concrete blocks on a sand laying course laid on a 100 mm or 150 mm sub-base as shown on the drawings, laid on subgrade. In general blocks should conform to the requirements of the Specification for Precast Concrete Paving Blocks as per B.S.6717.

The laying course shall consist of washed sand with a particle size of 0-5 mm containing not more than 3% silt plus clay by weight. The sand shall be obtained from a single source, allowed to drain before use and shall be covered with suitable sheeting to minimize moisture changes.

Sub-base shall be 100 mm or 150 mm thick and shall be laid in accordance with Aggregate Road Base specification. The material used in any instance shall be as shown on the drawings.

Curbstone in the shape and color approved by Engineer shall be installed at the edges of interlock sidewalks/pavements.

All Local authorities/ Municipalities requirements with regard to pavement width, color, level. .etc. shall be met by Contractor..

Interlock tiles strength shall be as per British standards (Minimum strength is 49 N/mm2 to comply with BS 6717).

Cement content shall not be less than 400Kg/m3 of concrete.

Shapes and colors of the interlock tiles samples are to be approved by the engineer before supply and installation.

Spaces between interlock tiles should be filled with clean white sand and compacted with plate compactor as required.

Interlock tiles samples are to be approved by the engineer before supply and installing.

12	Protection

All floor, wall and ceiling finishes shall be protected from damage during subsequent work, and shall be thoroughly cleaned before handing over the works.