SECTION: 3

CONCRETE WORK

1	   General

All materials shall be subject to such tests as the Engineer may direct and provision for such tests shall be included in the price for such materials inserted in the Bill of Quantities or Schedule of Rates unless otherwise provided for. In case such tests required by the Engineer, an independent and officially authorized lab shall carry out such tests and sampling.

Properly representative samples of all materials to be used in the works shall be submitted by the Contractor for the Engineer's approval when required.

Where tests are required by the Engineer, the Contractor shall take samples and send to a firm experienced in analysis of the material. Reports shall be submitted to the Engineer. The Contractor shall bear all expenses consequent to the provision, taking and cartage, etc. of samples, in addition to the costs of performing the tests and reporting the results.

The Engineer reserves the right to reject any material which, in his opinion is objectionable in any respect, not withstanding its apparent compliance with the relevant Standards. Any such rejected material shall be removed from the site at the Contractor's expense at once.

2		Formwork for Concrete

The Contractor shall supply, design, erect, strike and remove the formwork and be entirely responsible for its stability and safety so that it will carry the fresh concrete and all incidental loadings and preserve it from damage and distortion during its placing, vibration, ramming, setting and curing. It shall be so constructed as to leave the finished concrete to the dimensions shown on the Drawings and of a material capable of providing the surface finish specified. In any event, the maximum permissible deflection under all loads shall not exceed 2mm or 1/600 of the free span, whichever is less.

Formwork shall be of timber and / or metal and shall include all temporary concrete moulds and their supports. Bolts to be used for fixing the formwork shall be approved by the Engineer before staring the work.

For concrete surfaces which are to remain exposed wrought formwork shall be used. Wrought formwork shall be of timber or steel framing lined with 12mm thick smooth-faced plywood or an equal lining approved by the Engineer, or of metal, suitable to obtain a fair face finish on the concrete. All external angles or fair faced in-situ concrete shall have chamfers formed with 15x15mm (5/8"x5/8") wrought hardwood angle fillets planted in the angles of the formwork, unless larger chamfers are shown on the drawings.

Water tanks formwork shall be constructed and faced with plywood or other approved material to give a smooth surface free from all irregularities. Special water tight ties with an internal water barrier ring and end cones shall be used. Ties location shall carefully studied to give an appropriate seen after formwork dismantling.

Formwork ready to receive concrete shall be thoroughly clean and the internal faces properly painted with an approved shutter oil or other preparation.  Joints shall be tight to prevent leakage.

Wherever required and prior to placing of the reinforcement the internal surfaces of all formwork shall be treated with an approved mould oil.

All formwork shall be inspected and approved by the Engineer prior to concreting. This approval, however, does not relieve the Contractor of any of his responsibilities.

The striking of all formwork shall be carried out with the greatest of care to avoid damage to concrete.

The formwork to vertical surfaces such as walls, columns and sides of beams may be removed in accordance with the table below although care must be taken to avoid damage to the concrete, especially to arises and features.

Minimum periods in days for striking other formwork should be in accordance with the following table, or as directed by the Engineer

Ordinary Portland Cement

Concrete

-Slabs				  	    3

(props left under)

-Beam soffits				    7

(props left under)

-Props to slabs				    7

-Props to beams				    16

-Vertical surfaces

walls, columns and sides of beams  	    1

Formwork, shuttering, props, or any other means   of temporary or semi-permanent support shall not be removed from the concrete until the concrete is sufficiently strong to carry safely the load (dead and temporary).

The Contractor shall inform the Engineer when he is ready to strike the formwork, or remove any form of temporary support, and shall obtain his written consent before proceeding.

The times given for the removal of props are based on the assumption that the total live plus dead weight to be supported at the time of removal is not more than one half of the total design load .

For horizontal members where the loading is to be a higher proportion of the total design load these times may need to be increased.

The Contractor shall be responsible for any damage to the concrete work caused by or arising from the removal and striking of the forms and supports any advice, permission or approval by the Engineer relative to the removal and striking of forms and supports shall not relieve the Contractor from this responsibility.

Any work showing signs of damage through premature loading is to be entirely reconstructed at the Contractor's expense.

The Contractor shall confirm positions and details of all

(a)  Permanent fixings

(b)  Pipes and conduit

(c)  Holes and chases

to ensure that alterations are not made without the knowledge and approval of the Engineer.

The Contractor shall fix inserts or box out as required to correct positions before placing

concrete, and shall form all holes and chases.  He shall not cut hardened concrete without

approval.

3	Reinforcement for Concrete

Steel reinforcement shall generally be hot rolled mild, medium or high yield steel smooth round or deformed bars complying with BS 4449 or similar approved standard.

In case any other type of reinforcement is required, it shall comply with the requirements of the Particular Specification.

All reinforcement shall be free from rust and mill scale and any coating such as oil, clay, paint etc which might impair the bond with the concrete.

Manufacturer's test certificates for all classes of reinforcement shall be supplied when required.  Specimens sufficient for three tensile tests and three cold-bending tests per ten tons of bars or fraction thereof and for each different size of bar shall be sampled under the supervision of the Engineer. Testing shall be in accordance with BS 4449 or other approved standard and batches shall be rejected if the average results for each batch are not in accordance with the specification. All tests should be made on the Contractor's expense.

All steel is to be totally free from dirt, paint, loose rust or scale when in position ready for concreting.

The Contractor shall cut and bend bars to BS 4466 and to schedule provided unless otherwise instructed by the Engineer.

Straight sections of bars must be kept out of winding. The internal radius of bends shall in no case be less than four times the diameter of the bar, except for stirrups, column binders, and wall shear bars which are to be bent to fit closely around the main bars.

Great care is to be taken to bend stirrups and columns binders separately and to the sizes shown.

All bars will be cut and bent cold using approved machines.

Lengthening of bars by welding, and rebending of incorrectly bent bars will not be permitted, except where requested by the Engineer.

The Contractor shall provide on site facilities for hand bending to deal with minor adjustments.

Unless otherwise allowed for in the particular specification splices in reinforcing bars shall be formed by lapping. Such laps in bars in any member shall be staggered. Except as otherwise indicated on the drawings the minimum overlap of lapped splices shall be 50 bar diameters or 400mm whichever is greater.

The steel is to be fixed in position exactly as indicated, and the bars are to be securely wired together with 1.6 or 1.4mm soft iron wire or approved spring steel clips wherever necessary to prevent any displacement during concreting.

Plastic or Concrete Spacers (as per Engineer Approval), chairs and the like, temporary or permanent, are to be used as required to ensure that the steel has the exact amount of cover indicated. No permanent spacers may show on a surface where a fair faced concrete finish or a brushed aggregate finish are required.  Type of spacers shall be approved by the Engineer before starting the work.

Unless otherwise indicated, the minimum cover to the reinforcing bars is to be as listed below or equal to the diameter of the bar, whichever is greater.

Position					        Minimum cover - mm

-Main bars in internal faces of

columns and beams				       25

-Main bars in external faces of

columns and beams				       30

-Main bars in floor slabs and

soffits of roof slabs				       20

-Main bars in top of roof slabs			       20

-Outermost bars in internal faces

of walls					                    20

-Outermost bars in external faces of

of walls					               25

-Bars in top of ground slabs      			 20

-Bars near faces in contact with soil			 40

The placing of all reinforcement will be checked by the Engineer and in no case is concrete to be poured around any steel that has not been passed by him. The Contractor is to ensure that no steel is displaced from its position during the placement of concrete and until the concrete is set.

The insertion of bars into or removal of bars from concrete already placed will not be permitted. Reinforcement temporarily left projecting from the concrete at the joints shall not be bent without the prior approval of the Engineer.

Secondary reinforced concrete members for which no reinforcement details are given in the drawings or the Particular Specifications shall have a minimum ratio of reinforcement area to concrete area of 0.33 %.

4	Concreting

Cement

The cement used for all reinforced concrete in contact with earth shall be sulphate resistant type-V with C3A content ratio less than 5%.

The cement used superstructure reinforced concrete shall be Portland Cement conforming in all respects to ASTM Standard Specification C150, type 1, or to BS 12, unless otherwise required, bags shall contain 50kg net + 1%.

If cements other than the above are required they shall be covered fully by the Particular Specification.

The Contractor shall at all times furnish the Manufacturer's statement of the above Standard Specifications together with the 	date of manufacture, certified by an independent agency in the country of origin approved by the Engineer.

The cement shall be delivered to the site by the Contractor in the original sealed and branded bags or containers of the 	manufacturer in batches not exceeding 100 tons and shall be stored in a proper manner off the ground to prevent deterioration. Each batch shall be stacked separately and used in the order of delivery.  No cement shall be used which has been manufactured more than twelve months prior to its proposed use on site.

All cements whether stored in bulk, bags, or containers in warehouses or on site shall be

sampled for testing according to ASTM C183 (Methods of Sampling Hydraulic Cements). Test samples over and above those specified shall be taken at any time 	if so requested by the Engineer. Testing of cement shall be in accordance with the methods required by ASTM C150 and C175 or BS 12 or any other accepted by the Engineer.

Aggregates

This specification covers fine and coarse aggregates other than lightweight aggregates for use in the production of concrete.

When lightweight aggregates are required they shall be defined in the Particular Specification.

The aggregates shall be crushed gravel or stone and shall comply with BS 882 for graded or single size aggregate and shall be obtained from any quarry in the mountains approved by the Engineer. For convenience part of Clause 5 of BS 882 (grading) including Tables 1, 2 and 3 are reproduced herein.

Coarse aggregate: the grading of coarse aggregate, when analyzed by the method given for sieve analysis in BS 812 shall be within the limits given in Table 1.

Fine aggregate: the grading of a fine aggregate, when analyzed by the method of sieve analysis described in BS 812, shall be within the limits of one of the grading zones given in Table 2, except that a total tolerance of up to 5 per cent may be applied to the percentages under-lined. This tolerance may be split up; for example, it could be 1 per cent on each of three sieves and 2 per cent on another, or 4 per cent on one sieve and 1 per cent on another.

The fine aggregate shall be described as fine aggregate of the 	grading zone into which it falls, e.g. BS 882, Grading Zone 1.

NOTE:  It is intended that individual zones should not be specified in contract documents relating to concrete but that the concrete mixes should be modified to make the best use of the materials readily available.

If approved by the Engineer. Single-sized aggregate to BS 882 Table 1 may only be used for reinforced concrete when combined 	in two or more sizes to provide a well-graded mixture approved by the Engineer.

Sampling and testing of aggregates shall be as required by BS 882 and in accordance with BS 812 'Methods for Sampling and Testing

of Mineral Aggregates , Sands and Fillers' .  All sampling shall be done by or under the supervision of the Engineer.

The combined percentage of sulphates and chlorides by weight in coarse and fine aggregates shall not exceed 0.05 per cent (500ppm) of the combined weight of total aggregates.

Just before use the aggregate will be washed down with potable water to reduce the content of sulphates, chlorides and other extraneous material.

Table 1: Coarse Aggregate

| BS 410 | Percentage by weight passing BS sieves |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Test Sieve | Nominal size of Graded aggregate |  | Nominal size of Single-sized aggregate |  |  |  |  |  |
| mm | 400mm to 5mm | 200mm to 5mm | 14mm to 5mm | 63mm | 40mm | 20mm | 14mm | 14mm |
| 75.0 | 100 | - | - | 100 | - | - | - | - |
| 63.0 | - | - | - | 85-100 | 100 | - | - | - |
| 37.5 | 95-100 | 100 | - | 0-30 | 85-100 | 100 | - | - |
| 20.0 | 35-70 | 95-100 | 100 | 0-5 | 0-25 | 85-100 | 100 | - |
| 14.0 | - | - | 90-100 | - | - | 0 | 85-100 | 100 |
| 10.0 | 10-40 | 30-60 | 50-85 | - | 0-5 | 0-25 | 0-50 | 85-100 |
| 5.0 | 0-5 | 0-10 | 0-10 | - | - | 0-5 | 0-10 | 0-25 |
| 2.36 | - | - | - | - | - | - | - | 0-25 |

Table 2: Fine Aggregate

| BS 410 Test Sieve | Percentage by weight passing BS sieves |  |  |  |
| --- | --- | --- | --- | --- |
|  | Grading Zone 1 | Grading Zone 2 | Grading Zone 3 | Grading Zone 4 |
| mm |  |  |  |  |
| 10.00 | 100 | 100 | 100 | 100 |
| 5.00 | 90-100 | 90-100 | 90-100 | 95-100 |
| 2.36 | 60-95 | 75-100 | 85-100 | 95-100 |
| 1.18 | 30-70 | 55-90 | 75-100 | 90-100 |
| microns |  |  |  |  |
| 600 | 15-34 | 35-59 | 60-79 | 80-100 |
| 300 | 5-20 | 8-30 | 12-40 | 15-50 |
| 150 | 0-10 | 0-10 | 0-10 | 0-15 |

Handling Aggregates

The choice and preparation of sites for stockpiling of aggregates, the number and sizes of stockpiles and the methods adopted to prevent segregation of component sizes shall be agreed with the Engineer.

Coarse aggregate shall be stockpiled in three separate gradings: 38-19mm, 19-10mm, 10-5mm. When aggregates of different gradings are stockpiled close together the stockpiles shall be separated by bulkheads.

Stockpiles are to be on concrete or other hard surface sufficiently sloped so that water is not retained in the base of the stockpiles.

All aggregates are to be handled from the stockpile in such a 	manner as to secure a typical grading of the material, care being taken to avoid crushing the aggregates and contamination with extraneous matter.

Aggregates need not be stockpiled when a crushing-screening plant is used in tandem with a batching plant properly equipped with several bins for different sized aggregates having the appropriate weighing scales at such bin such that a mix of the desired gradation is obtained consistently and the whole operation is conducted to the satisfaction of the Engineer.

Water

Unless otherwise authorized in writing by the Engineer, only water from potable supply system may be used for mixing concrete and other products containing cement.

Similarly only potable water may be used for curing concrete and cement products during the first 24 hours after pouring. Later, fresh water, or other water containing not more than 4750 ppm dissolved solids of which not more than 1000 ppm may be chlorides, may be used for curing.

No additives of any kind shall be used in the concrete without the express approval in writing of the Engineer.

Quality of Concrete

Concrete shall be a mixture of cement.  Aggregates and water as covered respectively by 4.01 to 4.23 above.

Where air-entrainment is required, the method to be used shall be specified in the Particular Specification.

The mix proportions, workability and strengths of the various types of concrete shall conform to Table 4.

The terms contained in Table 4 are defined as follows: WATER/CEMENT RATIO: the term water/cement ratio means the ratio by weight of the water to the cement in the mix, 	expressed as a decimal fraction. The water is that which is free to combine with the cement in the mix.

This includes free water in the aggregate but excludes water absorbed or to be absorbed 	by the aggregate. The aggregate for this purpose shall be taken in a saturated surface-dry condition.

The absorption of the aggregates shall be determined in accordance with Section 4 of BS 812 or any other method approved by the Engineer.

The strengths specified are for ordinary Portland cement to BS 12 or Type 1 Cement to ASTM C150; if other types of cement are specified, the required strength shall be defined in the Particular Specification

Table 4 : Mix Proportions , Workability and Strength  Grades of Concrete

| Grade | Minimum Works cube Strength kg/cm2 |  | Max. Agg mm | Limits of agg./ Cement ration by weight |  | Use of concrete if not otherwise specified |
| --- | --- | --- | --- | --- | --- | --- |
|  | At 7 days | At 28 days |  | Max. | Min. |  |
| (A) | 150 | 200 | 20 | 7:1 | 5:1 | RC structures in general |
| B-200 | 150 | 200 | 37 | 8:1 | 6:1 | RC Foundations |
| (B) | 175 | 250 | 20 | 5.5:1 | 4:1 | High load columns |
| B-250 | 175 | 250 | 37 | 6.5:1 | 4.5:1 | High load foundations |
| ( C) | 200 | 300 | 20 | 5:1 | 3:1 | High load columns |
| B-300 | 200 | 300 | 37 | 5:1 | 3:1 | High load foundations |
| (D) | 100 | 150 | 20 | 10:1 | 8:1 | Plain concrete foundations |
| B-150 | 100 | 150 | 37 | 10:1 | 8:1 | Blinding layer under RC Foundations |
| (E) | 75 | 100 | 20 | 14:0 | 12:1 | Mass lean |
| B-100 | 75 | 100 | 37 | 14:1 | 12:1 | Concrete filling |

- Table 4 : Mix Proportions , Workability and Strength Standard Mixes

| Grade of Concrete | Minimum works - Cube Strength Kg/cm2 |  | Weight of dry sand per 50 k of cement | Weight of dry coarse aggregate per 50 kg of cement Workability |  |  |  |  |  |  |  |  |  | Max. desigm W/C ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 20mm max. size |  |  |  |  | 37mm max. size |  |  |  |  |  |
|  | 7 days | 28 days |  | Low | Med. |  | High |  | Low | Med. |  | High |  |  |
|  |  |  | kg | kg | Kg |  | kg |  | kg | kg |  | kg |  |  |
| B-200 | 150 | 200 | 91 | 193 | 159 |  | 136 |  | 226 | 193 |  | 170 |  | 0.55 |
| B-250 | 175 | 250 | 80 | 170 | 136 |  | 113 |  | 204 | 170 |  | 147 |  | 0.50 |
| B-300 | 200 | 300 | 68 | 147 | 113 |  | 91 |  | 170 | 136 |  | 113 |  | 0.45 |

Table 4 : Mix Proportions , Workability and Strength Workability

| Degree of Workability | 20 mm Max. size aggregate |  | 37 mm Max. size aggregate |  | Use for which Concrete is suitable |
| --- | --- | --- | --- | --- | --- |
|  | Slump Mm | Compacting Factor | Slump mm | Compacting Factor |  |
| Low | 13-25 | 0.82-0.88 | 13-50 | 0.82-0.88 | Simple reinforced sections with vibration |
| Medium | 25-50 | 0.88-0.94 | 50-101 | 0.88-0.94 | Heavily reinforced sections with vibration |
| High | 50-127 | 0.94-0.97 | 101-117 | 0.94-0.97 | Sections with heavily congested reinforcement where vibration is difficult |

In case cylinders are used for determination of concrete compressive strength in accordance with ASTM C 39, the 	corresponding cube strength shall be obtained by using a multiplication factor of 1.2.

AGGREGATE/CEMENT RATIO: the term aggregate/cement ratio means the ratio by weight of aggregate to cement in the mix.  For this purpose the aggregate is taken in a saturated surface-dry condition as for the water/cement ratio above.

FINE/TOTAL AGGREGATE RATIO:  the term fine/total aggregate ratio means the ratio by weight of the fine aggregate to 	the total aggregate in the mix expressed as a percentage. For this purpose the aggregate is also taken in a saturated surface-dry condition as for the water/cement ratio above.

VOLUME OF AIR ENTRAINED:  the air content expressed as a percentage by volume of concrete shall be determined by ASTM C231, 'Air Content of Freshly Mixed Concrete by the Pressure Method '.  At least one test for each 120 cubic meters of concrete shall be made.

SLUMP: the slump of the freshly mixed concrete shall be determined in accordance with Part 2 of BS 1881 or ASTM C143. 	At least one morning and one afternoon test shall be made and whenever directed by the Engineer.

STRENGTH OF CONCRETE:  Preliminary Test Cubes shall be taken from the trial mixes designed to select the job mix and shall be made and tested in accordance with Parts 3 and 4 of BS 1881.

SAMPLING FOR COMPLIANCE TESTING: Works Test Cubes shall be those used for control during construction and shall be made and tested in accordance with BS 5328 PART 4:1990.

The Contractor when tendering having knowledge of the source and types of cement , aggregate , plant and method of placing he intends to use shall allow for the aggregate/cement ratio and water/cement ratio which he considers will achieve the strength requirements specified and will produce a workability which will enable the concrete to be properly compacted to its full depth and finished to the dimensions and within the tolerances shown on the Drawings and required by the Particular Specification . In any event the aggregate/cement ratio and the water/cement ratio shall not exceed the upper limits specified in Table 4 for each type of concrete. Furthermore, the quantity of 	cement per cubic meter of concrete shall in no case be less than the minimum specified in Table 4.

As soon as possible after signature of the Contract, the Contractor shall prepare such trial mixes as required to satisfy the Engineer that the specified concrete strengths will be obtained using the materials and mix proportions in accordance with the above clauses. The proportion of cement shall be increased if necessary 	to obtain the strengths required.

From each trial mix, six Preliminary Test Cubes shall be made and tested at 7 days and four at 28 days, the test at 7 days being intended to give and early indication of possible variation from the required strength. If the difference between the highest and lowest test results from any one trial mix is more than 15 per cent of the average of the strength test results, the test is to be discarded and a further trial mix made, unless all test results so obtained are above the required strength. Separate trial mixes are required for each type of concrete. The trial mix or mixes agreed by the Engineer shall be designated job mixes and used as a basis for actual concrete production.

Batching and Mixing Of Concrete

All concrete shall be batched by weight and mixed mechanically.  Hand mixing shall not be allowed except only upon the written permission of the Engineer.

Concrete may either be batched and mixed on site or outside the site and transported thereto.

When mixed outside the site and transported to it, batching and mixing shall be in accordance with ASTM Specification C94, 'Standard Specification for Ready-Mixed Concrete'.

When mixed on site, batching and mixing shall be as follows:

BATCHING BY WEIGHT: The cement and each size of aggregate shall be measured by weight. The water may be measured by weight or volume. The weight-batching machines used shall be of a type approved by the Engineer and shall be kept 	in good condition while in use on the Works. Checks are to be 	made as required by the Engineer to determine that the weighing devices are registering correctly.

BATCHING AGGREGATE BY VOLUME:  When batching 	aggregates by volume is

allowed as and when required, the cement shall be batched by weight and the water by weight or volume . Each size of aggregate shall be measured in metallic containers the depth of which is at least equal to their greatest width. The containers shall be of such shape that their volume can be easily checked by measurement.

MIXING CONCRETE: the location of the batching and mixing plant shall be agreed with the Engineer.

The amount of concrete mixed in any one batch is not to exceed the rated capacity of the mixer .The whole of the batch is to be removed before materials for a fresh batch enter the drum.

On cessation of work, including all stoppages exceeding 20 minutes, the mixers and all handling plant shall be washed with clean mixing water. If old concrete deposits remain in the mixer drum, they shall 	be rotated with clean aggregate and water prior to production of new concrete.

Concrete mixed as above is not to be modified by the addition of water or in any other manner to facilitate handling or for any other 	reason.

Work in Cold or Hot Weather

Concrete is not to be mixed or placed at a shade air temperature below 2 deg .C on a rising thermometer or at a shade air temperature below 3  deg .C on a falling thermometer .

When the shade air temperature is 37 deg .C and rising, special precautions shall be taken during concerting operations, such as shading of the aggregates and plant, cooling of the mixing water 	or other methods approved by the Engineer, so that the temperatures of the concrete when placed shall not be in excess of 39 deg .C.

Fresh concrete placed at these temperatures shall be shaded from the direct rays of the sun to the satisfaction of the Engineer for a period of at least 24 hours.

Placing

Concrete shall be conveyed from the mixer to its final position in any suitable manner, provided there is no segregation, loss of ingredients or contamination.

It shall be placed in its final position before initial setting takes place and within 20 minutes of the addition of the water to the mixer without using any additives. In case additives will be used, the manufacturer specifications of such additives must be handed over to the Engineer to be approved before using it.

The order of placing concrete shall be such as to prevent water from collecting at the ends, corners and along the faces of forms. It shall not be placed in large quantities at a given point and allowed to run or be worked over a long distance in the form.

Whenever possible concrete shall be placed and compacted in 	even layers with each batch adjoining the previous one.

The thickness of the layers shall be between 150 and 300mm for reinforced concrete and up to 450mm for plain (non -reinforced ) concrete, the thickness depending on the width of forms, the amount of reinforcement and the need to place  each layer before the previous one stiffens .

Concrete shall not be allowed to drop freely for more than 2 meters. To convey the concrete as near as possible to its final position, drop chutes of rubber or metal shall be used for small sections and bottom dump buckets or other suitable vessels for large sections.

Concrete shall be carefully compacted when placed to ensure a dense and uniform mass free from air holes and cavities. Concrete type "A" , "B"& "C" shall be compacted by vibration , whereas type 'D' and 'E' concrete may be vibrated or rammed , tamped and rodded . Vibration shall be performed by mechanical or electro -	mechanical vibrators. The vibrators shall be of the plunger (poker) type for insertion in the concrete:  except that plate type vibrators (external) shall be used if requested by the Engineer.

The plunger (poker) type vibators shall have a diameter compatible with the lowest spacing of reinforcement, a sufficiently high 	frequency and be properly handled by experienced personnel. They hall be immersed at regular intervals  close  enough  to vibrate  all   of the concrete , but not too close to affect previously vibrated and partially set concrete . Each immersion shall continue until shortly after air bubbles cease to appear on the surface of the concrete, but shall not last more than 30 seconds. 	The vibrators shall be withdrawn gradually and vertically to ensure that no air pockets are formed.

When external vibrators are used 	as directed by the Engineer, they shall be clamped to the forms whenever possible to avoid large impact during handling, and the forms shall be so constructed as to withstand the additional vibrations.

All vibrations, compaction and finishing operations shall be  	completed within 15 minutes from the time of placing the concrete in its final position. Until it has hardened sufficiently to carry weight without distortion, workers shall not be allowed to walk over 	freshly placed concrete.

Concreting of any one part or section of the work shall be carried out in one continuous operation, and no interruption of concreting work will be allowed without the approval of the Engineer. Where beams and slabs together form an integral part of the structure they shall be poured in one operation.

A record is to be kept by the Contractor on site of the time and date of placing the concrete in each portion of the works and the number and identification of the Works Test Cubes, corresponding to these portions. Such records are to be handed to the Engineer weekly during the progress of the work.

If placing of concrete by pumping is required it shall be specified in the Particular Specification.

Admixtures

No admixtures of any type shall be used in the preparation of 	concrete or concrete products unless so required by the Particular 	Specification or unless so directed by the Engineer. In case any such admixtures are used the rates and methods of application shall be strictly in accordance with the manufacturer's instructions which must be approved by the Engineer before using it.

Curing

Freshly placed concrete shall be protected from rain, dust storms, chemical attack and the harmful effects of heat, wind, flowing water, vibrations and shocks. This protection shall continue until the concrete is sufficiently set such that it is no longer damaged by these factors.

The Engineer shall determine when the protection is no longer required, but in any case this shall not be less than 24 hours after the time of placing.

Concrete shall be cured for at least seven days and as required by the Engineer. Curing shall be effected by the direct application of water to the surface of the concrete or by other approved curing 	methods or curing compounds applied in accordance with the manufacturers specifications. In case the application of such curing compounds is delayed for any reason, the concrete shall be kept moist until the application is made.

Timber formwork covering the concrete shall be moistened with water at frequent intervals to keep it from drying during the curing period. Metal formwork exposed to the sun must be shaded from its direct rays, painted white or otherwise protected during the curing period.

Formed Finishes

1 - Basic finish

General requirements:

(1)	Produce an even finish with a sheet material.

(2)	Arrange panels in a regular pattern.

(c) Blowholes not more than about 10mm in diameter will be permitted but otherwise surface is to be free from voids honey combing and other large defects.

(d) Variation in color resulting from the use of an from discoloration due to contamination or grout leakage.

The finish will be left as struck; making good or small defects will normally be permitted but only after inspection by the Engineer.  All blowholes shall be filled with a matching mortar to an approved sample unless otherwise instructed by the Engineer. All faces shall be protected from damage, especially arrisses.

All faces shall be protected from rust marks and other surface 	disfigurements. Form tie holes shall be filled with a matching mortar to an approved sample accepted by the Engineer.

2 – Fair-Faced Finish

General

Concrete    surfaces    which    are   described   as  finished    fair   shall   be  finished   free   from honeycombing   and excessive   air holes, fins,  and projections   arising  from  defective  mixing, placing,  or  formwork   and  shall,  if  necessary,   be filled  with  mortar  from an approved brand (such as Fosroc or equivalent)  and  rubbed  with  fine carborundum   stone.  The finish shall be integral with the body of the concrete and shall not be obtained by means of an applied rendering. The quality of the surface of concrete exposed to view shall be consistent throughout the project.

Crack Repair

Where shrinkage  cracking,  early  thermal  cracking  or compaction  cracking  occurs,  cracks equal to or exceeding   0.2 mm wide  shall be sealed  by epoxy  resin to be approved by Engineer

Where  cracks   are  less than  0.2  mm,  cracks  shall  be  painted  with  a latex filler  primer prior to painting.

Approval   by Engineer of Fair-Faced   Finishes:

- Submit  for the approval  of the  Engineer,  a sample  panel  of not less than 60 x 120 cm and complete   circular  column  mock-up   to demonstrate   the  quality  of the exposed  concrete  to be produced   by forms.

- The  quality   of  the  finished   Work  shall  be  measured   against  the  quality  of the  approved sample  panel  and  the Work  of inferior  quality  shall  be repaired  or replaced  as directed   by the engineer,  without  any additional   cost.

- Construction    joints,    in  special    cases   of  weather    conditions    and  if  approved    by  the engineer,   shall  be  studied   in  detail  ahead  of  time  and  the  joints  shall  be  grooved   in  a predetermined   pattern  approved  by the Engineer.

Quality Control Testing Etc.

Prior to commencing the work the contractor shall make available on site the following minimum  approved equipment  kept in good condition at all times :

- Six Cube moulds.

- Slump cones.

- Thermometer.

- Any other accessories as required by the Engineer.

All samples and testing shall be done in the presence of the Engineer or his authorized representative either on site or in an approved testing laboratory in the area.

The frequency of testing shall be as noted in the clauses of this section and whenever required by the Engineer.

The works Test Cubes shall be made as follows for types of concrete (A), (B) , and (C)  :

(a) At least three times weekly per mixing plant.

(b) At least once for three individual parts of the structure.

(c) At least once per 100 cubic meters of Concrete or fraction thereof.

For types (D), and (E) concrete the rate shall be once per each 100 cubic meters or fraction thereof.

At least six cubes shall be made at one time. Two of the six cubes are to be tested at seven (7) days. The remaining four cubes are to be tested at 28 days, and their average strength must not fall below the minimum strength specified for each type of concrete and the lowest test result shall not be more than 20% below the average of the four cubes.

When the result of 7-day test is unsatisfactory, the Contractor may elect to remove and replace the defective concrete without waiting for the 28-day test. If the result of the 28-day test is unsatisfactory all concreting shall be stopped at the Contractors expense and shall not proceed further without the written permission of the Engineer.

The Contractor shall then, in accordance with the instructions of the Engineer, remove cores and test same or conduct in- insitu tests in accordance with CP 144 from or on suspect portions of the 	works, under the supervision of the Engineer.

Concrete judged by the Engineer to be defective shall be forthwith cut out, removed and replaced at the Contractors own expense.

In the event of strengths consistently higher than those specified being obtained, a reduction in the number of tests may be authorized by the Engineer.

The following pile tests shall be made by the Contractor to ensure strength and quality of concrete:

-Integrity Test (non-destructive) for all piles

-Static Load Test for 2% of piles (shall not be less than 2 Piles)

The actual concrete cover to all steel at any point should not be smaller than the required nominal cover by more than 5mm.

The effective depth of fully or nearly fully stressed tensile reinforcement should not be

less than that given on the drawings by an amount exceeding 5 per cent  of the effective

depth of the section being considered or 5mm whichever  is the greater .

Ready mixed concrete

Ready - mixed concrete as defined in BS 1926, batched off the site will be used with agreement of the Engineer and shall comply with all requirements of the Contract. The quality and strength of cements shall be determined by site tests. No test results supplied 	by Ready-Mix Supplier shall be accepted as proof of the quality and strength of the concrete.

The concrete shall be carried in purpose made agitators operating continuously, or in truck mixers. The concrete shall be compacted and in its final position within 1 hour of the introduction of cement to the aggregate or as agreed by the Engineer. The time of such introduction shall be recorded on the Delivery Note together with the weight of the constituents of each mix.

When truck mixed concrete is used, water shall be added under supervision either at the site or at the central batching plant as agreed by the Engineer but in no circumstances shall water be added in transit.

Unless otherwise agreed by the Engineer truck mixer units and their mixing and discharge performance shall comply with the requirements of BS 4251. Mixing shall continue for the number and at the rate of revolutions recommended in accordance with BS 4251 or , in the absence of the manufacturer's instructions, mixing shall continue for not less than 100 revolutions at a rate of not less than 7 revolutions per minute .

Prior to any ready mixed concrete being ordered, the Contractor shall submit to the Engineer details of the supplier and shall arrange for the Engineer to inspect the supplier's works if required.

Truck-mixer units shall be maintained and operated strictly in accordance with the man

4	Protection of Concrete (Waterproofing)

- Buildings Substructure Waterproofing (clinic, fire station, police station)

Use Liquid Applied Waterproofing membrane (SuperProof from SKY for Building and Construction or equivalent) to all substructure surfaces in contact with earth such as footings, tie beams, column necks …etc

Liquid applied waterproofing shall be a cold applied, rubberized, flexible bitumen, material in liquid form which when applied dried within 3 hours @ 20 °C. The membrane shall form a tough durable resilient, impermeable barrier to water and most aqueous reagents, adhering to the structural surface. The membrane shall be suitable for hot climates.

A primer or bonding agent if recommended by the manufacturer of the membrane shall be provided, before the application of the liquid membrane.

The minimum thickness of the membrane shall be 1mm unless otherwise indicated on Drawings.

The membrane shall be handled and applied strictly in accordance with the manufacturer's written instructions. Surfaces to be covered shall be clean, flat, dry and free from any matter likely to adversely affect the performance of the waterproofing. The liquid membrane shall be mixed and applied in two coats by spray or squeegee to obtain the required minimum thickness, strictly in accordance with the manufacturer's instructions.

- Water Tanks Substructure Waterproofing

Use Torch Applied SBS Waterproofing Membrane as shown on drawings.

The waterproofing membrane for protection of concrete in contact with earth shall be one layer SBS heavy laminate bituminous felt, reinforced with 200gm/m2 of non woven spun-bonded polyester and modified bituminous compound presenting high thermal stability, plasticity and flexibility characteristics as detailed on drawings and as specified in this Section. The thickness of the membrane shall be 4mm as specified and indicated on drawings.

The typical characteristics of a 4mm thick membrane shall be as follows:

Tests; Unit; Required Val.; Tolerance. Thickness; mm; 4; ± 5%. Aeric Mass; Kg/m; 4.4; ±10%. Tensile strength; Long Tranv; N/5 cm N/5 cm; 900 750; ±20% ±20%. Lap joint strength; Long Tranv; N/5 cm N/5 cm; 950 750; ±20% ±20%. Elongation at break; Long Tranv; % %; 50 55; ±15% ±15%. Cold Bending; 0C; -200; < -5. Form Stability; 0C; 100; >100. Water pressure resistance (DIN 16935); KPa; No leakage at 1000 mm water head/24 hrs.; < 1000. Softening point (ASTM D36); 0C; 130; <130. Down penetration 250C (ASTM D5); dmm; 25; ±5.

Workmanship:

-Waterproofing membrane shall be laid strictly in accordance with the manufacturer’s

instructions.

- Apply materials carefully to provide a completely waterproof, continuous membrane.

- Ensure that surfaces to be covered are clean, dry, smooth and free from voids,   sharp protrusions.

Primer:

Type(s) recommended for the purpose by the sheet manufacturer. Apply by mopping, brushing or spraying to achieve an even and full cover of the surface. Allow to dry thoroughly before covering

Protection to Membrane:

Underground Tanks

Membrane installed under water tank foundation and shall be applied over 10cm thick blinding and protected by 5cm screed layer as shown on drawings.

Membrane installed behind water tank external walls shall be protected by 10cm thick block wall as shown on drawings

Elevated Tanks

Membrane installed under pile cap shall be applied over 10cm thick blinding and protected by 5cm screed layer as shown on drawings. Drop beams (radial and ring) under pile cap shall be waterproofed by applying the membrane on block wall and protected by bituminous sheets 3.4mm thick.

- Waterproofing of Internal Surfaces Water Tanks (Underground and Elevated)

Use tow component epoxy polysulphide based coating. The material shall cure to form a non-toxic tough yet flexible seamless coating that is chemical and abrasion resistant.

The coating shall be suitable for potable water and from an excellent brand such as Fosroc (Nitocote EPSW) or equivalent. The material shall be strictly applied according to manufacturer instructions and shall be approved by Engineer.

Surface preparation prior to application of waterproofing material shall be done using special cementituos grouts such as such as Supercast PC-Fosroc or any other equivalent material.

Typical characteristics of 500 micron thick coating as follows:

| Volume solids | 100% |
| --- | --- |
| Specific Gravity | 1.351 |
| Tensile Strength (ASTM D 412): | 5 N/mm2 |
| Elongation (ASTM D 412): | 60 % |
| Tear Strength (ASTM D 1004): | 14 N/mm2 |
| Hardness (ASTM D 2240 | 70 Shore A |
| Service temperature: | 30 to 70 ºC |
| UV resistance (ASTM G53-91): | Resistance |
| Abrasion Resistance (ASTM D4060, CS-17 wheel 500 gm 100 Cycles 500 Cycles 1000 Cycles | 10-15 mg 70-75 mg 90 mg |
| Crack Bridging Capability | min. 2.5mm |

A leakage test shall be carried by the contractor by filling the tanks with water for 24 hours.  If leakage exists it shall be repaired by Contractor to Engineer satisfaction. The test shall be repeated until no leak appears.

The Contractor shall submit to the Engineer a guarantee stating that all Works of waterproofing system have been carried out in accordance with the drawings and specifications and shall be guaranteed free from defects in material and workmanship and shall be leak-proof for a period of ten (10) years from the date of issuance of the completion certificate.  The Contractor shall agree to repair (including any replacement of materials) any leaks resulting from defective materials or workmanship during the guarantee period at no additional cost to the Client.

- Polyethylene Sheet

Polyethylene sheets  200  microns  thick  shall  be  provided  to  areas  as  indicated  on  the drawings (such as slab on grade) either in transparent or black colour to gauges shown therein. Polyethylene sheets shall be manufactured from 100% prime first grade quality resins to BS 6515:1984. Materials manufactured from recycled, off spec. or waste materials shall not be accepted. The polyethylene sheet shall exhibit all the characteristics of BS 6515:1984 and the Contractor shall produce necessary test certificates to the Engineer to prove the same. Overlaps shall not be less than 100mm and shall be sealed together using an approved adhesive or tape. The material shall be supplied, stored and installed in accordance with the manufacturers written instructions.

- Protection Boards

Protection boards for protection to water proofing membranes shall be from a reputed manufacturer compatible for application to bitumen or rubber membrane.  Protection boards shall be preformed semi rigid asphalt boards 3 mm thick formed of selected blend of asphalt and inorganic mineral fillers reinforced with asphalt saturated felt on one side and a fiberglass mat weather coated and with a bond breaking film on the other side.

- Water Stop

Water stops shall be of polyvinyl chloride (PVC) and shall be of sizes shown on the Drawings from a manufacturer approved by the Engineer. Water stops shall be produced from virgin PVC base resin and shall not contain any reclaimed material whatsoever.

Care shall be taken to correctly position and secure water stops in position during installation and concreting. The manufacturer's recommended securing devices shall be used.

The center line of the water stop should coincide with the joint line. Splices in the continuity, and at ends shall be heat sealed as recommended by the manufacturer. The handling, storage and installation of the water stops shall be carried out strictly in accordance with the manufacturer's instructions and to the satisfaction of the Engineer.

Submit detailed shop drawings along with samples of the product, manufacturers product catalogues and certificates for the approval of the Engineer.

Extreme care shall be taken by the contractor while placing/ compacting concrete in the vicinity of water-stops to ensure the following:

-  No air pocket/honey combing is included/formed.

-  The correct alignment of the water stop is maintained without any wrinkles/twisting.

-  No damage is caused to the water stops.

Specified concrete cover to reinforcement is maintained around the water-stops.

Technical Data

-Tensile Strength         :   > 13.0 N/mm2

-Minimum Elongation   :  At break > 300%

-Joints                          : Heat sealed or as recommended by manufacturers

-Size                             : 250mm wide and (4-5) mm web thickness unless noted

otherwise.

- Treatment/Waterproofing of Pile Head

Pile head shall be completely encapsulated using special materials from an excellent brand such as Fosroc or equivalent as shown in drawing.

Typical materials used by Fosroc include:

- High strength epoxy grout Supercast EPT-Fosroc as final top layer

- Cement grout Supercast PC-Fosroc for surface preparation and leveling up

- Water Stop

5	PILING WORKS

1.0        General

1.1         Works in accordance with Specifications

    - Piling shall conform in all respects with the principles contained in BS 8004.

    - Unless otherwise stated, concrete, reinforcement and formwork shall be in accordance with the requirements in Specification on Concrete for Structures.

    - In the event that the provisions of other specification clauses cause ambiguity or conflict with the requirement of these Specification clauses, the latter shall take precedence unless otherwise approved by the Engineer.

1.2       Setting Out

The Contractor shall be required to employ an approved Licensed Surveyor who will set up the positions of the piles as shown in the pile layout plans of the detailed design. The Contractor will be responsible for the accuracy of location and positioning of each pile. The Contractor will made any errors in setting out and any consequential less to the employer good to the satisfaction of the Engineer.

1.3       Tolerances

(a)         Position

The pile heads shall be positioned as shown   on the Drawings within a maximum deviation of 7:5mm in either direction from its design position.

(b)

Verticality

For bored cast-in-situ piles, the maximum permitted deviation of the finished pile from the vertical at any level is 1 in 150.  The contractor shall demonstrate to the satisfaction of Engineer the pile verticality is within the allowable tolerance.

(c)       Correction

Should piles be installed outside these tolerances affecting the design of the structure, the Contractor shall propose remedial design and carry out immediate remedial measure to the approval of the Engineer.

1.4         Sequence of Installation of Working Piles

The Engineer reserves the absolute right and the Contractor shall recognize such right to direct the  installation  of  working  piles  in  any  sequence   the  Engineer   deems  necessary  for  the satisfactory  completion of the works.

1.5        Forcible Correction Not Permitted

Where piles have not been positioned within the specified limits, no method of forcible correction will be permitted.

.

1.6        Rejected Piles

Any piling work rejected by, the Engineer not truly constructed and installed in accordance with this Specification shall be replaced or rectified by  the contractor the approval of the Engineer and this include  reinstallation of  piles and the design and construction of a modified foundation and also construction of additional compensation  piles.

1.7       Records

The contractor shall keep a record of all piles installed and a copy of the record of the work done each day shall be given to the Engineer within 24 hours. The engineer shall first approve the form of record before piling works commence. Any comment by the Engineer shall be incorporated into the record form.

All unexpected boring or installation conditions shall be noted in the records.

Two (2) bound sets of collated and certified (by the contractor’s P.E.) piling records of all piles shall be submit ted by the Contractor to the Engineer after the completion of the piling works.

2.0        Bored Cast in-Place Concrete Piles

2.1       General

The  Contractor  shall carry out the works  in accordance  with a method  statement  which  has been  approved  by the  Engineer.  This  method  statement  shall  include,  inter alia,  length  of temporary  casing, if required, details of the constituent  materials  of any drilling  fluid used for stabilization, if any, the method of inspection, details of the concrete  design  mix,  concreting method,  the minimum time between the completion of one pile and the commencement  of the next, and the pattern of construction.

Unless otherwise described in the Specifications, reinforcement and concrete shall comply with the requirements in Specification on Concrete for Structures.   The Contractor shall ensure that damage does not occur to completed piles through his method of working. The Contractor shall submit to the Engineer a pile installation programme. The proposed sequence and timing of pile installation   shall be such that the installation works shall not cause any damage to adjacent piles. Piling works shall not commence until approval of the Engineer has been obtained.   No bored pile excavation shall commence within 8m of any concreted pile which has not been cured for 24 hours.

2.2         Tolerances

Tolerances shall be in accordance with the requirements in Clause 1.3 herein.1

2.3       Concrete

(a)      Trial Mix

The Contractor shall arrange to have a trial mix in the presence of the Engineer prior to the commencement of field work.  The trial mix shall be carried out in accordance to the design mix submitted to the Engineer.

(b)         Concrete for Piles

Unless otherwise stated, concrete used shall comply with Specification on Concrete for Structures and as approved by the Engineer. The grade of concrete shall be 35 (characteristic strength of 35 N/mm2 at 28 days) with minimum cement content of 400kg per cubic meter of concrete. Concrete admixture shall only be used with the permission of the Engineer, and shall be used strictly in accordance with Specification on Concrete for Structures.

(c)	 Concrete Testing

A set of at least three 6” cubes shall be taken for every 10 cubic meters or every group of 10 batches of concrete used for the piling works. For the latter, the samples shall be taken from one single batch randomly selected from the group of batches. One cube of each set shall be tested at seven days and the remaining two at 28 days after casting. The piling works and each cube shall be properly marked and identified with details relating the specimen to the borehole in which the concrete is used.

Test shall be carried out by approved lab. Test results shall be submitted to the

Engineer within 48 hours after testing..

The Contractor shall not carry out the specified cube strength tests without prior notice to the Engineer. The tests must be witness by the Engineer or his representative.    The contractor shall provide sufficient quantity of all necessary equipment at site to carry out these tests.

(d)         Workability

Slump test shall be undertaken for every truckload of concrete.   Slump measured  at the time of discharge into pile shaft or at the time of discharge  into the concrete  pump hopper  shall  be  in  accordance  with  the  standards  shown  below  unless  otherwise approved.

A concrete pump shall be used to place concrete directly into the pile shaft.

| Sl. No. | Types of pile | Slump of Concrete |  |
| --- | --- | --- | --- |
|  |  | Minimum | Maximum |
| 1 | Driven cast-in-situ piles | 100 | 180 |
| 2 | Cast-in-situ bored piles |  |  |
|  | a) Water free unlined bore with wide space reinforcement | 100 | 180 |
|  | b) Tremie concreting | 150 | 180 |
| 3 | Under reamed piles |  |  |
|  | a) Water free unlined holes | 100 | 150 |
|  | b) Tremie concreting | 150 | 200 |

The concrete for piles shall be as specified in the design requirement with suitably enriched cement content to permit a high slump mix.   Alternatively, the Contractor may incorporate an approved set retarding additive into the mix to ensure extended workability of the concrete after placement. It is held that the Contractor has included these provisions in the unit rate for the pile.

(e)           Failure of Concrete Cube Tests

If the concrete cubes as tested failed to satisfy the criteria as prescribed in specification, the contractor shall undertake all necessary additional and consequential remedial/compensatory work to the approval of the engineer. The piles shall be rejected as in clause 1.6 “Rejected Piles”.

2.4	Pile Excavation

(a)       Boring near recently cast Piles

Piles shall not be bored next to other piles, which have recently been cast less than 24 hours or contain unset concrete, whichever longer to avoid damage to any of these piles.

(c)        Stability of Boreholes

It  is  held that  the  Contractor has allowed in  the  unit rate of  the pile  for  the implementation of all necessary measures, including the provision of all  materials, labour and plant, for maintaining the stability of the sides of boreholes during bored pile installation and successful completion of the piles.  The Contractor shall submit his proposed methods for agreement prior to commencement of boring operations.

.

Temporary casings, if required, shall be thin walled mild steel cylindrical casing, spirally welded or other similar construction. The dimensions and quality of the casing shall be adequate to withstand without damage or distortion all handling, construction and ground stresses to which they will be subjected, including preventing concrete from within the pile from displacing soft soil or soil squeezing in and displacing fresh concrete. The casing shall have an internal diameter not less than the specified pile diameter. They shall be free of significant distortion, of uniform cross-section throughout each continuous length and free from internal projections and encrusted concrete, which might prevent the proper formation of piles. The joints of casings shall be reasonably watertight.

(j)          Continuity of Construction

A pile constructed in a stable soil without the use of temporary casing or other support shall   be bored and concreted   without   prolonged   delay to ensure   that the   soil characteristics are not significantly altered.

(k)         Surface Water

All boreholes shall be protected from the possibility of any surface water entering the hole from time to time and until the hole is completed and ready to be concreted.

(I}          Excavation Materials

Surplus earth resulting from piling operations shall be used where required or removed from site as directed by the Engineer.

2.5       Placement of Reinforcement

Reinforcement shall be free from rust and mud and not be placed until inspected and accepted. Reinforcement cages shall be sufficiently rigid to ensure that they remain at their correct level

During the lifting and placing of the concrete and the extraction of temporary lining tubes.

Reinforcement shall be maintained in its correct position during concreting of the pile.   The minimum cover to all reinforcement shall not be less than 70mm unless stated otherwise.

Plastic or concrete  spacer (as per Engineer approval)  shall be  provided  at every  3m interval,  size and  minimum  yield strength  of reinforcement  shall be as specified in the Drawing.   Details by which the Contractor plans to ensure the correct cover to and the Engineer shall approve position of the reinforcement.

The main longitudinal reinforcing bars in piles not exceeding 12 meters in length shall be in one continuous length unless otherwise specified.  In piles longer than 12 meters and required to be reinforced  throughout  their full lengths when  specified, joints  with staggered  laps of alternate bars will be permitted in main longitudinal oars at 12- meter nominal intervals unless otherwise specified in the Drawings, Joints in reinforcement  shall comply with the specific requirements of BS8110 clause 3.12.8.

The  Contractor  shall  submit  for  approval  a  method  statement  on  the  manner  by which  he intends to lower reinforcement  cages into pile shafts. Where tack welding is carried out on pile reinforcement  for the  purpose  of hoisting,  such welding  shall  be located  only within  the top

100mm of each reinforcement cage.  Where the top of a reinforcement cage being lowered is to be lapped to £he next cage, as in the case of tension piles exceeding 12 meters in length, the

Contractor  shall provide  adequate  sacrificial  steel  to  compensate  any lapped  reinforcement which  has been tack welded, where such tack welding  is the requirement  of the Contractor for his  hoisting  operation.    Sacrificial steel shall be of the same grade and size as that of the compensated bar.

If required by the Engineer, reinforcement cages shall be flushed with fresh water to remove accumulated salts or other deposits immediately prior to lowering into the pile shaft.

2.6    Concreting Bored Piles

Immediately after the boring for the pile has been completed, approval to commence concreting shall be sought and, when this has been obtained, concreting shall start   forthwith and continue without interruption.  All concrete for cast-in-place piles shall be compacted to produce a dense homogeneous mass by a method agreed by the Engineer.

The concert for each pile shall be from the same source.  The Contractor is to ensure that the supply from whatever source (Whether site-mixed or ready-mixed) is of sufficient quantity so that concrete for each pile shall be placed without such interruption.

All holes bored shall be concreted within the same day.  In the event of rain, the Contractor is to provide adequate-shelter to keep the hole dry and to concrete under cover.

The method placing and the workability of concrete shall be such that a continuous monolithic

concrete shaft of the full cross-section is formed.   The method of placing shall be approved by the Engineer. The  Contractor  shall  take  all  precautions  in the  design  of the  mix  and  the placement of concrete to avoid arching of the concrete in the pile shaft. No spoil, liquid or other deleterious matter shall be allowed to contaminate the concrete.

Agreed measures shall be taken to avoid segregation and bleeding, and that the concrete at the bottom of the pile is not deficient in grout.  The concrete shall be placed by pump.  The free fall of the

concrete from the bottom of the tube shall not exceed 1.5 times the diameter of the pile. The concrete shall be placed as quickly as possible where the ground is liable to deteriorate on exposure.

Backfilling  of  Empty  Bore - On completion  of concreting,  the remaining  empty  bore  shall  be

backfilled with sand or lean concrete unless  otherwise agreed by the Engineer.

Any consequences causing the pile rejected by the Engineer due to supply of concrete shall be on

contractor's own risk.

2.7    Stripping Pile Heads and Bonding

The piles shall be constructed to a sufficient height above the required cut-off levels ('overcast') to ensure that all concrete at and below cut-off level is homogeneous and free of laitance and deleterious  matter. The Contractor shall be required to provide adequate reinforcement with sufficient length to project above cut-off levels so that the reinforcement can be properly bonded in the capping beam.  After completion of piling, the Contractor shall excavate and cut back the piles as necessary to verify the cut-off levels and to give accurate details of the pile positions as compared with the positions indicated on the pile layout plans of the detailed design. Defective concrete in pile heads shall be cut away and made good with new concrete well bonded to the pile head.  If the pile is under cast, it shall be built-up with new concrete and a permanent casing.

2.8         Casting Level

Concrete shall be finished not less than 300mm above the cut-off level ('overcast') to ensure that all concrete at and below cut-off level is homogeneous and free of laitance and deleterious matter. The Engineer depending on site condition may require a thicker overcast, and this shall be carried out.    The  overcast  shall  be  chipped  off  to  cut-off  level  later  by the Contractor.

2.9	    Defective Concrete

Defective concrete in the pile heads shall be cut away and made good with new concrete well bonded into the old concrete.

2.10 	    Piling Records

Submission of the record shall be in accordance with Clause 1.9 herein.

The record shall contain all information required by the Engineer including the following:

(1) (2) (3) (4) (5) (6) (7) (8) (9)

(10) (11) (12) (13) (14) (15) (16) (17) (18)

(19) (20) (21) (22) (23) (24) (25) (26)

Name of Supervisor

Pile forming equipment including Rig No.

Length, diameter and reference number of the borehole

Existing ground level

Cut-off level, rock level, pile toe level

Length of pile

Log of material encountered and level of change in strata and where boring stops

Speed of boring through soil or rock shall be recorded for every meter of drilling

Depth bored and details of inclination or displacement of the pile during boring and date of inspection

Length of reinforcement cage, reinforcement details

Water table below ground level Levels where seepage occurs Results of tests on soils

Results of tests on concrete cubes (slump test)

Length of temporary casing if used

Date and actual volume of concrete placed in piles, time start and complete

Concrete level after each truck of concrete

Details of all inspections

Details of all obstructions, delays and other interruption Signature of the Resident Engineer or his representative Weather condition

Method of casting

Date and time boring start, complete, and speed of drilling

Type of stabilising fluid

Collapse of bore or loss of drilling fluid

Cavities or slump zones encountered

3.0       PILE TESTS

3.1      Integrity Test

3.11       General

Piles shall  be  selected  by  the  Engineer  for  testing  and  detection  of  major  faults,  necking,    discontinuities,  and cross  sectional areas of the piles. Integrity testing of piles shall be carried out by an independent testing organization approved by the Engineer.

If the results of the tests show that the pile or piles are defective, the pile or piles shall be treated as faulty and shall be rejected unless the Contractor can demonstrate to the approval of the Engineer effective remedial measures that will be carried out.

The results of tests shall be printed out immediately during tests with printer facility at site and submit to Engineer at site. The Engineer's interpretations and conclusions arrived at on the test results shall be final.

Integrity Test shall be made by Contractor for all piles and its cost shall be deemed included in concrete unit price

3.12        Shock Method

(a)         Preparation of the Pile Head

The pile head shall be clearly exposed, free from debris, etc. and not more than 1.0 meter above or below ground level, otherwise the surrounding soil shall be built up or excavated to meet this condition.   The pile head shall be smooth over its complete cross-section, free from irregularities and perpendicular to the vertical axis of the pile.

The pile head shall consist of sound concrete.  This shall be achieved during the concreting of the pile by flushing out all weak mortar, etc. from the top of the pile head and carefully screeding off to provide a smooth level surface in sound concrete. Alternatively.   if the  pile  head  is  prepared  after  concreting,  all  weak  mortar.  Broken concrete.  Etc. shall be removed from the pile head to expose sound concrete over its complete cross-section.  After cleaning it off to ensure a sound bond, a very thin screed (maximum 1cm) of strong sand/cement mortar, rapid hardening compound, shall be spread to provide a smooth working surface for the shock test equipment. The mortar shall be allowed to harden before testing.

Any reinforcement or other inclusions protruding from the pile head shall not prevent the testing team from giving the pile the required impact force over the center of the pile and the placing of a 5cm diameter (approx.) electronic pick-up at about 10cm from the periphery of the pile.  Access shall be provided for the service van within 30 meters of the pi e.

l

(b)         Shock Test Equipment

The shock  which  is to  be imparted  onto the  pile head  shall  be  carried  out  using  a suitable hammer  or any approved method which  is capable of transmitting vibration to the  base of the pile shaft. The  electronic  pick-ups  located  on the pile head shall  be approved   velocity  transducers   or  accelerometers   connected  through  an  approved frequency  analyser  to a X-Y plotter. The mechanical admittance shall be plotted on a vertical scale and the frequency on the horizontal scale. Both the horizontal and vertical scales shall be varied as required. The equipment shall have an independent power supply.

(c)         Shock Test

The Contractor shall provide the qualified and experienced testing team with a site plan showing the pile layout and a list of the piles to be tested.

Before testing.  the  heads  of  the  piles  shall  be  inspected  by  the  testing  team  for regularity  and  soundness  and any unsatisfactory  pile heads shall  be reported  to the Engineer.  They shall be made good to the satisfaction of the Engineer and smoothed

3.13       Proof Coring of Pile Shafts

The Contractor shall check the quality of the concrete in the shafts of working piles as directed by the Engineer.  This shall be achieved by a vertical diamond core hole drilled through the center region of the pile from pile head to required depth.   The Engineer shall approve the location of the drill hole and depth.  Full core recovery shall be attempted.  The core so produced shall not be less than 50mm in diameter.  The minimum number of piles for proof coring test shall not be less than 1 % of the total number of working piles or as specified in the Bill of Quantities.

For each pile to be cored, the coring work shall be completed before the concrete in the pile has reached an age of 28 days to allow the cores to be tested for unconfined compression tests at

28 days. The Engineer shall mark the sections of the core to be tested and the Contractor shall arrange for testing in an approved laboratory.  A minimum of six (6) unconfined compression tests shall be conducted on cores obtained from a pile.  Additional  number  of the  unconfined compression  tests  may  be requested  by the  Engineer  if in the opinion  of the  Engineer  the quality of the concrete of the pile is doubtful.

The cored hole in the pile shall be grouted after testing.  The grout shall be an approved  dense cement  grout  with  minimum  28  days  strength  of  equal  or  higher  than  the  strength  of  the concrete of the bored pile. If the pile  is found to be faulty in the opinion of the Engineer because of defects such as cracks, over-breaks,  necking, cavity, inclusion of foreign deleterious  materials, poor  quality  concrete,  etc.,  the  pile shall  be rejected  and the  Contractor  shall  undertake  all necessary remedial measures to the approval of the Engineer.

3.2       Static Load Test (Compression) Using Knetledge

3.21       General

The Static Loading Test (SLT) involves the direct measurement of pile head displacement in the response to a physically applied test load. It is the most fundamental form of pile load test and is considered as the bench‐mark of pile performance.

Static Load Test shall be executed by Contractor on 2% of working piles (not less than 2) or on one test pile. The cost of said test shall be borne by the Contractor and shall be deemed included in concrete unit price.

Load to be applied on working piles = from zero up to 150% of design load

Load to be applied on test pile = from zero up to 250% or 300% of design load (depending on   specification adopted)

3.22	Scope of Work

For the SLT the load is most commonly applied via a jack acting against a reaction beam, which is restrained by an anchorage system or by jacking up against a reaction mass (“Kentledge” or dead weight). The anchorage system may be in the form of cable anchors or reaction piles installed into the ground to provide tension resistance. The nominated test load is usually applied in a series of increments in accordance with the appropriate Code, or with a pre‐determined load testing specification for a project. Each load increment is sustained for a specified time period, or until the rate of pile movement is less than a nominated value.

Static load testing methods are applicable to all pile types and may be carried out on either Working piles or Test piles. Trial piles are specifically constructed for the purpose of carrying out load tests and therefore, are commonly loaded to failure. Testing of working piles however, is limited to prove that a pile will perform satisfactorily at the serviceability or design load, plus an overload to demonstrate that the pile has some (nominated) reserve capacity.

3.23	Method

The pile head shall be prepared usually with casing (for cast in situ piles) to be above the ground by a sufficient length or a minimum of 300mm.

A.    Assemble the Kentledge system as shown in the diagram below with sufficient care when stacking and placing the I‐beams the geometry of the arrangement should also aim to minimize interaction between the test pile, reaction system and reference beam supports. Allow a 10% to 20% margin on the capacity of the reaction against maximum test load.

Install two or more reaction piles, or anchors, for the reaction frame after the installation of the test pile.

Anchors, if used, must be designed with sufficient free length so as not to interfere with the load test pile or the reference system. Design the reaction frame and reaction piles to resist four times the pile design load indicated in the contract documents without undergoing a magnitude of deflection exceeding 75 percent of maximum travel of the jack.

B.    A hydraulic jack and reacting against a set of steel beams tied to anchor piles is placed.

C.    Fix (4 or 2) nos. Dial gauges on an independent ‘frame’ to measure the pile head displacement.

D.   Movement of the pile head shall be measured using the dial gauge and checked with a leveling instrument and scale rules fixed to their holders. The scale rule shall have an accuracy of 1mm, visually interpretable to 0.5mm.

E.    All testing equipment shall be protected from unnecessary disturbance prior to and throughout the load test.

F.   The loading sequence shall follow the client’s specification including the step and duration. The loading usual procedure is to increase the load in stages until the proposed working load and a certain factor of safety is reached and then to unload and to leave the load off until the rise or rebound substantially ceases. The pile may be tested in three standards cycles:

•   The 1st cycle tests the pile to its 150% of the Design Load.

•   The 2nd cycle tests the pile to its 200% of the Design Load.

•   The 3rd cycle tests the pile to its ultimate load, defined as 250% ‐300% of its Design Load.

The following loading sequence relates ASTM D1144-07 & Euro Code 7 (EC7)

The Maintained Load Test Procedure for Compression will be used as follows:

200% of the Designed Load

ASTM D1144‐07

300% of the Designed Load

ASTM D1144‐07

% of Designed

Minimum time of

Reading

% of Designed

Load

Minimum time of load

holding

Reading

Interval

Load

load holding

Interval

0 %                                          ‐                                     ‐

0 %                                  ‐                          ‐

25 %                                      1 hr.                           10 min

50 %                             1 hr.                   10 min.

75 %                             1 hr.                   10 min.

100 %                            1 hr.                   10 min.

125 %                            1 hr.                   10 min.

150 %                            1 hr.                   10 min.

175 %                            1 hr.                   10 min.

200 %                           12 hr.                     1 hr.

150 %                            1 hr.                   20 min.

100%                             1 hr.                   20 min.

50 %                             1 hr.                   20 min.

0 %                              1 hr.                   20 min.

75 %                                      1 hr.                           10 min.

100%                                     1 hr.                           10 min.

125 %                                     1 hr.                           10 min.

150 %                                     1 hr.                           10 min.

175 %                                     1 hr.                           10 min.

200 %                                   12 hr.                             1 hr.

150 %                                     1 hr.                           20 min.

100%                                     1 hr.                           20 min.

50 %                                      1 hr.                           20 min.

0 %                                       1 hr.                           20 min.

50 %                                   20 min.                         10 min.

100%                                  20 min.                         10 min.

150%                                  20 min.                         10 min.

200%                                  20 min.                         10 min.

210%                                  20 min.                         10 min.

220%                                  20 min.                         10 min.

230%                                  20 min.                         10 min.

240%                                  20 min.                         10 min.

250%                                  20 min.                         10 min.

260%                                  20 min.                         10 min.

270%                                  20 min.                         10 min.

280%                                  20 min.                         10 min.

290%                                  20 min.                         10 min.

300%                                     2 hr.                           10 min.

225%                                  20 min.                         10 min.

150%                                  20 min.                         10 min.

75%                                    20 min.                         10 min.

0%                                     20 min.                         10 min.

150% of the Designed Load

Euro Code 7 (EC7)

% of Designed Load     Minimum time of holding load

0 %

25 %                                        30 min.

50 %                                        30 min.

75 %                                        30 min.

100 %                                         6 hours

75 %                                        10 min.

50 %                                        10 min.

25 %                                        10 min.

0 %                                          1 hour

100 %                                        1 hour

125 %                                        1 hour

150 %                                       6 hours

125 %                                       10 min.

100 %                                       10 min.

75 %                                        10 min.

50 %                                        10 min.

25%                                         10 min.

0%                                           1 hour

250% of the Designed Load

Euro Code 7 (EC7)

% of Designed Load                 Minimum time of holding load

0 %

25 %                                                    30 min.

50 %                                                    30 min.

75 %                                                    30 min.

100 %                                                   6 hours

75 %                                                    10 min.

50 %                                                    10 min.

25 %                                                    10 min.

0 %                                                      1 hour

100 %                                                    1 hour

125 %                                                    1 hour

150 %                                                   6 hours

125 %                                                   10 min.

100 %                                                   10 min.

75 %                                                    10 min.

50 %                                                    10 min.

25%                                                    10 min.

0%                                                      1 hour

100 %                                                   30 min.

150 %                                                   30 min.

175 %                                                   30 min.

200 %                                                   30 min.

225 %                                                   30 min.

250 %                                                   6 hours

150 %                                                   10 min.

100 %                                                   10 min.

50 %                                                    10 min.

0 %                                                     10 min

Following each application of an increment of load the load shall be held for not less than the period shown in the above table .For any period when the load is constant, time and settlement shall be recorded immediately on reaching the load and prior to the next step of load.

G.   Records shall be kept promptly throughout the testing period. A copy shall be extended to the Superintending Officer at the end of the test.

Diagram of Compression Load Test Setup using Kentledge System

Diagram of Compression Load Test Setup using Reaction Frame System

3.24	Results of Tests

The test results will be reported in the form of Time, load, and settlements

-      Load vs. settlement curve.

-      Time vs. settlement curve.

-      Time vs. load curve.

-      Report and recommendations on the ultimate pile capacity.

-      Schedule of loading.

-      Certification of calibration (Dial Gauges and Pressure measure)

3.25	Acceptance Criteria

The acceptance of a Static Pile Load Test will be based on the following:

-      The pile was installed in accordance with its respective specification.

-      The pile was tested in accordance with the test procedures contained in this Method of

Statement.

-        The acceptable test pile meets any other criteria indicated in the contract documents, and

All reports and certifications have been submitted as outlined in “Test Results”