SECTION: 6

PLASTER WORK

1	General

The British Standards (BS) govern the work covered in this section.

2	Materials

Portland cement, fine aggregate and water shall be as previously specified in Concrete Work section.

The colour pigments shall be of an approved manufacture, lime proof and non-fading.

The sand for plastering shall be clean fine sand and shall be chemically and structurally stable. The sand shall be sieved and graded in accordance with the Table of Grading given below.

Table Of Grading

BS 410 Sieve No.	Approximate Size  mm	  Sand  Passing Through Sieve        Percentage :  UNDERCOAT                  FINISH COAT

7			2.4				95-100			100

14			1.2				80-95			95-100

25			0 .6				30-55			30-85

52			0.3				5-50			5-50

100			0.15				0-10			0-10

Note: the above figures represent the limits of percentages (by weight) passing sieves of the sizes mentioned.

Imported lime shall be of the hydrate type complying with BS 890.

Bonding agents where required shall be of a type approved by the Engineer, and shall be used as recommended by the manufacturer

The Contractor shall ensure that supplies of materials are sufficient to give consistent and uniform colour to surface finishes which are not to be painted.

3  	Mixing

The methods of measuring and mixing shall be as laid down under Concrete Work section, and the proportions shall be in accordance with the Mixing Table given below.

Mixing Table

Nominal mix	  Ratio	Cement  Kg	Fine Aggregate          or Sand m	(I) ( dry hydrate ) kg

1:5 cement		289	1.00	-

1:4 cement		361	1.00	-

1:3 cement		476	1.00	-

1:2 cement		577	1.00	-

1:2 cement		721	1.00	-

1:1 cement		1442	1.00	-

1:5 cement with 20% (I)	 1:5:1	 289	 1.00	 124

1:4 (I) with 10% cement	 1:10:2	 145	 1.00	 161

* I = Imported Lime

With regard to the lime mortars gauged with cement, the addition just before use of the cement to small quantities of the lime/sand mix shall preferably take place in a mechanical mixer and mixing shall continue for such time as will ensure uniform distribution of materials and uniform colour and consistency.  It is important to note that quantity of water used shall be carefully controlled.

4  	Plastering and Similar In-Situ Finishing's and Backings

All plastering shall be executed in a neat workmanlike manner. All faces except circular work shall be true and flat and angles shall be straight and level or plumb.

Plastering shall be neatly made good up to metal or wooden frames and skirting and around pipes or fittings.  Angles shall be rounded to 5mm radius.

Surfaces of undercoats shall be well scratched to provide a key for finishing coats.  Screed marks or making good on undercoats shall not show through the finishing coats.

Surfaces described as trowelled smooth shall be finished with a 	steel trowel to a smooth flat surface free from trowel marks.

Surfaces described as floated shall be finished with a wooden or felt float to a flat surface free from trowel marks.

All tools, implements, vessels and surfaces shall at all times be kept scrupulously clean and strict precautions shall be taken to prevent the plaster or other materials from being contaminated by pieces of partially set material which would tend to retard or accelerate the setting time .

Coating work shall not be started until all:

a) required openings, chases or other apertures have been cut

b) pipes, fixtures, fixing pads and plugs have been fixed

c) making good has been completed .

The Contractor shall protect all existing work and approaches, with boards, dust sheets etc. All droppings onto finished work shall be cleaned off immediately.

The Contractor shall ensure that all plant and tools are kept clean and free from previous mixes.

The Contractor shall make good defective or damaged coatings before starting decoration works.

5	Preparation for Plaster etc.

All surfaces to be plastered shall be clean and free from dust, loose mortar and all traces of salts.  Projections and concrete fins shall be hacked off. Traces of mould oil, paint, grease, dust and other incompatible materials shall be removed by scrubbing with water containing detergent.

Where cement plaster is to be applied the surfaces shall first be wetted and dashed with a mixture of Portland cement and sand (1:2) mix to form a key.  This should be kept wet with a fine water spray until set, and allowed to harden before applying undercoat for a minimum of 3 days.

All surfaces shall be thoroughly sprayed with water and all free water allowed to disappear before plaster is applied.

Bonding agents where required shall be applied in accordance with the manufacturer's instructions and must be approved by the Engineer.

Before plastering is commenced all junctions between differing materials shall be reinforced in accordance with clause 9.21.

6	Curing Of Plaster etc.

Each coat of plaster should be kept damp for the first three days. Care must be taken to prevent too rapid drying out during hot weather and in drying winds.

The Contractor shall therefore provide a protective covering of plastic or similar impervious sheeting which must be hung so that it is clear of the finished surface.

Any cracking, discoloration or other defects caused by inadequate protection shall be remedied at the Contractor's expense.

7   	Uses of Plaster etc.

The type, mix and thickness of plaster for each location shall be as stated in the Particular Specification or shown on the Drawings, and shall generally be selected from the Schedule of Plasters given in Table P1.

Table P1: Schedule of Plasters

DESCRIPTION	Render and Spray Cement and Sand	Plain Face Cement and Sand	Gauged Plastering Lime and Sand with Cement

Total			Walls	13	15	13

Thickness		Ceilings	10	10	10

Undercoats		Mix Surface	1:4 Floated	1:4 Scratched	1:10:2.5 Scratched

Thickness (mm)		Walls	10	as required	as required

Ceilings	7	as required	as required

Finishing Thickness	Mix Surface	1:1 Sprayed	1:4 trowelled or floated	1:10:2.5 trowelled or floated (mm)

Walls	3	as required	as required

Ceilings	3	as required	as required

Remarks	 External use External or internal use may be applied in one coat to ceiling only if finished thickness is 12mm and the required surface finish is obtained.	Inhternal use may be applied in one coat if finished thickness is 12mm and the required surface finish is obtained.

8       Application of Plaster etc.

After preparation of the surfaces the undercoat shall be applied to the required thickness between screeds laid, ruled and plumbed as necessary. When nearly set the surface of the undercoat shall be scratched. The undercoat shall be allowed to set hard and shall be cured. Where plastering is applied in one coat or where roughcast is to be applied the scratching should be omitted.

The finishing coat shall be applied to the required thickness by means of a laying - on trowel and finished to give the required surface.

The surfaces shall be finished to a true plane to correct line and level, with all angles and corners to a right angle unless otherwise specified, and with walls and reveals plumb and square.  The surfaces shall be finished to within 3 mm of a straight edge 1.80m long placed on face of plaster.

Undercoat shall be worked well into the interstices of metal work to obtain maximum key.

Each coat shall be applied firmly to achieve good adhesion, and ruled to an even surface.

Each coat shall be applied to each wall and ceiling surface in one continuous operation.

Each coat shall be applied at full thickness down to floor level or skirting lath.

All undercoats shall be cross scratched to provide key for next coat.

Cement based undercoats shall be allowed to dry out thoroughly to ensure that drying shrinkage is substantially complete before applying subsequent coat.

50 mm each side of angle bead to be finished with neat Keene's cement before plaster finishing coat is applied. Where angle beads are not specified, angles shall be formed with pencil round arris.

Smooth Finish

Finished with a steel laying trowel to an even surface.

Wood Float or Plain Finish

Finished with a dry wooden float as soon as wet sheen has disappeared from surface to give overall even texture.

Rough Textured Finish

Finished with a cork or carpet float to provide a rough but even open-textured surface.

Scraped finish

Finished with laying trowel to uniform thickness and after coat has set but before it is too hard , aggregate exposed by scraping surface of skin to approved texture .

Rough Cast Finish

Thrown on while wet with trowel or scooped to an even texture and left as cast.

Dry Dash Finish

Top coat of rendering finished to uniform thickness; while coating is plastic, aggregate thrown on to cover surface and particles pressed lightly into mortar to ensure adhesion.

Sprayed Finish

The sprayed finish shall be applied with an approved machine to give a finish of even texture and thickness. The sprayed finish shall be applied in three separate coats allowing time for drying between coats.

Application in one continuous operation to build up a thick layer will not be permitted. The total finished thickness of the four sprayed coats shall be not less than 3 mm.  The sprayed finish shall not be applied until all repairs and making good to the undercoat are completed. Rainwater pipes, fittings and the like shall first be fitted, then removed during the spraying process and refitted and jointed afterwards. Any plaster which adheres to other pipes, doors, windows and the like shall be carefully removed before it has set.  Curing shall take place after the application of the fourth coat.

9 	Steel Mesh Lathing, Stops and Beads

Steel mesh lathing shall be galvanized type weighing 1.6kg/m.

Steel rods for distancing shall be hot rolled mild steel round bars to BS 4449, diameter to approval, galvanized to BS 729 or bitumen coated.

Steel clout nails shall be to BS 1202: Part 1, Table 3, galvanized to BS 729.

Galvanized steel angle bead with 50 mm galvanized expanded metal mesh on both sides of bead.

Mesh lathing shall be fixed with the long way of the mesh at right angles to supports.

In horizontal work it shall be fixed with all mesh strands sloping in the same direction.

In vertical work it shall be fixed with all mesh strands sloping inwards and downwards from face of coating.

Lathing shall be fixed from the center outwards so that it is taut.

Lathing shall not be lapped within 100mm of angles or curves.

Junctions of lathing shall be reinforced at corners with 75 x 75 mm angled plain mesh, fixed to rails with tying wire at not more than 100mm centers.

Ends of wire shall be bent away from face of coating.

Beads and stops shall be fixed plumb, square and true to line and level.

Metal angle beads shall be fixed to solid backgrounds with plaster dabs, and shall be fixed to timber supports with 28mm clout nails. Both types of fixing shall be on each side of angle at not more than 600mm centers.

At junctions between dissimilar solid backgrounds in the same plane and with the same coating, steel lathing shall be fixed with 38 mm clout nails or with staples.  They shall be driven into drilled and plugged holes or into fixing bricks or plugs built in or cast in:

(a) At single junctions, lathing to be not less than 450mm wide, fixed each edge at 100 mm centers.

(b) At columns, lathing to extend not less than 150mm beyond each junction, fixed each edge and centrally at 100 mm centers.

Side edges of lathing shall be lapped not less than 25mm, and secure with tying wire at not more than 100mm centers.

Ends of lathing shall be lapped 40mm at supports and 50mm between supports, and secured with tying wire at not more than 100m centers.

Lathing fixed to metal supports shall be fixed with hair-pin shaped tying wire ties at not more than 100mm centers , passed over the support with both ends through mesh , twisted tight , ends cut off and bent flat .

Concrete, blockwork or masonry backgrounds shall be drilled and plugged at not more than 100x400mm centers and the lathing shall be fixed with 38mm clout nails or wire staples driven at an angle to tauten the mesh.