SECTION: 11

PAINTING AND DECORATING

1	General

Every possible precaution shall be taken to keep down dust before and during painting processes. No paint shall be applied to surfaces structurally or superficially damp and all surfaces must be ascertained to be free from condensation, efflorescence etc. before the application of each coat.

Primed or undercoated woodwork and metalwork should not be left in an exposed or unsuitable situation for an undue period before completing the painting process. No exterior or exposed painting shall be carried out under adverse weather conditions, such as rain, extreme humidity, dust storms etc.

Metal fittings such as ironmongery etc. not required to be painted shall first be fitted and then removed before the preparatory processes are commenced. When all painting is completed the fittings shall be cleaned and refixed in position.

The contractor will be required to repaint at his own expense any work on which the paint is found to be incorrectly applied.  The contractor shall be responsible for protecting from damage the paint work and all other work during and after painting operations including the provision of all necessary dust sheets, covers etc.

Brushes, pails, bottles etc., used in carrying out the work shall be clean and free from foreign matter. They shall be thoroughly cleaned before being used for different types or classes of material.

The number of coats stated in this specification is the minimum, and the Contractor must apply sufficient coats to achieve a proper even finish to the approval of the Engineer.

2	Materials

The decorating materials shall be obtained from approved manufacturers and shall be supplied in the manufacturers' sealed and branded containers.

All materials must be thoroughly stirred before use, unless not recommended by the manufacturer.

Details of mixing and application shall be in accordance with the specifications of the manufacturers concerned and to the approval of the Engineer.

The mixing of paints etc. of different brands before or during application will not be permitted. No dilution of painting materials shall be allowed except strictly as detailed by the manufacturers and as approved by the Engineer.

Mordant solution shall be of approved manufacture.

Rust inhibitors shall be of approved manufacture.

Stopping for woodwork to receive clear finish shall be tinted to match surrounding woodwork, to the approval of the Engineer.

Stopping for internal woodwork, plywood, hardboard, and fiberboard, shall be linseed oil putty, tinted to match the colour of the undercoat.

Stopping for external woodwork shall be white lead paste and gold size well mixed.

Thinners shall be approved turpentine or white spirit.

Priming paints shall be:

(a) For woodwork: Leadless grey priming paint in accordance with the recommendations of the decorative coating manufacturer.

(b) For steelwork: red oxide priming paint.

(c) For galvanised, zinc or aluminum alloy surfaces: grey zinc chromate priming paint.

(d) For plaster, concrete and brickwork, ceiling boards etc.: alkali resisting priming paint in accordance with the recommendations of the decorative coating manufacturer

Undercoating shall be:

(a)  Zinc oxide based undercoating paint;

(b) White lead based undercoating paint. Colours shall approximate to the finishing paint.

(c) Synthetic alkyd based undercoating in accordance with the recommendations of the decorative coating manufacturer.

Finishing paints shall be:

(a) Zinc oxide based oil paint.

(b) White lead based oil gloss finishing paint.

(c) Synthetic alkyd based finishing paint as approved by the Engineer.

Petrifying liquid shall be used undiluted as supplied by the manufacturer A small quantity of water paint of the finishing colour may be mixed with the petrifying liquid.

Water paint shall be an approved brand of washable oil-bound water paint. Thinning shall be done with petrifying liquid or fresh water only.

Emulsion paint shall be of the Polyviny1 Acetate (PVA) type obtained from an approved manufacturer. The precise specification shall comply with the manufacturer's normal 	practice. In all cases thinning shall be done with thinners supplied by the manufacturer or fresh water only.

Stain for woodwork shall be an approved brand of oil stain.

Polyurethane lacquer for woodwork shall be of an approved manufacture.

Preparation Process

3	Internal Plaster, Fair Faced Concrete and Block work

Surfaces shall be allowed to dry out completely and cracks shall be cut out and made good with suitable hard plaster or cement and sand mix as appropriate, such repaired portions shall be allowed to dry out. No painting shall be carried out on plastering less than five weeks old.

Efflorescence shall be completely removed by rubbing down with dry coarse cloths followed by wiping down with damp cloths and allowed to dry. All surfaces shall be rubbed down with fine glass paper and brushed free of dust before applying any form of decoration.

Surfaces which are to receive water paint shall be treated with one coat of petrifying liquid applied by brush  and allowed to dry for at least 24 hours before the application of water paint .  A period of 24 hours or longer if necessary, shall be allowed between subsequent coats.

Fair faced concrete and/or cement and sand plastered surfaces which are to receive oil paint shall be given one thin coat of oil putty and allowed to dry for at least two days .

The surfaces shall then be rubbed down with fine glass paper and given a second thin coat of oil putty and when completely set The surfaces shall then be rubbed down with fine glass paper and given a second thin coat of oil putty and when completely set

All surfaces which are to receive oil paint shall be treated with one coat of alkali resisting priming paint applied by brush and allowed to completely harden.

4	Fibre Boards etc.

SOFT BOARDS: where used externally or under humid conditions will receive one coat of priming paint and one coat of undercoat on back face and edges.

SOFT BOARDS: where used internally will receive one coat of priming paint and one coat of emulsion paint on back, face and edges.

HARD BOARD: composite panels will be treated in the same way as soft boards under humid conditions.

ACOUSTIC BOARDS: will be treated on the face in the same way as plaster, but the paint may be applied by spray; the backs and edges should not be treated.

ASBESTOS: if surfaces are to receive oil paint later one coat of priming paint should be applied.  If surfaces are to receive water paint or emulsion paint no priming paint will be necessary.

5	Steelwork Including Windows, Louvers etc. Internally and Externally

If delivered galvanised, the surfaces shall be cleaned to remove grease and dirt before priming. Where rusting has occurred through damage to the galvanizing, such rust shall be removed by wire brushing back to clean metal and the galvanizing made good with a rust inhibiting agent.

All components of steel structure shall be cleaned by sand blasting.

The surface shall then be treated with one coat of mordant solution and one coat of zinc chromate priming paint.

If delivered primed, the surfaces shall be examined to ascertain that the priming paint is hard, firmly adhering and in good condition. If not satisfactory, the priming paint shall be removed and the surfaces cleaned to remove rust, and reprimed. If the condition of the priming paint is satisfactory, the surfaces shall be cleaned to remove grease and dirt, minor damage to the priming paint being made good with red oxide priming paint after removal of rust.

If delivered unprimed and not galvanised, the surfaces shall be cleaned to remove grease and dirt, and wire brushed and scraped to remove all rust and scale before applying a red oxide priming paint.

Priming paint shall be brushed well into the surface and shall be allowed to dry and harden thoroughly before the application of subsequent coats.

Items of steelwork such as frames to roller shutters, covers to expansion joints etc., which are to be built into walls, shall first be primed.

6	Exposed Service Pipes

Copper and brass pipework shall have the surfaces slightly abraded with glass paper and white spirit or similar solvent and wiped clean. No priming paint will be necessary, the surfaces being finished in two coats of gloss paint.

Steel pipes will be treated as for steelwork with the exception that galvanised pipes are to be treated with a zinc-chromate priming paint.

Coated soil pipes shall be wiped clean and treated with two coats of knotting followed by priming paint as described below.

7       Woodwork Required to be Painted

Surfaces shall be cleaned to remove grease and dirt.  The surface of teak shall be cleaned with white spirit to remove free oil.  The preparation process shall then be:

(a) KNOT: all knots shall be treated with shellac knotting

(b)PRIME: one coat of primer shall be thoroughly applied by brush to all surfaces and when dry a further coat to be applied to end-grain surfaces.

(c) STOP : when priming paint is hard , all cracks , holes , open joints etc. shall be made good with hard stopping and all open grain surfaces filled smooth with linseed oil putty or an approved 	filler and rubbed down with fine glass paper .

No joinery shall be primed until it has been approved by the Engineer Priming shall be carried out on the site and not in the factory.

Items of carpentry work which are to be built into walls etc. shall be first treated by twice coating with creosote or other approved preservative.

8	Woodwork Required to be Stained

Surfaces shall be cleaned to remove grease and dirt.  The wood shall then be stopped, filled and rubbed down.  In the case of teak free oil shall be removed by cleaning with white spirit.

Finishing Processes

9	Internal Plaster

Where emulsion paint is specified three coats shall be applied by brush in addition to any priming paint.

Where water paint is specified two coats shall be applied by brush in addition to the Petrifying liquid. The water paint shall be thinned to the consistency of thick cream.

Where oil paint is specified this shall be two or three coat work as detailed in the particular Specification, applied by roller or brush , but not by spray , to produce hard gloss , oil gloss , eggshell or flat finish as required .

The finishing coat of paint to walls and ceilings shall be applied after the completion and testing of the electrical installation.  Any paint splashes on electrical fittings shall be carefully cleaned off.

10	Fibre Boards etc.

Both acoustic and plain soft or hard boards will be treated as for plaster, but the paint may be applied by spray.

Water paint or emulsion paint shall be applied by brush to the specification of the manufacturers.  Where a board is likely to be exposed to extreme humidity, i.e kitchen and external corridors and covered ways, an oil paint shall be used on the face after fixing .

11	Steelwork and Exposed Service Pipes

Internally, apply one coat gloss paint over two undercoats.

Non-ferrous pipes shall be finished in two coats of gloss paint.

Externally, apply two coats gloss paint over one undercoat.

12	Woodwork Required to be Painted

As for steelwork.

13	Woodwork Required to be Stained

The woodwork, internally and externally, shall be stained as directed on site, rubbed down, brushed off, and treated with two coats of polyurethane.

14	Protection of Factory Finished Work

The contractor is to allow for protecting all factory finished doors, frames windows , suspended ceilings and the like at all times to ensure that factory finishes are not damaged and must make good or replace a defective component at his own expense .

15	Suspended Ceiling (Vinyl Coated Gypsum Tiles)

General

This section specifies suspended ceilings and other proprietary finishing systems to be incorporated in the Works.

The Contractor shall submit manufacturer’s literature and data, shop drawings and samples.

The Contractor shall perform all attendance upon other trades and protect all works specified under this section from damage during subsequent operations, make good any defects, clear away upon completion, clean throughout and leave all work in perfect condition to the approval of the Engineer.

All materials and manufactured items shall be delivered in their original packages, containers, etc. bearing the name of the manufacturer and the brand. All items shall be carefully loaded, transported, unloaded and stored in an approved manner, protected from damage and exposure to weather or dampness during transit and after delivery to site. Damaged items shall be rejected.

Product Data

Vinyl coated gypsum tiles suspended ceiling shall consist of 600 x 600 x 9 mm tiles laid into pre-decorated, proprietary exposed aluminum grid, metal suspension system with matching edge trims.

Vinyl coated non-combustible tiles shall be produced from a reinforced gypsum board faced with vinyl washable pattern layer (around 0.07mm thickness for vinyl caot), also backing with aluminum pet foil (around 0.024mm thickness) . It shall not contain any asbestos or other inorganic materials. The board shall be semi- compressed and cured in a high pressure autoclave to provide a high degree of dimensional and chemical stability.

The suspended ceiling including the suspension system shall be installed strictly in accordance with the manufacturers written instructions.

16	Decorative Render for Buildings External Surfaces

All external plastered elevations (block walls and concrete surfaces) for clinic, police and civil defense buildings shall be coated with decorative render from an excellent brand such as Ventonit (VetoCoat Base WR EG) or equivalent to color and texture approved by Engineer. The coating shall be applied in strict compliance with manufacturer instructions.

17	Epoxy Coating for Elevated Water Towers External Surfaces

All external concrete surfaces of elevated water towers shall be painted with two coats of flexible epoxy paint based on epoxy polyurethane resins from an excellent brand (such as Fosroc, National Paint, Juton or equivalent)  to be approved by Engineer. Color and texture as per Client approval. The coating shall be applied in strict compliance with manufacturer instructions including surface preparation using special materials. The coating shall have excellent strength, water resistance, flexibility and chemical & UV resistance.