SECTION: 12

GLAZING

1	Sheet Glass

Sheet glass shall be flat-drawn clear sheet glass, of the substances shown below.

Nominal Substance or thickness 	Limits of thickness         mm                inch	Approximate Weight         lb/ft2	Normal  Maximum Size            inch

20oz		2.75-3.05   0.108-0.120	  1 1/2		80x48

26oz	 3.1-3.50   0.1 22-0.138  	1 3/4	80x48

32oz		3.8-4.20     0.150-0.165	2	80x48

3/16 in	 	4.65-5.25   0.183-0.207	 2 1/2	50 ft2 max width 84 in

7/32 in	5.3-5.80     0.209-0.228	3	50 ft2 max width 84 in

1/4 in	6.25-6.75   0.246-0.266	3 1/2	75 ft2  max width 84 in

2		Plate Glass

Plate glass shall be cast, rolled or drawn glass ground and polished on both surfaces, of the thicknesses shown below.

Limits For Clear Plate Glass

Nominal Substance or thickness 	Limits of thickness         mm            inch	Approximate    Weight           lb/ft2	Normal Mximum Size inch

3/16		3.97-5.56     0.156-0.219	 2 1/2	100x72

1/4	5.56-7.94     0.219-0.312  	 3 1/4	175x98

3/8	9.13-10.72   0.359-0.422	5	280x130

1/2	 	11.91-13.49 0.469-0.531	  6 1/2	156x96

3		Obscured Glass

Obscured glass shall be figured rolled glass, and of the thicknesses shown below.

Nominal  Substance or thickness 	Limits of thickness         mm                inch	  Approximate    Weight           b/ft2	Normal  Maximum Size            inch

1/8	2.94-4.4       0.116-0.173  	1 1/2	100x48

3/16 	4.5 -6.1        0.177-0.240	2 1/2	 100x48

1/4 	6.0 -7.0 .      0.237-0.276	 3 1/2	100x48

4	   Wired Glass

Wired glass shall be polished Georgian wired having both surfaces ground and polished and with square mesh inserted during rolling   of the thicknesses shown below.

Limits For Wired Glass

Nominal thicknesss  	Limits of thickness		      mm                inch	Approximate Weight      lb/ft2	Normal  maximum size		 inches

1/4	5.5-7.2       0.216-0.283	   3 ½	130x72

5		Heat - Absorbing Glass

Heat - absorbing glass shall be floated glass substantially opaque to infra-red radiations of the thicknesses shown below.

Limits For Heat Absorbing Plate Glass

Nominal thickness	:    6mm

Light transmittance	:    0.49

Reflectance		:    0.10

Absorptance		:    0.34

Shading coefficient	:    0.76

Normal maximum size	:    4500 x 2500mm

6		Mirror Glass

Mirror glass shall be silvering Quality polished plate glass silvered on one side, copper-backed, varnished and painted of the thickness given in clause 2.02. Edges of mirrors shall be beveled.

7		Putty

Putty shall only be used when specified in the Particular Specification and where possible materials described in 14.01 shall be used.

Putty for glazing to metal shall be tropical grade metallic glazing quality and shall be approved.

8		Glazing Beads

Wooden glazing beads shall be of teak, splayed and rounded to the sizes shown on the Drawings and neatly mitered and bradded.

Metal beads shall be supplied with metal windows and doors and these shall be sprung or screwed on according to design.

9		Glazing To Wood Without Beads

The rebates shall be previously treated with one coat of priming paint and the bedding putty inserted. The glass shall be embedded in the putty and secured by sprigs .The front putty shall be inserted to form a triangular miter filling from the edge of the rebate to 2mm from the sight line. The bedding putty shall be trimmed off level with the sight line to form a neat back putty.

When the putty has hardened sufficiently the painting shall be carried out and care shall be taken to seal the joint between putty and glass by painting up to the sight line.

10		Glazing To Wood With Beads

The rebates shall be previously treated with one coat of priming paint and the bedding putty inserted. The glass shall be embedded in the putty and secured by the beads.

The bedding putty shall be trimmed off level with the sight line to from a neat back putty and the painting shall be carried out.

11		Glazing To Metal Without Beads

The rebate shall be previously treated either by rust proofing or priming as described elsewhere and the bedding putty inserted. The glass shall be embedded in the putty and secured by pegs or clips inserted in holes in the rebates.

The front putty shall be inserted to from a triangular mitred filling from the edge of the rebate to 2mm back from the sight line. The bedding putty shall be trimmed off level with the sight line to from a neat back putty. When the putty has hardened sufficiently the painting shall be carried out and care shall be taken to seal the joint between putty and glass by painting up to the sight line.

12		Glazing To Metal With Beads

The rebates shall be previously treated by rust proofing or priming as described elsewhere and the bedding putty inserted .The glass shall be embedded in the putty and secured by the Beads. The bedding putty shall be trimmed off level with the sight line to from a neat back putty and painting shall be carried out.

13		Glazing Without Putty

Where specified, wash leather, ribbon velvet, flannel, felt, asbestos or similar materials shall be used in place of putty forinternal glazing in conjunction with beads. The material should be fitted so that it covers all parts of the glass which will be covered by the rebate and bead.

14		Mirrors

Mirrors shall be fixed to walls with compressive spacers, fibre washers and chromium plated dome - headed screws, screwed into prepared plugs let into walls and set flush with surrounding wall finish.

Mirrors used as wardrobe doors or as wall linings are to be bedded	with an approved mastic on a painted block - board backing not less than 12mm (1/2") thick to walls and 18mm (3/4") thick to doors. Glass sizes will be whole size to doors and minimum 900mm (3'0") wide to wall linings unless otherwise detailed, and backings continuous where possible.

Joints in backings must coincide with joints in mirrors.

15		Cleaning etc

The Contractor shall replace all scratched, cracked or borken glass and clean all glazing on both sides and all mirrors before handing over.