# tiling

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to floor and wall ceramic tiling.  Tiles may be specified by manufacturer’s brand name or by generic type, plus essential characteristics such as size, colour, surface, edge type etc. Bedding, grouting, fixing and jointing requirements should also be specified. There is no central standard, though the BS 6431 series  is used for the tiles themselves.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Segmental pavers – mortar bed, or Segmental pavers – sand bed for brick, stone and concrete pavers.

- Stone cladding for interior and exterior stone cladding or facing.

- Stone and terrazzo tiling for stone and manufactured stone tiling and terrazzo tiling.

Worksection(s) on which this worksection relies

The following worksections must be included, if this worksection is used, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by this worksection. You may need to create new text, modify this text or use an applicable worksection. Examples include:

- External tiling directly exposed to weather.

- Tiling fixed to substrates subject to vibration.

- Tiling fixed to previously tiled or painted substrates.

- Tiling subject to permanent immersion e.g. swimming pools.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Use the Concrete formwork, Concrete reinforcement, Concrete in situ and Concrete finishes worksections for concrete substrates

- Use the Flooring and decking worksection for framed substrates

- Use the Waterproofing – wet areas  worksection for waterproofing wet areas.

- Layout, set-out point, tiling pattern and movement joints to your office documentation policy.

For bathrooms generally, see SAA HB52. Ceramic tile is deemed to comply with the BCA requirements for fire hazard indices (see BCA Specification C1.10).

The tiling system selected should be suitable for substrate deflections as follows:

- Floors span > 3.0 m: < 1:480.

- Floors spans < 3.0 m: < 1:360.

- Walls: < 1:360.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

- Concrete finishes, for substrate finish.

- Lining, for substrate installation.

- Plastering, for substrate application.

- Stone and terrazzo tiling.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Floor preparation and set out of floor tiles before fixing.

- Wall preparation and set out of wall tiles before fixing.

- Control joints before sealing and grouting.

Hold points, if required, should be inserted here.

### Submissions

#### Samples

Submit labelled samples of tiles, including fittings, accessories, grout and sealants, illustrating the range of variation in colour and finish.

### Interpretations

#### Definitions

For the purposes of this worksection the definitions given below apply.

The adhesive definitions are based on AS 4992.1(Int).

- Substrates: The surfaces on which tiles are bedded.

- Bedding: Mixtures of materials which are applied to substrates in a plastic state and dry and cure to adhere tiles to substrates.

- Adhesive bedding: Tiling adhered by adhesives.

- Mortar bedding: Tiling adhered in a cementitious mortar bed.

- Pavers: Slabs made from clays, stone, precast concrete and/or other inorganic raw materials generally over 20 mm thick used as coverings for floors and supported over continuous substrates.

- Tiles: Thin slabs made from clays and/or other inorganic raw materials used generally as coverings for floors and walls and adhered to continuous supporting substrates.

- Natural stone: Tiles cut from natural stone.

- Industrial cast: Tile products of reconstituted stone. Also known as manufactured stone.

- Cementitious: Manufactured cement based pre-finished tiles.

- Terrazzo – cementitious: Manufactured cementitious terrazzo tiles formed in a suitable machine to give sufficient compaction and density to the finished surface, and moisture cured before grinding and honed at the place of manufacture. Thickness usually 35 mm.

The tile definitions are based on AS 4662. The standard tabulates shape types by four water absorption groups.

- Wet areas: Areas within buildings with water supply and drainage systems.

Rely on approved samples for general quality compliance. Samples of sand may be required for major works, where testing for grading is necessary . Where tiles and accessories are specified as  proprietary items use this clause as a means of confirmation.

Tiling should not proceed without a successful flood test of wet area membranes. A method is suggested in the Commentary and should be specified in Waterproofing – wet areas . Delete if not required.

### Tolerances

#### Completed tiling

Conform to the Tolerances table.

#### Tolerances Table

| Property | Tolerance criteria |
| --- | --- |
| Alignment: Deviation of the finished tiles from a 3 m straight edge laid against any joints | < 4 mm |
| Flatness: Deviation of any plane surface under a 3 m straight edge laid in any direction on an area of uniform grade | < 4 mm |

## Products

### Tiles and accessories

Provide tiles and accessories to the Wall tiling and Floor tiling schedules.

#### Tiles

Coves, nosings and skirtings: To be matching stop-end and internal and external angle tiles moulded for that purpose.

Exposed edges: To be purpose-made border tiles with the exposed edge glazed to match the tile face. If such tiles are not available, round edge with grout.

List accessories such as glazed round edge tiles, step treads to stairs, landings, and thresholds, sills, copings and tile vents over bath vents.

### Adhesives

AS 4992.1(Int) is expected to replace AS 2358 in 2005.

#### Type

General: Provide adhesives to the Wall tiling schedule and to the Floor tiling schedule and compatible with the materials and surfaces to be adhered.

Prohibited uses: Do not provide the following combinations:

- Cement-based adhesives on wood, metal, painted or glazed surfaces, gypsum-based plaster.

- Organic solvent-based adhesives on painted surfaces.

- Organic PVC-based adhesives and organic natural rubber latex adhesives in damp or wet conditions.

- PVA (polyvinyl acetate) based adhesives in wet areas or externally.

### Mortar

#### Materials

Cement: Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

- White cement: Iron salts content  1%.

- Off-white cement: Iron salts content  2.5%.

Lime: Confirm source of Lime with Employers representative to ensure highest quality Lime is used in the mortar. Protect from damage on site and store minimum 300mm above ground in waterproof storage facility.

Sand: Fine aggregate with a low clay content selected for grading, sharp and free from efflorescing salts.

Measurement of volume: Measure binders and sand by volume using buckets or boxes. Do not allow sand to bulk by absorption of water.

#### Bedding mortar

Proportioning: Select proportions from the range 1:3 – 1:4 cement:sand to obtain satisfactory adhesion. Provide minimum water.

Terra cotta tiles: Use proprietary polymer modified mortar.

Alternatively: Site gauged. Site gauged mixes are preferred by experienced tradesmen as it gives them the opportunity to make adjustments for  moisture content.

#### Water

General: To be clean and free from any deleterious matter.

### Grout

#### Type

Cement based proprietary grout: Mix with water. Fine sand may be added as a filler in wider joints.

Terra cotta tiles: Use proprietary polymer modified grout.

Portland cement based grout: Mix with fine sand. Provide minimum water consistent with workability.

- For joints < 3 mm: 1 cement:2 sand.

- For joints  3 mm: 1 cement:3 sand.

The selection of the grout type is integral to the performance of the tiling system as a whole and is best left to the warrantor as noted for adhesives.

#### Pigments

Pigments for coloured grout: Provide colourfast fillers compatible with the grout material. For cement-based grouts, provide lime-proof natural or synthetic metallic oxides compatible with cement.

See BS EN 12878 for specifications. Grout colour can be nominated in the  template Schedules.

## Execution

Provide tiling systems to walls, floors and other substrates as follows:

- Consistent in colour and finish.

- Firmly bonded to substrates for the expected life of the installation.

- Resistant to expected impacts in use.

- Set out with joints accurately aligned in both directions and wall tiling joints level and plumb.

- To direct all water flowing from supply points to drainage outlets without leakage to the substrate or adjacent areas.

Refer to AS 3958.1 and AS 3958.2 and also to BRANZ 003 and SAA HB52 for guidance.

### Substrates

#### Drying and shrinkage

Before tiling, allow at least the following times to elapse (for initial drying out and shrinkage) for these substrates:

- Concrete slabs: 42 days.

- Concrete blockwork: 28 days.

- Toppings on slabs and rendering on blockwork: A further 21 days.

### Preparation

If Waterproofing – wet areas is not included, import  wet area membranes and include here.

#### Ambient temperature

If the ambient temperature is less than 5 or more than 35°C, do not lay tiles.

#### Substrates

Ensure substrates are as follows:

- Clean and free of any deposit or finish which may impair adhesion or location of tiles.

- If solid or continuous, excessive projections are hacked off and voids and hollows are filled with a cement:sand mix not stronger than the substrate nor weaker than the bedding.

Absorbent substrates: If suction is excessive, control it by dampening but avoid over-wetting and do not apply mortar bedding to substrates showing surface moisture.

Dense concrete: If not sufficiently rough to provide a mechanical key, roughen by scratching or hacking to remove 3 mm of the surface and expose the aggregate; then apply a bonding treatment.

If there are particular requirements for substrate preparation to suit a particular tiling system, specify them here.

### Tiling generally

#### Sequence

General: Fix wall tiles before floor tiles.

#### Cutting and laying

Cutting: Cut tiles neatly to fit around fixtures and fittings, and at margins where necessary. Drill holes without damaging tile faces. Rub edges smooth without chipping.

Laying: Return tiles into sills and openings. Butt up to returns, frames, fittings, and other finishes.

#### Variations

Distribute variations in hue, colour, or pattern uniformly, by mixing tiles or tile batches before laying.

#### Protection

Floor tiles: Keep traffic off floor tiles until the bedding has set and attained its working strength.

Cleaning: Keep the work clean as it proceeds and protect finished work from damage.

### Setting out

#### Tile joints

Set out tiles to give uniform joint widths within the following limits:

- Ceramic floor tiles: 4 to 6 mm.

- Quarry  floor tiles: 6 to 12 mm.

- Terrazzo and stone pavers to floor: 2 to 3 mm.

- Large and/or irregular floor tiles: 6 to 12 mm.

- Mounted mosaics: To match mounting pattern.

- Ceramic wall tiles: 3 to 5 mm.

- Terrazzo and stone wall panels: 2 to 3 mm.

These values are drawn from AS 3958.1 and may be varied as required to suit tiles or the effect required.

#### Margins

Provide whole or purpose-made tiles at margins where practicable, otherwise set out to give equal margins of cut tiles. If margins less than half tile width are unavoidable, locate the cut tiles where they are least conspicuous.

#### Fixtures

If possible position tiles so that holes for fixtures and other penetrations occur at the intersection of horizontal and vertical joints or on the centre lines of tiles. Continue tiling fully behind fixtures which are not built in to the tiling surface. Before tiling ensure that fixtures interrupting the tile surfaces are accurately positioned in their designed or optimum locations relative to the tile layout.

### Falls and levels

#### Grading

Grade floor tiling to even and correct falls to floor wastes and elsewhere as required. Make level junctions with walls. Where falls are not required lay level.

Fall, general: 1:100 minimum.

The Building and Construction Council of NSW suggests a minimum fall of 1:60 in their “Medium Density Housing Quality Scheme: Quality Handbook” (1994).

Fall, in shower areas: 1:60 minimum.

### Bedding

#### Preparation of tiles

Adhesive bedding: Fix tiles dry; do not soak.

See the Commentary on the topic of adhesive bedding.

Mortar bedding: Soak porous tiles in water for half an hour and then drain until the surface water has disappeared.

Terra cotta tiles: Use pre sealed tiles or apply a breathable sealer and lay dry. If a final sealed finish is selected, use a compatible laying sealer.

Edit these alternatives as required.

#### Bedding

Use bedding methods and materials which are appropriate to the tile, the substrate, the conditions of service, and which leave the tile firmly and solidly bedded in the bedding material and adhered to the substrate. Form falls integral with the substrate.

#### Thin adhesive beds

Provide only if the substrate deviation is less than 3 mm when tested with a 3 m straight edge. Cover the entire tile back with adhesive when the tile is bedded.

Thickness: 1.5 – 3 mm.

#### Thick adhesive beds

Provide on substrates with deviations up to 6 mm when tested with a 3 m straight edge, and with tiles having deep keys.

Nominal thickness: 6 mm.

#### Adhesive bedding application

Apply adhesive by notched trowel to walls and floors and direct to tiles if required, to provide evenly distributed coverage after laying.

Wall tile spacers: Do not use spacer types that inhibit the distribution of adhesive.

Use of cruciform spacers can result in some adhesives failing. The sliding motion is required to break the skin and facilitate adhesion.

Curing: Allow the adhesive to cure for the period nominated by the manufacturer prior to grouting or allowing foot traffic.

#### Mortar beds

For floor tiles: Either lightly dust the screeded bed surface with dry cement and trowel level until the cement is damp, or spread a thin slurry of neat cement, or cement-based thin bed adhesive, on to the tile back. Do not provide mortar after initial set has occurred.

- Nominal thickness: 20 to 40 mm.

### Movement joints

#### General

Provide movement joints to the Tile movement joints schedule and as follows:

Sometimes called expansion joints. Their purpose is to accommodate movement in the tiles or the substrate, or both. Movement may be caused by tile growth, substrate shrinkage, thermal expansion and contraction, and the like. See also the Commentary.

- Location:

- Over structural (isolation, contraction, expansion) joints.

- Close to external corners in large tiled areas.

- Around the perimeter of the floor.

- At junctions between different substrates.

- To divide large tiled areas into bays, maximum 5 m wide, maximum 16 m2.

- At abutments with the building structural frame and over supporting walls or beams where flexing of the substrate is anticipated.

- Depth of joint: Right through to the substrate.

- Sealant width: 6 – 10 mm.

- Depth of elastomeric sealant: One half the joint width, or 6 mm, whichever is the greater.

#### Movement joint materials

Divider strip: A proprietary expansion joint consisting of a neoprene filler sandwiched between plates with lugs or ribs for mechanical keying. Set flush with the finished surface.

Sealant: Two-pack self-levelling non-hardening mould resistant, one-part silicone or polyurethane sealant applied over a backing rod. Finish flush with the tile surface.

Backing rod: Compressible closed cell polyethylene foam with a bond-breaking surface.

Location: State here or refer to a Finishes schedule.

Divider strip:

- Joint side-plate material: e.g. “Perforated brass angles”.

- Joint fixing: e.g. “Mortar bed”.

Proprietary slide plate:

- Material: e.g. stainless steel.

- Insert colour: Nominate colour or omit if no insert.

Sealant:

- Type: e.g. “Polysulphide (two part)”. For major movement joints a proprietary system of sliding plates may be required.

- Colour: State requirement if sealant is to be specially coloured.

Edit joint strip type as required.

### Grouted and caulked joints

#### Grouted joints

Commence grouting as soon as practicable after bedding has set. Clean out joints as necessary before grouting.

Face grouting: Fill the joints solid and tool flush. Clean off surplus grout. Wash down when the grout has set. When grout is dry, polish the surface with a clean cloth.

Edges of tiles: Grout exposed edge joints.

#### Mosaic tiles

Grouting mosaics: If paper faced mosaics are to be bedded in cement mortar, pre-grout the sheeted mosaics from the back before fixing. After fixing, rub grout into the surface of the joints to fill any voids left from pre-grouting. Clean off surplus grout. When grout has set, wash down. If necessary use a proprietary cement remover.

#### Sealant joints

Use where it is necessary to seal joints between tiles and other surfaces to keep them watertight. If movement is anticipated, use a movement joint. If watertightness is not required, grouting may be sufficient.

Provide joints filled with sealant and finished flush with the tile surface as follows:

- Where tiling is cut around sanitary fixtures.

- Around fixtures interrupting the tile surface, for example pipes, brackets, bolts and nibs.

- At junctions with elements such as window and door frames and built-in cupboards.

Width: 5 mm.

Depth: Equal to the tile thickness.

### Joint accessories

Describe either by proprietary item or by essential properties such as material, size (including radius of coves and nosings), pattern, colour. Specification by proprietary item (brand name and manufacturer) will usually be the most certain method of getting the right formulation for a particular purpose.

#### Floor finish dividers

Finish tiled floors at junctions with differing floor finishes with a corrosion resistant metal dividing strip suitably fixed to the substrate, with top edge flush with the finished floor. Where changes of floor finish occur at doorways make the junction directly below the closed door.

e.g. “Ribbed brass strip, 1 mm thick”.

### Completion

#### Cementitious terrazzo tiled surfaces

In situ grind and polish the completed installation with equipment nominated by the tile supplier.

#### Spare tiles

Supply spare matching tiles and accessories of each type for future replacement purposes. Store the spare materials on site where directed by the Employers representative.

Quantity: At least 1% of the quantity installed.

Vary the quantity if required.

#### Cleaning

Clean tiled surfaces using an appropriate tile cleaning agent, and polish.

See also the Commentary on slip resistance.

These schedules refer to the selections of the product/material by its properties, but does not locate it within the project. For this you should prepare a separate document e.g. a Finishes schedule to locate the various finishes by reference to a designation code or abbreviation of the finish.

Tile type, bedding and grout, refer to instructions to the Wall tiling schedule.

Edge: Tiles for chemical resistant floors should be machine cut to provide precision edges.

Slip resistance grade: Refer to Commentary.

Tactile tiles: See AS/NZS 1428.4.

Tactile tile colour: A colour contrast is required, in both wet and dry conditions, between the tactile indicators and the adjacent surface and that the colour provides a luminance contrast to the surrounding surface of not less than 0.3 (30%).

Separation layer:

- Type: e.g. “Building paper”, “Polyethylene film”, or “Bituminous felt membrane”.

Bedding: Traditional mortar beds are now usually confined to thick bed applications such as floor tiling where the bed thickness is varied to obtain falls, or where the bedding is over a separation layer. Edit as required. Site gauged mixes are preferred by experienced tradesmen as it gives them the opportunity to make adjustments for  moisture content.

- Type: e.g. “Bedding mortar” or “Adhesives.” If “adhesive” it will be necessary to specify the type, either generically using the generic terms employed in the standards or by a proprietary item designation. Select either, or both if tiles are to be adhered over a cured mortar screed. Mortar beds laid over separation layers may need to be reinforced.

- Reinforcement: Usually a light gauge galvanized steel mesh.

The impact insulation laboratory value should be the deemed to satisfy value nominated in the BCA. If the field test option is adopted the value for the impact insulation field test should satisfy the BCA.