# Carpets

Worksection application

This worksection is applicable to broadloom carpet, carpet tiles and associated underlay materials.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Resilient finishes for vinyl, rubber and epoxy floor finishes.

Worksection(s) on which this worksection relies

The following worksections must be included, if this worksection is used, to provide a complete specification:

- General requirements

Material not included in NATSPEC

Some projects may include items not covered by this worksection. You may need to create new text, modify this text or use an applicable worksection. Examples include:

- Coir or seagrass matting.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Nominate the locations of finishes and finish abutments, movement joints and note fixed partitions on drawings to your office documentation policy.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

- Concrete finishes for substrates.

- Flooring and decking for substrates.

- Access floors.

- Floor sanding and finishing for substrates.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Subfloor prepared to receive the carpet installation.

- Fixings, edge strips, and underlay installed ready to lay carpet.

Hold points, if required, should be inserted here. e.g. moisture content in concrete substrates.

### Submissions

#### Samples

General: Submit labelled production run samples illustrating the range of colour and pattern available in the required carpet types.

Sample size:

- Carpet: 1 m long x roll width or 1 m wide, whichever is less.

Edge strip: Submit a 300 mm length of each type.

Accessories: Submit one sample of each of the following:

- Carpet gripper.

- Heat-bonding tape.

- Bonding adhesive.

## Products

### Carpet

Tolerances can be critical e.g. where corridor size and carpet body size are nominally the same. Delete if not appropriate.

#### Batching

Carpet laid in a single area and of a single specified type, quality, colour and design, must come from one manufacturing batch and dye lot.

#### Insect resistance

Insecticide: Provide carpets and underlays composed entirely of materials either inherently resistant to insect attack, or treated against insect attack, including by moth and carpet beetle.

### entry Mats

#### Coir mats

Provide a mat made to fit each designated mat recess to the Entry mats schedule. Refer to drawings for locations.

Location: e.g. Door GD1.

Mat type: e.g. Coir, rubber, woven synthetics and hinged aluminium and carpet composites - are best specified as proprietary items. Options such as colour, depth and durability should also be addressed.

Mat size: A dimension of at least 1.25 m, preferably 2 m, in the direction of travel at doorways is recommended.

### Adhesives and tapes

#### Adhesives

Compatible with the floor covering material, and suitable for bonding it to the subfloor.

e.g. Peel up or permanent stick or delete if not adhesive fixed. Subject to manufacturer’s advice on suitability, adhesive fixing may be used to fix carpet direct to concrete (but not timber) subfloors, or to hard underlays. Resists partial rucking of tufted carpet subject to wheeled or heavy foot traffic. The peel-up method has the advantage of easy removal. The permanent stick method makes the carpet difficult to remove for replacement, but is otherwise preferable.

Friction compound: Suitable for holding tiles in position without permanent sticking.

#### Hot-melt adhesive tapes

Commercial grade glass fibre and cotton thermoplastic adhesive coated tape 60 mm wide on a 90 mm wide metal foil base and backed with silicon-coated release paper.

There may be other types. Consult the carpet manufacturer for recommendations on type, grade and size of tape suitable for the selected carpet.

### Strips

#### Preformed gripper strips

Commercial grade plywood carpet gripper strip with 3 rows of rust-resistant angled pins of length appropriate to the carpet type.

Or architectural grade.  AS/NZS 2455.1 covers domestic grade and commercial grade gripper strips.

Size (minimum): 33 mm wide x 7 mm thick.

Location: At edges, except where edge strips are used. Provide double gripper strips to edges where recommended.

#### Edge strips

Type: Heavy duty edge strip appropriate to the floor covering type (tackless or adhesive fixed), capable where necessary of accommodating different levels of adjacent floor finishes.

Form: Metal moulding or extrusion, with vinyl inserts.

Location: At exposed edges of the carpet, and at junctions with differing floor finishes or finishes of a different thickness. Where edge strips occur at doorways, locate the junctions directly below the closed door.

## Execution

### Substrate

#### Substrates

AS/NZS 2455.1 Appendix A requires the (sub)contractor to seek advice from the purchaser about relevant details of the subfloor and contains extensive contractual requirements.

General: Ensure substrates conform to the Substrate tolerance table and are as follows:

- Clean and free of any deposit or finish which may impair adhesion or location and functioning of movement joints.

#### Substrate Tolerance Table

| Property | Length of straight edge laid in any direction | Max. deviation under the straight edge |
| --- | --- | --- |
| Flatness | 3000 mm | 8 mm |
| Smoothness | 200 mm | 2 mm |

Concrete substrate correction: Remove projections and fill voids and hollows with a levelling compound compatible with the adhesive.

Moisture content: Do not commence installation unless the following periods have elapsed:

- Concrete slabs: 42 days.

- Toppings on slabs: A further 21 days.

Consider including the following:

“If raised areas are corrected by grinding test the freshly exposed concrete surface for pH and obtain verification of compatibility with the adhesive”. Freshly exposed concrete has high alkalinity and problems have been encountered overseas.

Fixtures: Remove door stops and other fixtures, and refix in position undamaged on completion of the installation.

### Laying carpet

#### Setting out

Lay the carpet in continuous lengths without cross joins in the body of the area. Where unavoidable cross joins occur at doorways, locate the joins directly below the closed doors.

Restricting cross joins to doorways can lead to undue expense, particularly in direct-stick installations. Amend as you see fit. Note requirement for proposed layout in shop drawings under Submissions.

Partition layout: Confirm that permanent partitions have been installed before starting carpet laying.

#### Fixing underfelt

Stapling is an option in AS/NZS 2455.1 clause 3.5.3 (f). Delete if dual bonded underlay (double stick) is noted below.

Glue continuously to concrete at edges and joints with a 100 mm wide strip to each piece, and at 600 mm centres both ways with 150 mm diameter patches.

#### Seaming methods

Woven carpet: Machine or hand sew. Do not provide glued taped seams.

Tufted carpet: Seam with hot-melt adhesive tape.

#### Fixing

Permanent stick method: Immediately after laying, and again one hour later, roll the carpet from the centre diagonally towards each edge using a 65 kg multi-wheeled roller. Do not roll foam-backed carpet.

Dual bonded underlay: Fix with adhesive between carpet and underlay, and between underlay and subfloor.

Gripping system: Preformed gripper strip and tackless edge strip. Space fixings at 150 mm maximum centres.

Nominate fixing method in SELECTIONS.

#### Cutting laid carpet

Method: Where penetrations through laid carpet are necessary for electrical, telephone or other outlets, cut the carpet either by cross cutting or by cutting rectangular or circular openings.

### Laying on stairs

#### Fixing method

To concrete stairs: Adhesive fixing.

#### Laying method

Closed rise types: Apply the floor covering continuously to the treads and risers.

e.g. “Approved extruded anti-slip aluminium nosing” or “Purpose-made moulded anti-slip vinyl section”, or specify by proprietary name.

### Completion

#### Cleaning

Progressively clean the work. Remove waste, excess materials and adhesive.

Final cleaning: When the installation is complete, clean the carpet as necessary to remove extraneous matter, marks and soiling and to lift the pile where appropriate.

Protection: provide fabric drop sheets. Do not use plastic sheeting. If wheeled traffic is to follow carpet installation protect with hardboard sheets butted and fixed with adhesive tape.

Refer to the Carpet and laying schedule for types and locations of carpets.

If there is more than one type of carpet installation, complete a schedule for each type. Delete items from the schedule which are not applicable to the carpet type (or write “Not applicable”). Consult carpet manufacturers for technical and performance requirements of selected carpet types, or specify outright by proprietary item.

If specifying by proprietary item, identify the manufacturer, brand name, catalogue number, pile fibre and other characteristics sufficient to identify and price the selected carpet. If these particulars are not available, specify by the generic properties in this schedule.

Location: e.g. “Shown on the drawings”, or specify here the floors, stairs and other surfaces to be carpeted. Use the defined codes.

Generic type: e.g. the “structure classification” of AS 2454, in which the basic categories are pile carpets and non-pile carpets. Pile carpets are subdivided into woven pile (plain, Jacquard, Wilton, Axminster), tufted pile, knitted, bonded, needled (most carpet tiles), knotted, and flock.

Colour and pattern: Select colour from a large (1 m²) sample under final lighting conditions. Wilton is restricted to a maximum of five colours.

ACCS Grade: Carpets are graded under the Australian Carpet Classification Scheme, which has been operated by the Carpet Institute of Australia (CIA) for over 15 years. Specifying this grade means that many of the generic items dealt with in the schedule do not need to be addressed at all. Carpets are graded in terms of durability and appearance retention, with 6 residential grades, and 8 contract grades, running from Light Duty, to Extra Heavy Duty and Stairs.

Pile fibre:

- Composition: Wool, nylon, polypropylene, acrylic, polyester, viscose, cotton or hair, or percentage mixtures of these such as 80/20 wool-nylon. Also, anti-static nylon which contains stainless steel threads.

- Pile finish: Cut pile, loop pile or cut-loop pile.

- Pile thickness above substrate: Dense carpet with short pile wears better than less dense carpet with longer pile of the same mass.

Primary backing: Jute for weft, cotton or polypropylene or PVA for warp. Note that some backings act as vapour barriers causing condensation damage to timber or particleboard subfloors. Plastic backing for carpet tiles is more stable than bitumen backing.

Secondary backing: For some tufted (non-woven) carpets.

Treatments: Static and fire are less of a problem for wool than for other carpet types.

Dimensions: For carpet tiles, and for width of broadloom (commonly 3.66 m) or body (690 or 910 mm) carpet.

Fixing method: AS/NZS 2455.1 covers gripper, direct-stick, and double-bond systems. Generally, select from the following:

- Direct permanent stick for latex foam backed and fibre bonded pile carpets, and non-pile carpets. Only high density carpets should be direct-stuck.

- Friction compound for carpet tiles (often, one tile in six).

- Gripper strip for all other carpets.

Where adhesive-fixing, permanent stick is preferred to peel-up although it makes carpet replacement more difficult. Adhesive fixing is generally suitable for concrete floors or hard underlays, but not timber floors.

Seaming method: See AS/NZS 2455.1 clause 3.3.2. Hand sewn is better than taped.

There are possible health risks from some chemicals used in carpet manufacture, installation and maintenance, particularly styrenebutadiene latex backing, and the glues used to fix down some carpets and carpet tiles.

Refer to BCA Specification C1.10 for fire hazard properties requirements. Carpet is not a deemed-to-comply material, nor is it exempted.