# Stainless steel benching

Worksection application

This worksection is applicable to stainless steel benches and associated fitments usually for commercial applications such as kitchens, laboratories and hospitals.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Joinery for domestic sink units.

- Metalwork for custom-made stainless steel fixtures and stainless steel finishes.

Worksection(s) on which this worksection relies

The following worksections must be included, if this worksection is used, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by this worksection. You may need to create new text, modify this text or use an applicable worksection. Examples include:

- Large stainless steel fabrications such as exhaust flues for heavy industries.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Dimensions given on the drawings should not be repeated in this worksection, and vice versa.

- The dimensions that have been given in the worksection text are to set a standard for the information shown on the shop drawings on the assumption that the designer will supply outline drawings only.

Therefore some of the prompts or dimensions given here may be redundant in a project that has been fully detailed, and should be deleted.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

AS 1756 has a type test for strength and support in normative Appendix A for domestic sinks, which could be adapted here.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the units when fabrication is complete, before delivery.

Hold points, if required, should be inserted here.

### Submissions

#### Samples

Submit samples to the Sample table for approval by the Employers representative.

Sample Table

| Description | No. of samples |
| --- | --- |
| Typical joints of welded or fabricated items | 2 |
| The finish to all stainless steel items | 2 |

If delivery involves a goods lift nominate the car size and capacity.

These shop drawing requirements assume the installation is fully detailed. Edit as required.

Nominate the item or component.

See AS/NZS 1554.6 clause 4.6 on the method of qualification of welding procedure by testing.

Stainless steel: For each batch of stainless steel supplied to the works, submit the certificate of compliance specified for the applicable standard.

These shop drawing requirements assume the installation is fully detailed. Edit as required.

#### Site welding

General: If site welding is proposed, submit details indicating location and process.

## Products

### Materials

#### Stainless steel

Plate, sheet, strip, bar and pipe: To ASTM standards.

Neither AS 1769 nor AS 1528.1 covers square tube. Local manufacturers work to the ASTM.

Type: 304.

304 is the usual choice. The alternative, type 316, is suitable for more corrosive environments such as some laboratory benching. For critical applications, seek professional advice on grade selection.

#### Stainless steel sheet

Surface finish: Fine brushed finish not including to underside of shelves, and door backs and drawer backs.

Or HL (Hairline). No. 4. is defined in ASTM A480, cited in ASTM A240. No. 4 is also known as ‘general purpose polished finish’, and is widely used for restaurant and kitchen equipment. HL (Hairline) is more polished than 4.

Thickness: 1.2 mm minimum.

Or, 1.6 mm. But check other specified thicknesses first.

#### Particleboard

Use moisture resistant particleboard minimum thickness 12mm to splashback and 25mm to benchtop as substrate for support of flat sheet.

#### Plywood

Use external grade structural plywood minimum thickness 12mm to splashback and 25mm to benchtop as substrate for support of flat sheet.

### Components

#### Fasteners

Stainless steel fasteners are mostly imported. The metric standards referenced in the Adhesives, sealants and fasteners worksection are mostly ISO-based and can be used for metric stainless steel fasteners. For imperial fasteners, American ANSI standards would be appropriate.

Material: Stainless steel.

Dimensional system: Metric.

Bolt and screw heads: Polished, pan type or countersunk.

Hexagon heads may be used in concealed locations.

#### Hardware

Material: Stainless steel.

Or chrome-plated brass.

Handles: Stainless steel unless noted otherwise.

e.g. 150 mm D-handles.

#### Sealants

The use of the term “food grade” has been avoided as it is undefined by manufacturers and standards. Some manufacturers  certify that their product can meet the requirements of the United States Food and Drug Administration.

Type: Neutral cure one-part silicone.

Performance: Flexible. Resistant to growth of mould, bacteria and fungi. Colourfast.

e.g. Grey, silver, black, white.

#### Adhesive

Type: Spray contact adhesive.

Or 2 pack flexible tile adhesives. Epoxy is too brittle.

## Execution

### Fabrication generally

#### Stainless steel welding

Refer to AS/NZS 1554.6 clause 3.1.2, Appendix B and Appendix G, for what may need to be specified. See WTIA TN11 for a commentary on the AS/NZS 1554 series. Defaults for welding materials, quality and joints taken from AS 1756.

Process: Gas tungsten arc welding.

Weld type: Butt.

Or, fillet. Butt is best.

Surface finish: Grade I, 120 grit.

Welding materials: Compatible with metal being welded.

Weld quality: Free from imperfections such as cracks and pits. Grind and polish to give required surface finish. Continuous exposed welds.

Joints: Strength at least that of parent metal. Free from crevices and folds.

Joint position: At corners and edges as far as possible. Minimise joints in flat panels.

#### Protection

Provide temporary self-adhesive plastic film to stainless steel surfaces.

#### Hardware fixing

Drill and tap, or weld fix.

#### Linishing grain direction

Benches and shelves: Lengthwise.

Bowls: Horizontal to sides, parallel to bench grain to bottom. Mitre at bottom corners.

Abutting surfaces: Parallel where possible.

### Bench tops fabrication

#### Bench tops

Material: Stainless steel sheet.

Thickness: 2 mm.

Refer to drawings for details of bench construction and nominal overall sizes. Confirm all dimensions on site before fabricating bench units.

Exposed corners: Radius exposed corners at least 5 mm, including back vertical corners of upstands.

5 mm radius comes from the urinals standard. 3 mm is an alternative.

Internal back vertical corners: Fuse only from behind.

Wet bench perimeter: Except at wall flashing, provide a raised bead, with a fascia.

Raised bead could be a 45 splayed bead 20 mm high, 25 mm wide. Nominate if required.

Dry bench perimeter: Except at wall flashing, provide a fascia.

#### Fascia

Fascia height: 30mm unless noted otherwise.

Commonly 50 mm. Delete if shown on the drawings.

Fascia return: Full depth of bench top unless noted otherwise.

e.g. 15 mm at the bottom, finishing 35 mm clear of bench legs, giving a 50 mm set back. Delete if shown on the drawings.

#### Drainer

Drainer falls to sinks: 1:50, 450 mm long.

Drainer surface: Plain.

From AS 1756. Domestic pressed sinks may be fluted or dimpled. Edit as required.

Or, horizontal - ensure fascia depth is adequate.

#### Wall splashback

Type: Integral.

Height above bench: 300mm unless noted otherwise.

e.g. 150 mm minimum, to suit tile coursing if any. Delete if shown on the drawings.

Ends: Return for full width of bench top.

e.g. as for non-tiled wall, or 20 mm horizontally, 20 mm up under tiles. Delete if shown on the drawings.

#### Fixing to support frame

Type: Screw fix benchtop to support frame through welded lugs on front and back frames at 600mm centres into plywood or particleboard substrate. Provide star washers under screwheads.

If no substrate is used, weld benchtop to frame on welded lugs on front and back frames at maximum 300mm centres.

Or for lighter use (e.g. domestic), screw to timber backing. Text may not suit a timber-backed bench top.

Select from the following:

- Anti-drum material (cheapest and perhaps least effective).

- 16 mm particleboard, continuous, adhesive-fixed to underside of bench top, sealed at edges.

- 16 mm or 18 mm plywood, continuous, adhesive-fixed to underside of bench top, sealed at edges.

- High moisture resistant Glamapyne™

### Bowl fabrication

#### Bowls

May be integral with the draining surface, or welded to it for complex shapes. Stamping or pressing is used for domestic sinks.

Type: Deep drawn stainless steel.

Thickness:

- Capacity < 75 L: 1.6 mm.

- Capacity  75 L: 2 mm.

Internal radii: 25 mm minimum.

AS 1756 (domestic sinks) specifies a minimum of 5 mm.

Minimum depth: 250 mm.

Or, 150 mm. AS 1756 (domestic sinks) specifies 125 mm.

Wastes:

A 3.5 mm minimum recess is commonly provided around outlet.

- Size (minimum):  50mm diameter.

- Position: Centred in single bowls, adjacent in double bowls.

Or, in the rear corner 100 – 112 mm minimum from the sides of the bowl. Or show on the drawings and delete here.

- Plug: Heavy-duty commercial.

Consider specifying a chain for security.

Fall to waste (minimum):

- Capacity < 75 L: 10 mm.

- Capacity  75 L: 25 mm.

Revise to suit shape of bowls.

### Frame fabrication

#### Bench top support frame

Support: Provide sufficient support so that no load is placed on the waste pipe or water connections.

- Design deflection (maximum): 3 mm.

5 mm in AS 1756.

Members: 31.8 x 31.8 x 1.6 mm stainless steel pipe. Seal ends.

Extent: Perimeter and at sides of bowls, with additional members spaced as follows:

- 1.6 mm sheet: 350 mm maximum centres.

- 2 mm sheet: 500 mm maximum centres.

Revise figures upwards for timber-backed bench tops e.g. for 2 mm sheet, 900 mm may be satisfactory.

Maximum unsupported area: 0.3 m2.

If 25mm plywood or particleboard substrate is used, the benchtop can be supported on front and back rails only, with additional members at 1200mm maximum centres.

Connections: Welded.

Or for lighter (e.g. domestic) use, screw fix to timber.

#### Bench legs

Members: 31.8 x 31.8 x 1.6 mm stainless steel pipe. Seal ends.

Or 25.4 x 25.4 x 1.6 mm.

Fixing to bench top support frame: Weld all around at junctions.

Spacing: 1200 mm maximum.

Or 1000 mm, or 1500 mm. Consult fabricator - the further apart the more flexible the bench in use.

Fixing to walls: Predrilled 100 x 50 x 2 mm stainless steel plate welded to legs at 600 mm high.

Clear of wall to allow for coved skirtings. Alternatively bench can be fixed to wall with stainless steel angles, or ‘P’ frame bracket.

Feet: Nylon or chrome-plated aluminium, adjustable vertically ± 25 mm. Threaded section must not protrude from leg.

### Shelving fabrication

#### Under bench shelving

Material: Stainless steel.

Thickness: 1.6 mm.

Or, 1.2 mm.

e.g. 230 mm, 250 mm, 300 mm. Delete if shown on the drawings.

Shelf support: 30 x 30 x 5 mm stainless steel angles.

- Extent: Perimeter, with additional angles spaced to give a maximum unsupported area of 0.3 m2.

- Connections: Welded.

Or stainless steel 31.8 x 31.8 x 1.6 mm pipe, with sealed ends to stop vermin such as cockroaches!

Fixing of support to legs: Welded.

If 25mm plywood or particleboard substrate is used, the shelf can be supported on front and back rails only, with additional members at 1200mm maximum centres.

Could be done on site, or not if the bench is shipped as a 3D frame.

Fixing of shelf to support: as for benchtop support.

Screw or stainless steel pop rivets.

#### Over bench shelving

Material: Stainless steel.

Thickness: 1.6 mm.

Or 1.2 mm.

e.g. 1350 mm, or 1400 mm, or 1560 mm if there are pot hooks underneath. Delete if shown on the drawings.

Shelf support: 25.4 x 25.4 x 1.6 mm stainless steel pipe brackets minimum 300mm high above the shelf level. Seal ends.

- Spacing: 900 mm maximum with 25mm substrate or shelf fabricated with 30 x 30 x 5 mm stainless steel angles, 600mm with 12mm substrate.

- Fixing to wall: Two 50 x 50 x 5 mm stainless steel plates, fixed with at least two M8 bolts. Weld to top and bottom of the support brackets.

Or use L-shaped brackets.

Fixing of shelf to support: Screw fix minimum of 3 times through tube into side of shelf or shelf angles. Seal between shelf and support.

Or weld fix, possible if the bench is shipped as a 3D frame.

### Drawers fabrication

#### Drawers

Material: Stainless steel.

Thickness: 1.2 mm.

Construction: Welded.

Frames: Removable, and interchangeable with other drawer frames. Provide extension-type drawer slide mechanism and front panel. Provide rubber stops at rear.

Front panel: 20 mm thick double pan construction.

e.g. 380 mm wide, 500 mm deep, 125 mm high. Size to suit pan sizes. See AS 4027. Delete if shown on the drawings.

Housing: Back and 2 sides, of a neat external appearance.

e.g. 450 mm wide, 550 mm deep, 200 mm high. Size to suit liner sizes. Delete if shown on the drawings.

Runners: Incline to rear so drawers roll closed. Provide stop so drawer cannot be pulled out accidentally.

Filing cabinet type runners, or aluminium ball bearing roller guides. Stainless steel runners are difficult to get.

Locks: Chrome-plated brass.

Or stainless steel (hard to get)? Alternatively, provide for padlocks.

### Installation generally

#### Welding

Preference should be given to any other fixing method other than site welding. Obtain approval from the Employers representative for any proposed site welding.

Site (or field) welding is not recommended but may be unavoidable.

#### Sealing

Gaps < 5 mm wide: Apply sealant at the following locations:

- Butt joints between benches.

- Between benches, including flashings, and walls.

- Spaces and gaps under benches.

Gaps 5 mm wide: Close with stainless steel infill panels.

#### Floor fixing

8 mm diameter stainless steel dowels, sealed to floor with silicone sealant.

### Completion

#### Protection

General: Temporary self-adhesive plastic film: Remove from stainless steel surfaces.

Delete if not required.