# Concrete pavement

Worksection application

This worksection is applicable to the supply and placement of concrete for the purposes of internal concrete pavements such as loading docks, carparks and internal roadways.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Asphaltic concrete.

- Sprayed bituminous surfacing.

- Segmental pavers – mortar bed.

- Segmental pavers – sand bed.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Site preparation.

- Earthwork.

- Pavement base and subbase.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Industrial pavements with loads exceeding highway loading.

- Documenting this and related work

- You may document this and related work as follows:

- The thickness of concrete pavements and required reinforcement should be shown on the drawings.

- Show location, types of joints and joint details on the drawings.

- Show required concrete finish (e.g. broom finish) on the drawings.

## General

### Interpretation

#### Definitions

For the purposes of this worksection the definitions given below apply.

- Absolute level tolerance: Maximum deviation from design levels.

- Relative level tolerance: Maximum deviation from a 3 m straight edge laid on the surface.

The Definitions subclause can be edited to suit the project or deleted if not required.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Concrete formwork, reinforcement and dowels in position.

- Commencement of concrete placing.

Hold points, if required, should be inserted here.

### Submissions

#### Products – proposals

Curing compounds: If it is proposed to use a liquid membrane-forming curing compound submit certified test results for water retention.

Curing by the covering sheet method: Submit details of the proposed covering material.

Repair materials: Submit proposals for epoxy resin/grout and elastomeric sealant.

### Tests

#### General

Perform tests of the type and frequency necessary to adequately control the materials and processes used in the construction of the works and in conformance with the Pavement tests table.

Performed by the contractor (or a testing authority appointed by and reporting to the contractor) to maintain control during the course of the works over his materials and processes, independently of compliance assessment testing. It is usual to specify a minimum requirement. The contractor may elect to perform additional tests for his own purposes and at his expense.

#### Compliance assessment tests

Timing: Obtain materials samples at the time of delivery to the site.

Location: Sample from selected sample sites within designated uniform test lots, consisting of an area placed, or compacted or both in one day. Test lots must be uniform in terms of material properties and density.

Specimen type: A set of compression test specimens shall consist of four 200 x 200 x 200 mm cubes, each cube being one specimen.

The specimens within each set shall be tested at the following ages in conformance with the Pavement tests table.

-	One at 7 days for information.

-	Two at 28 days. The 28 day strength shall be taken as the average of the two specimens. If one specimen in this test shows evidence of improper sampling, molding or testing, it shall be discarded. The remaining specimen shall be considered the test result. Should both specimens show the specified defects, the entire test shall be discarded.

-	The fourth shall be retained as a spare to be tested as required.

#### Discharge slump tests

Carry out slump tests at approximately one quarter and three quarter points of the load during discharge.

Working slump: 100mm

Maximum slump: 125 mm. Note concrete with slump greater than this value will be rejected and removed from the site at the contractors cost.

#### Flexural strength assessment of concrete

AS 1379 clause 5.3.1 provides for indirect control of flexural strength by first establishing a relationship between mean compressive strength and mean flexural strength, and then monitoring the mean compressive strength. The worksection provides for direct assessment where this is required.

Acceptance criterion: The average strength of any set of 3 consecutive project samples must not exceed the specified maximum value.

#### Pavement Tests Table

| Samples | ASTM C172 |
| --- | --- |
| Curing | ASTM C31 |
| Testing | ASTM C39 |
| Slump Determination | ASTM C143 |
| Air Content | ASTM C231 or C173 |

Compliance assessment schedule:

- May be performed by the contract administrator, or by an independent testing authority, or partly by the contract administrator and partly by an independent authority.

- Tests performed by the contract administrator have contractual implications and must be specified in the schedules.

- Use these schedules to specify the items to be tested, the test method, and the frequency, where these requirements are not specified in the worksection or standards or shown on the drawings. This will include material property tests, (base, subbase, aggregates, cement, bitumen, asphalt joint seals), density tests (subgrade, base, subbase, asphalt), and asphalt mix tests. Special or additional concrete tests may also be specified here.

- Type of test: If the test relates to properties or tests specified in the Template, use the terms from the Template to describe the test.

- Testing authority: e.g. “Contract administrator” or “Independent testing authority”.

- Test frequency: e.g. per 1000 t, per load, per 1000 m2, per day.

Coarse aggregate durability assessment schedule: AS 2758.1 clause 9.3 provides alternative assessment methods for durability of coarse aggregate. Consult the engineer and specify here the properties to be assessed.

## Products

### Products

#### Reinforcement

All reinforcing shall be supported and wired together to prevent displacement by construction loads, or the placing of concrete, beyond the tolerances specified in ACI 301. Any tack or spot welding of reinforcement shall not be performed without approval from the Employers Representative.

Reinforcement shall be free of loose rust and of any other coating which may adversely affect the bond.

Splices in bar reinforcement shall be located and lapped as shown on the design drawings. Bars in lapped splices shall be in contact unless otherwise shown on the design drawings. Additional splices, if required, shall be made only at locations, and in a manner approved by the Employers Representative. Welded splices shall not be used. All lap splices in bar reinforcement shall be fully in compliance with ACI 318-02.

Welded wire fabric used in concrete paving shall have lapped splices made so that the overlap between the outermost cross wires of each fabric sheet is at least 50 mm.

Unless specifically indicated on the design drawings, splicing by means of proprietary mechanical splices shall not be used.

Concrete spacers, metal or plastic bar spacers i.e. chairs, shall be used for obtaining proper spacing of reinforcement from the bottom and sides of formwork.

Show on the drawings sizes and location of reinforcement and dowels.

#### Dowels

Provide each dowel in one piece, straight, cut accurately to length with ends square and free from burrs. Fix in locations as shown on the design drawings.

#### Aggregate

Aggregate size:

- For fixed form placement: < 40 mm.

- For slip form placement: To be a size compatible with the paving machine.

Washing: Wash aggregate as necessary or as directed to remove significant dust or achieve requirements for soluble salt content or concrete drying shrinkage.

#### Aggregate Sieve Table

| Sive size |  |  | Percent by weight passing |
| --- | --- | --- | --- |
| mm | in |  |  |
| Coarse Sieves |  |  |  |
| 25 | 1 | 90-100 |  |
| 19 | 3/4 | 40-85 |  |
| 12.5 | 1/2 | 10-40 |  |
| 9.5 | 3/8 | 0-15 |  |
| Fine Sieves |  |  |  |
| 4.75 | No. 4 | 95-100 |  |
| 2.36 | No. 8 | 80-100 |  |
| 1.18 | No. 16 | 50-85 |  |
| 600 μm | No. 30 | 25-60 |  |
| 300 μm | No. 50 | 5-30 |  |
| 150 μm | No. 100 | 0-10 |  |

Consider specifying in the Conditions of tendering that tenderers are to nominate their proposed sources of supply, and to supply samples from the sources for testing. Appropriate tests and limits would then be derived for the approved reference samples. Test methods and limits such as those given in AS 2758.1 may not be applicable to material from a particular source. Vary as necessary.

#### Cement

Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

Cement shall be free from any hardened lumps and foreign matter. It shall have a minimum of 90% of particles by weight passing the 75-micron sieve, an initial setting time in excess of 30 minutes and a final setting time of less than 7 hours.

Cement shall be stored in a waterproof shaded area. The cement stacks shall be placed at a minimum distance of 300mm from the walls. The damp proof floor shall be constructed by raising it minimum 300mm above the ground.

#### Curing products

Curing compounds: Obtain approval from the Employers Representative for all curing compounds prior to use.

Covering sheet materials: To be opaque polyethylene film, or burlap-polyethylene sheet, or equivalent material.

#### Concrete

Ready-mixed concrete shall comply with M-150 (1:2:4) for non-reinforced mass concrete and M-200 (1:1.5:3) for reinforced concrete and the requirements of these standards.

On site batch mixed concrete shall have characteristics and proportions of concrete ingredients which conform to those specified in M-150 (1:2:4) and M-200 (1:1.5:3).

Admixtures: Introduce in solution in a portion of the mixing water. Ensure a uniform distribution of the admixture in the batch within the mixing period.

Mixing time: Measure the mixing time after solid materials are in the mixer, provided that mixing water is introduced before a quarter of the mixing time has elapsed. Increase mixing time if necessary to obtain the required uniformity and consistence of concrete. Do not overmix such that additions of water are needed.

See AS 1379 Table A1.

Transport: Transport and discharge the concrete without segregation.

Elapsed delivery time: Discharge truck mixed concrete within a time (t hours) determined as follows, where T is the temperature of the concrete in degrees Celsius:

- t = 2 - 0.05T.

## Execution

### Placing

See AS 3600 clauses 19.1.3 and 19.1.4.

#### Rate

Place at a rate of at least 25 linear metres of pavement per hour.

#### Tolerances

Edges abutting gutters: Within  5 mm of the level of the actual gutter edge.

Rigid pavement surface:

- Absolute tolerance: ± 10 mm.

- Relative tolerance: 5 mm.

Concrete surface course: + unspecified, - 5 mm.

Joint locations (rigid pavement): 15 mm.

#### Cold weather

Subbase: Ensure that the subbase surface is free of frost.

Cold weather concreting shall be in accordance with the following:

a. The guidelines of ACI 306R shall be followed when the Forecasted Mean Daily Temperature drops below 4°C for three consecutive days. The minimum concrete temperature when delivered at the site shall be in accordance with the Minimum cold weather temperature table.

b. If water or aggregate is heated above 38°C, the water shall be combined with the aggregate in the mixer before cement is added. Cement shall not be mixed with water or with mixtures of water and aggregate having a temperature greater than 38°C.

c. Concrete shall only be poured when the ambient temperature is rising.

d. All concrete shall be insulated from freezing for the greater of following:

1. 	3 days

2. 	Until the concrete reaches an in-place compressive strength of 35 kg/cm2,

e. All materials shall be free from frost.

f. Accelerating admixtures shall not be used without approval from the Employers Representative.

Maintain the concrete at a temperature of at least 10C for at least 24 hours after placing.

#### Admixtures

General: Do not add calcium chloride, salts, chemicals or other material to the mix to lower the freezing point of the concrete.

Minimum Cold Weather Temperature Table

| AIR TEMPERATURE °C | MINIMUM CONCRETE TEMPERATURE °C |  |
| --- | --- | --- |
|  | For Sections With Smallest Dimension Less Than 300 mm | For Sections With Smallest Dimension 300 mm Or Greater |
| -1 to 4 | 16 | 13 |
| -18 to -1 | 18 | 16 |
| Below -18 | 21 | 18 |

#### Hot weather

Avoid premature stiffening of the mix and reduce water absorption and evaporation losses. If the temperature of the surrounding air is higher than 32C:

- Mix, transport, place and compact the concrete as rapidly as possible, and cover with an impervious membrane or hessian kept wet until moist curing begins.

- Hold the concrete to a temperature  32C when placed.

Hot weather concreting shall be in accordance with the following:

a. Concrete temperatures shall be kept within desirable limits using methods recommended in ACI 305R.

b. For mass concrete, i.e., concrete sections having a minimum dimension of 750mm or greater, the maximum acceptable concrete temperature is 21°C at time of discharge.

c. For other concrete structures, the maximum acceptable concrete temperature is 32°C at time of discharge.

d. If ice is used as part of the mixing water, mixing should be continued until the ice is completely melted.

e. Retempering shall not increase the water content above that in the mix design.

#### Placing in fixed forms

Place concrete uniformly over the width of the slab or lane and so that the face is generally vertical and normal to the direction of placing. Hand spread concrete using shovels, not rakes.

Compact concrete using internal mechanical vibration of sufficient amplitude to produce noticeable vibrations at 300 mm radius. Insert vibrators into the concrete to the depth which will provide the best compaction, but not deeper than 50 mm above the surface of the subbase, and for a duration sufficient to produce satisfactory compaction, but not longer than 30 seconds in any one location.

This clause assumes that the concrete will be spread, compacted and finished by hand. If a paving machine is to be used some modification may be needed to the subclauses Spreading and Vibration, and the clause Finishing. Consult the engineer.

#### Slip form placing

Spreading: Place the plastic concrete in a uniform layer over the width of the slab being placed. Do not damage the existing surface and edge of previously constructed concrete.

Vibration: Use suitable internal vibrators or surface type equipment with vibrating beam or beams of adequate power to fully compact the whole depth of the concrete.

Slab edges: Use supplementary immersion type vibrators next to slab edges if necessary to ensure that the sides of slabs present a uniform dense appearance free from honeycombing or areas deficient in fines over at least 95% of the surface.

This clause is appropriate for small-scale projects. For major works (large pavement areas, heavy traffic, heavy loadings, etc.) additional requirements may need to be specified. Consult the engineer.

#### Finishing

Immediately after placement and spreading and compaction of the plastic concrete, start finishing operations to achieve finish shown on the drawings.

#### Curing

Protect fresh concrete from premature drying and from excessively hot or cold temperatures. Maintain the concrete at a reasonably constant temperature with minimum moisture loss for the curing period.

- Temperature: Maintain the concrete at a temperature > 5C for at least 7 days.

Curing compound method: Spray the entire surface including edges using a mechanical sprayer, at a uniform application rate of at least 0.35 L/m2. Respray defective areas within 30 minutes. Respray within 3 hours after heavy rain. Apply as a continuous coating without visible breaks or pinholes.

Covering sheet method: Immediately after finishing operations cover concrete using damp hessian or cotton mats overlapped at least 150 mm and anchored against displacement by wind or other interference. Keep the mats continuously damp until covered by the covering sheet material. Repair tears and the like immediately.

- Joint sawing: Sheet materials may be removed for the minimum distance and period to permit joint sawing, provided the concrete is kept moist by other means.

Moist curing method: Immediately after finishing operations keep the concrete surface continuously damp by spraying constantly with water, fog, or mist, using suitable spraying equipment.

Minimum curing time: 7 days.

See AS 3600 clause 19.1.5.

If a particular curing method is required select it here.

### Joints

#### Joints

Construct expansion, contraction and construction joints straight and plumb. Make transverse joints normal to longitudinal joints. Extend transverse expansion and contraction joints continuously from edge to edge of the pavement through interconnected slabs.

Transverse construction joints: To be as follows:

- Planned location: Terminate each day’s placing operation at a transverse construction joint located to coincide with a planned contraction or expansion joint.

- Unplanned joints: If placement is interrupted for 30 minutes or longer, form a tied transverse construction joint within the middle third of the distance between planned joints but no closer than 1.5 m to the nearest planned joint. If necessary remove placed concrete back to the required location.

Expansion joints: Provide formed full depth joints around structures and features which project through, into or against the pavement, and elsewhere as required.

### Completion

#### Protection

Keep traffic, including construction plant, off the pavement entirely during curing, and thereafter permit access only to necessary constructional plant vehicles until the pavement is at least 14 days old.

#### Traffic on pavement

General: Give notice before opening the pavement to traffic before the work is completed. Provide adequate means of protection.