# Cementitious toppings

There is a Product Partner for this worksection. Click the logo to be redirected to their page	.

Worksection application

This worksection is applicable to cement-based toppings on floors and steps. There is no relevant standard in Australia but there are numerous guides available from BRANZ and the Cement and Concrete Association.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Concrete in situ.

- Concrete finishes.

- Terrazzo in situ.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Polymer cement and polymer modified cement toppings (see BS 8204-3).

- Resin or polymer seamless toppings.

- Self-levelling or self-smoothing underlays to floor finishes.

- Backgrounds other than cast in situ concrete.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- None.

- Documenting this and related work

- You may document this and related work as follows:

- Show the location of this and other floor finishes on drawings to your office documentation policy.

- Use the specification to define the type(s) of toppings.

- Show the arrangement and details of joints should on the drawings.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

### Interpretations

#### Abbreviations

For the purposes of this worksection the abbreviations given below apply.

- BCS: Bonded – cement and sand.

- BFC: Bonded – fine concrete.

- FFC: Floating – fine concrete.

- MGR: Monolithic – granolithic.

- SFC: Separated – fine concrete.

The Abbreviations subclause can be edited to suit the project or deleted if not required.

### Tolerances

#### General

Thickness:

These tolerances are intended to accommodate the combinations of concrete sub-floor variations and nominal thicknesses specified.

- Thickness < 15 mm: ± 2 mm.

- Thickness ≥ 15 < 30 mm: ± 5 mm.

- Thickness ≥ 30 mm: ± 10 mm.

Flatness: Measured under a 3000 mm straightedge laid in any direction on a plane surface:

- Grade A: < 3 mm.

- Grade B: ≥ 3 < 5 mm.

- Grade C: ≥ 5 < 10 mm.

These tolerances are unlikely to be precise enough for superflat pavements required in high bay warehouses. See ACI 302.1R and ASTM E1155 test method for determining Ff floor flatness and Fl floor levelness numbers. Note that Austroads  AP-G63 specifies 3 mm for new highways and 5 mm for local roads so grade C is quite generous.

## Products

### Products

There is a wide range of products available. Only the most general descriptions are provided but these may be sufficient unless specific products are selected.

#### Admixtures

Introduce in solution in a portion of the mixing water. Ensure a uniform distribution of the admixture in the batch within the mixing period.

Introduce in solution in a portion of the mixing water. Ensure a uniform distribution of the admixture in the batch within the mixing period.Introduce in solution in a portion of the mixing water. Ensure a uniform distribution of the admixture in the batch within the mixing period.The use of admixtures should not be permitted unless there is confidence that there will an improved outcome.

#### Aggregates

Coarse aggregate: To be nominal single size.

Fine aggregate: To be fine, sharp, well-graded sand with a low clay content and free from efflorescing salts.

Aggregates have a significant impact on shrinkage. The sizes given are ranges.

#### Bonding products

To be proprietary products manufactured for bonding cement-based toppings to concrete backgrounds.

#### Cement

Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

#### Colouring products

To be proprietary products manufactured for colouring cement toppings.

Integral pigment proportion:  5% by mass of cement.

#### Coloured chips

To be marble chips of selected colour or proprietary products manufactured for distribution in cement toppings.

#### Concrete

On site batch mixed concrete shall have characteristics and proportions of concrete ingredients which conform to those specified in M-150 (1:2:4).

#### Curing products

To be proprietary products manufactured for use with cement-based toppings and with the floor finish to be laid on the toppings.

#### Mixes

Provide concrete as follows or select mix proportions to the Mixes table.

- Air entrainment: ≤ 3%.

- Nominal coarse aggregate size: ≤ 0.3 x topping thickness.

- Slump: 80 mm.

Water quantity: Use the minimum necessary to achieve full compaction and prevent excessive water being brought to the surface during compaction.

#### Mixes Table

| Mix type |  | Thickness (mm) | Upper and lower limits of proportion by mass (mm) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Cement | Fine aggregate | Coarse aggregate |
| Bonded – cement and sand | BCS | 35 | 1 1 | 3 4.5 | 0 0 |
| Bonded – fine concrete | BFC | 40 | 1 1 | 3 3 | 1 2 |
| Floating – fine concrete | FFC | 100 | 1 1 | 3 3 | 1 2 |
| Monolithic – granolithic | MGR | Floors and treads: 25 Risers and skirtings: 13 | 1 | 2 | 1 |
| Separated – fine concrete | SFC | 70 | 1 1 | 3 3 | 1 2 |

This table, as an alternative to pre-mixed concrete to AS 1379, allows a degree of flexibility to select a mix to suit the conditions. Can be edited to suit or left to stand.

#### Movement control joint products

Provide products manufactured for use with cement based toppings and accommodate the anticipated movement of the backgrounds and/or the toppings.

#### Sealing products

Provide proprietary products manufactured for the sealing of movement joints in cement-based toppings.

#### Slip-resistance products

Provide proprietary products manufactured to improve the wet-slip resistance of toppings.

- Silicon carbide granules:

- Granule size:  300 < 600 µm.

- Colour: Black.

#### Surface treatment products

Provide proprietary products manufactured for use with cement- based toppings to change the characteristics of the surface of the finished topping.

#### Reinforcement

All reinforcing shall be supported and wired together to prevent displacement by construction loads, or the placing of concrete, beyond the tolerances specified in ACI 301. Any tack or spot welding of reinforcement shall not be performed without approval from the Employers representative.

Reinforcement shall be free of loose rust and of any other coating which may adversely affect the bond.

#### Water

General: To be clean and free from any deleterious matter.

Refer to the Cementitious toppings schedule for details of toppings and locations.

## Execution

### Preparation

#### Backgrounds

Ensure backgrounds have:

- Any deposit which may impair adhesion of monolithic or bonded toppings cleaned off.

- Excessive projections hacked off and voids and hollows filled with a mix not stronger than the background nor weaker than the topping.

- Hardened concrete roughened by scratching or hacking to remove 2 mm of the surface and expose the aggregate.

#### Bonded toppings

Before laying topping wash the subfloor with water and use a bonding product or treat as follows:

- Keep wet for ≥ 2 hours.

- Remove surplus water and brush on neat cement or a clean slurry of cement and water.

- Place the topping while the slurry is wet.

### Application

#### Laying

Spread the mix and compact and level the surface to finished levels.

Monolithic toppings: Lay while concrete subfloor is plastic and surface water is no longer visible.

Toppings over 50 mm thick:

- Lay in two layers of equal thickness.

- Place a layer of reinforcement between the layers of toppings. Lap reinforcement 100 mm and tie. Do not create four way laps.

#### Floating and trowelling

Machine float finish:

- After levelling, consolidate the surface using a machine float.

- Cut and fill and refloat immediately to a uniform, smooth, granular texture.

- Hand float in locations inaccessible to the machine float.

- Flatness: Grade B.

Steel trowel finish: After machine floating finish as follows:

- When the surface has hardened sufficiently, use steel hand trowels to produce the final consolidated finish free of trowel marks and uniform in texture and appearance.

- Flatness: Grade A.

Wood float finish: After machine floating finish as follows:

- Use wood or plastic hand floats to produce the final consolidated finish free of float marks and uniform in texture and appearance.

- Flatness: Grade A.

#### Floor finish dividers

Finish cementitious toppings at junctions with differing floor finishes with a corrosion resistant metal dividing strip suitable fixed to the background, with top edge flush to the finished floor. If changes of floor finish occur at doorways make the junction directly below the closed door.

#### Monolithic toppings

Coved skirtings: Form coves in the topping material, and finish the top to a neatly struck line. Mitre internal and external angles.10 mm radius to top of skirting. 25mm radius to junction between floor and skirting.

#### Movement control joints

This is a default only, in the absence of further consideration. Joints should be detailed and the arrangement shown on the drawings.

Provide movement control joints to divide toppings into bays as follows

- Form in situ using square edge steel forms and trowelling a 3 mm radius to edges.

- Form a groove, extending at least one quarter the depth of the section, either by using a grooving tool, by sawing, or by inserting a premoulded strip.

- Install a movement control joint product.

Bay sizes:

- Area: ≤ 15 m2.

- Length to width ratio: ≤ 1:1.5.

Joints in background: Provide movement control joints in toppings to coincide with joints in the background.

#### Slip-resistance treatment

Stair treads: Form two grooves and fill with a silicon carbide two-part resin.

- Dimensions: 10 mm deep, 15 mm wide, length  width of tread less 100 mm.

- Position:

- First groove: Centre 35 mm from tread nose.

- Second groove: Centre 60 mm from step nose.

Plane surfaces: Apply silicon carbide granules after floating and before the topping surface has set, and trowel into the surface so that the granules remain exposed.

- Application rate: 1 kg/m2 evenly distributed.

#### Surface colouring

Apply the colouring product or coloured marble chips after floating and before the topping surface has set and trowel into the surface so that it is even in colour distribution.

#### Temperature

If the ambient temperature is less than 10ºC or more than 30ºC ensure that the temperature of mixes, backgrounds and reinforcement are, at the time of application, greater than 5ºC or less than 35ºC.

### Completion

#### Curing

General: Prevent premature or uneven drying out and protect from the sun and wind.

Curing: Use a curing product or, as soon as it has set sufficiently, keep the toppings moist by covering with polyethylene film for seven days.

This table lists typical properties of the finished work and the products and/or processes which you may need to specify by defining values for the properties.

You can edit the body of the specification and/or you can provide further information here.

Values can be words or numbers with units. You can have a single column of values or you can have multiple columns to define different 'types' which can then be referenced on schedules and drawings. Use the specification to define one or more types and not to locate or enumerate them – use drawings and schedules to do that.

This single table may be divided into multiple tables if you prefer. It may be used merely as a checklist in which case ensure that essential properties are adequately defined in other documents. You can add or delete rows and columns and edit their names as required.