# Stonework

Worksection application

This worksection is applicable to new dimension stone masonry.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Stone repair for repair and cleaning of existing stone masonry.

- Stone cladding for stone cladding panels that rely entirely on structural fixings for support.

- Stone and terrazzo tiling for internal stone tiling.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Stone carving and monumental masonry.

- Documenting this and related work

- You may document this and related work as follows:

- Designed features.

- Envelope elements on elevations such as banding patterns and changes in textures.

The appointment of a specialist stonework consultant is advisable for all stages of most projects involving stonework design and construction.

For information on thermal mass, refer to BDP EDG Note DES4.

## General

This worksection is aligned to AS 3700, which covers natural stone masonry as well as brickwork and blockwork. AS 3700 deals comprehensively with design, materials, and workmanship, but is oriented towards loadbearing construction, rather than non-loadbearing cladding.

AS 3700 is cited in the BCA for structural sufficiency, for fire-resistance level, and for wall ties in cavity walls for walls between wet areas in adjoining residential units, and for sound transmission.

AS/NZS 4455 covers dimension stone units, up to a point.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- The prepared stone sample range.

- Lintels in position.

- Damp proof courses in position.

Hold points, if required, should be inserted here.

### Tolerances

#### Dimensions of stone units

Maximum deviation from required dimensions:

- Loadbearing stone in cut blocks:  4 mm.

- Other stone used in foundations or not exposed to view: No size requirement unless noted otherwise in this worksection .

## Products

### Natural stone

#### Stone types

Sandstone defects: Minor shale laminates and minor concentrations of carbonaceous material (tea leaves) are acceptable in visible faces. Neither defect is acceptable in carved or moulded work.

Granite defects: Igneous stone (e.g. granite) obtained from quarry stone extracted in blocks sufficiently large to suit the project requirements, and containing no more than a small degree of microcracking.

#### Stone selection

Grading: Select stone of the designated quality grade.

Matching: Within each grade, select stone for the best match of colour and pattern.

#### Source of stone supply

Ensure the stone quarry or supplier can provide all stone required for the project without the need to find alternative supplies.

The supply source should be selected only after comprehensive pre-tender investigations, preferably by the stonework consultant, of potential suppliers’ ability to provide stone of the required type and quality, in the required quantities, in time to meet the construction program, and at an acceptable price. The investigations should include pre-contract testing of stone for the properties required in the project, and examination of the supplier’s quality assurance program.

Delete if no alternative source will be considered.

### Mortar

#### Mortar materials

Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

- White cement: Iron salts content  1%.

- Off-white cement: Iron salts content  2.5%.

Lime: Confirm source of Lime with Employers representative to ensure highest quality Lime is used in the mortar. Protect from damage on site and store minimum 300mm above ground in waterproof storage facility.

Sand: Fine aggregate with a low clay content selected for grading, sharp and free from efflorescing salts. River or pit sand should be sharp, angular, hard, clean uncoated particles free from clay and organic impurities.

Water: Water to be used for the mixing of mortar should be clean and free from oil, acid, alkali, salts, organic materials or other substances that are harmful to the mortar mix.

- Crushed stone: Fine aggregate consisting partly or wholly of crushed stone, made from material of the same type as the stone facing.

The installation of stone tiles or pavers commonly follows the practices outlined in AS  3958..

Measurement of volume: Measure binders and sand by volume using buckets or boxes. Do not allow sand to bulk by absorption of water.

#### Mortar

Standard and ratio of mix for all mortar shall be M-400 (1:3), M-300 (1:4), M-250 (1:5) and M-200 (1:6).Provide minimum water.

Pure white cement is imported, not made in Australia. If required specify as a proprietary item.

State “May” (or may not) “be used”. If premixed mortar is permitted, include “Provide set-retarding chemical agents”.

#### Mortar mix

High strength mortar may be appropriate for granites, weaker for sandstone and limestone. A permeability greater than that of the stone is desirable where there is possibility of salt attack. Specify mortar with required strength and durability. See AS 3700 clause 5.4 for appropriate durability for various exposure conditions classified in Table 5.1.

The M4 group (see AS 3700 Table 10.1) are high strength types; use only for calculated and highly stressed masonry underpinning, etc.

If lime putty is used, make appropriate adjustments for the water content in the putty (and for voids in stiff lime putty), otherwise the lime content of the mortar will be insufficient.

M1 mixes should be used only in restoration work to match existing construction. See AS 3700, Appendix G.

Mortar mixing shall be done in a mechanical mixer unless the Employers representative specifically permits hand mixing. If hand-mixing is done, the operation shall be carried out on a clean watertight platform and cement & sand shall be first mixed dry in the required proportion to obtain a uniform color and then the mortar shall be mixed for at least two minutes after addition of water.

Cement Mortar shall be mixed in such quantities as can be used in the work within 30 minutes. Mortar, which has taken initial set, shall not be used, nor shall it be re-mixed with fresh mortar.

Preparing lime putty:

- Using hydrated lime: Add lime to water in a clean container and stir to a thick creamy consistency. Leave undisturbed for at least 16 hours. Remove excess water and protect from drying out.

- Using quicklime: Run to putty as soon as possible after receipt of quicklime. Partly fill clean container with water, add lime to half the height of the water, then stir and hoe ensuring that no lime remains exposed above the water. Continue stirring and hoeing for at least 5 minutes after all reaction has ceased, then sieve into a maturing bin. Leave undisturbed for at least 14 days. Protect from drying out.

Mortar proportions (cement:lime:sand):As defined on the drawings.

Sand stockpile: Ensure sand is dry and stored undercover to avoid errors in volume batching during the mixing process.

It may not always be possible to stockpile the sand for the whole of the works, as required by the Template. It is necessary to keep the sand dry, because moist sand can cause “bulking” errors in volume batching.

## Execution

Refer to Stonework construction schedule for details of stonework and mortar types.

### Workmanship generally

#### Cutting

Perform the necessary cutting and shaping of stone to designated profiles including weathering, jointing, chasing, forming grooves. Make the bed, face and back joints of the stone square and true where dimensioned stone is required.

#### Carving and moulding

Achieve a clean sharp finish. Carry out all work identified on the drawings to the approval of the Employers representative.

### Laying units

#### Bedding

Remove dust and foreign material from the bedding surfaces. Water the face of the stone units so that full strength joints are achieved. Where possible, bed and joint the stone in one operation. Lay each stone on a full bed of mortar. Solidly fill and grout vertical joints as the work proceeds. Point up joints around flashings as necessary.

#### Natural bed

Obtain specialist advice on local stone characteristics, which may require departures from the Template requirements for natural bed.

Lay loadbearing sedimentary stone with its natural bed at 90 degrees to the load, except for the following:

- Cladding panels: In non-loadbearing cladding panels, form each panel with its natural bed at right angles to the face.

There are many situations where edge bedding is inappropriate. Obtain specialist advice. Specify which stones (if any) are to be edge bedded, or show them as such on the drawings.

#### Temporary support

Provide support as necessary to the stone while the mortar is curing, using bracing, joint spacers, or both.

Bracing and joint spacers: Non-damaging and non-staining softwood wedges soaked in water. Do not allow metal pinch bars to bear directly on the stone.

#### Raking and toothing

Raise advanced work no more than 1.5 m above the general level, and rake back. Do not tooth stonework for subsequent additions except where toothing is shown on the drawings.

#### Bonding

Bond the masonry so as to provide stability and monolithic structural action to the stonework assembly.

### Stone foundations

A typical clause for domestic type construction in limestone or sandstone.

#### Stone footings

AS 2870 is cited in the BCA at clause F1.10 for damp-proofing under slabs on ground.

Construct the footing course entirely of through stones, and if stepping is necessary, overlap the stepped courses at least 300 mm.

#### Subfloor stone foundation walls

Note stone types in Stone masonry schedule.

Minimum foundation wall thicknesses:

- Supporting masonry walls 100 mm thick: 300 mm.

- Supporting masonry walls 250 mm thick: 450 mm.

- Supporting masonry walls 370 mm thick: 600 mm.

Stone sizes:

- Maximum height: 350 mm.

- Minimum height: Generally 175 mm; through stones 300 mm.

Bond pattern: Provide through stones as follows:

- All stones in top and bottom courses.

- Elsewhere as header units.

Slab bearings: Provide continuous bearing at least 100 mm wide to the edge of suspended slabs.

Select from:

- Cast stone to match facings, with bronze wire mesh.

- Terra cotta 230 x 160 mm.

- Bronze wire mesh in a 470 x 160 mm concrete frame.

- 65 mm diameter vitreous clay pipe laid to fall to the outside.

- Galvanized cast iron.

- Other: Nominate.

### Damp-proof courses

#### Material

Material: Embossed Polyethylene sheeting. Install sheeting at base of all walls to stop moisture rising up wall structures.

#### Location

The defaults are not comprehensive. Typical damp-proof course and flashing applications should be shown on the drawings. If they are, delete the following as appropriate. Coordinate damp-proof courses with slip joints and with termite shields.

Provide damp-proof courses as follows:

- Walls built off slabs on ground: In the bottom course of the wall on top of the slab.

- Walls adjoining infill floor slabs: In the course above the slab. Project 40 mm and dress down over the membrane turned up against the wall.

#### Installation

Lay in long lengths. Lap full width at angles and intersections and at least 150 mm at joints. Step as necessary, but not exceeding 2 courses per step. Sandwich damp-proof courses between mortar.

AS/NZS 2904 is cited in the BCA at clause F1.9(b)(i) for damp-proof courses. This clause is varied in SA for salt damp.

Type: e.g. (building regulations may govern):

- Bitumen coated aluminium 0.45 mm (or 0.55 mm) thick, to AS/NZS 2904 (similarly bitumen coated copper, zinc, and lead). Roll labelling is a requirement.

- 0.5 mm annealed aluminium faced both sides with embossed black polyethylene in bitumen (suitable for salt damp conditions).

- Embossed black polyethylene to AS/NZS 2904.

- Aluminium alloy 3203 or 5050A to AS/NZS 1734, 0.6 mm thick.

- Lead to AS 1804, mass 12 kg/m2, etc.

- Bitumen coated DPCs are not suitable where subject to salt attack. Aluminium in contact with wet cement may corrode.

Lead is attacked by free alkali present in portland cement concrete and mortars, the corrosion products being oxides of lead.

Special treatment for severe conditions, e.g. mastic sealing, or pop riveting laps in metal materials.

### Jointing and pointing

#### Joints

Size (mm): Not less than 3mm or more than 5mm for dimensioned stonework. Size may vary for non dimensioned stonework from 10mm to 30mm. Joint size should not exceed this without approval of the Employers representative.

Jointing material: Mortar with a strength less than the stonework. Lime putty where identified on drawings for special dimensioned stonework.

Pointing material: Coloured mortar or mortar as above, refer to Schedule or drawings. Lime putty where identified on drawings for special dimensioned stonework.

### Sealant jointing

#### Preparation for jointing

Immediately before jointing remove loose particles from the joint, using brushes or compressed air.

#### Taping

Protect the stonework surface on each side of the joint using 50 mm wide masking tape or equivalent means. On completion of pointing remove the tape and remove any stains or marks from the stonework surface.

#### Jointing materials

Use recommended jointing and pointing materials which are compatible with each other and with the contact surfaces and non staining to finished surfaces.

Priming: Apply the recommended primer to the surfaces in contact with sealant materials.

Sealant colour: Refer to Schedule or drawings.

Foamed materials (in compressible fillers and backing rods): Closed cell or impregnated types which do not absorb water.

#### Sealant application

Apply the sealant to dry joint surfaces. Do not apply the sealant in unsuitable weather conditions (e.g. when the ambient temperature is outside the range 5 – 50C) or outside the recommended working time for the material or the primer.

#### Joint finish

General: Produce a smooth, slightly concave surface using a tool designed for the purpose.

### Completion

#### Cleaning

Cleaning: Leave the stonework clean on completion.

Refer to the Stonework construction schedule and drawings for details of locations, types and extent of built in components.