# pavers – sand bed

Worksection application

This worksection is applicable to proprietary clay and concrete segmental paving on sand bedding for use in vehicular pavements, footpaths and landscaped areas.

This worksection does not apply to industrial pavements, or to public roads and streets.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Segmental pavers – mortar bed.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Earthwork.

- Pavement base and subbase.

- Pavement ancillaries.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- None.

- Documenting this and related work

- You may document this and related work as follows:

- Show laying pattern and extent on the drawings.

- Specify proprietary paver and traffic loading capacity on the drawings.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

From AS 2870 clause 2.1 and AS 3727 clause 3. Edit  to suit the project or deleted if not required.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Completed base preparation.

- Completed trial set-out for segmental paving.

Hold points, if required, should be inserted here.

### Tolerances

#### Tolerances

Conform to the Surface level tolerances table:

#### Surface Level Tolerances Table

| Item | Level tolerance |  |
| --- | --- | --- |
|  | Absolute | Relative |
| Vehicular pavements | ± 10 mm | 10 mm |
| Footpaths | ± 10 mm | 5 mm |

## Products

### Materials

See the Commentary on materials and maintenance.

#### Bedding sand

Grading: All sand must pass through a sieve with 2.0mm apertures.

Moisture content: Uniform in moisture content with spread.

Deleterious material: Free of deleterious material, such as soluble salts which may cause efflorescence.

Coordinate with Bedding sand/Grading. Complete if those requirements are insufficient. More detailed grading tables for bedding materials are available from the Clay Brick and Paver Institute (CBPI) and the Cement and Concrete Association of Australia (CCAA).

#### Joint filling sand

Grading: All sand must pass through a sieve with 1.0mm apertures.

Moisture content: The sand shall be dry when spread.

Deleterious material: Free of deleterious material, such as soluble salts which may cause efflorescence.

### Components

#### Concrete and clay segmental paving units

Provide labelled samples of all pavers for approval of the Employers Representative prior to use. Ensure that the horizontal dimensions of each paver have a maximum variation of 3mm in 300mm. Any pavers outside this tolerance will be rejected and removed from the site. Ensure that all pavers are free from fault lines, cracked edges, surface flakes, mould marks or other defects before use.

#### Stone paving units

Provide labelled samples of all pavers for approval of the Employers Representative prior to use. Ensure that all stone pavers are free from fault lines, cracked edges, surface flakes or other defects before use.

## Execution

Refer to Paving schedule for details of pavers and bedding.

### Subgrade preparation

#### General

The subgrade shall be prepared in accordance with the Earthwork worksection.

### Subbase and base

#### General

The subbase and base shall be prepared in accordance with the Pavement base and subbase worksection.

### Bedding sand

#### General

Preparation: Remove all loose material from the prepared base.

Spreading: Screed uncompacted sand over prepared base in a uniform manner to achieve a 30 mm thick layer. Maintain sand at a uniform loose density.

### Laying paving

#### General

Pattern: Paving units are to be laid on the screeded sand bedding to the nominated pattern shown on the drawings.

Joints: Paving units are to be laid with a 2 – 3 mm gap between adjoining units.

Cut courses: Do not use cut units with a plain dimension of less than 50 mm.

Control joints: Where paving units are to be placed over control joints in an underlying concrete base, a joint is to be provided in the pavers. The joint shall be 10 mm wide and filled with approved jointing material.

### Compaction of bedding

#### General

After laying of the paving units the sand bedding shall be fully compacted using a vibrating plate compactor.

Joint filling: All paving units are to be compacted to design levels prior to the commencement of joint filling.

### Joint filling

#### General

Spread dry sand over the paving units and fill the joints by brooming. Undertake one or more passes with the vibrating plate compactor and refill the joints with sand. Repeat the process until the joints are completely filled.

Timing: Fill joints on the same day that pavers are compacted.

### Protection of the work

#### General

Protection: All vehicular and pedestrian traffic shall be prevented from using the pavement until all compaction and joint filling is completed and all edge restraints are in place.

### Cleaning

#### Cleaning

General: Leave pavements clean on completion.

Pavers: Select masonry units and segmental pavers for abrasion resistance, compressive strength, non-slip and weathering properties. For advice on selection, see CBPI Manual 1. Tabulate if more than one type of unit is used. Consult manufacturers for detailed specifications, or specify as proprietary items. The manufacturer’s name and product brand name is usually the best way to specify particular (as distinct from generic) products.

Material: e.g. Clay, cementitious.