# Concrete- finishes

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to the production of formed and unformed finishes to concrete surfaces in building and associated structures. It needs to be used in conjunction with the Concrete in situ worksection, particularly the curing and the completion (surface protection) sections, and the Concrete formwork worksection. The surface finishes dealt with are the more common ones. Project specific finishes not included need to be added.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Shotcrete for shotcrete finishes.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Concrete in situ.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

- None.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- Concrete in situ.

- Concrete formwork.

## General

### Tolerances

#### General

Unformed surfaces: Confirm conformance with the Tolerance classes table for the class of finish nominated using a straight edge placed anywhere on the surface in any direction.

#### Tolerances Class Table

| Class | Measurement | Maximum deviation (mm) |
| --- | --- | --- |
| A | 3 m straight edge | 3 |
| B | 3 m straight edge | 6 |
| C | 600 mm straight edge | 6 |

## Products

### Materials

#### Surface hardeners, sealers and protectors

Supply: If required by the project documentation, provide proprietary products in accordance with the manufacturer’s written requirements.

## Execution

### Surface modifiers

#### General

Application: Apply to clean surfaces in accordance with the manufacturer’s requirements.

### Unformed surfaces

#### General

Screed and level slab surfaces to finished levels, to tolerance class C.

#### Finishing methods

Broom finish: After floating draw a broom or hessian belt across the surface to produce a coarse even-textured slip-resistant transverse-scored surface.

Machine floated finish: After screeding and when the concrete has stiffened sufficiently, work the slab surface using a machine float. Hand float in locations inaccessible to the machine float. Cut and fill to tolerance class B and refloat immediately to a uniform, smooth texture.

Scored or scratch finish: After screeding, give the surface a coarse scored texture using a stiff brush or rake drawn across the surface before final set.

Steel trowelled finish: After machine floating, use power trowels to produce a smooth surface relatively free from defects. Then, when the surface has hardened sufficiently, use steel hand trowels to produce the final finish free of trowel marks and defects, and uniform in texture and appearance, to tolerance class A.

Wood float finish: After screeding, machine produce the final finish using a wood float, to tolerance class B.

#### Polished finishes

Water blast: After steel trowelling, water blast the cured surface to provide texture or to form patterns without exposing the coarse aggregate using medium pressure water jets. Ensure that aggregate is not removed to a depth greater than 10mm.

Applied finish: To a steel trowel finished surface, apply a proprietary liquid or dry shake material in accordance with the manufacturer’s written requirements.

Burnished finish: Continue steel trowelling until the concrete surface attains a polished or glossy appearance.

The range of treatments to achieve and to embellish polished concrete surfaces is large, and includes colouring, texturing, patterning by saw cutting or inlaying of metal or timber strips or of tiles or pavers. The effect required should be comprehensively documented by the architect. Add to the list of polished finishes as necessary.

#### Surface finishes

General: Provide surface finishes in conformance with the Concrete-integral finishes schedule.

### Formed surfaces

#### General

Provide formed concrete finishes in conformance with the Concrete-formed surface finishes schedule.

Damage: Do not damage concrete works through premature removal of formwork.

#### Curing

General: If forms are stripped when concrete is at an age less than the minimum curing period, commence curing exposed faces as soon as the stripping is completed.

Ensure that concrete has adequate strength or is back propped.

#### Finishing methods

If exposed formed concrete elements are to have a finish other than off the form, provide details of proposed procedures. If not identified otherwise, all formed surfaces will be off form finish.

Exposed aggregate finish: Remove the vertical face forms while the concrete is green but set. Wet the surface and scrub using stiff fibre or wire brushes, using clean water freely, until the surface film of mortar is mechanically removed, and the aggregate uniformly exposed. Do not use acid etching. Rinse the surface with clean water.

Floated finishes:

- Sand floated finish: Remove the forms while the concrete is green. Wet the surface and rub using a wood float. Rub fine sand into the surface until a uniform colour and texture are produced.

- Grout floated finish: Remove the forms while the concrete is green. Dampen the surface and spread a slurry, using hessian pads or sponge rubber floats. Remove surplus slurry and work until a uniform colour and texture are produced.

Only the more common finishing methods are listed. Add other project specific requirements (e.g. polished, coloured).

#### Surface repairs

Surface repair method: Before commencing repairs, submit proposals to the Engineer for approval.