# Pavement base and subbase

Worksection application

This worksection is applicable to the supply, spreading, compaction and trimming of base and subbase courses of flexible pavements.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Asphaltic concrete.

- Sprayed bituminous surfacing.

- Concrete pavement.

- Segmental pavers – mortar bed.

- Segmental pavers – sand bed.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Site preparation.

- Earthwork.

- Stormwater – site.

- Pavement ancillaries.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Base and subbase courses in public roads. Where works are to be completed within public roads the relevant government authority specifications and requirements will apply.

- Where bound base and subbase is proposed, consult the engineer.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- Asphaltic concrete.

- Sprayed bituminous surfacing.

- Concrete pavement.

- Segmental pavers – mortar bed.

- Segmental pavers – sand bed.

- Pavement ancillaries.

- Documenting this and related work

- You may document this and related work as follows:

- Base and subbase course thicknesses and levels should be shown on the drawings.

- Design traffic in (ESA’s) to be shown on the drawings.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

The Definitions subclause can be edited to suit the project or deleted if not required.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Prepared sub grade.

- Proof rolling of base prior to sealing.

Hold points, if required, should be inserted here.

### Tests

#### Compaction control tests

The placement and compaction criteria of fill shall be in accordance with K20-1CS.

#### Frequency of compaction control tests

Not less than the following (whichever requires the most tests):

- 1 test per layer per 25 lineal metres for 2-lane roads.

- 1 test per layer per 1000 m2 for car parks.

- 3 tests per layer.

Extract from AS 3798 Table 8.1. The required frequency may need adjustment on large scale projects or confined areas. Where specific recommendations are given in the geotechnical report, for the site, these should replace the extract from AS 3798 Table 8.1 listed above.

## Products

### Base and subbase material

#### General

Base and sub-base materials shall comply with the Base and subbase compliance schedule.

The Base and subbase compliance table is based on the requirements of AUS-SPEC 1. State Road Authority specifications are also commonly used for specification of base and subbase materials but differ from state to state. Modify the compliance requirements as necessary.

## Execution

### Subgrade preparation

#### General

Sub-grade preparation to be undertaken in accordance with the Earthwork worksection.

### Subbase and base compaction

#### General

Compact each layer of fill to the required depth and density, as a systematic construction operation.

Based on AS 3798 Table 5.1. Modify where geotechnical engineer’s requirements differ. Modify to suit locally available materials giving consideration to the potential for some natural materials to break down if over compacted.

Unstable areas: Any unstable areas which develop during rolling or are identified by proof rolling shall be removed for the full depth of the layer and disposed of and replaced with fresh material.

#### Compaction requirements

Apply uniform and sufficient compactive effort over the whole area to be compacted. Use rollers appropriate to the materials and compaction requirements.

“Sufficient compactive effort” implies that compaction will continue until the required density is achieved, or until failure is acknowledged; for the latter case, the subclause Rectification applies.

For critical works, where the method of achieving the performance requirement (i.e. density) cannot be left to the contractor’s discretion, detailed prescription of compaction plant characteristics may be desirable. Standard method of testing may be unsuitable where the materials contain a high proportion of large or “oversize” particles. Consult the engineer.

#### Moisture content

During spreading and compaction, maintain materials at the optimum moisture content to permit maximum compaction of the material.

If the requirements of this worksection are not appropriate other requirements may be specified here. The tolerance of + 1%, - 2% is appropriate for base materials which have been mixed with water in a pugmill before placing on the pavement. However if base materials are placed dry and water is subsequently added, a tolerance of  2% may be used. Alternatively the moisture content limits may be specified by percentage of optimum (e.g. 60% to 90% of optimum).

Spraying: Maintain moisture content. Use water spraying equipment capable of distributing water uniformly in controlled quantities over uniform lane widths.

### Placing base and subbase

#### General

Weak surfaces: Do not place material on a surface which has been so weakened by moisture that it will not support, without damage, the constructional plant required to perform the work.

Spreading: Spread material in uniform layers without segregation.

Moisture content: Maintain wet mixed materials at the required moisture content before and during spreading. Add water to dry mixed materials through fine sprays to the entire surface of the layer after spreading, to bring the material to the required moisture content.

Layer thickness: 150 mm maximum and 75 mm minimum (after compaction). Provide equal layers in multilayer courses.