# Steelwork painting

This worksections is applicable to the surface preparation of and coating application to structural steelwork or steel products using paint coating systems where corrosion protection is appropriate due to climatic or environmental conditions. It can be used for new work and for maintenance painting.

Related material located elsewhere in NATSPEC

This worksection does not apply to coating of steelwork in situations where corrosion protection is necessary nor economically feasible, as would be the case where anticipated corrosion rates are too low to compromise the structure or sacrificial corrosion of sections has been allowed for in the selection of section thicknesses. AS/NZS 2312 Section 1.2 lists typical situations for which coating for corrosions resistance is not required. For these cases use the Structural steel worksection.

For applications where hot dip galvanizing is appropriate refer to and include in the specification the Steel – hot dip galvanized coatings worksection.

Worksections on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Metals and prefinishes for prefinished steel, stainless steel and other metals.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- None.

Worksection cross referencing

Other worksections that reference this worksection are:

- Painting.

## General

The abbreviations subclause can be edited to suit the project or deleted if not required.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Surfaces after preparation prior to application of first coating.

- Coating after application of final coat.

Hold points, if required, should be inserted here.

### Samples

#### Painting and coating colour

Submit a sample of the finished product for each different coating system.

Size of each sample: 200 x 200 mm.

Customise to suit.

## Products

### General

#### General

All protective coatings must be handled, stored, mixed and applied strictly in accordance with the manufacturer’s instructions and Product Data Sheets.

## Execution

### Protection

#### Surroundings

Provide protection of the surroundings to the coating works and ensure that no abrasive, overspray or paint waste debris is released either to air, ground or to any watercourse. Repair or clean damage as appropriate.

#### Contamination

Ensure protection of sensitive items during surface preparation and coating works. Do not permit surface preparation debris to contaminate coated surfaces which are not yet dry, nor cause damage to any other services or equipment.

#### Stacking and handling

Do not stack, handle or transport coated items until the coating has sufficiently cured so as to resist handling actions.

Stack and handle all steelwork using fabric slings or padded chains, used in a manner that ensures that no damage is caused to the coating system. Adopt soft packaging, carpet strips or other deformable materials between all steel items. Do not permit steel to steel contact in any situation.

Water ponding: Stack coated items so that water ponding does not or cannot occur whilst the items are in storage, transport or “lay down”.

#### Repair of coating damage

If damage occurs repair so as to ensure that the full corrosion protection ability of the system is reinstated.

Refer to Commentary.

### Surface preparation

#### General

Coatings shall be applied only to properly prepared and cleaned surfaces.

#### Surface preparation

Ensure all surfaces are free from oil, grease, dirt, bird droppings or any other contaminants, particularly soluble contaminants.

Surface defects: Remove or correct other surface defects, including cracks, laminations, deep pitting, undercutting, weld spatter, slag, burrs, fins and sharp edges.

Remove all weld spatter by grinding or chipping.

#### Priming

Prime coat all surfaces with zinc rich primer on the same day as the completion of surface preparation works. In every case, the specified surface preparation standard, in both cleanliness and profile, shall be evident at the time that the primer coating is applied.

### Coating application

#### General

Apply the coatings in accordance with the Interior and Exterior painting schedules..

#### Final surface preparation or coating application

Limits: If the following climatic/substrate conditions are present do not apply coating:

- The ambient air temperature is below 5°C or above 40°C.

- The substrate temperature is below 10°C or above 35°C.

- The surface to be coated is wet or damp.

Defects: Apply materials so as to produce an even coating free from film defects.

e.g. missed areas, voids, overspray, overbuild, lumps, runs, sags and/or inclusions.

Detail: Stripe coat all welds, bolt holes, sharp edges and difficult to spray areas by brushing in with the prime coat and intermediate coat material prior to the full coating application.

To assist in achieving an adequate coating DFT in these vulnerable areas.

#### Subsequent coats

Ensure that before any subsequent coating layer is applied, the surface condition of the preceding coat is complete and correct in all respects, including its cleanliness and freedom from defects. Correct any defects before the next coating layer is applied.

Emphasise in the contract documents that the coating manufacturer or the owner will not incur any expenses related to any rework due to a failure by the coating contractor to meet the designated acceptance criteria on any surface preparation or coating application deliverable.

The foregoing principally relates to conditions during the night-time after coating application.

Delete either structure or element as appropriate. Copy the schedule blank as required and complete to cover all structures and elements. The surface preparation column is the place to nominate requirements such as soluble salt determination.

Refer to the Commentary for a sample schedule.