# Plastering

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection covers traditional wet plastering and rendering, though proprietary and special systems may feature in the project specifications and drawings. It includes work on lath, and on panelling of various materials.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. See for example:

- Painting for high build finishes.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Brick and block construction.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Trowel applied high build finishes (Granosite).

- Proprietary plastering systems developed for autoclaved aerated concrete products.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Locate plastering systems on drawings and schedules to your office documentation policy.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

- Brick and block construction.

- Painting.

### Interpretation

#### Abbreviations

Created to allow cross-referencing between the Mixes table, Corrosion resistance and durability table and other documentation e.g. finishes schedules.

For the purpose to this worksection the abbreviations given below apply.

- CRF: Cement render – finish.

- CRM: Cement render – medium.

- CRS: Cement render – stronger.

- CRW: Cement render – weaker.

- LF: Lime felting render- weaker.

- GPF: Gypsum plaster – finish.

The Abbreviations subclause can be edited to suit the project or deleted if not required.

### Inspection

#### Notice

Give sufficient notice so inspection may be made of the following:

- Backgrounds immediately before applying base coats.

- Finish treatments before decoration.

Hold points, if required, should be inserted here.

## Products

### Materials and components

#### Accessories

Beads: To be metal proprietary sections manufactured to be fixed to backgrounds and/or embedded in the plaster to form and protect plaster edges and junctions.

The use of admixtures should not be permitted unless there is confidence that there will be an improved outcome. Their use in lieu of suitable sands should be resisted unless no reasonable alternative is available.

#### Aggregates

Sand: To be fine, sharp, well-graded sand with a low clay content and free from efflorescing salts.

See the Commentary on this topic.

#### Bonding products

To be proprietary products manufactured for bonding cement-based plaster to solid backgrounds.

#### Cement

Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

Type GP is a general purpose cement. Other types are defined in the standard and there is a separate standard for masonry cement which contains plasticisers and other additives. The mixes specified here are for Portland cement Type GP. Do not permit the substitution of masonry cement for general purpose cement or of plasticisers for lime without full consideration.

#### Colouring products

To be proprietary products manufactured for colouring cement plaster.

Integral pigment proportion: 5% by mass of cement.

AS 2185 and AS 2590 are now made obsolescent, but still available.

#### Curing products

To be proprietary products manufactured for use with the plaster system.

#### Gypsum plaster

To be a proprietary product containing calcium sulfate hemihydrate with additives to modify setting.

AS 2592 is now made obsolescent, but still available.

#### Lime

Confirm source of Lime with Employers representative to ensure highest quality Lime is used in the mortar. Protect from damage on site and store minimum 300mm above ground in waterproof storage facility.

Preparing lime putty:

- Using hydrated lime: Add lime to water in a clean container and stir to a thick creamy consistency. Leave undisturbed for at least 16 hours. Remove excess water and protect from drying out.

- Using quicklime: Run to putty as soon as possible after receipt of quicklime. Partly fill clean container with water, add lime to half the height of the water, then stir and hoe ensuring that no lime remains exposed above the water. Continue stirring and hoeing for at least 5 minutes after all reaction has ceased, then sieve into a maturing bin. Leave undisturbed for at least 14 days. Protect from drying out.

In plastering lime should not be used straight from the commonly available hydrated lime bag. This product is quicklime that had been partially hydrated by addition of water to leave a powder which should be further slaked and allowed to mature as a putty.

#### Mixes

See the Commentary on this topic.

Select a mix ratio to suit the application in conformity to the Mixes table.

Measurement: Measure binders and sand by volume using buckets or boxes. Do not allow sand to bulk by absorption of water.

Plaster mixing: Machine mix for greater than 3 minutes and less than 6 minutes.

Strength of successive coats: Ensure successive coats are no richer in binder than the coat to which they are applied.

#### Mixes Table

| Mix type |  | Application | Upper and lower limits of proportions by volume |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Gypsum | Cement | Lime | Sand |
| Cement render coats in: - Single or multi-coat systems with integral finishing treatments - Base coats in multi-coat systems with cement or gypsum finishes | CRS | Dense and smooth concrete and masonry Thrown finishing treatments Tiled finishes Gypsum finishes Cement finishes | - - | 1 1 | 0 0.5 | 3 4.5 |
|  | CRM | Clay or concrete masonry | - - | 1 1 | 0.5 | 4.5 6 |
|  | CRW | Lightweight concrete masonry and other weak backgrounds | - - | 1 1 |  | 6 9 |
| Cement finish coats | CRF | Cement render base coats | - - | 1 1 | 1 | 1.5 2 |
| Lime felting finish coats | LF | Cement render base coats |  |  | 1 | 3 |
| Gypsum finish coats | GPF | Cement render base coats | 3 1 | - - | 1 1 | - 1 |

#### Movement control joint products

To be proprietary products manufactured for use with the plastering system and to accommodate the anticipated movement of the backgrounds and/or the plaster.

#### Water

To be clean and free from any deleterious matter.

Refer to the Plastering schedule for details of plastering and locations.

## Execution

### Preparation

#### Substrates

Ensure substrates have:

- Any deposit or finish which may impair adhesion of plaster cleaned off.

- If solid or continuous, excessive projections hacked off and voids and hollows filled with plaster stronger than the first coat and not weaker than the background.

Absorbent substrates: If suction is excessive, control it by dampening but avoid over-wetting and do not plaster backgrounds showing surface moisture.

Dense concrete: If not sufficiently rough to provide a mechanical key, roughen by scratching or hacking to remove 2 mm of the surface and expose the aggregate then apply a bonding treatment.

Painted surfaces: Remove paint and hack the surface at close intervals.

Untrue substrates: If the substrate is not sufficiently true to ensure conformity with the thickness limits for the plaster system or has excessively uneven suction resulting from variations in the composition of the background, apply additional coats.

There may be particular locations, or particular types of substrates (e.g. “dense concrete”, “existing brickwork”) required to achieve particular types of plaster finish. Such variations are best minimised. Particular substrate preparation may be required e.g. “Scabbling”, “Bonding treatment”, or a combination of methods. If so, specify them but only if it is certain what is required.

#### Beads

Location: Fix beads as follows:

- Angle beads: At all external corners.

- Drip beads: At all lower terminations of external plaster.

- Mechanical fixing to background: at 300 mm centres.

- Movement control beads: At all movement control joints.

- Stop beads: At all terminations of plaster and junctions with other materials or plaster systems.

#### Bonding treatment

If bonding treatment is required, throw a wet mix onto the background as follows:

- Cement plaster: 1 part cement to 2 parts sand.

- Gypsum plaster: 1 part gypsum to 2 parts sand.

Curing: Keep continuously moist for 5 days and allow to dry before applying plaster coats.

Thickness: From greater than 3mm but less than 6 mm.

Proprietary bonding products may also be specified or approved.

#### Embedded items

If there are water pipes and other embedded items, sheath them to permit thermal movement. Ensure embedded items will have a suitable level of corrosion resistance prior to embedment.

### Application

#### Plastering

General: Provide plaster finishes as follows:

- Resistant to impacts expected in use.

- Free of irregularities.

- Consistent in texture and finish.

- Firmly bonded to substrates for the expected life of the application.

- As a suitable substrate for the nominated final finish.

Base coats: Scratch-comb each base coat in two directions when it has stiffened.

See the Commentary on this topic.

#### Finishing treatments

Plain:

- Bag: To be a finish mainly free from sand by rubbing the finish coat with a Hessian pad when it has set firm.

- Carborundum stone: To be a smooth finish free from sand by, rubbing the finish coat with a fine carborundum stone when it has set hard.

- Steel trowel: To be a smooth dense surface by steel trowelling which is not glass-like and is free from shrinkage cracks and crazing.

- Wood or plastic float: To be an even surface by wood or plastic floating the finish coat on application.

#### Incidental work

Return plaster into reveals, beads, sills, recesses and niches. Plaster faces, ends, and soffits of projections in the background, such as string courses, sills, and other wall features. Trim around openings. Plaster exposed inside of built-in cupboards.

#### Joining up

If joining up is required, ensure joints will not be visible in the finished work after decoration.

#### Movement control joints

Provide movement control joints in the finish to coincide with movement joints in the background. Ensure that the joint in the background is not bridged during plastering.

- Depth: Extend the joint right through the plaster and reinforcement to the background.

- Width: 3 mm, or the same width as the background joint, whichever is greater.

Damp-proof courses: Do not continue plaster across damp-proof courses.

V-joints: Provide V-joints, cut right through the plaster to the background, at the following locations:

- Abutments with metal door frames.

- Abutments with other finishes.

- Junctions between different backgrounds.

Describe or detail joints and locate them on elevations.

#### Plaster thickness

Conform to the Plaster thickness table.

#### Plaster Thickness Table

| Plaster | Application | Upper limit of thickness (mm) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Single coat systems | Multi-coat systems |  |  |
|  |  |  | Base coat(s) | Finish coat | System |
| Cement render base coats and cement or gypsum finish coats | On smooth dense concrete | 12 | 10 | 4 | 13 |
|  | On clay and concrete brickwork and other backgrounds | 15 | 13 | 4 | 16 |

#### Temperature

If the ambient temperature is less than 10ºC or more than 30ºC ensure that the temperature of mixes, backgrounds and reinforcement are, at the time of application, greater than 5ºC or less than 35ºC.

See the Commentary on this topic.

### Tolerances

#### General

Conform to the Tolerances table.

#### Tolerances Table

| Property | Tolerance criteria: Permitted deviation (mm) |
| --- | --- |
| Features1: Verticality in 2000 mm | 3 |
| Features: Horizontality in 2000 mm | 3 |
| Soffits: Horizontality in 2000 mm | 5 |
| Walls: Verticality in 2000 mm | 5 |
| Walls: Flatness2 in 2000 mm | 4 |
| 1 Features: Conspicuous horizontal or vertical lines including external corners, parapets, reveals, heads, sills, movement control joints and mouldings. |  |
| 2 Flatness: Measured under a straightedge laid in any direction on a plane surface. |  |

Note the distinction between features and plane surfaces such as walls and soffits.

### Completion

#### Curing

General: Prevent premature or uneven drying out and protect from the sun and wind.

Keeping moist: If a proprietary curing agent is not used, keep the plaster moist as follows:

- Base coats and single coat systems: Keep continuously moist for 2 days and allow to dry for 5 days before applying further plaster coats.

- Finish coats: Keep continuously moist for 2 days.

This schedule lists typical properties of the finished work and the products and/or processes which you may need to specify by defining values for the properties.

You can edit the body of the specification and/or you can provide further information here.

Values can be words or numbers with units. You can have a single column of values or you can have multiple columns to define different 'types' which can then be referenced on schedules and drawings. Use the specification to define one or more types and not to locate or enumerate them – use drawings and schedules to do that.

This single table may be divided into multiple tables if you prefer. It may be used merely as a checklist in which case ensure that essential properties are adequately defined in other documents. You can add or delete rows and columns and edit their names as required.