# Brickwork

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to unreinforced, reinforced and prestressed masonry for manufactured units of clay, calcium silicate and concrete laid in mortar and for autoclaved, aerated concrete (AAC) units laid in thinbed mortar, and used in building and related construction. It includes built-in items such as ties and lintels.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Monolithic stabilised earth walling.

- Earth block walling.

- Stone masonry.

- Flooring and decking.

- Roofing.

- Partitions – brick and block, for interior fitout masonry walls.

- Plastering.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- Partitions – brick and block.

- Documenting this and related work

- You may document this and related work as follows:

- If durability, (lateral) stability or fire resistance are issues, ensure that they are properly dealt with in the drawings.

## General

Familiarity with this standard is essential.

Design to AS 3700 is assumed not to be the contractor’s responsibility. Therefore it is essential that the drawings indicate the design requirements for the masonry elements, including dimensions, strength and fire resistance rating.

Only particular requirements for the project should be added to this specification.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Set out of brickwork to lintels, arches and other architectural features.

- Damp-proof courses, in position.

- Lintels, in position.

Add Hold points, if required.

## Products

### Materials

Only particular requirements for the project should be added in the project specification. See AS 3700 clause 1.4. The standard contains defaults which should be adequate for most small-works masonry.

#### First Class Bricks

First Class Bricks shall be made from good brick earth free from saline deposits, and shall be sand molded. They shall be thoroughly burnt by coal without being vitrified, of uniform and good color, shall be regular and uniform in size, shape and texture with sharp square edges and parallel faces. They must emit a clear metallic ringing sound when struck one against another. They shall be free from flaws, cracks, chips, stones, and nodules of lime or canker. A First Class Brick shall not absorb more than 1/6th of its weight of water after being soaked for one hour.

#### Second Class Bricks

Second Class Bricks shall be as well burnt as First Class or may be slightly over burnt but not vitrified, and must give a clear ringing sound when struck one against another. Slight irregularities in size, shape or color are acceptable provided irregular or uneven courses do not result. Second Class Bricks may have slight chips or flaws but must be free from lime or canker nodules. They shall not absorb more than 1/4th of their weight of water after being soaked for one hour.

#### General

Machine made pressed bricks shall be standard commercial products. The Employers Representative prior to use in the Works shall approve the use of machine made pressed bricks.

Bricks not meeting the above requirements shall not be used in brickwork.

First and Second Class Bricks should have the following dimensions after burning: 250mm x 120mm x 70mm. The unit weight of First and Second Class Bricks shall not be less than 1100 kg/m3.

The crushing strength of bricks shall be tested in a laboratory. The average crushing strength of First and Second Class Bricks shall not be less than 17MPa (N/mm2).

At the start of the works samples of the bricks shall be tested for crushing strength and water absorption, and brickwork shall only commence when the Employers Representative has approved the bricks. The Contractor may then only change the source of supply of bricks after samples from the new supplier have similarly been tested and approved.

Brick growth is a particular problem with polychromatic brickwork – detail accordingly. See also RAIA Advisory Note AN14.01.602.

#### Mortar materials

Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

- White cement: Iron salts content  1%.

- Off-white cement: Iron salts content  2.5%.

Lime: Confirm source of Lime with Employers Representative to ensure highest quality Lime is used in the mortar. Protect from damage on site and store minimum 300mm above ground in waterproof storage facility.

Sand: Fine aggregate with a low clay content selected for grading, sharp and free from efflorescing salts. River or pit sand should be sharp, angular, hard, clean uncoated particles free from clay and organic impurities.

Water: Water to be used for the mixing of mortar should be clean and free from oil, acid, alkali, salts, organic materials or other substances that are harmful to the mortar mix.

The installation of stone tiles or pavers commonly follows the practices outlined in AS  3958..

Measurement of volume: Measure binders and sand by volume using buckets or boxes. Do not allow sand to bulk by absorption of water.

#### Mortar

Proportioning: Standard and ratio of mix for all mortar shall be M-400 (1:3), M-300 (1:4), M-250 (1:5) and M-200 (1:6).Provide minimum water.

Edit to the mortar mixes required for the project, and schedule the location where each is to be used.

Thin bed mortars for AAC are proprietary materials purpose-made, and so not covered by this table.

### Components

Alternatively, bitumen coated aluminium, copper or copper alloys, lead or zinc sheeting.

This is a common size - they weigh 14 – 16 kg each. CSIRO Bulletin 5 clause 5.2 recommends length 1.5 x width. The recommended upper limit for safe manual handling is 16-20 kg (See NOHSC 2005 National Code of Practice for Manual Handling). Size chosen should suit wall thickness, bearing in mind that thick walls can be made using thin blocks.

CSIRO Bulletin 5, Boulder, AEBH, CSI and New Mexico concur. Except that New Mexico sets a maximum length of 50 mm. CSIRO Bulletin 5 clause 2.4.2 stipulates a maximum depth of 5 mm in one place, and 10 mm in another. The text defaults to the more stringent.

#### Nailing blocks

Solid timber, or hollow timber box filled with earthen mortar. Timber unseasoned or thoroughly pre- wetted.

For partitions, and for door and window jambs, cabinets etc. See CSIRO Bulletin 5 figure 1.6 for alternatives. Use of moist timber overcomes problems with timber expanding in situ.

#### Steel components, including reinforcement

All steel components to be galvanised for maximum durability after incorporation into the structure.

AS 3700 clause 5.5, Table 1 defines ratings R0 – R4. Vary to suit.

Or ladder type, according to CSI. Only required in non-earthquake areas. Delete accordingly.

Preferably show any required reinforcement on the drawings.

#### Window and Door lintels

Lintels: Use steel, concrete or timber lintels in accordance with the manufacturers’ technical literature or conform to the Steel angle and T-lintels table.

Preferably show on the drawings and delete this subclause.

Lintels may also be reinforced concrete, reinforced masonry, epoxy-coated steel, or treated/durable timber.

As an alternative to individual lintels, use a continuous reinforced concrete lintel all around the building e.g. in cyclonic or earthquake-prone areas. Show on the drawings.

#### Steel Angle and T-lintels Table

| Maximum span (mm) | Wall height above  600 mm |  |  | Wall height above > 600 mm,  1800 mm |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Angle lintel size | T-Lintel dimensions: H x W x T (mm) | Bearing min. (mm) | Angle lintel size | T-Lintel dimensions: H x W x T (mm) | Bearing min. (mm) |
| 1000 | Two 75 x 50 x 5 Unequal angles | 81 x 150 x 6 | 100 | Two 125 x 75 x 8 Unequal angles | 136 x 150 x 6 | 200 |
| 2000 | Two 100 x 75 x 6 Unequal angles | 136 x 150 x 6 | 150 | Two 150 x 90 x 8 Unequal angles | 156 x 150 x 6 | 200 |
| 2400 | Two 125 x 75 x 8 Unequal angles | 156 x 150 x 6 | 150 | Two 150 x 90 x 10 Unequal angles | 160 x 150 x 10 | 250 |
| 2800 | Two 150 x 90 x 8 Unequal angles | 158 x 150 x 8 | 200 | Two 150 x 100 x 10 Unequal angles | 210 x 200 x 10 | 300 |
| 3000 | Two 150 x 90 x 10 Unequal angles | 160 x 150 x 10 | 200 | Two 150 x 100 x 12 Unequal angles | 210 x 200 x 10 | 300 |

The table assumes that the lintels are in walls as follows:

- 400 mm maximum thick.

- Upper storey or single storey openings.

- In non-cyclone areas.

- Supporting ceiling/roof framing of span less than 8 m with combined dead and live load not exceeding 1.15 kPa.

#### Timber lintels

Size: Width of the wall and in conformance with the Timber lintels height table.

Grade: Best quality of imported Russian timber or suitable approved local timber.

Bearing: 300 mm (minimum).

#### Timber Lintels Height Table

| Maximum span (mm) | Lintel height (mm) |
| --- | --- |
| 1200 | 150 |
| 1800 | 150 |
| 2400 | 200 |
| 3000 | 250 |

Assumed conditions for timber lintels are:

- Upper or single storey construction in non-cyclonic wind speed area.

- Light timber roof of maximum span no greater than 8 m.

- Extent of earth wall above lintel no greater than 600 mm.

- No openings in earth wall directly above lintel.

- Lintel subject to uniformly distributed loads only.

#### Timber fixing plates

Size: 200 x 50 mm (minimum).

#### Holding-down bolts

Type: 10 mm diameter threaded rod.

See CSIRO Bulletin 5 Figure 1.4 for alternatives. Design required for earthquake and cyclonic conditions.

The BCA Housing Provisions limit earthwalls to design wind speed W41, and to earthquake design category H1 and H2.

Termination: Horizontal 5 x 100 x 200 mm steel plate, weld-fixed, or with nuts.

Vary to suit.

Depth of embedment:

- Length (minimum): 450 mm.

## Execution

Refer to Brickwork construction schedule for details of brickwork and mortar types.

### General

#### General

Construction of masonry brickwork shall not commence until the Employers Representative has accepted the footings on which it is to be placed.

Brickwork shall be built plumb, curved or battered as shown on the Drawings or as may be required, by skilled masons and properly supervised workmen. Bricks shall be clean and if necessary, they shall be scrubbed. Bricks shall be soaked in water for at least one hour before use.

Unless otherwise specified bricks shall be laid in English Bond, with frogs downward. All horizontal joints shall be parallel and level. Vertical joints in alternate courses shall come directly over one another. Joint thickness shall be 6mm and shall in no case exceed 8mm. The height of four courses including 4 bed joints shall rise 300mm. Set out brickwork with joints of uniform width and minimise cutting of masonry units.

Walls shall always be carried up regularly along their entire length unless otherwise directed by the Employers Representative.

#### Mortar mix

High strength mortar may be appropriate for granites, weaker for sandstone and limestone. A permeability greater than that of the stone is desirable where there is possibility of salt attack. Specify mortar with required strength and durability. See AS 3700 clause 5.4 for appropriate durability for various exposure conditions classified in Table 5.1.

The M4 group (see AS 3700 Table 10.1) are high strength types; use only for calculated and highly stressed masonry underpinning, etc.

If lime putty is used, make appropriate adjustments for the water content in the putty (and for voids in stiff lime putty), otherwise the lime content of the mortar will be insufficient.

M1 mixes should be used only in restoration work to match existing construction. See AS 3700, Appendix G.

Mortar mixing shall be done in a mechanical mixer unless the Employers Representative specifically permits hand mixing. If hand-mixing is done, the operation shall be carried out on a clean watertight platform and cement & sand shall be first mixed dry in the required proportion to obtain a uniform color and then the mortar shall be mixed for at least two minutes after addition of water.

Cement Mortar shall be mixed in such quantities as can be used in the work within 30 minutes. Mortar, which has taken initial set, shall not be used, nor shall it be re-mixed with fresh mortar.

Preparing lime putty:

- Using hydrated lime: Add lime to water in a clean container and stir to a thick creamy consistency. Leave undisturbed for at least 16 hours. Remove excess water and protect from drying out.

- Using quicklime: Run to putty as soon as possible after receipt of quicklime. Partly fill clean container with water, add lime to half the height of the water, then stir and hoe ensuring that no lime remains exposed above the water. Continue stirring and hoeing for at least 5 minutes after all reaction has ceased, then sieve into a maturing bin. Leave undisturbed for at least 14 days. Protect from drying out.

Mortar proportions (cement:lime:sand):As defined on the drawings.

Sand stockpile: Ensure sand is dry and stored undercover to avoid errors in volume batching during the mixing process.

#### Protection from contamination

Protect masonry materials and components from ground moisture and contamination.

Other options include English, Flemish, stack, or running 100 mm stagger for AAC units.

Existing work: e.g. “Rod and bond to match existing”.

#### Building in

Embedded items: Build in fixing blocks, brackets, lintels and accessories as the construction proceeds.

Steel door frames: Fill the backs of jambs and heads solid with mortar as the work proceeds.

Heads of some steel door frames may be used as lintels. Consult manufacturer.

#### Joining to existing

If jointing to existing work is required, provide a straight joint. Do not tooth new masonry into existing work.

#### Chasing

Chasing of brickwork shall be to the Brickwork chasing table and subject to the following limitations:

- Parallel chases on opposite faces of a wall shall not be closer than 600 mm to each other.

#### Brickwork Chasing Table

| Brick thickness (mm) | Depth of chase (maximum mm) |
| --- | --- |
| More than 250 thick | 35 |
| 250 thick | 25 |
| 100 thick non load bearing walls only | 20 |

#### Joint finish

Lay brickwork on a full bed of mortar. Fill perpends solid.

Finish:

- Externally: Tool to give a dense water-shedding finish for face brickwork or rake not more than 10mm to give a key for render finish.

- Internally: If wall is to be plastered, rake not more than 10 mm to give a key.

Aerated autoclaved concrete blocks and perforated clay blocks will be to rods other than those listed in the worksection. Refer to manufactured details.

#### Temporary support

If the final stability of the brickwork or blockwork is dependent on structural elements to be constructed after the brickwork, provide proposals for temporary support or bracing for the approval of the Employers Representative.

### Facework

#### Cleaning

General: Clean progressively as the work proceeds to remove mortar smears, stains and discolouration.

AS 3700 clause 11.10 applies. Choice of correct cleaning method is the contractor’s responsibility.

#### Colour mixing

Evenly distribute the colour range of units and prevent colour concentrations and “banding” unless specifically identified as a feature of the brickwork.

Delete or amend if facework commences at a higher level.

Delete if shown on the drawings.

Amend if appropriate.

### Damp-proof courses

#### Damp-proof courses

Material: Embossed Polythene sheeting. Install sheeting at base of all walls to stop moisture rising up wall structures.

See AS 3700 clauses 4.7.3 and 10.6. BCA at clause F1.9(b) permits two options for damp-proof courses – to AS/NZS 2904 or impervious termite shields. This is varied in SA to address the effects of salt damp.

#### Location

The defaults are not comprehensive. Typical damp-proof course and flashing applications should be shown on the drawings. If they are, delete the following as appropriate. Coordinate damp-proof courses with slip joints and with termite shields.

Provide damp-proof courses as follows:

- Walls built off slabs on ground: In the bottom course of the wall on top of the slab.

- Walls adjoining infill floor slabs: In the course above the slab. Project 40 mm and dress down over the membrane turned up against the wall.

#### Installation

Lay in long lengths. Lap full width at angles and intersections and at least 150 mm at joints. Step as necessary, but not exceeding 2 courses per step. Sandwich damp-proof courses between mortar.

Lap sealing: Specify special treatment for severe conditions, e.g. mastic sealing, or pop riveting laps in metal materials.

Wall ties for cavity walls and masonry veneer require design to transfer the appropriate loads, see AS 3700 clauses 4.10 and 7.7.

This table simplifies the requirements of AS 3700.

### Control of movement

Location and details are best shown on the drawings. If they are shown there, delete the following as appropriate.

#### Joints

Provide joints as follows:

- Expansion joints for brickwork:

- Maximum length of continuous wall face: 8 m.

- Closest joint location to external corner: 2.5m

- Maximum vertical spacing: 8 m.

- Width of control joint:  10 mm  20 mm.

- Width of horizontal joint: 15 mm  20 mm.

Filler material: Provide compatible sealant and bond breaking backing materials which are non-staining to masonry.

- Bond breaking materials: To be non-adhesive to sealant, or faced with a non-adhering material.

- Foamed materials: To be closed-cell or impregnated, not water-absorbing.

Preferably show on the drawings.

Joint filling:

- Installation: Clean the joints thoroughly and insert an easily compressible backing material before sealing.

- Sealant depth: Fill the joints with a gun-applied flexible sealant for a depth of at least two-thirds the joint width.

- Refer to the Brickwork construction schedule and drawings for details of locations, types and extent of built in components. Preferably show on the drawings.

AS 4072.1 is cited in BCA at clause C3.15(a), on openings in fire-resistant elements for service installations.

Use the columns A, B and C to schedule type or location. Delete or add columns as required.

Give sufficient information to identify the required unit; or show this information on the drawings. Alternatively refer to approved samples.

Location: e.g. “All masonry”, or “Facework”, “External leaves of cavity walls”, “Internal leaves of cavity walls”, “Internal partition walls”, “Underpinning”, “Work below ground level”. If different types of units are required for different locations, it may be preferable to show the various locations on the drawings.

Characteristic unconfined compressive strength: For engineered masonry, where standard defaults (e.g. AS/NZS 4455 clause 2.3) are inadequate; a certificate may be required.

Category: To AS 3700 clause 1.5.2.22(a).

Type: To AS 3700 clause 1.5.2.22(b).

Name or type: Verify that the nominated manufacturer can supply the selected bricks or blocks in the necessary quantities, including purpose-made specials if required, in time to meet the construction program. Alternative sources may be given where practicable.

Work size: Commonly 230 x 110 x 76 mm for bricks and 390 x 190 x 190 mm for blocks, but many other sizes are available (e.g. for blocks: 90, 140 and 290 mm thick). For AAC blocks and perforated clay blocks, check with manufacturers. For AAC units the wall blocks are all 200 mm high and 600 mm long - thickness ranges from 75 to 300 mm.

Unit joints: “Ironed with a 12 mm diameter rod”, “Cut and struck”, “Weatherstruck”, “Flush jointed”, “Raked out 5 mm deep and ironed square (or half round)”, “Broomed”, “To match existing”, or “As shown on the drawings”, etc. Raked joints are generally not recommended. The exposed mortar face should be compressed. Tuck pointing, if required, should be clearly specified.

Damp-proof course type: e.g. Bitumen coated and flashing material, metal, polyethylene, see AS/NZS 2904 clause 7.

Salt attack resistance category: e.g. Exposure, General purpose or Protected as described in AS/NZS 4456.10 Appendix A.

BCA Housing Provisions Figure 3.3.3.5 has acceptable steel lintel sizes in domestic situations.

Lintel types include steel, precast reinforced concrete or prestressed concrete and reinforced terra cotta.

Precast proprietary concrete lintels are also available and may be specified as an alternative to steel.

Consult the structural engineer before using proprietary lintels with concrete or calcium silicate bricks, or clay bricks with more than 25% perforation.

If proprietary lintels are required, specify. Heads of some steel door frames may be used as lintels. Consult manufacturer.

Lintel type: e.g. steel angle or product name.