# Light timberwork

Worksection application

This worksection is applicable to light timber framing where particular project specific requirements (generally outside the scope of AS 1684) need to be met.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Structural timber.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Proprietary components or systems installed in accordance with the manufacturer’s published requirements.

- Members and systems covered by industry accepted published tables.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- Structural timber.

- Documenting this and related work

- You may document this and related work as follows:

- Where light timber members outside the scope of AS 1684 are being used for structural framing, it is important that the structural drawings either define performance criteria (loading, deflection, exposure) or detail the member sizes and the connection details. If the former is adopted, independent certification by a professional engineer of the design and documentation, and of the erected framing, are appropriate.

- Specify light timber members used in non-load bearing partitions as in the Partitions – framed and lined worksection.

- Show on the drawings any further special requirements.

## General

See SAA HB108 and SAA SEM148 for guidance and commentary on AS 1720.1.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Timber framing after erection before lining or cladding.

- Roof framing and connection to wall and ceiling structures.

If independent certification is being required, delete this clause.

Hold points, if required, should be inserted here.

### Submissions

#### Design

The Contractor is to confirm that all proposed member sizes are available for the project in accordance with the drawings and BOQ. If selected sizes are not available, seek alternatives and obtain approval from the Employers representative.

Delete if not required.

## Products

### Timber

#### Timber grades

Structural timbers:

- Appearance grade if exposed to view in the finished work:
Use best quality timber free from twists, knots, splits and other visual or physical defects.

- Structural grade if concealed in the building:

- Lower quality timber with some visual defects are acceptable but with minimal physical defects.

If a particular authority is to be used, name it here. Forestry departments in each state usually offer timber inspection services.

### Sheet products

#### Structural plywood panels

All structural plywood panels used for construction purposes are to be approved by the Employers representative. Refer to drawings and BOQ for details of locations and sizes. All structural plywood is to be tested before use to the satisfaction of the Employers representative to ensure that it will be suitable for the proposed use.

Use branded or certified plywood products where possible.

Plywoods sourced in Queensland are generally made from hoop and slash pine. Radiata pine is the main timber used elsewhere in Australia. Imported plywoods may well contain rainforest timbers. For bracing see Sections 8 of AS 1684 parts 2, 3 and 4.

“F7”, “F8”, “F11”, “F14”, “F17”, “F22”, “F27”, “F34”.

#### Hardboard or fibreboard panels

All hardboard or fibreboard panels used for construction purposes are to be approved by the Employers representative. Refer to drawings and BOQ for details of locations and sizes. All material is to be tested before use to the satisfaction of the Employers representative to ensure that it will be suitable for the proposed use.

Use branded or certified products where possible.

L, M or H, low, medium or high bending strength.

### Components

#### Steel post bases

Alternative engineered designs are of course acceptable. Amend as required.

Minimum dimensions:

- Stirrup: 75 mm wide x 6 mm thick.

- Dowel: 20 mm diameter heavy tube.

Location: To timber posts supported off concrete slabs or footings.

Finish: Galvanize after fabrication.

#### Fasteners

Material:

Use best quality steel bolts, washers and nuts for bolted connections. Washers to be used both sides of timber to avoid crushing of the timber at the connection point.

Use best quality screws to avoid damage to screw heads during tightening process.

Use best quality bright steel nails for internal work protected from the weather and galvanised nails for external fixings exposed to the weather.

Lightweight allow bolts and screws will not be permitted.

Do not use steel or copper nails in western red cedar exposed to weather or dampness. Specify aluminium, galvanized, or silicon bronze nails. Silicon bronze fasteners, not galvanized steel, are recommended for CCA treated timbers. Many other timbers, if moist, will corrode steel fasteners.

Installation: Pre drill holes in hardwood timber to avoid splitting the timber.

Do not split or otherwise damage the timber or fastener by hammering bolts or screws into the timber.

Refer to AS/NZS 2904, e.g. “Bitumen coated aluminium 0.5 mm thick” (or similarly coated copper or lead), “Aluminium 0.6 mm thick”, “Copper 0.5 mm thick”, “Zinc 0.7 mm thick”, “Lead 20 kg/m2”.

Standard finish is fine sawn. Specify “Sanded finish” if required.

## Execution

### General

#### Protection from weather

General: Provide temporary protection for members until permanent covering is in place.

### Floor framing

#### Bearers and joists

For timber floors supporting tiled finishes it is recommended joists be 20% over sized. (BRANZ Good Tiling Practice)

Levelling: Level bearers and joists by packing for the full width of the member.

Joints: Locate joints only over supports:

- Minimum bearing of bearers: 50 mm.

- Minimum bearing of joists: 30 mm.

Fixing: Secure bearers and joists to supports to provide restraint against lateral movement.

Joist restraint: If joist timber is unseasoned, the span  3000 mm, provide solid blocking between each joist in rows at 1800 mm centres and at the ends of the joists over the supports.

- Members: Provide bearers and joists where shown on the drawings and in the BOQ.

#### Flooring

- Provide flooring of structural plywood where shown on the drawings and in the BOQ.

### Roof and ceiling framing

#### Wall plates

Fix timber wall plates to top of masonry walls with either straps or bolts, or provide fixings cast into the ring beam as required.

Check with the local authority for additional requirements.

#### Ceiling framing

- Construct timber framed ceilings where shown on drawings with battens fixed to underside of trusses or ceiling joists as required.

#### Additional support

Provide a frame member behind every joint in fibre cement sheeting or plywood lining to ensure that the lining is fully supported.

#### Roof cladding boards

Provide roof cladding boards minimum of 20mm thick to full extent of roof structure to support flat metal sheet roofing where shown on drawings. Securely fix to structure and ensure that the top surface is as smooth as possible to avoid damage to the roof sheeting.

AS/NZS 4200 Parts 1 and 2 are cited in the BCA at clause F1.6, for sarking-type materials.

### Trusses

If the contractor is not required to design the trusses, provide the necessary detail drawings including bracing and fixing details.

#### Installation

Where trusses are exposed, consider whether stricter tolerances on straightness and plumb are necessary.

General limitations of AS 4440 include:

- Residential and light commercial structures.

- Rectangular plans or combinations of rectangular with:

.	-	Maximum roof pitch of 45.

.	-	Maximum truss span 16 m.

.	-	Maximum truss spacing of 900 mm, or 1200 mm for sheet metal roofs in area of design wind classification N3 or lower.

.	-	Maximum design gust wind speed of 74 m/s (wind classification C3) for ultimate limit state method.

Support: Support trusses on bottom chord at two points only, unless designed for additional support.

Plumb: Within H/200, where H is the height.

Vertical movement: Over internal walls provide at least 10 mm vertical clearance and use bracing methods which allow for vertical movements.

Construction: Construct trusses strictly in accordance with the drawings. If variations are proposed due to construction fabrication or installation issues, obtain approval from the Employers representative before changing the design.

### Completion

#### Tightening

Tighten bolts, screws and other fixings so that joints and anchorages are secure at all times.

#### Clean up

Remove all shavings, discarded chips and pieces of timber from the structure during construction and clean up all working areas prior to Completion.