# Painting

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to the in situ application of coating films.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Metals and prefinishes for shop applied paint finishes to services components.

- Timber finishes and treatment for preservative and water repellent treatments.

- Steel – hot dip galvanized coatings or Steel – protective paint coatings for protective coatings to structural steel and to external metal fixtures.

- Floor sanding and finishing for clear finishes to timber floors.

Worksection(s) on which this worksection relies

The following worksections must be included, if this worksection is used, to provide a complete specification:

- General requirements.

Associated material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

Worksection cross-referencing

Other worksections that reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Adapt the schedules in Selections to a Finishes schedule to your office documentation policy.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

- Metals and prefinishes for shop applied paint finishes to services components.

- Timber finishes and treatment for preservative and water repellent treatments.

- Steel – hot dip galvanized coatings or Steel – protective paint coatings for the protection of structural steel and external metal fixtures.

- Floor sanding and finishing for clear finishes to timber floors.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the substrate immediately before application of paint finishes.

### Submissions

#### Clear finish coated samples

Submit pieces of timber or timber veneer matching the timber to be used in the works, prepared and coated in accordance with the paint system.

#### Opaque coated samples

Provide approx 600x600mm samples on representative substrates of each paint system showing surface preparation, colour, gloss level and texture.

## Products

### Paints

See the Commentary on paints.

#### Combinations

Do not combine paints from different manufacturers in a paint system.

Clear timber finish systems: Provide only the combinations of putty, stain and sealer recommended by the manufacturer of the top coats.

#### Delivery

Deliver paints to the site in the manufacturer’s labelled and unopened containers.

#### Tinting

Provide only products which are colour tinted by the manufacturer or supplier.

If tinting is by contractor, add tinters or stainers only if this is without detriment to the durability or aesthetic performance of the product.

Appendix P contains three schedules. The first lists toxic pigment components such as barium and cadmium, the second lists toxic solvents, and the third deals with lead. First Schedule paints are banned, in Appendix P, for use on roofs, furniture, fences, and gates, surfaces of non-industrial buildings and in premises used for products intended for human consumption. Third Schedule paints are banned, in Appendix P, from use on roofs, furniture, fences, walls, gates, buildings, bridges and in premises used for products intended for human consumption. Check for any state variations..

#### Putty

Non-timber substrates: Oil-based or polymeric based.

Timber finishes: Lacquer or water based only.

## Execution

### Preparation

Refer to the Commentary on preparation.

#### Order of work

Other trades: Before painting, complete the work of other trades as far as practicable within the area to be painted, except for installation of fittings and laying flooring materials.

Clear finishes: Complete clear timber finishes before commencing opaque paint finishes in the same area.

#### Protection

Fixtures: Remove door furniture, switch plates, light fittings and other fixtures before starting to paint, and refix in position undamaged on completion of the installation.

Adjacent surfaces: Protect adjacent finished surfaces liable to damage from painting operations.

Under no circumstances is the painter allowed to get paint on any surface which is not to be painted. The painter is required to protect all surfaces other than the one which is to be painted immediately, with coverings. These include, but are not limited to: drop cloths, masking tape, plastic sheeting, and paper. No paint may be allowed on glass, stone, floors, stone walls, suspended ceilings, windows or any other surface which is not mean to be painted.

#### “Wet paint” warning

Place notices conspicuously and do not remove them until paint is dry.

#### Restoration

Clean off marks, paint spots and stains progressively and restore damaged surfaces to their original condition. Touch up damaged decorative paintwork or misses only with the paint batch used in the original application.

#### Substrate preparation

Prepare substrates to receive the painting systems.

Cleaning: Clean down the substrate surface. Do not cause undue damage to the substrate or damage to, or contamination of, the surroundings.

Filling: Fill cracks and holes with fillers, sealants, putties or grouting cements as appropriate for the finishing system and substrate, and sand smooth.

Clear finish: Provide filler tinted to match the substrate.

Clear timber finish systems: Prepare the surface so that its attributes will show through the clear finish without blemishes, by methods which may involve the following:

- Removal of discolourations, including staining by oil, grease and nailheads.

- Puttying.

### Painting

Provide coating systems to substrates as follows and as scheduled:

- Consistent in colour, gloss level, texture and thickness.

- Free of runs, sags, blisters, or other discontinuities.

- Fully adhered.

- Resistant to expected impacts in use.

- Resistant to environmental degradation within the manufacturer’s stated life span.

#### Number of coats

Unless specified as one coat or two coat systems, each paint system consists of at least 3 coats comprising priming coat and 2 top coats.

Consider adding a subclause as following:

“Applicator
Certified under the Painting Contractors’ Certification Program, or an approved equivalent”.

The PCCP Scheme, established by APAS, is supported by the Blast Cleaning and Coating Association, the Corrosion Prevention Centre, the Australian Institute of Steel Construction, and the Australian Paint Manufacturer’s Federation. This is likely to be a requirement for public sector projects. There are few certified contractors at present.

#### Drying

Ensure that the moisture content of the substrate is at or below the recommended maximum level for the type of paint and the substrate material.

#### Paint application

Apply the first coat immediately after substrate preparation and before contamination of the substrate can occur. Apply subsequent coats after the manufacturer’s recommended drying period has elapsed.

#### Priming before fixing

Apply one coat of wood primer (2 coats to end grain) to the back of the following before fixing in position:

- Timber door and window frames.

- Bottoms of external doors.

- Associated trims and glazing beads.

#### Spraying

If the paint application is by spraying, use conventional or airless equipment which does the following:

- Satisfactorily atomises the paint being applied.

- Does not require the paint to be thinned beyond the maximum amount recommended by the manufacturer.

- Does not introduce oil, water or other contaminants into the applied paint.

#### Sanding

Clear finishes: Sand the sealer using the finest possible abrasive and avoid cutting through the colour. Take special care with round surfaces and edges.

#### Repair of galvanizing

For galvanized surfaces which have been subsequently welded, prime the affected area.

## Selections

### Paint systems

Alternatives for paint system descriptions are offered as follows:

- By APAS.

- By brand.

Edit as required.

#### Paint system description

Choose from the following paint systems and substrates and paint in accordance with manufacturers recommendations and Interior and Exterior painting schedules:

#### Paint Systems:

Flat water based: Interior

Low gloss water based: Interior

Flat or low gloss water based: Exterior

Semi-gloss water based: Interior

Semi-gloss water based: Exterior

Gloss water based: Interior

Gloss water based: Exterior

Semi-gloss, oil based: Interior

Full gloss, oil based: Interior

Full gloss, oil based: Exterior

Texture finish, water based: Interior

Texture finish, water based: Exterior

Varnish clear: Interior

Varnish clear: Exterior

Varnish tinted: Interior

Opaque timber finish, water based: Exterior

Clear or tinted timber finish, oil based: Interior

Clear or tinted timber finish, oil based: Exterior

Paving paint - Semi gloss oil based

Roofing paint, oil based

Low flame spread specialised coating

Substrate Types:

Existing paintwork (oil based)

Existing paintwork (water based)

Concrete

Cement render

Fibre cement

Brickwork

Stonework

Set plaster

Glass reinforced gypsum plaster

Plasterboard (paper faced)

Iron and steel

Aluminium

Metallic-coated steel

Oil-based air-drying primed metal

Organic or inorganic zinc primed metal

Timber

Particleboard

UPVC

The Painting Schedules refer to the paint system by its final coat. If a paint or clear finish system is referred to by its APAS specification code edit and include the APAS Paint System Tables as appropriate.

The Painting Schedules refer to the paint system by its final coat. If a paint or clear finish system is referred to by the manufacturer’s brand name, create Brand name paint system tables similar to the APAS paint system tables to specify in addition to the final coat, the manufacturer’s appropriate stains, primers, sealers and undercoats, that are suitable for the substrate and compatible with the finish coat and each other.

If a surface is to be painted but no system is nominated select the system from AS/NZS 2311 clause 5.1, using System 1 where a choice is offered.

Specify additional coats if necessary to:

- Prepare porous or reactive substrates with prime or seal coats consistent with the manufacturer’s recommendations.

- Achieve the total film thickness or texture.

- Achieve a satisfactory opacity.

#### Colour selection

See the Commentary on colour selection.

As nominated in the Interior and Exterior painting schedules.

Characteristic: e.g. “Minimum dry film thickness:”, “Texture profile:”, “Gloss level:”. See Paint systems schedules for examples of paint systems to which these additional requirements may apply.

In particular, for Texture finish, latex - interior, and Texture finish, latex - exterior, specify minimum dry film thickness and texture profile. For One pack polyurethane clear - Interior, and Two pack polyurethane clear - Interior, specify gloss level.

Requirements: e.g. for minimum dry film thickness, 300 m; for texture profile, Medium; for gloss level, Flat, Low gloss, Semi-gloss, Gloss or Full gloss.

If the selection is a paint system by brand, modify the APAS table to substitute the manufacturer’s recommendations for the 1st, 2nd, and 3rd coats.