# Concrete - general

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to the use of in situ concrete for building and associated structures. It is the central and core worksection for concrete construction specification, and will almost invariably be used in conjunction with a combination of the related concrete worksections. In the event that related work is so limited as to not warrant a separate worksection parts of related worksections that are applicable should be incorporated into this worksection. For example, surface finishes for a slab on ground may require specification only of a class of finish for formed (edge) surfaces and a flatness class and finish type for the unformed surface. Similarly, formwork may be limited to simple forms.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Concrete formwork.

- Concrete reinforcement.

- Concrete finishes.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

- Worksection cross referencing

- Other worksections that cross reference this worksection are:

- Concrete formwork.

- Concrete reinforcement.

- Concrete post-tensioning.

- Concrete finishes.

## General

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Base or subgrade before covering.

- Membrane or film underlay installed on the base.

- Completed formwork, and reinforcement, cores, fixings and embedded items fixed in place.

- Surfaces or elements to be concealed in the final work before covering.

- Commencement of concrete placing.

### Submissions

#### Products – proposals

Curing compounds: If it is proposed to use a liquid membrane-forming curing compound submit certified test results for water retention.

Curing by the covering sheet method: Submit details of the proposed covering material.

Repair materials: Submit proposals for epoxy resin/grout and elastomeric sealant.

### Tests

#### General

Perform tests of the type and frequency necessary to adequately control the materials and processes used in the construction of the works and in conformance with the Concrete tests table.

Performed by the contractor (or a testing authority appointed by and reporting to the contractor) to maintain control during the course of the works over his materials and processes, independently of compliance assessment testing. It is usual to specify a minimum requirement. The contractor may elect to perform additional tests for his own purposes and at his expense.

#### Compliance assessment tests

Timing: Obtain materials samples at the time of delivery to the site.

Location: Sample from selected sample sites within designated uniform test lots, consisting of an area placed, or compacted or both in one day. Test lots must be uniform in terms of material properties and density.

Specimen type: A set of compression test specimens shall consist of four 200 x 200 x 200 mm cubes, each cube being one specimen.

The specimens within each set shall be tested at the following ages in conformance with the Concrete tests table.

-	One at 7 days for information.

-	Two at 28 days. The 28 day strength shall be taken as the average of the two specimens. If one specimen in this test shows evidence of improper sampling, molding or testing, it shall be discarded. The remaining specimen shall be considered the test result. Should both specimens show the specified defects, the entire test shall be discarded.

-	The fourth shall be retained as a spare to be tested as required.

#### Discharge slump tests

Carry out slump tests at approximately one quarter and three quarter points of the load during discharge.

Working slump: 80mm

Maximum slump: 110 mm. Note concrete with slump greater than this value will be rejected and removed from the site at the contractors cost.

#### Flexural strength assessment of concrete

AS 1379 clause 5.3.1 provides for indirect control of flexural strength by first establishing a relationship between mean compressive strength and mean flexural strength, and then monitoring the mean compressive strength. The worksection provides for direct assessment where this is required.

Acceptance criterion: The average strength of any set of 3 consecutive project samples must not exceed the specified maximum value.

#### Concrete Tests Table

| Samples | ASTM C172 |
| --- | --- |
| Curing | ASTM C31 |
| Testing | ASTM C39 |
| Slump Determination | ASTM C143 |
| Air Content | ASTM C231 or C173 |

## Execution

### Products

#### Reinforcement

All reinforcing shall be supported and wired together to prevent displacement by construction loads, or the placing of concrete, beyond the tolerances specified in ACI 301. Any tack or spot welding of reinforcement shall not be performed without approval from the Employers Representative.

Reinforcement shall be free of loose rust and of any other coating which may adversely affect the bond.

Splices in bar reinforcement shall be located and lapped as shown on the design drawings. Bars in lapped splices shall be in contact unless otherwise shown on the design drawings. Additional splices, if required, shall be made only at locations, and in a manner approved by the Employers Representative. Welded splices shall not be used. All lap splices in bar reinforcement shall be fully in compliance with ACI 318-02.

Welded wire fabric used in concrete paving shall have lapped splices made so that the overlap between the outermost cross wires of each fabric sheet is at least 50 mm.

Unless specifically indicated on the design drawings, splicing by means of proprietary mechanical splices shall not be used.

Concrete spacers, metal or plastic bar spacers i.e. chairs, shall be used for obtaining proper spacing of reinforcement from the bottom and sides of formwork.

Show on the drawings sizes and location of reinforcement and dowels.

#### Dowels

Provide each dowel in one piece, straight, cut accurately to length with ends square and free from burrs. Fix in locations as shown on the design drawings.

#### Formwork

Construct formwork with timber or steel elements to support the concrete for full duration of critical curing period. Construct in a durable manner with sufficient props and fixings to ensure that the formwork remains in position at all times.

#### Aggregate

Aggregate size:

- For fixed form placement: < 40 mm.

- For slip form placement: To be a size compatible with the paving machine.

Washing: Wash aggregate as necessary or as directed to remove significant dust or achieve requirements for soluble salt content or concrete drying shrinkage.

#### Aggregate Sieve Table

| Sive size |  |  | Percent by weight passing |
| --- | --- | --- | --- |
| mm | in |  |  |
| Coarse Sieves |  |  |  |
| 25 | 1 | 90-100 |  |
| 19 | 3/4 | 40-85 |  |
| 12.5 | 1/2 | 10-40 |  |
| 9.5 | 3/8 | 0-15 |  |
| Fine Sieves |  |  |  |
| 4.75 | No. 4 | 95-100 |  |
| 2.36 | No. 8 | 80-100 |  |
| 1.18 | No. 16 | 50-85 |  |
| 600 μm | No. 30 | 25-60 |  |
| 300 μm | No. 50 | 5-30 |  |
| 150 μm | No. 100 | 0-10 |  |

Consider specifying in the Conditions of tendering that tenderers are to nominate their proposed sources of supply, and to supply samples from the sources for testing. Appropriate tests and limits would then be derived for the approved reference samples. Test methods and limits such as those given in AS 2758.1 may not be applicable to material from a particular source. Vary as necessary.

#### Cement

Cement shall conform to the requirements of ASTM specification C-150 Type 1 or similar approved standard for normal Portland cement.

Cement shall be free from any hardened lumps and foreign matter. It shall have a minimum of 90% of particles by weight passing the 75-micron sieve, an initial setting time in excess of 30 minutes and a final setting time of less than 7 hours.

Cement shall be stored in a waterproof shaded area. The cement stacks shall be placed at a minimum distance of 300mm from the walls. The damp proof floor shall be constructed by raising it minimum 300mm above the ground.

#### Curing products

Curing compounds: Obtain approval from the Employers Representative for all curing compounds prior to use.

Covering sheet materials: To be opaque polyethylene film, or burlap-polyethylene sheet, or equivalent material.

#### Concrete

Ready-mixed concrete shall comply with M-150 (1:2:4) for non-reinforced mass concrete and M-200 (1:1.5:3) for reinforced concrete and the requirements of these standards.

On site batch mixed concrete shall have characteristics and proportions of concrete ingredients which conform to those specified in M-150 (1:2:4) and M-200 (1:1.5:3).

Admixtures: Introduce in solution in a portion of the mixing water. Ensure a uniform distribution of the admixture in the batch within the mixing period.

Mixing time: Measure the mixing time after solid materials are in the mixer, provided that mixing water is introduced before a quarter of the mixing time has elapsed. Increase mixing time if necessary to obtain the required uniformity and consistence of concrete. Do not overmix such that additions of water are needed.

See AS 1379 Table A1.

Transport: Transport and discharge the concrete without segregation.

Elapsed delivery time: Discharge truck mixed concrete within a time (t hours) determined as follows, where T is the temperature of the concrete in degrees Celsius:

- t = 2 - 0.05T.

### Polymeric film underlay

#### Location

Provide a vapour barrier under slabs on ground including integral ground beams and footings.

Provision of a vapour barrier for external slabs on ground prevents water loss to the subgrade and has the potential to reduce slab curling at edges and corners.

#### Installation

Lay over the base, lap joints at least 200 mm and seal the laps and penetrations with waterproof adhesive tape. Face the laps away from the direction of concrete pour. Patch or seal punctures or tears before pouring concrete. Cut back as required after concrete has gained strength and forms have been removed.

#### Base preparation

According to base type, as follows:

- Concrete working base: Remove projections above the plane surface, and loose material.

- Graded prepared subgrade: Blind with sufficient sand to create a smooth surface free from hard projections. Wet the sand just before laying the underlay.

## execution

### placing- general

#### Cold weather

Subbase: Ensure that the subbase surface is free of frost.

Cold weather concreting shall be in accordance with the following:

a. The guidelines of ACI 306R shall be followed when the Forecasted Mean Daily Temperature drops below 4°C for three consecutive days. The minimum concrete temperature when delivered at the site shall be in accordance with the Minimum cold weather temperature table.

b. If water or aggregate is heated above 38°C, the water shall be combined with the aggregate in the mixer before cement is added. Cement shall not be mixed with water or with mixtures of water and aggregate having a temperature greater than 38°C.

c. Concrete shall only be poured when the ambient temperature is rising.

d. All concrete shall be insulated from freezing for the greater of following:

1. 	3 days

2. 	Until the concrete reaches an in-place compressive strength of 35 kg/cm2,

e. All materials shall be free from frost.

f. Accelerating admixtures shall not be used without approval from the Employers Representative.

Maintain the concrete at a temperature of at least 10C for at least 24 hours after placing.

#### Admixtures

General: Do not add calcium chloride, salts, chemicals or other material to the mix to lower the freezing point of the concrete.

Minimum Cold Weather Temperature Table

| Air Temperature °C | Minimum Concrete Temperature °C |  |
| --- | --- | --- |
|  | For Sections With Smallest Dimension Less Than 300 mm | For Sections With Smallest Dimension 300 mm Or Greater |
| -1 to 4 | 16 | 13 |
| -18 to -1 | 18 | 16 |
| Below -18 | 21 | 18 |

#### Hot weather

Avoid premature stiffening of the mix and reduce water absorption and evaporation losses. If the temperature of the surrounding air is higher than 32C:

- Mix, transport, place and compact the concrete as rapidly as possible, and cover with an impervious membrane or hessian kept wet until moist curing begins.

- Hold the concrete to a temperature  32C when placed.

Hot weather concreting shall be in accordance with the following:

a. Concrete temperatures shall be kept within desirable limits using methods recommended in ACI 305R.

b. For mass concrete, i.e., concrete sections having a minimum dimension of 750mm or greater, the maximum acceptable concrete temperature is 21°C at time of discharge.

c. For other concrete structures, the maximum acceptable concrete temperature is 32°C at time of discharge.

d. If ice is used as part of the mixing water, mixing should be continued until the ice is completely melted.

e. Retempering shall not increase the water content above that in the mix design.

#### Placing in fixed forms

Place concrete uniformly over the width of the slab and so that the face is generally vertical and normal to the direction of placing. Hand spread concrete using shovels, not rakes.

Compact concrete using internal mechanical vibration of sufficient amplitude to produce noticeable vibrations at 300 mm radius. Insert vibrators into the concrete to the depth which will provide the best compaction, but not deeper than 50 mm above the surface of the subbase, and for a duration sufficient to produce satisfactory compaction, but not longer than 30 seconds in any one location.

#### Elapsed delivery time

General: Ensure that the elapsed time between the wetting of the mix and the discharge of the mix at the site is in conformance with the Elapsed delivery time table. Do not discharge below 10C or above 32C.

#### Elapsed Delivery Time Table

| Concrete temperature at time of discharge (C) | Maximum elapsed time (hours) |
| --- | --- |
| 10 – 24 | 2.00 |
| 24 – 27 | 1.50 |
| 27 – 30 | 1.00 |
| 30 – 32 | 0.75 |

#### Finishing

Immediately after placement and spreading and compaction of the plastic concrete, start finishing operations to achieve finish shown on the drawings.

#### Curing

Protect fresh concrete from premature drying and from excessively hot or cold temperatures. Maintain the concrete at a reasonably constant temperature with minimum moisture loss for the curing period.

- Temperature: Maintain the concrete at a temperature > 5C for at least 7 days.

Curing compound method: Spray the entire surface including edges using a mechanical sprayer, at a uniform application rate of at least 0.35 L/m2. Respray defective areas within 30 minutes. Respray within 3 hours after heavy rain. Apply as a continuous coating without visible breaks or pinholes.

Covering sheet method: Immediately after finishing operations cover concrete using damp hessian or cotton mats overlapped at least 150 mm and anchored against displacement by wind or other interference. Keep the mats continuously damp until covered by the covering sheet material. Repair tears and the like immediately.

- Joint sawing: Sheet materials may be removed for the minimum distance and period to permit joint sawing, provided the concrete is kept moist by other means.

Moist curing method: Immediately after finishing operations keep the concrete surface continuously damp by spraying constantly with water, fog, or mist, using suitable spraying equipment.

Minimum curing time: 7 days.

NOTE: AS 1379 nominates a limit of 90 minutes which can be waived by agreement between the customer and supplier, if, after that period, the consistency of the concrete is such that it can be properly placed without the addition of any more water to the mixer.

### Cores, fixings and embedded items

#### Adjoining elements

For adjoining elements to be fixed to or supported on the concrete, provide for the required fixings. If required, provide for temporary support of adjoining elements during construction of the concrete.

#### Protection

Grease threads. Protect embedded items against damage.

Compatibility: Ensure inserts, fixings and embedded items are compatible with each other, with the reinforcement and with the concrete mix to be used.

Corrosion: If in external or exposed locations, galvanize anchor bolts and embedded fixings.

#### Structural integrity

Fix cores and embedded items to prevent movement during concrete placing. In locating cores, fixings and embedded items, reposition but do not cut reinforcement, and maintain cover to reinforcement.

#### Tolerances

Maximum deviation from correct positions:

- Cores and embedded items generally: 10 mm.

- Other fixing bolts: 3 mm.

### compaction

#### Compaction

Methods: Use immersion and screed vibrators accompanied by hand methods as appropriate to remove air bubbles and to fully compact the mix.

Vibrators: Do not allow vibrators to come into contact with partially hardened concrete, reinforcement or items including pipes and conduits embedded in concrete. Do not use vibrators to move concrete along the forms. Avoid over-vibration that may cause segregation.

#### Placing

Use placing methods which avoid segregation and loss of concrete, and which minimise plastic settlement. Maintain a generally vertical and plastic concrete edge at faces of a pour.

Layers: Place concrete in layers  300 mm thick, such that each succeeding layer is compacted before previous layer has taken initial set.

#### Rain

General: Do not expose concrete to rain before it has been placed and set.

#### Vertical elements

In vertical elements, limit the free fall of concrete to 1500 mm per 100 mm element thickness, up to a maximum free fall of 3000 mm, using enclosed vertical chutes or access hatches in forms.

### Construction joints

#### Location

Do not relocate or eliminate construction joints, or make construction joints not shown on the drawings. If emergency construction joints are made necessary by unforeseen interruptions to the concrete pour, submit a report on the action taken.

#### Joint preparation

Roughen and clean the hardened concrete joint surface. Remove loose or soft material, free water, and foreign matter. Dampen the surface just before placing the fresh concrete and coat with a neat cement slurry.

### Expansion joints

#### Joint filling

Joint filling: Fill with jointing materials. Finish visible jointing material neatly flush with adjoining surfaces.

Preparation: Before filling, dry and clean the joint surfaces, and prime.

Watertightness: Apply the jointing material so that joints subject to ingress of water are made watertight.