# vinyl finishes

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to resilient sheet and tile laid finishes and seamless applied flooring with associated underlay. It also covers seamless in situ coatings and synthetic sporting surfaces.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Carpets for carpets.

Worksection(s) on which this worksection relies

The following worksections must be included, if this worksection is used, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Nominate the locations of finishes and finish abutments, movement joints and note fixed partitions on drawings to your office documentation policy.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

- Concrete finishes for substrates.

- Flooring and decking for substrates.

- Access floors.

- Floor sanding and finishing for substrates.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the substrate immediately before fixing vinyl finishes.

Hold points, if required, should be inserted here.

### Submissions

#### Samples

If the specification does not state selected properties such as colour and texture, the effect of this clause is to require the submission of samples covering the full range of those properties. The specification should define the item with enough precision, either by description, or by reference to preselected samples, or as a proprietary item, to enable the contractor to identify (and price) it. Where the covering is specified as a proprietary item use this clause as a means of confirmation.

Range: Submit labelled samples of vinyl finishes illustrating the range of colour, pattern or texture as seen in the finished work.

Minimum size per sample:

- Sheet: 450 x 450 mm.

- Linear accessories (coving, skirting, stair nosing, protection strips, and the like): A piece 300 mm long.

Welded joints: Submit a sample joint 300 mm long.

#### Identification

Labelling: Label each sample, giving brand, product name, and manufacturer’s code reference

## Products

### Marking

#### Identification

Deliver materials to the site in the manufacturer’s containers legibly marked to show the following:

- Manufacturer’s identification.

- Product brand name.

- Product type.

- Dimensions and quantity.

- Handling and installation instructions.

### Sheets and tiles

#### Edges of sheets and tiles

Ensure edges are firm, unchipped, machine-cut accurately to size and square to the face, and that tile edges are square to each other.

Generally synthetic, available in various grades for specific uses e.g. where oils, fat, grease, acids and solvents are used. The surface is commonly moulded into patterns - usually raised studs. Static dissipative grades are available for static control - protection against electro-static discharge (ESD).

#### Polyvinyl chloride (PVC)

Resilient floor covering, jute or polyester felt backing: To BS EN 650.

Resilient floor covering, with foam layer: To BS EN 651.

Refer to the Vinyl sheet and tile schedule for details.

Proprietary PVC products will generally be imported and comply with overseas standards. See RAIA EDG PRO13 and PRO14, on PVC. Where slip resistance is a requirement ensure that the product maintains its resistance for the product’s service life. See also the Commentary on slip resistance. Consult the manufacturer on suitability for service conditions, especially for severe conditions such as underfloor heating or high humidity.

Counter topping grade is available but is less durable than laminate for heavy usage. Antistatic material is available where static control is required, consult with manufacturer for special installation procedures.

Select adhesives recommended by the resilient finishes manufacturer. Special adhesives may be required for antistatic and conductive applications.

## Execution

### Preparation

#### Substrates

Ensure substrates conform to the Substrate tolerance table and are as follows:

- Clean and free of any deposit or finish which may impair adhesion or location and functioning of movement joints.

#### Substrate Tolerance Table

| Property | Length of straight edge laid in any direction | Max. deviation under the straight edge |
| --- | --- | --- |
| Flatness | 3000 mm | 4 mm |
| Projections | 100 mm | 1 mm |

Cleaning concrete surfaces: Mechanically remove the following surface treatments:

- Sealers and hardeners.

- Curing compounds.

Concrete substrate correction: Remove projections and fill voids and hollows with a levelling compound compatible with the adhesive.

Consider including the following:

“If raised areas are corrected by grinding test the freshly exposed concrete surface for pH and obtain verification of compatibility with the adhesive”. Freshly exposed concrete has high alkalinity and problems have been encountered overseas.

Moisture content: Do not commence installation unless the following periods have elapsed:

- Concrete slabs: 42 days.

- Toppings on slabs: A further 21 days.

#### Working environment

Do not start work before the building is enclosed, wet work is complete and dry, and good lighting is available. Protect adjoining surfaces.

### Sheet and tile installation

#### Sheet set out

Set out sheets to give the minimum number of joints. Run sheet joints parallel with the long sides of floor areas, vertically on walls.

#### Tile set out

Set out tiles from the centre of the area. Wherever possible cut tiles at margins only, to give a cut dimension of at least 100 mm x full tile width. Match edges and align patterns. Arrange the material so that variation in appearance is minimised.

#### Joints

Non-welded: Butt edges together to form tight neat joints showing no visible open seam.

Delete if joints are welded.

#### Junctions

Scribe neatly up to returns, edges, fixtures and fittings. Finish flush with adjoining surfaces.

#### Rolling

Where rolling is required, roll the finish in 2 directions before the adhesive sets, using a 70 kg multi-wheeled roller.

#### Cleaning

Keep the surface clean as the work proceeds.

Cork tiles can be sealed or given a clear finish.

Two-pack polyurethane will give the floors a harder finish with some loss of resilience. Coordinate with the Painting worksection.

### Vinyl sheeting

#### Welded joints

Select from the alternatives and note in the Welded joints schedule.

Heat welding: After fixing, groove the seams using a grooving tool and weld the joints with matching filler rod and using a hot air welding gun. When the weld rod has cooled, trim off flush.

Was developed specifically for homogeneous sheet. It may be used for vinyl chip sheet but will be more conspicuous than cold welding and will not have the same strength as heat welding in homogeneous sheet.

Cold welding: Apply seaming compound 100 mm wide to the substrate centrally under the seam. Roll the seam until the compound is forced up into the joint. Clean off flush using a damp cloth.

Is less conspicuous and may be preferable for that reason.

Epoxy jointing: Join seams with epoxy adhesive.

For slip retardant vinyl sheet.

### Stairs

Rubber nosing tiles are an alternative to forming standard tiles to radius. Proprietary anti-slip PVC or aluminium, or PVC combined riser, nosing and tread are also available. Stair stringer profile with tapered edge is available in 300 mm width.

#### Vinyl

Preformed: Provide purpose-made vinyl stair finish combining riser, nosing and tread in the one element. Lay each step consecutively with the joint at the bottom of each riser.

Formed in situ: Fit the sheet vinyl to each tread, and to the riser above, in one piece, coved in the angle. Accurately scribe, cut and fit to stair nosings and perimeters.

#### Stair nosings

Aluminium: Purpose-made extruded anti-slip aluminium nosing.

Vinyl: Purpose-made moulded anti-slip section, matching the stair finish.

Refer to the Stair vinyl finishes schedule.

### Joints and accessories

Refer to the Vinyl finishes joint and accessories schedule for details.

At areas of heavy use, particularly with wheeled traffic, consider specifying a prototype test for the joint product installation using the anticipated wheeled equipment.

#### Junctions

Finish junctions flush with adjoining surfaces. Where changes of floor finish occur at doorways locate the joint on the centreline of the closed door leaf.

If the floor finish is to be divided into bays, specify here the bay size, dividing strip or joint filler. Delete if not required. be subject to heavy use.

Accessory type: Specify required accessories, such as nosings, wedge fillets, tile edge trim, wall and capping trim and state whether they are to be a proprietary item, purpose-made or formed (see Junctions).

For floor wastes to wet areas consult with manufacturer for special requirements e.g. flanged fittings to clamp over finish, and coordinate with the Sanitary drainage clause in the Wastewater worksection.

#### Cover strips

Provide edge cover strips at junctions with different floor finishes and to exposed edges.

Metal cover strip: Extruded tapered strip 25 mm wide, of the same thickness as the sheet or tile. Fix with masonry anchors at 200 mm maximum centres.

e.g. ‘Brass’, ‘Stainless steel’ or ‘Aluminium’.

UPVC cover strip: Feather-edge strip matching the floor finish, fixed with contact adhesive.

#### Movement joints

Location: Provide movement joints as follows:

- Over structural (isolation, contraction, expansion) joints.

- At junctions between different substrates.

Depth of joint: Right through to the substrate.

Sealant width: 6 – 10 mm.

Depth of elastomeric sealant: One half the joint width, or 6 mm, whichever is the greater.

#### Vinyl skirting

Select from the following.

Feather edge: Moulded PVC skirting section.

Intended for use with PVC or similar flat surface floor finishes, feather edge provides coverage of floor termination at the vertical surface. Occasionally used where partitions are retro fixed over carpet.

Flat skirting: Flat PVC skirting section.

Flat PVC skirtings are intended for use with carpet and provide a solid margin to assist the carpet laying process. Skirtings may be cut from sheet material but are more costly.

Fixing: Fix to walls with contact adhesive.

Minimum height: 100 mm.

If moulded pieces are not available to match the rubber floor finish, consider using vinyl skirtings.

#### Coves and nosings

Provide where a continuous surface is required e.g. Wet areas, wet mopping, hygiene and clean rooms. A sealant or cover mould may be necessary at the joint with the wall finish, the door jamb profile and width may require special consideration to ensure a sealed overlap where the coving terminates at the door jamb.

Coved skirtings: Carry the flooring material up over a profiled coving section to form skirting, weld all joints. Minimum radius of 20mm  to coving.

Vary radius as required.

### Completion

#### Protection

Keep traffic off floors until bonding has set or for 24 hours after laying, whichever period is the longer. Do not allow water in contact with the finish for 7 days.

Reinstatement: Repair or replace faulty or damaged work. If the work cannot be repaired satisfactorily, replace the whole area affected.

#### Spare materials

General: Supply spare matching covering materials and accessories of each type for future replacement purposes. Store the spare materials on site where directed.

Quantity: At least 1% of the quantity installed.

#### Cleaning

Consult resilient finish manufacturers for cleaning instructions and recommendations on polishing, etc. Polyurethane reinforced vinyls do not require sealing or polishing (they are mopped and dry buffed), and other vinyl floors only require mopping. For installations in existing buildings, consult the building user as to current maintenance procedures, type of polish used, etc., and make the new installations compatible as far as possible.

Clean the finished surface. Buff and polish. Before handover, mop and leave the finished surface clean and undamaged on completion.

Refer to the Vinyl sheet and tile schedule for details and locations of vinyl finishes.

Much of the scheduled information will be unnecessary if resilient finishes are specified by proprietary item.

Include any particular requirements not otherwise specified, such as resistance to wear, indentation, chemicals, light or fire. Consult manufacturer.

Type: e.g. ‘Linoleum’, ‘Cork’, ‘Rubber’, ‘Vinyl (PVC)’, ‘Antistatic vinyl’, ‘Conductive vinyl’, ‘Cushion backed vinyl’, ‘Vinyl counter topping’.

Form: e.g. ‘Sheet’ or ‘Tile’ (Vinyl, linoleum, cork, rubber); Unbacked flexible sheet, Semi-rigid floor tiles, Flexible floor tiles, Inlaid vinyl sheet (PVC).

Pattern: e.g. ‘Marbled’ or ‘Plain’ (Linoleum, PVC).

Tile laying pattern: e.g. “Checkerboard” or “Stretcher bond”.

Thickness: e.g.:

- For cork: 4.75 mm or 6.3 mm (6.3 mm is recommended for concrete floors).

- For rubber: 2.7, 4, 5, or 6 mm.

- For flexible terrazzo tiles: 4.76 mm.

- For flexible PVC sheet or tiles: 1.5, 2, 2.5 or 3 mm.

- For semi-rigid PVC tiles: 1.5, 2, 2.5, or 3 mm.

- For linoleum sheet or tiles: 2 or 2.5 mm.

Surface:

- For cork: Smooth surface only.

- For rubber: May be smooth, textured, or studded. For studded sheet or tile state form and profile of studs. Consult manufacturer for available forms.

- For PVC: Normally smooth surface, but various textured or inlaid anti-slip surfaces are available. Semi-rigid tiles may have a factory-applied protective coating. Consult manufacturer for details of the available surfaces.

Tile dimensions: 300 x 300 mm is standard size for PVC tiles and 305 x 305 mm for Portuguese cork tiles. Rubber tiles are usually 1000 x 1000 mm or 500 x 500 mm. Consult manufacturer for available sizes and thicknesses.

Underlay: e.g. ‘Trowelled’, ‘Hardboard’, ‘Fibre cement sheet’. Consult manufacturers of resilient flooring for recommended underlay for particular applications. State thickness.