# Glass blockwork

Worksection application

This worksection is applicable to three types of fully framed glass block (or brick) installation:

- Mortar-jointed which can take high wind loads and is permanent, so is suited to exposed installations. Panels can be large, and are rigid - resilience under loads derives from perimeter expansion joints.

- Fire-rated which has the same properties as the mortar-jointed system but offers a one-hour fire rating, with limited panel size.

- Sealant-jointed which can be used for demountable interior partitioning, and for smaller external windows, is resilient under load, has thinner joints (and consequently better light transmission) and avoids wet trades.

All three might be used in a single project, and so they are dealt with separately to avoid confusion. There is no central standard.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. See for example:

- Concrete worksections for reinforced concrete frames.

- Brick and block construction and Light steel framing for openings in walls.

- Brick and block construction, Light steel framing and Light timber framing for lintels over.

- Structural steel for channel mullions and transoms.

- Light steel framing and Metalwork for steel frames.

- Doors and hatches for aluminium frames.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Show on the drawings elevations, sections and details.

- This worksection assumes full design by the principal’s consultants, and no design by the contractor. Accordingly, wind loads, acoustic ratings, thermal performance and the like are not provided. Nor are related completion tests such as for sound transmission loss, heat gain and so on.

## General

There is no Australian, British or US standard for glass blocks. Many are imported from Germany and Japan and are made to the standards cited here. Another draft German standard for glass block walling is DIN EN 12725.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Frame and expansion jointing installed, before reinforcing.

- Perimeter and vertical reinforcing installed, before placing mortar and blocks.

Hold points, if required, should be inserted here.

### Submissions

#### Samples

Glass blocks: Submit 2 blocks of each type showing size, colour, design and pattern of faces.

Accessories: Submit samples of reinforcing, fasteners, expansion materials and sealant.

## Products

### Mortar-jointed panels

Consult manufacturers. Consider deflection of lintels over - panels cannot support building loads. Maximum deflection of structural members supporting glass block panels must not exceed L/600. Curved walls can be built (requiring curved frames) - radii depend on block size.

Prefabricated fully framed panels are available. See also the Commentary.

#### Perimeter

Frames:

Assumes 100 mm wide blocks. 75 x 40 x 6 mm for 80 mm wide blocks. Weck allows aluminium or steel channels. Some systems use proprietary frames.

- Size: 100 x 50 x 6 mm.

- Material: Aluminium channel.

e.g. galvanized after cutting, welding and drilling, for steel; anodising or powder coating for aluminium.

- Fixing: 10 mm masonry anchors with galvanized washers.

e.g. Dynabolts.

- Drainage: Drill holes in web of sill channel.

Consider size, spacing, location e.g. outer half.

Expansion jointing and sill channel lining: 10 mm (minimum) x width of the channel rebate.

If necessary, increase thickness to accommodate expansion or deflection of the structure – the panel must be isolated from these sorts of loads.

e.g. Polystyrene foam, premoulded high density glass fibre, foamed synthetic rubber, or polyethylene foam.

#### Glass blocks

Refer to Glass block schedule for block types.

Specials are available for corners, ends of walls, and so on. Bullet-resistant blocks are available.

#### Mortar

Cement: Slow setting Portland cement with low shrinkage.

White for white joints.

- Hydrated lime: calcium, or pressure-hydrated dolomitic lime if > 92% of active ingredients are hydrated.

Delete if lime is not used.

Sand: Clean sharp river mineral sand, salt free, no admixtures, no iron compounds.

White for white joints.

Water: Clean, potable.

Mortar and pointing mix by volume (cement:lime:sand): 1:0.25:3. As dry as practicable.

Pigments: Powder oxides.

- Colour: Refer to Glass block schedule

Reinforcement: 4.5 – 6 mm diameter, in lengths to suit full width or height of panel, as appropriate.

Or, 2 parallel 4 mm diameter wires at 40/50 mm centres (depends on block thickness) with electrically welded cross-wires at 200 mm intervals, hot-dip galvanized after fabrication. For large panels or panels subject to high wind loads, consult the manufacturer and/or consulting engineer – larger rods (e.g. 8 mm) may be needed (affecting joint thickness, to maintain clearance). Full length, to avoid laps.

Could be stainless steel in marine or other corrosive environments. Corrosion resistance of panel anchors, if used, should match reinforcing.

Or, polyethylene foam, neoprene, glass fibre.

### Fire-rated panels

For fire-rated panels, the maximum permitted overall steel frame size under the Pilkington type test is 2635 x 2635 mm. The Blokup type test limit is 2410 x 2410 mm. In Ordinance 70 Specification No 2, the opening was limited to 5.2 m2, 2415 mm height and 2375 mm width. Consider deflection of lintel over – panels cannot support structural loads. See also the Commentary.

#### Perimeter

Frames:

The Weck system uses a 100 x 50 x 3 mm frame, fully mitred and welded. Weck also offers a 100 x 50 mm rebate set into the surrounding AAC masonry. The Blokup system specifies a 120 x 60 mm deep rebate to all four sides. Ordinance 70 Specification No 2 specified that jambs and lintel are to be recessed 57 mm deep and 22 mm wider than the blocks.

- Size: 150 x 75 x 9 mm.

- Material: Mild steel channel.

- Fixing: 10 mm masonry anchors with heavy galvanized washers.

e.g. Dynabolts.

- Drainage: Drill holes in web of sill channel.

Expansion jointing:

- Type: Ceramic fibre blanket, 38 mm (minimum) x width of channel rebate.

Sill channel lining: Ceramic fibre board, 12 mm (minimum) x width of channel rebate.

#### Glass blocks

Refer to Glass block schedule for block types.

#### Mortar

Cement: Slow setting Portland cement with low shrinkage.

According to Ordinance 70 Specification No 2.

Sand: Clean sharp river mineral sand, salt free, no admixtures, no iron compounds.

Water: Clean, potable.

Mortar and pointing mix by volume (cement:sand): 1:3. As dry as practicable.

- Compressive strength (minimum): 10 MPa at 2 days, 35 MPa at 28 days.

Pigments: Powder oxides.

- Colour: Refer to Glass block schedule

Reinforcement: 6 mm diameter, in lengths to suit full width or height of panel, as appropriate.

#### Finish

Sealant: Fire resistant non-setting non-staining waterproof elastomeric sealant, hardening only at the surface.

e.g. Dow Corning 7900.

### Sealant-jointed panels

The default text is based on the Stek-Fix system. Refer also to the Commentary.

#### Perimeter

Frames: Proprietary extruded aluminium frame.

Anodised or powder coated.

- Fixing: 12 gauge 40 mm long stainless steel pan head screws, with nylon masonry plugs where appropriate.

Or 10 mm masonry anchors.

Sill frame can be supplied predrilled.

#### Glass blocks

Refer to Glass block schedule for block types.

See Instruction for Mortar-jointed panels (clause 3.1).

#### Panels

Reinforcement: 50 x 3 mm flat bars.

The BlokUp system uses a proprietary extruded aluminium vertical separation strip, which fits into edge recess of blocks.

Hot dip galvanized steel, with galvanized ends (or two coats of zinc-rich metal primer), or high tensile aluminium. The steel can span up to a metre more, allowing bigger panels.

Block-locating clips: Proprietary plastic clips designed to clip on the reinforcement and fit the glass block edges.

#### Finish

Grouting sealant: Silicone.

- Colour: Refer to Glass block schedule

## Execution

Note on drawings or provide a schedule to your office documentation policy. Mortar-jointed panels

#### Ambient conditions

General: Do not install below 5C. Maintain panels above 5C for the first 48 hours after construction.

#### Perimeter

Frames: Erect 4-sided frame mitred at corners, spaced 5 mm clear of the structure on packing.

Fixing: 400 mm centres. Centre hole on each side circular, other holes slotted longitudinally 50 mm.

- Packing: 75 x 75 x 2 mm zinc-plated steel.

- Sill channel: Lay sill channel lining in rebate.

- Jamb and head channels: Adhesive-fix expansion jointing in rebates.

#### Panels

Laying blocks: By hand, may be knocked into position using a rubber or soft nylon hammer. Align block patterns consistently. Prevent mortar extrusion under load while setting.

Bond: Stack bond.

Reinforcement:

- Frame: Two rods all round, hooked and connected with wire at the corners. Horizontal rods to be a tie rod assembly, with 6 mm diameter tie rods at 200 mm centres, spacing the main rods 40 – 45 mm apart.

- Joint: Two rods in at least every second horizontal joint, and every tenth vertical joint. Overlap 230 mm (minimum) at corners. Do not tie vertical rods to horizontal rods. Do not impinge on expansion joints. Tie joint reinforcement to frame reinforcement.

- Cover (minimum): 15 mm to outside face, 10 mm to inside face, 5 mm to blocks.

Joints:

- Widths (clear): 10 – 15 mm. For curved walls, 5 – 20 mm for vertical joints.

- Width tolerance:  3 mm.

- Placing mortar: Do not retemper mortar. Do not furrow joints. Fill channel frame and panel joints.

- Pointing: Point before mortar has hardened. Neatly tool to a smooth, dense concave joint. Remove excess mortar from glass surfaces using a damp cloth before mortar set occurs, without damaging the glass. Protect against premature drying, but do not moisten.

### Sealant-jointed panels

#### Perimeter

Frames:

- Assembly: Mitre frame at corners. Assemble with connection angles and cleats, drill, and fix frame to angles with blind rivets.

Or self tapping screws.

- Fixing jamb frames: Position screws to clear the ends of the reinforcing bars. Fix screws with neoprene washers and through the packing, at 400 mm (maximum) centres, and pairs 100 mm from ends.

Assumes horizontal reinforcing. Do not fix head frame. Could use this specification for sill frame too.

- Fixing sill frame: Fix screws with neoprene washers and through the packing, at 800 mm (maximum) centres, and 100 mm from ends.

Delete if not required.

- Packing: Locate to square the frame, maximum 10 mm, to sill and jamb frames only.

#### Panels

Laying blocks: Select and orient glass blocks to ensure consistent coursing dimensions. Lightly clean edges with steel wool.

Block-locating clips: Locate onto sill frame profile 20 mm from each corner and centred at every perpend, ribbed side up. Insert in perpends, including at jamb frames, centred at course centre line. Clip onto reinforcing bars 20 mm from the ends and centred at every perpend, ribbed side up. Insert above top course 20 mm from each corner and centred at every perpend.

Assumes horizontal reinforcement.

Bond: Stack bond.

Joint reinforcement: Joint: Run reinforcement horizontally, and slot into the jamb frame channels on top of the glass block courses, except the top course, finishing 3 mm short of the jamb frame rebate faces.

Assumed the horizontal dimension is the short dimension of the panel. Reinforcement may be vertical or horizontal. Vertical reinforcement should stand on 3 mm spacers.

Joints:

- Widths: 3 – 4 mm.

#### Finish

Jointing: Clean and dry substrates. Execute work neatly, without gaps and holes. Inject structural sealant into blockwork joints to a depth of 5 – 8 mm.

Grouting: Clean and dry substrates. Execute work neatly, without gaps and holes. Apply grouting sealant to mitred frame corner joints, and apply to blockwork joints, including at the perimeter frame, to both panel faces. Remove excess sealant from glass at completion, without damaging the glass.

### Maintenance

#### Mortar-jointed and fire-rated panels

Final clean: Wash using clean water. Remove dry powder using a clean soft dry cloth.

For hard to remove powder or stains, the use of an “extra fine” steel wool (grades 000 or 0000) is suggested by Pittsburgh Corning.