# Waterproofing

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to tanking and membrane applications to roofing, balconies, concrete slabs over below ground spaces and planter boxes.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. See for example:

- Concrete reinforcement.

- Cementitious topping.

- Terrazzo in situ.

- Waterproofing – wet areas.

- Hydraulic design and install.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection. For example:

- Swimming pools.

Worksection cross-referencing

Other worksections that cross reference this worksection are:

- None.

Documenting this and related work

You may document this and related work as follows:

- Location, extent and type of membrane including details of junctions with flashings and damp-proof courses on the drawings.

## General

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

### Interpretations

#### Definitions

For the purposes of this worksection the definitions given below apply.

- Substrates: The surfaces on which membrane systems are laid.

- Bitumen: A viscous material comprising complex hydrocarbons which is soluble in carbon disulphide, softens when it is heated, is waterproof and has good powers of adhesion. It is produced as a refined by-product of oil.

- Bond breakers: Layers which prevent membranes from bonding to the backgrounds.

- Membranes: Impervious barriers to liquid water which may be:

- Liquid applied: Membranes applied in liquid or gel form and air cured to form a seamless film.

- Sheet applied: Membranes applied in sheet form with joints lapped and bonded.

- Membrane systems: Combinations of membranes, flashings, drainage and accessories which form waterproof barriers and which may be:

- Loose-laid.

- Bonded to backgrounds fully or partially.

Define the project specific ”traffic” in the Selections clause.

The Definitions subclause can be edited to suit the project or deleted if not required.

Delete if not required.

### Inspection

#### Notice

Give sufficient notice so that inspection may be made as follows:

- Background preparation completed.

- Before membranes are finished, covered up or concealed.

Hold points, if required, should be inserted here.

Consider adding text to describe inspections by representatives of the product manufacturer.

For large or complex projects consider adding the following requirements:

“Daily reports: Provide daily reports of membrane placed including:

- The location and element where each membrane was placed.

- The method of placing and climatic conditions.

Personnel: Employ a suitably qualified person to monitor the placing and protection of the membrane and prepare the daily report”.

## Products

### Membranes

#### Membrane systems

To be proprietary membrane systems where possible having certification from an international testing organisation.

Delete if a proprietary membrane is specified but check for compliance with the standard.

#### Internal roof outlets for membrane roof

Proprietary funnel shaped sump cast into the roof slab, set flush with membrane, with a flat removable grating and provision (e.g. clamp ring) for sealing the membrane into the base of the outlet.

e.g. “Flat” or “Domed”.

Surface fixed and sealed or cast in.

## Execution

Refer to Single layer, Multi layer and Liquid waterproofing system schedules for details of systems.

### Preparation

#### General

Prepare backgrounds as follows:

- Fill all cracks in backgrounds wider than 1.5 mm with a filler compatible with the membrane system.

- Fill voids and hollows in concrete backgrounds with a concrete mix not stronger than the background.

- Remove excessive projections.

- Remove deleterious and loose material.

- Leave the surface free of contaminates, clean and dust free.

#### Moisture content

Concrete backgrounds: Cure for > 21 days.

#### Falls

Verify that falls in backgrounds are > 1:100.

#### Joints and fillets

Internal corners: Provide 45° fillets.

External corners: Round or arris edges.

Movement control joints: Prepare all background joints to suit the membrane system.

#### Priming

If required, prime the backgrounds with compatible primers to ensure adhesion of membrane systems.

### Application

#### Protection

Protect membrane from damage during installation.

#### Drains

Prevent moisture from tracking under the membranes at drainage locations.

Drains and cages: Provide grates or cages, to prevent blockage from debris.

Overflows: Turn the membranes into the overflow to prevent moisture from tracking behind the membrane.

#### Sheet joints

Bituminous sheet membranes:

- Side laps > 50 mm.

- End laps > 100 mm.

Synthetic rubber membranes:

- Factory–vulcanized laps > 40 mm.

- Field side laps > 50 mm for side laps.

- Field end-laps > 100 mm for end laps.

#### Curing of liquid applied systems

To the manufacturers’ instructions.

#### Movement control joints

See AS CA55 clause 3.6.4 on major movement joints.

Locate over movement control joints in the substructure.

Fillets and bond breakers: Provide of sufficient dimension to allow the membrane to accommodate the movement.

Bonded membranes: Carry movement joints in the substrate through the surface finish.

#### Membrane terminations

Edge protection: Provide upturns above the maximum water level expected from the exposure conditions of rainfall intensity and wind.

- Minimum height of 200mm for all upturns above membrane level unless noted otherwise on the drawings.

- Anchoring: Secure sheet membranes along the top edge.

- Edge protection: Protect edges of the membrane.

- Waterproofing above terminations: Waterproof the structure above the termination to prevent moisture entry behind the membrane using cappings, waterproof membranes or waterproof coatings.

#### Membrane vertical penetrations

- Pipes, ducts, and vents: Provide separate sleeves for all pipes, ducts, and vents and have them fixed to the substrate. Minimum height of 200mm for all sleeves above membrane level unless noted otherwise on the drawings.

.

#### Overlaying finishes on membranes

Compatibility: If a membrane is to be overlayed with another system such as tiles, pavers, ballast, insulation, soil, and the like, provide an overlaying system that is compatible with and not cause damage to the membrane.

Ensure that no damage is caused to the membrane during the laying of the overlay material. If any damage occurs immediately stop work and repair the damage before proceeding with the overlay process.

Bonded or partially bonded systems: If the topping or bedding mortar requires to be bonded to the membrane, provide sufficient movement joints in the topping or bedding mortar to reduce the movement over the membrane.

Geotextile product of the recommended grade.

Traffic: Indicate if membrane is to be trafficable.

Nature of traffic: e.g. pedestrian, wheeled, load.