# Pavement kerb, channel and linemarking

There is a Product Partner for this worksection. Click the logo to be redirected to their page.

Worksection application

This worksection is applicable to the installation of channels, kerbs and linemarking.

Related material located elsewhere in NATSPEC

Related material may be found in other worksections. For example:

- Asphaltic concrete.

- Sprayed bituminous surfacing.

- Concrete pavement.

- Segmental pavers – mortar bed.

- Segmental pavers – sand bed.

Worksection(s) on which this worksection relies

The following worksections must be included, with this worksection, to provide a complete specification:

- General requirements.

- Site preparation.

- Earthwork.

- Pavement base and subbase.

Material not included in NATSPEC

Some projects may include items not covered by NATSPEC. For these you may need to create new text, modify this text or use an applicable worksection.

- Documenting this and related work

- You may document this and related work as follows:

- Show all kerb types and kerb details on the drawings.

- Show all linemarking types and locations on the drawings.

## General

### Inspection

#### Notice

Give sufficient notice so that inspection may be made of the following:

- Set out of kerbs and channels.

- Set out of linemarking prior to painting.

### Tolerances

Kerbs and channels conform to the following:

- Absolute level tolerance:  10 mm.

- Maximum deviation from design alignment: 50 mm.

- Maximum deviation from a 3 m straightedge placed on horizontal, vertical, or sloping surfaces required to be straight: 5 mm.

Linemarking to conform to the following:

- The location of markings shall not vary from the locations shown on the drawings by more than 50 mm.

List worksections cross referenced by this worksection. (General requirements references the other general worksections e.g. Metals and prefinishes do not repeat them here.) You may also wish to direct the contractor to other worksections where there may be work that is closely associated with this work.

### Interpretation

#### Definitions

General: For the purposes of this worksection the definitions given below apply.

- Absolute level tolerance: Maximum deviation from design levels.

- Relative level tolerance: Maximum deviation from a 3 m straightedge laid on the surface

- Channels and kerbs: Includes all forms of concrete gutters, dish drains, grated drains and mountable barrier kerbing.

The Definitions subclause can be edited to suit the project or deleted if not required.

## Products

### Materials

#### Concrete

Ready-mixed concrete shall comply with M-150 (1:2:4) for non-reinforced mass concrete and M-200 (1:1.5:3) for reinforced concrete and the requirements of these standards.

On site batch mixed concrete shall have characteristics and proportions of concrete ingredients which conform to those specified in M-150 (1:2:4) and M-200 (1:1.5:3).

#### Pavement marking paint

Provide samples of pavement marking paint and technical specifications for approval by the Employers Representative prior to use on site.

See Appendix A of AS 2876 for typical details of sections.

## Execution

### Linemarking

#### Setting out

Set out the work to ensure that all markings are placed in accordance with the drawings.

#### Surface preparation

Clean dry surface: Pavement markings shall only be applied to clean dry surfaces. Clean the surface to ensure a satisfactory bond between the markings and wearing surface of the pavement.

Wet weather: Pavement marking shall not be carried out during wet weather or if rain is likely to fall during the process.

Provision for traffic: Provide for traffic while undertaking the work and protect the pavement markings until the material has hardened sufficiently so that traffic will not cause damage.

Mixing of paint: All paint shall be thoroughly mixed in its original container before use to produce a smooth uniform product.

#### Application of paint

Pavement markings shall be straight or with smooth, even curves where intended. All edges shall have a clean, sharp cut off. Any marking material applied beyond the defined edge of the marking shall be removed leaving a neat and smooth marking on the wearing surface of the pavement.

#### Removal of pavement markings

General: Remove pavement markings, no longer required, from the wearing surface of pavements without significant damage to the surface.

### Channels and kerbs

#### General

Before placing any kerb and/or gutter, the foundation material shall be shaped and compacted to form a firm base. Where placed on pavement courses, the foundation shall be compacted to the requirements of the Pavement base and subbase worksection.

Kerb and/or gutters may be constructed in fixed forms, by extrusion or by slip forming in accordance with the drawings. The foundation, concrete quality, curing and testing details shall be in accordance with the Concrete Paving worksection.

#### Tolerances

The level at any point on the surface of the gutters shall be within ± 10 mm of design levels. When a straight edge 3 m long is laid on top of or along the face of the kerb or on the surface of gutters, the surface shall not vary more than 5 mm from the edge of the straight edge.

#### Joints

Contraction joints: Formed every 3 m of gutter length for a minimum of 50% of cross sectional area. The joint shall be tooled 20 mm in depth to form a neat groove of 5 mm minimum width.

Expansion joints: 15 mm in width for the full depth of the kerb and gutter. Joints shall be constructed at intervals not exceeding 15 m and where the gutter is attached to pits and retaining walls. Expansion joints shall consist of approved preformed jointing material.

Concrete pavement: Where kerbs and/or gutters are cast adjacent with a concrete pavement the same type of contraction, construction and expansion joints specified in the concrete base shall be continued across the kerb and/or gutter.

#### Backfill

Timing: After the new kerb and gutter has been constructed and not earlier than three days after placing, the spaces on both sides of the kerb and/or gutters shall be backfilled and reinstated in accordance with the drawings.

Material: Backfill material behind the kerb shall consist of granular material, free of organic material, clay and rock in excess of 50 mm diameter.

Compaction: Backfill material behind the kerb shall be compacted in layers not greater than 150 mm thick.